The Malaysian Journal of Analytical Sciences Vol 14 No 1 (2010): 41 – 49

Effect of HTAB Concentration on THE SynthesIS OF nanostructured TiO2 TOWARDS ITS Catalytic activities

(Kesan Kepekatan HTAB Terhadap Sintesis TiO2 Nanostruktur Ke Atas Aktiviti Pemangkinannya) 

Ruslimie C. A, Mohd Hasmizam Razali* and Wan M. Khairul
Department of Chemical Sciences, Faculty of Science and Technology,

Universiti Malaysia Terengganu, 21030, Kuala Terengganu,

Terengganu, Malaysia

*Corresponding author: mdhasmizam@umt.edu.my

Abstract

Titanium dioxide, TiO2 photocatalyst was synthesised by microemulsion method under controlled hydrolysis of titanium butoxide, Ti(O(CH2)3)CH3 in Hexadecyl Trimethyl Ammonium Bromide, HTAB. The effect of various concentrations of surfactant in the range between 0.01-1.0 M were focused on by investigating their morphology, crystallite size, crystalline phase and specific surface area. After observation on their degradation performance, 0.5 M concentration of HTAB presented as a optimum concentration to synthesis TiO2 photocatalyst. These results also supported by XRD spectra which are exhibited size of photocatalyst in the range within 50-150 nm. As a result, the catalytic properties of the synthesised TiO2 nanostructure was performed by exhibiting good behaviour in photocatalytically degraded atrazine, 2-chloro-4-(ethylamino)-6 (isopropylamino)-S-triazine to unharmful compounds in the environment.

Keywords: TiO​2, microemulsion, photodegradation, atrazine.

References

1.
Kitano, M., Matsuoka, M., Ueshima, M. and Anpo, M. 2007. Recent Development in Titanium Oxide-based Photocatalysts. Applied Catalysis A: General, 325: 1-14.

2.
Yu, J., Su, Y., Cheng, B. And Zhou, M. 2006. Effect of pH on the Microstructures and Photocatalytic Activity of Mesoporous Nanocrystalline Titania Powders Prepared via Hydrothermal Method. Journal of Molecular Catalyst A: Chemical, 258: 104-112.

3.
Venkatachalam, N, Palanichamy, M. and Murugesan, V. 2007. Sol-gel Preparation and Characterisation of Nanosize TiO2: Its Photocatalytic Performance. Materials Chemistry and Physics, 104: 454-459.

4.
Yu, J., Yu, H., Cheng B., Zhou, M. And Zhao, X. 2006. Enhanced Photocatalytic Activity of TiO2 Powder (P25) by Hydrothermal Treatment. Journal Of Molecular Catalyst A: Chemical, 253: 112-118.

5.
Lu, C.-H. and Wen, M.-C. 2008. Synthesis of Nanosized TiO2 powders via a hydrothermal microemulsion process. Journal of Alloys and Compounds, 448: 155-158.

6.
Lee, M. S., Lee, G.-D., Ju, C.-S. and Hong, S.-S. 2005b. Preparations of nanosized TiO2 in reverse microemulsion and their photocatalytic activity. Solar Energy Materials and Solar Cells, 88: 389-401.

7.
Wang, J., Sun, J., Bian, X. 2004. Preparation of Oriented TiO2 Nanobelts by Microemulsion Technique. Material Science and Engineering, A 379: 7-10.

8.
Timothy, J. M. 1999. Sonochemistry. In an Introduction To The Uses of Power Ultrasound in Chemistry. ed. R. G. Compton. Oxford University Press. New York: pp 1-39. 

9.
Mohapatra, P., Mishra, T. and Parida, K. M. 2006. Effect of Microemulsion Composition on Textural and Photocatalytic Activity of Titania Nanomaterial. Applied Catalysis A: General, 310: 183-189.

10.
Chai, L.-Y., Yu, Y.-F., Zhang, G., Peng, B. and Wei, S.-W. 2007. Effect of Surfactant on Preparation TiO2 by Pyrohydrolysis. Transaction of Nonferrous Metals Society of China, 17: 176-180.

11.
Asim, N., Radiman, S. and bin Yarmo, M. A. 2007. Synthesis of WO3 in Nanoscale With the Usage of Sucrose Ester Microemulsion and CTAB Micelle Solution. Materials Letters, 61: 2652-2657.

12.
Zhanqi, G., Shaogui, Y., Na, T. and Cheng, S. 2007. Microwave Assisted Rapid and Complete Degradation of Atrazine using TiO2 Nanotube Photocatalyst Suspensions. Journal of Hazardous Materials, 145: 424-430.

13.
Lu, C.-H., Wu, W.-H. and Rohidas, B. K. 2008. Microemulsion-mediated Hydrothermal Synthesis of Photocatalytic TiO2 Powders. Journal of Hazardous Materials, 154: 649-654.

14.
Mishra, T., Hait, J., Aman, N., Gunjan, M., Mahato, B. and Jana, R. K. 2008. Surfactant Mediated Synthesis of Spherical Binary Oxides Photocatalytic With Enhanced Activity in Visible Light. Journal of Colloid and Interface Science, 327: 377-383.

15.
Li, X., He, G., Xiao, G.,Liu, H. and Wang, M. 2009. Synthesis and morphology control of ZnO nanostructures in microemulsions. Journal of Colloid and Interface Science, 333: 465-473.

16.
Awitor, K. O., Rafqah, S., Géranton, G., Sibaud, Y., Larson, P. R., Bokalawela, R. S. P., Jernigen, J. D. and Johnson M. B. 2008. Photo-catalysis using titanium dioxide layers. Journal of Photochemistry and Photobiology A: Chemistry, 119: 250-254.

17.
Lu, J., Bauermann, L. P., Gerstel, P., Heinrichs, U., Kopold, P., Bill, J. and Aldinger, F. 2009. Synthesis and characterization of TiO2 nanopowders from peroxotitanium solutions. Materials Chemistry and Physics, 115: 142-146.

18.
Górska, P., Zaleska, A., Kowalska, E. Klimczuk, T., Sobczak, J. W., Skawarek, E., Janusz, W. and Hupka, J. 2008. TiO2 Photoactivity in Vis and UV light: The Influence of Calcination Temperature and Surface Properties. Applied Catalyst B: environmental, 84: 440-447.

19.
Deorsola, F. A. and Valluri, D. 2009. Study of the Parameters in the Synthesis of TiO2 Nanospheres Through Reactive Microemulsion Precipitation. Powder Technology, 190: 304-309.

20.
Janus, M., Tryba, B., Kusiak, E., Tsumura, T., Toyoda, M., Inagaki, M. and Morawski, A. W. 2008. TiO2 nanoparticles with high photocatalytic activity under visible light. Catalysis Letters, 50: 177-183.

21.
Lee, M. S., Park, S. S., Lee, G.-D., Ju, C.-S. and Hong S.-S. 2005. Synthesis of TiO2 particles by reverse microemulsion method using nonionic surfactant with different hydrophilic and hydrophobic group and their photocatalytic activity. Catalysis Today, 101: 283-290.

22.
Pu, Y., Fang, J., Peng, F., Li, B. & Huang, L. 2007. Microemulsion synthesis of nanosized SiO/TiO2 particles and their photocatalytic activity. Chinese Journal of Catalysis, 28(3): 251-256.

23.
Li, Z., Du, J., Zhang, J., Mu, T., Gao, Y., Han, B., Chen, J. and Chen, J. 2005. Synthesis of Single Crystal BaMoO4 Nanofibers in CTAB Reverse Microemulsions. Materials Letters, 59: 64-68.

