The Malaysian Journal of Analytical Sciences Vol 14 No 2 (2010): 63 - 68
Carboxymethyl Chitosan-Fe3O4  Nanoparticles:  Synthesis and Characterization 
Nurul Hidayah Ahmad Safee, Md. Pauzi Abdullah*,  Mohamed Rozali Othman
School of Chemistry Science and Food Technology, 
Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600  Bangi, Selangor Darul Ehsan

*Corresponding author: mpauzi@ukm.my
Abstract

In this study, carboxymethyl chitosan bound Fe3O4 magnetic nanoparticles (CC-Fe3O4 NPs) was synthesized by the binding of carboxymethyl chitosan (CC) onto the surface of Fe3O4 magnetic nanoparticles, which was prepared by coprecipitating method. The CC-Fe3O4 nanoparticles was characterized by transmission electron microscopy (TEM), X-ray diffractometer (XRD), vibrating sample magnetometer (VSM), Nucleus Magnetic Resonans (NMR) and Fourier Transform Infra Red (FTIR).  TEM studies confirmed that the Fe3O4  and CC-Fe3O4 particles have a particle size ranges from 9.73-12.30 nm and 9.70-12.50 nm, respectively. The magnetic properties of the Fe3O4 particles were verified using VSM. Their saturation magnetization, remnant magnetization and coercivity were 61.0 emu/g, 2.70 emu/g and 38.20 G,  respectively. FTIR studies showed the appearance of peaks at 1629 cm-1 and 1397 cm-1 which were characteristic of COOM (M = metal ions) bands, indicating the formation of the iron carboxylate.

Keywords: Carboxymethyl chitosan , magnetic nanoparticles  

References

1. Ding, P.,  Huang, K.L. &  Li, G.Y. Kinetics of adsorption of Zn(II) ion on   chitosan derivatives.  2006. Int. J. Biol. Macromol. 39: 222– 227.

2.
Zhang L., Guo J. & Peng X., Jin Y.Preparation and release behavior of carboxymethylated chitosan/alginate microspheres encapsulating bovine serum albumin. 2004. J. Appl. Polym. Sci. 92: 878-882.

3.
Chen X.G. &  Park H.J., Chemical characteristics of O-carboxymethyl chitosans related to the preparation conditions. 2003. Carbohyd. Polym. 53: 355-359.

4.
Chang, Y.C., Chang, S.W. & Chen, D.H. 2006. Magnetic chitosan nanoparticles: Studies on chitosan binding and adsorption of Co(II) ions. Reactive & Functional Polymer 66: 335-341.

5.
Mohapatra, S.,  Pal, D.,  Ghosh, S. K. &  Pramanik, P. 2007. Design of Superparamagnetic Iron Oxide Nanoparticle  for Purification of   Recombinant Proteins. Journal of Nanoscience and Nanotechnology 7: 1–7.

6.
Sun, G., Chen, X., Li,Y., Zheng, B., Gong, Z., Sun, J., Chen, H., Li, J. & Lin, W. 2008. Preparation of H-oleoyl-carboxymethyl-chitosan and the function as a coagulation agent for residual oil in aqueous system. Front. Mater. Sci. China. 2(1): 105–112.

7.
Chang, Y.C. & Chen, D.H.  2005. Preparation and adsorption properties of monodisperse chitosan-bound Fe3O4 magnetic nanoparticles for removal of Cu(II) ions. Journal of Colloid and Interface Science 283:  446–451. 

8.
Brugnerotto, J., Lizardi, J., Goycoolea, F.M., Arguelles-Monal, W., Desbrieres,  J. and Rinaudo, M. 2001.An infrared investigation in relation with chitin and chitosan characterization. Polymer 42: 3569–3580.

9.
Shigemasa, Y., Matsuura, H.,  Sashiwa, H. and Saimoto, H. 1996. Evaluation of different absorbance ratios from infrared spectroscopy for analyzing the degree of deacetylation in chitin. International Journal of Biological Macromolecules 18: 237–242.

10.
El-Sherbiny, I.M.2009. Synthesis, characterization and metal uptake capacity of a newcarboxymethyl chitosan derivative. European Polymer Journal 45: 199–210. 

11.
Xu, X.Q., Shen, H., Xu, J. R. and  Li,X.J.2004. Aqueous-based magnetite magnetic fluids stabilized by surface small micelles of oleolysarcosine. Applied Surface Science 221(1-4): 430-436.

12.
Ragnhild, J., Hjerde, N., Varum, K.M., Grasdalen, H., Tokura, S. and Smidsrod, O. 1997. Chemical composition of O-(carboxymethyl)-chitins in relation to lysozyme degradation rates. Carbohydrate Polymers 34:131–139.

13.
de Abreu, F.R. & Campana-Filho S.P. Characteristics and properties of carboxymethylchitosan. Carbohydrate Polymers 75: 214–221.

14.
Zhu, A., Yuan, L., & Liao,  T. 2008. Suspension of Fe3O4 nanoparticles stabilized by chitosan and o-carboxymethylchitosan. International Journal of Pharmaceutics 350: 361–368.

15.
Morales, M.P., Veintemillas-Verdaguer, S., Montero, M.I., Serna, C.J., Roig, A., Casas, L.I., Martínez, B. & Sandiumenge, F. 1999. Surface and internal spin canting in γ-Fe2O3 nanoparticles. Chemistry of Materials 11(11): 3058-3064.

16.
Iglesias O. & Labarta A. 2001. Finite-Size and surface effects in maghemite nanoparticles:Monte Carlo simulations. Phys. Rev. B 63, 184416-1/184416-11.

17.
Ma, Z.Y., Guan, Y.P., Liu, H.Z., 2005. Synthesis and characterization of micronsized monodisperse superparamagnetic polymer particles with amino groups. J. Polym. Sci. A: Polym. Chem. 43: 3433–3439.

