The Malaysian Journal of Analytical Sciences Vol 15 No 1 (2011): 46 – 53

IONIC LIQUID SUPPORTED ACID-CATALYSED ESTERIFICATION OF LAURIC ACID
Zalita Yaacob1*, Nor Asikin Mohd Nordin2, Mohd Ambar Yarmo1
1School of Chemical Science  and Food Technology, 
Faculty of Science and Technology, 
Universiti Kebangsaan Malaysia, 43600 Bangi, Selangor Darul Ehsan, Malaysia.
2Department of Science, UTM SPACE, 
Universiti Teknologi Malaysia International Campus Jalan Semarak, 54100 Kuala Lumpur, Malaysia.
*Corresponding author: zalita_y@yahoo.com
Abstract

Ionic Liquid (IL) based on 1-n-butyl-3-methylimidazolium bis(trifluoromethylsulfonyl)imide (BMI.NTf2) under acidic condition was used as catalyst for the esterification reaction of fatty acid. Various acids namely sulphuric acid, perchloric acid, p-toulene sulphonic acid and various chloride salts such as zinc chloride (ZnCl2) and iron(III) chloride (FeCl3) immobilized in ionic liquid BMI.NTf2  gave acidic ILs. These acidic ILs were tested as catalysts for esterification reactions. Esterification of alcohol (methanol) with fatty acid (lauric acid) using ionic liquid BMI.NTf2 combined with H2SO4 (BMI.NTf2(H2SO4)) gave high activity (>85%) and selectivity (100%) observed over a period of 2 hours reaction with reaction temperature 70oC. The ester became easily separated due to IL forming biphasic with product after the reaction where ester accumulated as the upper phase and IL with water produced after reaction at lower phase. Catalytic activities comparison also be studied between acidic ionic liquid BMI.NTf2 with acidic ionic liquid ChCl.2ZnCl2 and conventional acid catalyst. These ILs were characterised by using FTIR, NMR and TGA. Results from FTIR were showed no significant difference between ILs with ILs in acidic condition. The TGA curve show BMI.NTf2 thermal's decomposition is ≥400oC but when BMI.NTf2 combination with H2SO4, TGA curve show weight loss increase and becomes unstable. The advantages of ILs as catalyst are “clean process” and “green chemistry” due to its behaviour such as non-volatile, no loss of solvent through evaporation and reduced environmentally impact. This ILs-catalyst system can be recycle for futher reaction. 

Keywords:  1-n-butyl-3-methylimidazolium bis(trifluoromethylsulfonyl)imide; Choline chloride; Ionic liquids; Acidic condition; Esterification; Fatty acid

References

1. Juan, Joon Ching., Zhang, Jingchang & Mohd Ambar Yarmo. 2007. Structure and reactivity of silica supported zirconium sulfate for esterification of fatty acid under solvent-free condition. Applied Catalysis, 332 : 209-215.
2. Mantri, K., Komura, K. & Sugi, Y. 2005. ZrOCl2.8H2O catalysts for the esterification of long chain aliphatic carboxylic acids and alcohols. the enhancement of catalytic performance by supporting on ordered mesoporous silica. Green Chemistry, 7 : 677-682.
3. Joseph, T., Sahoo, S. & Halligudi, S.B. 2005. Bronsted acidic ionic liquids: a green, efficient and reusable catalyst system and reaction medium for fischer esterification. Journal of Molecular Catalysis, 234 : 107-110.
4. Wasserscheid, P. &  Keim, W. 2000. Ionic liquids – new “solutions” for transition metal catalysis. Angew. Chem. Int. Ed, 39 : 3772 – 3789.
5. Duan, Z., Gu, Y and Deng, Y. 2006. Neutral ionic liquid [BMIm]BF4 promoted highly selective esterification of tertiary alcohols by acetic anhydride.  Journal of Molecular Catalysis A: Chemical, 246 : 70-75.
6. Wassercheid, P. & Welton, T. 2008. Ionic Liquids in Synthesis. Ed. 2. Vol. 1 & 2. Weinheim: WILEY-VCH Verlags GmbH & Co. KGaA.
7. Sunitha, S., Kanjilal, S., Reddy, P.S and Prasad, R.B.N. 2007. Liquid-liquid biphasic synthesis of long chain wax esters using the Lewis acidic ionic liquid choline chloride.2ZnCl2. Tetrahedron Letters, 48 : 6962-6965.
8. Lapis, A.A.M., Oliveira, L.F.d., Neto, B.A.D and Dupont, J. 2008. Ionic liquid supported acid/base-catalyzed production of biodiesel. ChemSusChem, 1 : 759-762.
9. Abbott, A.P., Capper, G., Davies, D.L. & Rasheed, R. Ionic liquid based upon metal halide/substituted quaternary ammonium salt mixtures. Inorg. Chem, 43: 3447-3452.
10. Zhang, Z.C. 2006. Catalysis in ionic liquids. Adv. Catal, 49: 153-237.
11. Welton, T. 2004.  Ionic liquids in catalysis. Coordination Chemistry Reviews, 248 : 2459-2477.
12. Johnson, K.E. 2007. What’s an ionic liquid. The Electrochemical Society Interface, Spring, 16 : 38-41.
13. Angueira, E.J and White, M.G. 2007. Super acidic ionic liquids for arene carbonylation derived from dialkylimidazolium chlorides and MCl3 (M = Al, Ga, or In). Journal of Molecular Catalysis A: Chemical, 277 : 164-170.

