The Malaysian Journal of Analytical Sciences Vol 15 No 2 (2011): 167 -174

DETERMINATION OF SIX PHTHALATES IN POLYPROPYLENE CONSUMER PRODUCTS BY SONICATION-ASSISTED 
EXTRACTION/GC-MS METHODS

Chong Kian Wei*, Loke Chui Fung and Michelle Pang

Chemistry and Biology Division,

 School of Arts and Science, Tunku Abdul Rahman College,

 Jalan Genting Kelang, Setapak, 53300 Kuala Lumpur, Malaysia

*Corresponding author: chongkw@mail.tarc.edu.my
Abstract

Studies on determination of six kinds of phthalates, i.e. dimethyl phthalate (DMP), diethyl phthalate (DEP), dibutyl phthalate (DBP), benzyl butyl phthalate (BBP), di-(2-ethylhexyl) phthalate (DEHP), and di-n-octyl phthalate (DnOP), in three kinds of plastic containers for food use, including food container, instant noodle cup and snack container, by gas chromatography in combination with mass spectrometry detector (GC-MS) in electronic ionization mode with selected-ion monitoring (SIM) acquisition method (GC-MS(EI-SIM)) have been carried out. Extraction, clean-up and analysis methods have been developed and optimized. Determination of samples were performed after sonication-assisted extraction with 1:9 toluene and dichloromethane, clean-up with Bio-Beads S-X8 gel-permeation column and analyzed by GC-MS methods. The characteristic ions, 163, 194 for DMP; 149, 177, 222 for DEP; 149, 233, 251 for DBP; 91, 149, 206 for BBP; 149, 176, 193 for DEHP; 149, 167, 279 for DNOP were chosen for quantitative studies. These techniques are possible to detect phthalates at the level of 1-70 mg/kg.  The overall recoveries were 79.2-91.1% with relative standard deviation (R.S.D.) values at 3.1-11.3%. Only DEHP was detected in the studied samples.

Keywords: Phthalates; Polypropylene Products; Sonication-assisted extraction; GC-MS (EI-SIM); Recoveries
References

1. Larsen, S.T., Hansen, J.S., Hansen, E.W., Clausen, P.A., and Nielsen, G.D. (2007). Airway inflammation and adjuvants effect after repeated airborne exposures to di-(2-ethylhexyl) phthalate and ovalbumin in BALB/c mice. Toxicology, 235, 119-129.

2. Ema, M. and Miyawaki, E. (2001). Adverse effects on development of the reproductive system in male offspring of rats given monobutyl phthalate, a metabolite of dibutyl phthtlate, during late pregnanacy. Reproductive Toxicology, 15, 189-194.

3. Gangi, J.D. (1999). Phthalates in PVC medical products from 12 countries. Greenpeace USA. pp:1-12. 

4. Rastogi, S.C., Jensen, G.H., and Worsoe, I.M. (2003). Compliance testing of phthalates in toys. National Environmental Research Institute Ministry of the Environment. pp:11-12.

5. Nakajin, S., Shinoda, S., Ohno, S., Nakazawa, H., and Makino, T. (2001). Effect of phthalate esters and alkylphenols on steroidogenesis in human adrenocorticol H295R cells. Environmental Toxicology and Pharmacology. 10, 103-110.

6. Foster, P.M.D., Cattley, R.C., and Mylchreest, E. (2000). Effects of Di-n-butyl Phthalate (DBP) on Male Reproductive Development in the Rat: Implications for Human Risk Assessment. Food and Chemical Toxicology. 38, 97-99.

7. Hines, C.J., Hopf, N.B., Deddens, J.A., Silva, M.J., and Calafat, A.M. (2009). Estimated daily intake of phthalates in occupationally exposed groups. Journal of exposure Science and environmental Epidemiology, 1-9.
8. Ito, R., Seshimo, F., Miura, N., Kawaguchi, M., Saito, K., and Nakazawa, H. (2005). High-through put determination of mono-and di(2-ethylhexyl) phthalate migration from PVC tubing to drugs using liquid chromatography–tandem mass spectrometry. Journal of Pharmaceutical and Biomedical Analysis. 39, 1036-1041.

9. Marin, M.L., Jimenez, A., Lopez, J., and Vilaplane, J. (1996). Analysis of poly(vinyl chloride) additives by supercritical fluid extraction and gas chromatography. Journal of Chromatography A. 750, 183-190.

10. Shen, H.Y. (2005). Simultaneous screening and determination eight phthalates in plastic products for food use by sonication-assisted extraction/GC–MS methods. Talanta. 66, 734–739.
11. Farahani, H., Norouzi, P., Dinarvand, R., and Ganjali, M.R. (2007). Development of dispersive liquid–liquid microextraction combined with Gas chromatography–mass spectrometry as a simple, rapid and highly Sensitive method for the determination of phthalate Esters in water samples.  Journal of Chromatography A. 1172, 105-112.

12. Kostanski, L.K., Keller, D.M., Hamielec, A.E. (2004). Size-exclusion chromatography-a review of calibration methodologies. Biochemical and Biophysical Methods. 58, 159-186. 

13. EPA method 3640A, Gel-permeation cleanup. 1994, USEPA, Washington DC, pp. l-24. 
14. Ripp, J. (1996). Analytical Detection Limit Guidance & Laboratory Guide for Calculating Analytical Detection Limits, Wisconsin Department of Natural Resources, Madison, WI 53707.
15. Official Journal of the European Communities (2002). Commission Directive 2002/72/EC of 6 August 2002 relating to plastic materials and articles intended to come into contact with foodstuffs.  Official Journal of the European Communities.
