The Malaysian Journal of Analytical Sciences Vol 16 No 1 (2012): 79 – 87

SYNTHESIS AND CHARACTERISATION OF PALLADIUM(II) SCHIFF BASE COMPLEXES AND  THEIR CATALYTIC ACTIVITIES FOR SUZUKI COUPLING REACTION

(Sintesis dan Pencirian Palladium(II) Bes-Schiff Kompleks dan Aktiviti Sebagai Pemangkin untuk Tindak Balas Suzuki)

Amalina Mohd Tajuddin1, Hadariah Bahron1*, Karimah Kassim1, Wan Nazihah Wan Ibrahim1 
and Bohari M.Yamin2  
1Faculty of Applied Sciences, 

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

2School of Chemical Sciences and Food Technology, 

Faculty of Science & Technology,

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: hadariah@salam.uitm.edu.my
Abstract

The syntheses, physico-chemical and spectroscopic characterization of salicylaldimine-type Schiff-base ligands (Hapbam, HapFbam) and their novel mononuclear Pd(II) complexes (HapbamPd, HapFbamPd) are reported herein. The compounds were characterized by elemental analysis, FT-IR, 1H NMR as well as magnetic susceptibility measurements. X-ray crystallography investigation of HapbamPd revealed that the Schiff bases behave as singly charged bidentate ligands, coordinating to the palladium centre in the ratio of ligand:metal of 2:1. The geometry of the palladium centre was a perfect square planar.  The catalytic potential of the Pd(II) complexes for Suzuki coupling reaction were investigated and monitored using GC. It was observed that both Pd(II) complexes displayed properties of good catalysts for the reaction, indicated by more than 90% conversion of the starting materials to the biphenyl product after 12 hours of reaction time at 100oC in inert conditions.  The catalytic activity was compared with that of commercially available palladium(II) acetate.

Keywords:  Schiff base, Palladium(II), Suzuki reaction

References
1. He, Y., and Cai, C., (2010). Polymer-supported macrocyclic Schiff base palladium complex: An efficient and reusable catalyst for Suzuki cross-coupling reaction under ambient condition. Catalysis Communications, 12, 678-683.

2. Nayak, S., Gamez, P., Kozlevcˇar, B., Pevec, A., Roubeau, O., Dehnen, S., and Reedijk, J., (2011). Coordination compounds from the planar tridentate Schiff-base ligand 2-methoxy-6-((quinolin-8-ylimino)methyl)phenol (mqmpH) with several transition metal ions: Use of [FeIII(mqmp)(CH3OH)Cl2] in the catalytic oxidation of alkanes and alkenes. Polyhedron, 29, 2291–2296.

3. Cui, J., Zhang M., and Zhang, Y., (2010). Amino-salicylaldimine-palladium(II) complexes: New and efficient catalysts for Suzuki and Heck reactions. Inorganic Chemistry Communications, 1, 81-85.

4. Dhara, K., Sarkar K., Srimani D., Saha, S.K., Chattopadhyaye P., and Bhaumik, A., (2010). A new functionalized mesoporous matrix supported Pd(II)-Schiff base complex; an efficient catalyst for the Suzuki-Miyaura coupling reaction. Dalton Transactions, 39, 6395–6402.
5. Ben-saber A.M., Maihub A.A., Hudere S.S., and El-ajaily M.M., (2005). Complexation behavior of Schiff base toward transition metal ions. Microchemical Journal, 81, 191-194.

6. Soliman, A.A., and Linert, W., (1999). Investigation on New Metal Chelates of 3-methoxy -salicylidene-2-aminothiphenol Schiff base. Thermochimica Acta, 338, 67-75.

7. Raman, N., Raja, Y.P., and Kulandaisory, A., (2001).  Synthesis and characterisation of Cu(II), Ni(II), Mn(II), Zn(II) and VO(II) Schiff base complexes derived from o-phenylenediamine and acetoacetanilide. Journal of Chemical Sciences, 113, 183-189.

8. Aslantas, M., Kendi, E., Demir, N., Sabik, A.E., Tümer, M., and Kertmen, M., (2009). Synthesis, spectroscopic, structural characterization, electrochemical and antimicrobial activity studies of the Schiff base ligand and its transition metal complexes. Spectrochimica Acta Part A, 74, 617-624.

9. Mohd Tajuddin, A., Bahron, H., Wan Ibrahim, W.N., and Yamin, B.M., (2010). Bis{2-[1-(benzylimino)ethyl]phenolato}-palladium(II). Acta Crystallographic , E66, m1100.

10. Brayton, D.F., Larkin, T.M., Vicic, D.A., and Navarro, O., (2009). Synthesis of a bis(phenoxyketimine) palladium(II) complex and its activity in the Suzuki-Miyaura reaction. Journal of Organometallic Chemistry, 694, 3008-3011.
