The Malaysian Journal of Analytical Sciences Vol 16 No 1 (2012): 24 – 30

SYNTHESIS AND CHARACTERISATION OF MALEATED POLYPROPYLENE-LALANG FIBER/POLYPROPELYNE COMPOSITES: 
OPTIMISATION PREPARATION CONDITIONS AND THEIR PROPERTIES
(Penyediaan dan Pencirian Komposit Polipropelena Termaleik/Gentian Lalang/Polipropilena: Keadaan Penyediaan Optimum dan Sifatnya)

Sharil Fadli Mohamad Zamri1*, Hasratul Nadiah Mohd Rashid1, Nurul’ Ain Jamion1 
and Rahmah Mohamed2
1International Education College (INTEC),

UiTM Campus Section 17, 40200 Shah Alam, Selangor

2Faculty of Applied Science,

Universiti Teknology MARA, 40450 Shah Alam, Selangor

*Corresponding author: sharil7240@salam.uitm.edu.my
Abstract

Polypropylene (PP) blend with natural lalang fiber (LF) were investigated in this study. LF was chosen in preparation of polymer composites because it is low cost, eco-friendly, abundance, renewable, biodegradable and shows excellent mechanical properties. Hence, LF has highly potential as a natural fiber filler in polymer composites. LF was prepared by drying the lalang leaves under the sun light and were crushed using hammer mill before they were soaked in 5 % sodium hydroxide (NaOH) solution.  The fiber was then washed with distilled water until neutral. LF was dried in an oven then grinded and sieved into specific sizes. LF/PP and maleated polypropylene/LF/PP (MAPP/LF/PP) composites were prepared by extrusion method using a twin-screw extruder between LF, PP and MAPP at different compositions. The LF/PP and MAPP/LF/PP composites were shaped into 3 mm sheet samples using an electric hydraulic hot press at the temperature of 180 ˚C. Several studies were carried out to investigate the optimum preparation conditions including the effect of size and percentage of LF, as well as the percentage of MAPP on their mechanical properties using tensile tester and izod impact tester. Meanwhile, the thermal properties of PP, 15% M size LF/PP and 1% MAPP/15% M size LF/PP composites were analyzed using thermogravimety analysis (TGA) and the characteristic of LF on the cross section of 15% M size LF/PP and 1% MAPP/15% M size LF/PP composites were investigated using a digital microscope.

Keywords: Lalang, Polypropylene, Extrusion, Maleated polypropylene, Polymer composite
References

1. Paiva, M. C., I. Ammar,I., Campos, A. R., Cheikh, R. B. and Cunha, A. M. (2007) Alfa fibres: Mechanical,  morphological and interfacial characterization. Composites Science and Technology 67 1132–1138.
2. Bessadok, A., Roudesli, S., Marais, S., Follain, N. and Lebrun, L. (2009) Alfa fibres for unsaturated polyester composites reinforcement: Effects of chemical treatments on mechanical and permeation properties. Composites: Part A 40 184–195.
3. Liu, W., Mohanty, A. K., Askeland, P., Drzal, L. T. and Misra, M. (2004) Influence of fiber surface treatment on properties of Indian grass fiber reinforced soy protein based biocomposites. Polymer 45 7589–7596.
4. Yang, H. S., Kim, H. J., Park, H. J., Lee, B. J. and Hwang, T. S. (2007) Effect of compatibilizing agents on rice-husk flour reinforced polypropylene composites. Composite Structures 77 (1) 45–55.
5. Wang, J., Gu, M., Songhao, B. and Ge, S. (2003) Investigation of the influence of MoS2 filler on the tribological properties of carbon fiber reinforced nylon 1010 composites. Wear 255 774–779.
6. Vilaseca, F., Valadez-Gonzalez, A., Herrera-Franco, P. J., Pèlach, M. A., López, J. P. and Mutjé, P. (2010) Biocomposites from abaca strands and polypropylene. Part I: Evaluation of the tensile properties. Bioresource Technology 101 387–395.
7. Ismail, H., Edyham, M. R., Wirjosentono, B. (2002) Bamboo fibre filled natural rubber composites: the effects of filler loading and bonding agent. Polymer Testing 21 139–144.
8. Bajwa, S. G, Bajwa,D. S., Holt, G., Coffelt, T. and Nakayama, F. (2011) Properties of thermoplastic composites with cotton and guayule biomass residues as fiber fillers Industrial Crops and Products 33 747–755.
9. Augier, L., Sperone, G., Vaca-Garcia, C. and Borredon, E. (2007) Influence of the wood fibre filler on the internal recycling of poly(vinyl chloride)-based composites. Polymer Degradation and Stability 92 1169-1176.
10. Bismarck, A., Baltazar-Y-Jimenez, A. and Sarlkakis, K. (2006) Green composites as Panacea? Socio-economic aspects of green materials. Environment, Development and Sustainability 8 (3) 445–463.
11. Wambua, P.,Ivens, J. and Verpoest I. (2003) Natural fibres: can they replace glass in fibre reinforced plastics? Composites Science and Technology 63 1259–1264.
12. Duc, A. L., ergnes, B. and Budtova T. (2011) Polypropylene/natural fibres composites: Analysis of fibre dimensions after compounding and observations of fibre rupture by rheo-optics. Composites: Part A 42 1727–1737
13. Ruksakulpiwat, Y., Suppakarn, N., Sutapun, W. and Thomthong, W. (2007) Vetiver–polypropylene composites: Physical and mechanical properties. Composites: Part A 38 590–601.
14. Xie, Y., Hill, C. A. S.,Xiao, Z., Militz, H. and Mai, C. (2010) Silane coupling agents used for natural fiber/polymer composites: A review. Composites: Part A 41 806–819.
15. Bachtiar, D., Sapuan, S. M and Hamdan, M. M. (2008) The effect of alkaline treatment on tensile properties of sugar palm fibre reinforced epoxy composites. Materials and Design 29 1285–1290.
16. Roman-Aguirre, M., Marquez-Lucero, A. and Zaragoza-Contreras E. A. (2004) Elucidating the graft copolymerization of methyl methacrylate onto wood-fiber. Carbohydrate Polymers 55 201–210.
17. Sgriccia, N., Hawley, M. C. and Misra, M. (2008) Characterization of natural fiber surfaces and natural fiber composites. Composites: Part A 39 1632–1637.
18. Beg, M. D. H., Pickering, K. L. (2008) Mechanical performance of Kraft fiber reinforced polypropylene composites: influence of fibre length, fibre beating and hygrothermal ageing. Composites: Part A 39 1748–1755.
19. Liu, S. P and Liang, C. W. (2011) Preparation and mechanical properties of polypropylene / montmorillonite nanocomposites - After grafted with hard/soft grafting agent. International Communications in Heat and Mass Transfer 38 434–441
20. Hirunpraditkoon, S and García, A. N. (2009) Kinetic study of vetiver grass powder filled polypropylene composites. Thermochimica Acta 482 30–38.
21. Qiu, W., Endo, T. and Hirotsu, T. (2005) A novel technique for preparing of maleic anhydride grafted polyolefins. European Polymer Journal 41 1979–1984.
22. Chand, N. and Dwivedi, U. K. (2006) Effect of coupling agent on abrasive wear behaviour of chopped jute fibre-reinforced polypropylene composites. Wear 261 1057–1063.
23. Kim, J. P., Yoon, T. H., Mun, S. P., Rhee, J. M. and Lee, J. S. (2006) Wood–polyethylene composites using ethylene–vinyl alcohol copolymer as adhesion promoter. Bioresource Technology 97 (3) 494–499.
24. Mohanty, S and Nayak, S. K. (2007) Dynamic and steady state viscoelastic behavior and morphology of MAPP treated PP/sisal composites. Materials Science and Engineering A 443 202–208.
25. Idicula, M., Boudenne, A., Umadevi, L., Ibos, L., Candau, Y and Thomas, S. (2006) Thermophysical properties of natural fibre reinforced polyester composites. Composites Science and Technology 66 2719–2725.

