The Malaysian Journal of Analytical Sciences Vol 16 No 1 (2012): 49 – 55

A STUDY ON the MIGRATION OF STYRENE 

FROM POLYSTYRENE CUPS TO DRINKS USING Online solid-phase extraction liquid chromatography (SPE-LC)
(Kajian Mengenai Migrasi Stirena daripada Cawan Polistirena kepada Minuman Menggunakan Teknik Ekstraksi Fasa Pepejal Kromatografi Cecair (SPE-LC))

Norashikin Saim, Rozita Osman*, Hurin Ain Wan Abi Sabian, Mohamad Rafaie Mohamed Zubir, 

Nazarudin Ibrahim
Faculty of Applied Sciences, 

Universiti Teknologi MARA, 40450, Shah Alam, Selangor

*Corresponding author: rozit471@salam.uitm.edu.my
Abstract

The migration of residual styrene from polystyrene cups to drinks has been a major concern in recent years worldwide. In this study, a three-factor response surface experimental design was used to evaluate the interactive effects of temperature (30-80 ºC), pH (5-7) and contact time (35-120 min) on the migration of styrene from polystyrene cups into water. Online solid-phase extraction liquid chromatography (SPE-LC) with diode array detector (DAD) was used for the separation and detection of styrene. Initial temperature of water was found significant in increasing the rate of migration of styrene whereas the effect of contact time was less significant. In terms of interactions between the effects, the relation between temperature and pH was the most significant. The amount of styrene in water varied from 0.3 to 4.2 μg/L with maximum migration obtained at initial water temperature of 80 °C and pH 5. 
Keywords:  migration of styrene, experimental design, polystyrene cups

References
1. Varner, S. L., and Breder, A. (1981). C.V. Headspace sampling and gas chromatographic determination of styrene migration from food-contact polystyrene cups into beverage and food simulants. J. Ass. Offic. Anal.Chem. Int. 64:1122–1130.
2. Varner, S. L., Breder, C. V., and Fazio, T. (1983). Determination of styrene migration from food-contact polymers into margarine, using Azeotropic distillation and head space gas chromatography. J. Ass. Offic. Anal.Chem. Int. 66:1067–1073.

3. Muratak, A., Avakis, S., and Yokoyama, K. (1991). Assessment of the peripheral, central and autonomic nervous system function in styrene workers. Am. J. Index Medicus 20:775–784.

4. Cohen, T., Carlson, G., Charnley, G., Coggon, D., Delzell, E., and Graham, J. D. (2002). A comprehensive evaluation of the potential health risks associated with occupational and environmental exposure to styrene. J. Toxicol. Env. Health B 5:1–263.
5. Khaksar, M.R and Ghazi-Khansari M (2009). Determination of migration monomer styrene from GPPS (general purpose polystyrene) and HIPS (high impact polystyrene) cups to hot drinks. Toxicology Mechanisms and Methods ; 19(3): 257–261.
6. Arvanitoyannis, I. S., and Bosena, L. (2004). Migration of substances from packaging materials to foods. Crit. Rev. Food Nutr. 44:63–76. 
7. Tawfik, M.S. and Huyghebaert, A (1998). Polystyrene cups and containers: styrene migration. Food Addit. Contam. 15(5), 592-599.

8. Till, D. E., Ehntholt, D. J., Reid, R. C., Schwartz, P. S., Schwopc, A. D., Sidman, R. R., and Whelan, R. H. (1982). Migration of styrene monomer from crystal polystyrene to food and food simulating liquid. Ind. Eng. Chem. Prod. Res. Dev. 21:161–185.

9. Mirhosseini, H., Tan, C. P., Hamid, N. S. A., & Yusof, S. (2008). Optimization of the contents of Arabic gum, xanthan gum and orange oil affecting turbidity, average particle size, polydispersity index and density in orange beverage emulsion. Food Hydrocolloids 22, 1212-1223.

10. Joglekar, A. M., & May, A. T. (1987). Product excellent through design of experiments. Cereal Foods World, 32, 857-868.

