The Malaysian Journal of Analytical Sciences Vol 16 No 2 (2012): 110 – 116

SYNTHESIS AND CATALYTIC ACTIVITY OF N,N’-BIS-(α-METHYL-SALICYLIDENE) – PROPANE -1,3- DIAMINEPALLADIUM(II)  AND ITS 4-METHYL DERIVATIVES IN HECK CARBON-CARBON COUPLING REACTION

(Sintesis dan Aktiviti Pemangkinan N,N’-Bis-(α-Metilsalisilidina-Propan-1,3-Diamina-palladium(II) dan Terbitan 4-Metil dalam Tindak Balas Gandingan Karbon-Karbon Heck)

Siti Kamilah Che Soh1,2, Mustaffa Shamsuddin1*, Bohari M. Yamin3
1Department of Chemistry, Faculty of Science,

Universiti Teknologi Malaysia, 81310 Skudai, Johor, Malaysia.
2Department of Chemical Sciences, Faculty of Science and Technology, 

Universiti Malaysia Terengganu, 21030 Kuala Terengganu, Terengganu, Malaysia.

3School of Chemical Sciences and Food Technology, Faculty of Science & Technology,

Universiti Kebangsaan Malaysia, 43650 Bangi, Selangor, Malaysia.

*Corresponding author: mustaffa@kimia.fs.utm.my
Abstract

Carbon-carbon bond formation is an important step in organic synthesis. Palladium(II) complexes have been widely used as catalyst in the transition metal catalysed bond formation. This paper reports the synthesis, characterization and catalytic performance of two palladium(II)-Schiff base complexes obtained from the condensation of 2’-hydroxyacetophenone and its 4’-methyl derivative with 1,3-diaminopropane followed by complexation with palladium(II) acetate, Pd(OAc)2. Ligands and complexes were characterized by NMR and FTIR spectroscopic methods as well as X-ray crystallographic analysis and CHN elemental analyses. The ligands acted as N,N,O,O tetradentate, coordinating to the palladium atom through both its imine nitrogens and phenolic oxygens. The efficiency of these palladium complexes were evaluated as catalysts in the Heck reaction of 4’-bromoacetophenone with methyl acrylate in the presence of sodium hydrogen carbonate as base in N,N-dimethylacetamide as solvent at reflux temperature 120 ºC. The activities of the catalysts were monitored by GC-FID. Both catalysts gave 100% conversion after 12 hours. The product of the reactions is 3-(4-Acetylphenyl)-acrylic acid methyl ester.
Keywords: Palladium, Schiff base, Heck reaction
References

1. Keles, M., Keles, T. and Serindag, O. (2008). Palladium complexes with bis(diphenylphosphino methyl)amino ligands and their application as catalysts for Heck reaction. Transition Met Chem. 33, 717-720.
2. Hartung, C. G., Köhler, K. and Beller, M. (1999). Highly Selective Palladium-Catalyzed Heck Reactions of Aryl Bromides with Cycloalkenes. Org Lett. 1, 709-711.
3. Blaser, H. U., Indolse, A., Schnyder, A., Steiner, H. and Stder, M. (2001). Supported Palladium Catalysts for Fine Chemicals Synthesis. J. Mol. Catal: A. Chem. 173,3-18.
4. Kayan, C., Biricikkk, N. and Aydemir, M. (2011). Aminophosphine ligands: Synthesis, Coordination Chemistry and Activity of Their Palladium(II) Complexes in Heck and Suzuki Cross-coupling Reactions. Transition Met Chem. 36, 513-520.
5. He, Y. and Cai, C. (2011). Polymer-Supported Macrocyclic Schiff Base Palladium Complex as an Efficient Catalyst for the Heck Reaction. Appl. Organomatal. Chem. 25, 799-803.
6. Lu, J. M., Ma, H., Li, S. S., Ma, D. and Shao, L. X. (2010). 2,2’-Diamino-6,6’-Dimethylbiphenyl as an Efficient Ligand in the Palladium-Catalyzed Suzuki-Miyaura and Mizoroki-Heck Reactions. Tetrahedron. 66, 5185-5189.
7. Basak, S., Sen, S., Mitra, S., Marschner, C. and Sheldrick, W. S. (2008). Square Planar Complexesof Cu(II) and Ni(II) with  N2O Donor Set of Two Schiff Base Ligands: Synthesis and Structural Aspects. Struct Chem. 19, 115-121
8. Wang, M., Zhu, H., Jin, K., Dai, D. and Sun, L. (2003). Ethylene Oligomerization by Salen-Type Zirconium Complexes to Low-Carbon Linear α-Olefins. J. Catal. 220, 392-398
9. Sheldrick, G. M. (2008). A Short History of SHELX. Acta Cryst. A64, 112-122.
10. Montazerozohori, M., Habibi, H. M., Hajjati, A., Mokhtari, R., Yamane, Y. and Suzuki, T. (2009). 2,2’-[(E,E)-1,1’-(2,2-Dimethylpropane-1,3-diyldinitrilo)diethyllidene]diphenol. Acta Cryst. E65, o1662-o1663. 
11. Soliman, A. A. and Linert, W. (1999). Investigations on New Transition Metal Chelates of the 3-Methoxy-Salicylidene-2-Aminothiophenol Schiff Base. Thermochimica acta. 338, 67-75.
12. Ibrahim, W. N. W., Shamsuddin, M. and Yamin, B. M. (2007). N,N’-bis-(5-Methyl-Methylsalicylidene)-2,2-Dimethylpropane-1,3-Diamine Palladium(II) : Catalyst for Heck Reaction. Malaysian. J. Anal. Sci. 11, 98-104.
13. Shamsuddin, M., Nur, A. M. M. and Yamin, B. M. (2005). N-[2-(Diphenylphosphanyl)benzylidene]-4-methylaniline. Acta Cryst. E61, o2263-o2264. 

