SYNTHESIS AND CHARACTERIZATION OF Ti-PHENYL@SiO2 CORE-SHELL NANOPARTICLES CATALYST
(Penyediaan dan Pencirian Pemangkin Ti-Phenyl@SiO2 Teras-Cangkerang Nanopartikel)

Syamsi Aini1,2,  Jon Efendi1,2, Hendrik Oktendy Lintang1, Hadi Nur1,*

1Ibnu Sina Institute for Fundamental Science Studies, Universiti Teknologi Malaysia,

81310 UTM Skudai, Johor, Malaysia
2Department of Chemistry, Faculty of Mathematics and Natural Sciences, Universitas Negeri Padang, 

Jln. Prof.  Dr. Hamka, Air Tawar, Padang 25131, West Sumatera, Indonesia

*Corresponding author: hadi@kimia.fs.utm.my
ABSTRACT
This study highlights the potential use of Ti-Phenyl@SiO2 core-shell nanoparticles as heterogeneous catalysis in oxidation reaction. The Ti-Phenyl@SiO2 was synthesized by reduction of TiCl4 and diazonium salt with sodiumborohydride to produce phenyl titanium nanoparticles (Ti-Phenyl), followed by the silica shell coating using tetraethyl orthosilicate (TEOS). The Ti-Phenyl@SiO2 nanoparticles were characterized by Fourier transform infrared (FTIR) spectrometer, diffuse reflectance (DR) UV-visible spectrometer, thermogravimetric analyzer (TGA), X-ray diffraction (XRD) spectrometer, field emission scanning electron microscope (FESEM) and transmission electron microscope (TEM). The core-shell size of Ti-Phenyl@SiO2 was in the range of 40 to 100 nm with its core composed with an agglomeration of Ti-Phenyl. The Ti-Phenyl@SiO2 was active as a catalyst in the liquid phase epoxidation of 1-octene with aqueous hydrogen peroxide as an oxidant.
Keywords: Ti-Phenyl@SiO2, core-shell, nanoparticles, epoxidation, aqueous hydrogen peroxide
ABSTRAK
Kajian ini menekankan potensi penggunaan Ti-Phenyl@SiO2 nanopartikel teras-cangkerang sebagai pemangkinan heterogen dalam tindak balas pengoksidaan. Ti-Phenyl@SiO2 telah disediakan dengan pengurangan TiCl4 dan garam diazonium dengan natrium borohidrida untuk menghasilkan titanium-fenil nanopartikel (Ti-Phenyl), diikuti oleh salutan cangkerang silika menggunakan tetraetil ortosilikat (TEOS). Ti-Phenyl@SiO2 nanopartikel telah dicirikan oleh spektrometer jelmaan Fourier inframerah (FTIR), spektrometer pantulan meresap (DR) UV-nampak, analyzer termogravimetri (TGA), spektrometer pembelauan sinar-X (XRD), bidang pelepasan mikroskop imbasan elektron (FESEM ) dan mikroskop elektron penghantaran (TEM). Saiz teras-cangkerang Ti-Phenyl@SiO2 adalah dalam lingkungan 40 hingga 100 nm dengan terasnya terdiri daripada penumpukkan Ti-Phenyl. Ti-Phenyl@SiO2 adalah pemangkin aktif dalam pengepoksidaan fasa cecair 1-oktene dengan hidrogen peroksida berair sebagai oksidan.

Kata kunci: Ti-Phenyl@SiO2, teras-cangkerang, nanopartikel, pengepoksidaan, hidrogen peroksida berair.
1. INTRODUCTION

The chemical properties of heterogeneous catalysts can vary depending on the dimensions of structure, the nature of environment of active site and depending on how the absorption of reactants takes place to the catalysts surface [1–4]. The ability to prepare catalysts in nanometer size for oxidation of hydrophobic reactant will open significant opportunities in chemistry and material science. Recently, metal-carbon nanoparticles with various organic moieties have been utilized for a number of applications, such as electronics, and catalysts [5–7]. 
The nanoparticles of metal-carbon covalent bonding with core-shell structures (M-C) are the compound with stronger metal-carbon bond, and with hydrophobic moiety at the surface. The addition of silica to the shell of M-C (M-C@SiO2) is an exciting challenge that improves the stability and selectivity of the resulting catalyst [8,9]. The unique method, structure and catalytic activity of Ti-Phenyl@SiO2 had not been explored. In this compound, the titanium has an empty d orbital, which can act as acidic Lewis and is a highly potential compound used as a catalyst [10]. The organic moiety (phenyl) at the surface of metal-carbon nanoparticles can act as absorbent of the organic substrate, and silica-shell (SiO2) to increase stability of the metal-carbon nanoparticles.  This paper reports the synthesis, characterization and catalytic activity of Ti-Phenyl@SiO2 nanoparticles in the core-shell structure for oxidation of 1-octene, with H2O2 as an oxidant.
2.  EXPERIMENTAL

2.1
Preparation of Ti-Phenyl@SiO2
The Ti-Phenyl@SiO2 was synthesized by reduction the TiCl4 (5 mmol) and phenyl diazonium fluoroborate (10 mmol) with sodiumborohydride (12 mmol) to produce titanium-phenyl nanoparticles (Ti-Phenyl), followed by coating of the Ti-Phenyl using tetraethyl orthosilicate (TEOS Fluka) in the range of 5 to 20 mmol. The Ti-Phenyl@SiO2 formed has a Si to Ti the mol ratio varied from 1 to 4, and labeled with Ti-Phenyl@SiO2(1), Ti-Phenyl@SiO2(2), Ti-Phenyl@SiO2(3), and Ti-Phenyl@SiO2(4). 
2.2
Characterizations

The Ti-Phenyl, Ti-Phenyl@SiO2(1), Ti-Phenyl@SiO2(2), Ti-Phenyl@SiO2(3), and Ti-Phenyl@SiO2(4) were characterized by Fourier transform infrared (FTIR) spectrometer, UV-Vis diffuse reflectance (UV-Vis DR) spectrometer, thermogravimetric analyzer (TGA), X-ray diffraction (XRD) spectrometer, field emission scanning electron microscope (FESEM), and transmission electron microscope (TEM). The FTIR spectra of all samples were collected on a Perkin Elmer Spectrum One (FTIR) spectrometer with 10 scans and resolution of 4 cm–1, in the range of 4000 – 400 cm–1. UV-Vis spectra of resulting catalysts were recorded using Perkin-Elmer Lamda 900 spectrometer. TGA and DTA graphs were obtained by using a Matter Toledo TGA/SDTA 851 instrument under N2 atmosphere with a flow rate of 20 ml min–1, in the temperature range of 25 to 900 oC, at the heating rate of 10 oC min–1, with 12 mg of sample. XRD patterns were recorded on a Bruker D8 advance instrument using Cu Kα radiation (λ = 1.5418 Å, kV = 40, mA = 40). Morphological structure and particle size were observed by field emission scanning electron microscopy (FESEM, JEOL JSM 6701F) with platinum coating (2 kV, 10 mA).
2.3
Activity of Ti-Phenyl@SiO2
To study the catalytic activity of Ti-Phenyl@SiO2, the oxidation of 1-octene by using aqueous H2O2 was used as a model reaction. In the oxidation, 1-octene (8 mmol, Merck), 30% aqueous H2O2 (15 mmol), and Ti-Phenyl@SiO2 (50 mg) were placed in round bottle glass with condenser. The reaction was performed with stirring at 80 oC for 8 h, and the resulting products were analyzed with the Gas Chromatograph (GC). 

3. RESULTS AND DISCUSSION

3.1 
Physical properties
The Ti-Phenyl@SiO2 nanoparticles have been synthesized in this research. Schematic representation of the reaction for synthesis of Ti-Phenyl@SiO2 is shown in Fig. 1. The mol ratio of TEOS to TiCl4 used to synthesize Ti-Phenyl@SiO2 nanoparticles catalysts were summarized in Table 1. 

[image: image13.png]



Figure 1. Schematic representation of the reaction for synthesis of Ti-Phenyl@SiO2.

Table 1. The mole ratios of TEOS to TiCl4 used to synthesize Ti-Phenyl@SiO2 nanoparticles catalyst.
	No.
	Mole ratios of  TEOS to TiCl4
	Catalysts

	1
	1 : 1
	Ti-Phenyl@SiO2(1)

	2
	2 : 1
	Ti-Phenyl@SiO2(2)

	3
	3 : 1
	Ti-Phenyl@SiO2(3)

	4
	4 : 1
	Ti-Phenyl@SiO2(4)


 SHAPE  \* MERGEFORMAT 



Figure 2.  The FTIR spectra of (a) Phenyl diazonium,  (b) Ti-Phenyl, (c) Ti-Phenyl@SiO2(1), (d) Ti-Phenyl@SiO2(2), (e) Ti-Phenyl@SiO2(3), and (f) Ti-henyl@SiO2(4).
Fig. 2 shows the FTIR spectra of phenyl diazonium, Ti-Phenyl, and Ti-Phenyl@SiO2 with Si to Ti mole ratio 1 – 4. The existence of aromatic ring on the phenyldiazonium can be seen from the =C–H stretch peak at 3075 cm–1 and 3014 cm–1, the =C– H bend out of plane at 667 cm–1 and 749 cm–1. The C=C stretch vibration at 1462 cm–1 and 1566 cm–1. On other hand for the Ti-Phenyl and Ti-Phenyl@SiO2 all of the =C–H and C=C peak shifted to the lower wavenumber. This is caused by the influence of Ti and SiO2 substituent into the aromatic ring. The sharp peak at 2294 cm–1 and at 1306 cm–1 correspond to N(N and C–N vibration of phenyl diazonium (C6H5N(N+) respectively, for the Ti-Phenyl (C6H5-Ti) and Ti-Phenyl@SiO2 (Ti-C6H5@SiO2) the peak at 2294 cm–1 and 1306 cm–1 disappeared. It means that led to the release of N(N and the binding of the phenyl to the titanium core via Ti–C covalent linkages. The existence of SiO2 shell on the Ti-Phenyl@SiO2 spectra can be seen with Si–O–Si vibration at 1000 – 1200 cm–1. The same FTIR spectra have been reported previously [6] for preparation of the palladium nanoparticles using aryl diazonium salt. The existence of Ti-Phenyl and Ti-Phenyl@SiO2 was further examined by UV-Vis measurements.

 SHAPE  \* MERGEFORMAT 


            

Figure 3. The UV-Vis spectra of (a) Ti-Phenyl, (b) Ti-Phenyl@SiO2(1), (c) Ti-Phenyl@ SiO2(2), (d) Ti-Phenyl@SiO2(3)  and  (e) Ti-Phenyl@SiO2(4).

The UV-Vis spectra of Ti-Phenyl and Ti-Phenyl@SiO2 are depicted in Fig. 3. The UV-Vis absorption of Ti-Phenyl showed a band at 266 nm. Band at 266 nm is ascribed as the forbidden transition to a homo nuclear exited state (π– π*) of aromatic bond to Ti. The broad band at 300 nm indicated that there is Ti metal in nanometer size [11]. The UV-Vis absorption of Ti-Phenyl@SiO2 shows bands at 257, 384 and 534 nm. Ti-Phenyl@SiO2 showed a longer wavelength with more intense peaks compared to than that of Ti-Phenyl. This is due to substitution of Ti to aromatic and dipole-dipole interaction on the surface of Ti-Phenyl with SiO2 (bathochromic and red shift) [6]. 

Chemical composition or thermal stability of the Ti-Phenyl and Ti-Phenyl@SiO2 was examined by using the TGA and Differential TGA (DTA) analysis, as presented in Fig. 4. A distinct degradation step can be clearly observed for Ti-Phenyl observed at 185 oC and 433 oC (see Fig. 4a). The weight loss at ca. 185 and 433 oC is associated with decomposition of organic moiety of Ti-Phenyl. When the decomposition of the organic moiety of Ti-Phenyl was compared to those of Ti-Phenyl@SiO2, only the weight loss at ca. 425 was observed in Ti-Phenyl@SiO2 suggesting that the Ti-Phenyl was trapped in the core structure (see Fig. 4b). 
Diffraction patterns of the Ti-Phenyl and Ti-Phenyl@SiO2 prepared with Si/Ti ratio was 1 to 4 are presented in Fig. 5. It is observed that Ti-Phenyl sample had very broad peaks at 2( = 35, 38, 40, 53, and 62 suggesting the titanium metal was in metallic form and nanometer size [12-14]. The very broad peaks were also observed in Ti-Phenyl@SiO2(1), Ti-Phenyl@SiO2(2), Ti-Phenyl@SiO2(3) and Ti-Phenyl@SiO2(4) samples. This suggests that the titanium metal particles were also in metallic form and nanometer size in the Ti-Phenyl@SiO2 samples. 

[image: image4.emf]Weight  / %

20

40

60

80

100

�C 50 100 150 200 250 300 350 400 450 500 550 600 650 700 750

�C 50 100 150 200 250 300 350 400 450 500 550 600 650 700 750

Ti-Phenyl

Ti-Phenyl@SiO

2

Ti-Phenyl@SiO

2

Ti-Phenyl

185 

0

C

433 

0

C

425 

0

C

Temperature  / 

o

C

-0.15

-0.10

-0.05

0.00

(a)

(b)

Heat flow  /  min

–

1


Figure 4. (a) TGA and (b) DTA curves for Ti-Phenyl and Ti-Phenyl@SiO2.
[image: image5.emf]20 40 60 80

2



/ deg.

Diffraction  Intensity / a.u.

20 40 60 80

2



/ deg.

Diffraction  Intensity / a.u.

(a)

(b)

NaCl

NaCl

Ti

Ti

Ti

Ti

Ti

(c)

(d)

(e)

(a)


Figure 5. The XRD patterns of (a) Ti-Phenyl, (b) Ti-Phenyl@SiO2(1), (c) Ti-Phenyl@SiO2(2), (d) Ti-Phenyl@SiO2(3) and (e) Ti-Phenyl@SiO2(4). 
The morphologies of Ti-Phenyl@SiO2 were obtained by a field emission scanning electron microscope (FESEM). As shown in Fig. 6, the catalyst particles are nearly spherical shape. The particles size of Ti-Phenyl@SiO2(1),  Ti-Phenyl@SiO2(2), Ti-Phenyl@SiO2(3) and Ti-Phenyl@SiO2(4)  are in the range of 20 to 35 nm. The size and crystallinity of Ti-Phenyl nanoparticles and the shell of Ti-Phenyl@SiO2 was verified with TEM image as below. 
Fig. 7 shows the TEM image of Ti-Phenyl and Ti-Phenyl@SiO2. The Ti-Phenyl particles size was in the range of 3 to 5 nm. The Ti-Phenyl@SiO2 has a core composed by agglomerate Ti-Phenyl with the core-shell sizes were in the range of 40 to 100 nm. The diffraction pattern obtained from the TEM image in Fig. 7 proved that the Ti was crystalline. 
              [image: image6.png]



[image: image1.emf]HBF

4, 

TiCl

4

, NaBH

4

Ti  metals

Phenyl

Hydrophobic moiety 

Porous silica

THF

Aniline

Diazonium  salt        

Ti-Phenyl

Ti-Phenyl@SiO

2 

NH

2

N N

+-

BF

4

TEOS

NaNO

2

[image: image9.png]


Figure 6. The FESEM photomicrograph of (a) Ti-Phenyl@SiO2(1), (b) Ti-Phenyl@SiO2(2), (c) Ti-Phenyl@SiO2(3)  and (d) Ti-Phenyl@SiO2(4).

3.2 

Activity of Ti-Phenyl@SiO2

Fig. 8 shows the turn over number (TON) of 1, 2-epoxyoctane and 1, 2-octanediol in the oxidation of 1-octene over Ti-Phenyl@SiO2(1), Ti-Phenyl@SiO2(2), Ti-Phenyl@SiO2(3), Ti-Phenyl@SiO2(4) catalysts with aqueous hydrogen peroxide. All the Ti-Phenyl@SiO2 catalysts showed the higher TON than that of TiO2 in the epoxidation of 1-octene to 1, 2-epoxyoctane. The reusability of the catalysts was carried in this study. Only ca. 15% decreases in the TON was observed when the catalysts were recycled (see Fig. 8).  The other possible products, i.e. 1,2-octanediol and 2-octanone were not observed in this catalytic reaction.   
[image: image7.png]Ti=Phenyl

\ ¥

Ti=Phenyl@SiO,




   

Figure 7.  TEM image of (a) Ti-Phenyl and (b) Ti-Phenyl@SiO2 core shell nanoparticles.

[image: image8.emf]0

0.1

0.2

0.3

a b c d e

1,2-epoxyoctane of the original catalysts

1,2-epoxyoctane of the recycle catalysts

Catalysts

TON


Figure 8. Epoxidation activity of (a) Ti-Phenyl@SiO2 (1), (b) Ti-Phenyl@SiO2 (2), (c) Ti-Phenyl@SiO2 (3), (d) Ti-Phenyl@SiO2(4) and (e) TiO2.

4. 
CONCLUSIONS

The Ti-Phenyl@SiO2 with core-shell structure was successfully synthesized by the silica coating to Ti-Phenyl by using tetraethyl orthosilicate (TEOS). The Ti-Phenyl@SiO2 has a core containing agglomerate Ti-Phenyl with the core-shell size was in the range of 40 to 100 nm. The Ti-Phenyl@SiO2 was active and reusable in the liquid phase epoxidation of 1-octene with aqueous hydrogen peroxide.
ACKNOWLEDGMENTS

We gratefully acknowledge the funding from Universiti Teknologi Malaysia (UTM), under Research University Grant (GUP. No. Q.J130000.7126.01H06). 
REFERENCES

1. Tatsumi, T. (2000). Importance of hydrophobicity in the liquid phase oxidation catalyzed by titanosilicates. Research on Chemical Intermediates, 26(1), 7-12.
2. Nur, H. Manan, A.F.N.A., Wei, L.K., Muhid, M.N.M., Hamdan, H. (2005). Simultaneous adsorption of a mixture of paraquat and dye by NaY zeolite covered with alkylsilane. Journal of Hazardous Materials, 117, 35-40. 
3.  
Nur, H., Hau, N.Y.,  Misnon, I.I., Hamdan, H., Muhid, M.N.M. Hydrophobic fluorinated TiO2-ZrO2 as catalyst in epoxidation of 1-octene with aqueous hydrogen peroxide. Materials Letters, 60, 2274-2277. 
4. 
Corma, A. Domine, M. Gaona, J.A. Jorda, J.L. Navarro, M.T. Rey, F. Pariente, J.P. Tsuji, J. McCulloch, B., Nemeth, L.T. (1998). Strategies to improve the epoxidation activity and selectivity of Ti-MCM-41. Chemical Communication. 2211-2212.
5.
Ghosh, D., Chen, S. (2008). Palladium nanoparticles passivated by metal-carbon covalent linkages. Journal of Materials Chemistry, 18(7), 755-762.

6. 
Ghosh, D., Pradhan, S., Chen, W., Chen, S. (2008). Titanium nanoparticles stabilized by Ti−C covalent bonds. Chemistry of Materials, 20(4), 1248-1250.
7. 
Chen, W., Chen, S., Ding, F., Wang, H., Brown, L. E., Konopelski, J. P. (2008). Nanoparticle - mediated intervalence transfer. Journal of the American Chemical Society, 130(36), 12156-12162.
8. 
Chou, K.-S., Chen, C.-C. (2007). Fabrication and characterization of silver core and porous silica shell nanocomposite particles. Microporous and Mesoporous Materials, 98(1-3), 208-213.

9. 
Arends, I. W. C. E., Sheldon, R. A. (2001). Activities and stabilities of heterogeneous catalysts in selective liquid phase oxidations: recent developments. Applied Catalysis A: General, 212(1-2), 175-187.
10. 
Corma, A., García, H. (2002). Lewis acids as catalysts in oxidation reactions: from homogeneous to heterogeneous systems. Chemical Reviews, 102(10), 3837-3892.
11. 
Ayi, A., Khare, V., Strauch, P., Girard, J., Fromm, K., Taubert, A. (2010). On the chemical synthesis of titanium nanoparticles from ionic liquids. Monatshefte für Chemie / Chemical Monthly, 141(12), 1273-1278.
12. 
Halalay, I. C., Balogh, M. P. (2008). Sonochemical method for producing titanium metal powder. Ultrasonics Sonochemistry, 15(5), 684-688.
13. Dhara, S., Giri, P.K. (2012). Ti nanoparticles decorated ZnO nanowires heterostructure: photocurrent and photoluminescence properties. Journal of Experimental Nanoscience, 1-9. 
14.

Uchida, M., Oyane, A. Kim, H.M., Kokubo, T., Ito, A. (2004). Biomimetic coating of laminin-apatite composite on titanium metal and its excellent cell-adhesive properties. Advanced Materials, 16(13), 1071-1074.                                                                                                                                                                                                                                                                                                      
4000





3200





2400





1800





1400





1000





600





Ti-C





   Wavenumber / cm -1





C=C





N(N





C-H stretching





C=C





C-N





C-H bending





C-H





Si-O-Si





Transmittance / a.u.





(a)





(b)





(c)





(d)





(e)





(f)





C=C





200





300





400





500





600





700





800





Wavelength / nm





300





266





384





534





(e)





(d)





(c)





(b)





(a)





257





Absorbance / a.u.








(c)








(a)





















































































































































































































































[image: image10.png]


[image: image11.png]


[image: image12.png]


Chart1



1,2-epoxyoctane of the original catalysts	a	b	c	d	e	0.17	0.22	0.25	0.25	2.9000000000000001E-2	1,2-epoxyoctane of the recycle catalysts	a	b	c	d	e	0.13	0.2	0.18	0.22	2.8000000000000001E-2	







Sheet1



		x		y1		y2

		TiPSiO2 (1)		0.42		0.3

		TiPSiO2 (2)		0.42		0.37

		TiPSiO2 (3)		0.42		0.3

		TiPSiO2 (4)		0.36		0.32



x	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	0	0.42	0.42	0.42	0.36	x	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	0	0.3	0.37	0.3	0.32	y1	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	0.42	0.42	0.42	0.36	y2	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	0.3	0.37	0.3	0.32	

Sheet2

												x		1,2-epoxyoctane yield of the original catalysts		1,2-epoxyoctane yield of the recycle catalysts

												TiPSiO2 (1)		0.42		0.3

												TiPSiO2 (2)		0.42		0.37

												TiPSiO2 (3)		0.42		0.3

												TiPSiO2 (4)		0.36		0.32

												TiO2		0.23		0.21



1,2-epoxyoctane yield of the original catalysts	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	0.42	0.42	0.42	0.36	1,2-epoxyoctane yield of the recycle catalysts	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	0.3	0.37	0.3	0.32	Catalysts



1,2-epoxyoctane yield (%)





Sheet3

																				TON mmol product / mmol cata;lysts								Perhitungan TON dari Rumus molekul catalysts yang diharapkan

						x		1,2-epoxyoctane yield of the original catalysts		1,2-epoxyoctane yield of the recycle catalysts										Catalysts		1,2-epoxyoctane of the original catalysts		1,2-epoxyoctane of the recycle catalysts				Ti-Phenyl@SiO2 Mr =		mmol  catalysts 		mol product1		mol product 2

						TiPSiO2 (1)		0.42		0.3										a		0.17		0.13				100 mg / 262		a= 0.3817  mmol		0.06695 mmol		0.047303mmol

						TiPSiO2 (2)		0.42		0.37										b		0.22		0.2				100 mg / 322.1		b= 0.3105 mmol		0.06715 mmol		0.06156 mmol

						TiPSiO2 (3)		0.42		0.3										c		0.25		0.18				100 mg / 382.2		c= 0.2616 mmol		0.067465 mmol0.047215 mmol

						TiPSiO2 (4)		0.36		0.32										d		0.25		0.22				100 mg / 442.3		d= 0.2261 mmol		0.05706 mmol		0.051101 mmol

						TiO2		0.23		0.21										e		0.029		0.028



1,2-epoxyoctane yield of the original catalysts	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	TiO2	0.42	0.42	0.42	0.36	0.23	1,2-epoxyoctane yield of the recycle catalysts	TiPSiO2 (1)	TiPSiO2 (2)	TiPSiO2 (3)	TiPSiO2 (4)	TiO2	0.3	0.37	0.3	0.32	0.21	Catalysts



1,2 -epoxyoctane/% 





1,2-epoxyoctane of the original catalysts	a	b	c	d	e	0.17	0.22	0.25	0.25	2.9000000000000001E-2	1,2-epoxyoctane of the recycle catalysts	a	b	c	d	e	0.13	0.2	0.18	0.22	2.8000000000000001E-2	





mailto:Ti-Phenyl@SiO2%20Mr%20=


