The Malaysian Journal of Analytical Sciences Vol 16 No 3 (2012): 247 – 255

RAPID SYNTHESIS AND CHARACTERIZATION OF NANOSODALITE SYNTHESIZED USING RICE HUSK ASH 

(Sintesis Cepat dan Pencirian Nanosodalit yang Disintesis Menggunakan Abu Sekam Padi)
Siti Haslina Ahmad Rusmili¹, Leny Yuliati² and Zainab Ramli1*
¹Department of Chemistry, Faculty of Science, 

²Ibnu Sina Institute for Fundamental Science Studies, 

Universiti Teknologi Malaysia,81310 Johor Bahru, Johor, Malaysia

*Corresponding author: zainab@kimia.fs.utm.my
Abstract

Rice husk ash (RHA) which contains more than 90 percent silica is proven to be an active silica source in zeolite synthesis. In this study, nanosodalite has been successfully synthesized hydrothermally at 60⁰C using RHA as silica source in alkaline medium at various crystallization times. Commercial fumed silica was used as comparison for the silica source. Analysis by XRD has shown that pure nanosodalite was formed in 3 hours and stable up to more than 24 hours when using RHA as silica source. On the other hand, fumed silica produced pure nanosodalite only at 4 hours while a mixture of zeolites was observed outside this time range. FESEM shows a worm-like morphology of nanosodalite in the size range of 50-100 nm while FTIR shows the formation of aluminosilicates bonds. Analysis on the dissolved silica in the gel reaction mixture demonstrates the decreasing mass of silica after prolong time of crystallization which indicates the consumption of the dissolved silica in crystal growth of nanosodalite. This study shows that RHA is a better silica source in stabilizing the nanosodalite phase in oxide gel reaction mixture as compared to fumed silica. 

Keywords: Rice husk ash , Commercial fumed silica, Zeolite, Nanosodalite
References
1. An, D, Guo, Y, Zhu, Y and Wang, Z. (2010). A green route to preparation of silica powders with rice husk ash and waste gas. Chemical Engineering Journal. 162: 509-514.

2. Tzong-Horng, L. and Chun-Chen, Y. (2011). Synthesis and surface characteristics of nanosilica produced from alkali-exracted rice husk ash. Materials Science and Engineering B. 176: 521-529.

3. Prasetyoko, D., Ramli, Z., Endud, S., Hamdan, H. and Sulikowski, B. (2006). Conversion of rice husk ash into zeolite beta. Waste Management. 26: 1173-1179.

4. Dalal, A.K. and Rao, M.S. (1985). Synthesis of NaX using silica from rice husk ash. Industrial and Engineering Chemistry Research and Development. 24: 465-468.

5. Ghasemi, Z. and Younesi, H. (2011). Preparation and characterization of nanozeolite NaA from rice husk ash at room temperature with organic additives. Journal of Nanomaterials. ID 858961.

6. King, R.S.P.,  Dann, S.E., Elsegood, M.R.J., Kelly, Mortimer, R.J. (2009). The synthesis, full characterization and utilization of template-free silica sodalite, a novel polymorph of silica. Chemistry – A European Journal. 15(22): 5441-5443.

7. Li, D., Yao, J.F. , Wang, H., Hao, Na, Zhou, D., Ratinac, K.R. and Ringer, S.P. (2007). Organic-functionalized sodalite nanocrystals and their dispersion in solvents. Microporous and Mesoporous Material. 106: 262-267.

8. Majano, G., Darwiche, A., Mintova, S. and Valtchev, V. (2009). Seed-induced crystallization of nanosized Na-ZSM-5 crystals. Industrial and Engineering Chemistry Research and Development. 48: 7084-7091.

9. Fagihihian, H. and Godasandeha, N. (2008). Synthesis of nanocrystalline zeolite Y from bentonite. Journal of Porous Materials. 16. No. 3: 331-335.

10. Pan, Y., Ju, M., Yao, J.F., Zhang, L.X. and Xu, N.P. (2009). Preparation of uniform nano-sized zeolite A crystals using manipulated organic-template free synthesis solutions. Chemical Communications. Issue 46: 7233-7235.

11. Xhan, B.Z., White, M.A., Robertson, K.N., Cameron, T.S. and Gharghouri, M. (2001). A novel organic-additive free synthesis of nanometer-sized NaX crystals. Chemical Communications. 13: 1176-1177.

12. Fan, W., Morozumi, K., Kimura, R., Yokoi, T. and Okubo, T. (2008). Synthesis of nanometer-sized sodalite without adding organic additives. Langmuir. 24: 6952-6958.
13. Ramli, Z. (1995) “Rhenium-Impregnated Zeolites: Synthesis, Characterization and Modification as catalysts in the Metathesis of Alkanes,” Ph.D. Thesis, Universiti Teknologi Malaysia.
14. Hamdan, H., Muhid, M.N.M., Endud, S., Listorini, E. and Ramli, Z. (1997). Journal of Non-Crystalline Solids. 211: 126-131.
15. Ding, L.H., Yang, H., Rahimi, P., Omotoso, O,. Friesen, W., Fairbridge, C., Shi, Y. and Ng, S. (2010). Solid transformation of zeolite A to sodalite. Microporous and Mesoporous Materials. 130: 303-308 

16. Xu, R. et al. (2007). Chemistry of zeolites and related porous materials: synthesis and structure. Wiley, pg 285-286

17. Charles M. Lukeheart and Robert A. Scott. (2008). Nanomaterials: Inorganic and Bioinorganic Perspectives. John and Wiley and Sons. pg 543-563
18. Auerbach, S.E, Carrado, A.K. and Dutta, K.P. (2003). Handbook of Zeolite Science and Technology.  5th Edition, Marcel Dekker Inc. pg. 129-195 

19. Naskar, M.K., Kundu, D. and Chaterjee, M. (2011). Coral-like hydroxyl sodalite particles from rice husk ash as silica source. Materials Letter. 65: 3408-3410

