The Malaysian Journal of Analytical Sciences Vol 16 No 3 (2012): 277 – 282

ELECTRODEPOSITED ZnO/Zn PHOTOCATALYSTS FOR THE DEGRADATION OF BENZENE-TOLUENE-XYLENE MIXTURE IN AQUEOUS PHASE
(Fotomangkin ZnO/Zn Electroendapan bagi Degradasi Campuran Benzena-Toluena-Xilena dalam Fasa Akueus)

Lee Chien Ju, Wan Azelee Wan Abu Bakar*, Rusmidah Ali 

Faculty of Science,

Universiti Teknologi Malaysia, 81310 UTM Skudai, Johor, Malaysia
*Corresponding author: wazelee@ kimia.fs.utm.my

Abstract

The recognition of the ability of volatile organic compounds, (VOCs) to pollute the ground water is now well documented. VOCs such as benzene, toluene and xylene from the petroleum industries processed water leaked through the underground old piping system into the soils and groundwater during its transportation to the wastewater plant. Photocatalysis have been used as a potential system in the degradation of VOCs in the wastewater. However, the powdered form photocatalysts that were used in various studies are difficult to be separated from the aqueous solution at the end of the treatment. Therefore, the main objective of this research is to prepare the electrodeposited photocatalysts for the degradation of aromatic hydrocarbon mixture, benzene-toluene-xylene (BTX) solution under UV light (354 nm). The concentrations of electrolyte and electrodeposition voltages used to prepare the photocatalysts were studied for their efficiency in the degradation. From the research, ZnO/Zn prepared in 0.8 M NaOH and under 12 V possessed the best catalytic degradation performance by degrading 32.37% of BTX in the solution. The ZnO/Zn photocatalyst was characterized using X-ray Diffraction Techniques (XRD) which illustrated high crystallinity of Zn species and reasonably high amorphous phase of ZnO species.

Keywords: Electrodeposited photocatalyst, benzene-toluene-xylene, UV-light, zinc oxide
References
1. Otenio, M. H., Lopes da Silva, M. T., Marques, M. L. O. and Roseiro, J. C. and Bidoial, E. D. (2005). Benzene, Toluene and Xylene Biodegradation by Pseudomonaas Putida CCMI 825. Brazilian Journal of Microbiology. 36. 258-261.

2. Dean, B. J. (1985). Recent Findings on the Genetic Toxicology of Benzene, toluene, xylenes and phenols. Mutat Res. 154. 153-181.
3. Baldwin, B. R., Nakatsu, C. H. and Nies, L. (2003). Detection and Enumeration of Aromatic Oxygenase Genes by Multiplex and Real-Time PCR.  Appl. Environ. Microbiol.. 69. 3350-3358.

4. Mesarch, M. B., Nakatsu, C. H. and Nies, L. (2000). Development of Catechol 2,3-Dioxygenase-Specific Primers for Monitoring Bioremediation by Competitive Quantitative PCR. Appl. Environ. Microbiol. 66. 678-683.

5. Chang, M., Voice, T. C., Criddle C. S. (1999). Kinetics of Competitive Inhibition and Cometabolism in the Biodegradation of Benzene, and p-Xylene by Two Pseudomonas Isolates. Biotech. Bioengin. 41. 1057-1065.

6. Oh, Y. S., Shareefdeen, Z., Baltzis, B. C. and  Bartha, R. (1994). Interactions Between Benzene, Toluene, and Xylene During Their Biodegradation. Biotech. Bioengin.44. 533-538.

7. Huang, H. H., Tseng, D. W. and Juang, L. C. (2007). Heterogeneous Photocatalytic Degradation of Monochlorobenzene in Water. J. Hazard. Mater. 156: 186–193.

8. Hariharan, C. (2006). Photocatalytic Degradation of Organic Contaminants in Water by ZnO Nanoparticles: Revisited. Applied Catalysis A: General. 304. 55-61.
9. Daneshvar, N., Salari, D. and Khataee, A. R. (2004). Photocatalytic Degradation of Azo Dye Acid Red 14 in Water on ZnO as an Alternative Catalyst to TiO2. Journal of Photochemistry and Photobiology A: Chemistry. 162. 317-322.

10. Shifu, C. and Yunzhang, L. (2007). Study on the Photocatalytic Degradation of  Glyphosate by TiO2 Photocatalyst. Chemosphere. 67. 1010–1017.
