The Malaysian Journal of Analytical Sciences Vol 17 No 1 (2013): 153 – 163

PALM OLEIN BASED BIOLUBRICANT BASESTOCKS: SYNTHESIS, CHARACTERISATION, TRIBOLOGICAL AND RHEOLOGICAL ANALYSIS

(Stok Asas Biolubrikan Berasaskan Minyak Sawit Olein: Sintesis, Pencirian, 
Analisis Tribologi dan Reologi)

Darfizzi Derawi1,2 and Jumat Salimon1*
1School of Chemical Sciences and Food Technology, Faculty of Science and Technology, 

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

2International Education College (INTEC), 

UiTM Section 17 Campus, 40200 Shah Alam, Selangor, Malaysia

*Corresponding author: jumat@ukm.my
Abstract

Palm olein (POo) was modified through chemical reaction to produce biolubricant basestock (di-oleate-POo and oleate-ether-POo). POo was epoxidised to produce epoxidised palm olein (EPOo), then ring opening process were performed by hydrolysis and alcoholysis to produce di-hydroxy-POo and hydroxy-ether-POo. Both intermediate products were esterified with oleic acid to produce di-oleate-POo and oleate-ether-POo. Detection analyses were done by using fourier transformation infra-red (FTIR), proton and carbon nuclear magnetic resonance (1H-NMR and 13C-NMR). Di-oleate-POo recorded of its oxidative stability (140 oC), pour point (-5 oC), flash and fire point (215 oC and 245 oC), kinematic viscosity about 417.5 cSt (40 oC) and 45.4 cSt (100 oC) with the viscosity index of 166. While, oleate-ether-POo recorded of its oxidative stability (178 oC), pour point (1 oC), flash and fire point (190 oC dan 210 oC), kinematic viscosity about 113.7 cSt (40 oC) and 21.5 cSt (100 oC) with the viscosity index of 217. The biolubricant basestocks grade of ISO VG 460 (di-oleate-POo) and ISO VG 100 (oleate-ether-POo) were successfully produced. Di-oleate-POo and oleate-ether-POo were Newtonian and non-Newtonian fluid. Both products were hydrodynamic lubricant with low friction coefficients at 40 oC and 100 oC.

Keywords: Biolubricant Basestock, Palm Olein, Tribology, Rheology
References
1. Kline & Company Inc. 2006. Competitive intelligence for the global lubricants industry 2004–2014, Kline & Company, Inc.

2. Loredana P., Cosmina P., Geza B., Gabriela V., Remus N. 2008. Basestock oils for lubricants from mixtures of corn oil and synthetic diesters. J Am Oil Chem Soc. 85: 71–6.

3. Erhan, S.Z., Adhvaryu, A. 2002. Vegetable-based base stocks. In: Erhan, S.Z., Perez, J.M. (Eds.), Bio-Based Industrial Fluids and Lubricants. Champaign, USA, AOCS Press.

4. Lawate, S. 2006. Environmentally friendly hydraulic fluids. In: Rudnick, L.R. (Ed.), Synthetics, Mineral Oils, and Bio-Based Lubricants. Chemistry and Technology, Taylor & Francis, CRC Press, PA, USA.

5. Sharma, B.K., Adhvaryu, A., Liu, Z., Erhan, S.Z. 2006. Chemical modification of vegetable oils for lubricant applications, JAOCS, 83: 129–136.

6. Birova A, Pavloviova A, Cvengro J. 2002. Lubricating oils based on chemically modified vegetable oils, J Synth Lubr. 18: 291.

7. Adhvaryu, A., Erhan, S.Z. 2002. Epoxidized soybean oil as a potential source of high temperature lubricants, Ind. Crop Prod. 15: 247–254.

8. Erhan, S.Z., Asadaukas, S. 2000. Lubricants base stocks from vegetable oils, Ind. Crop Prod. 11: 277–282.

9. Erhan, S.Z., Adhvaryu, A., Sharma, B.K. 2006. Chemically functionalized vegetable oils. In: Rudnick, L.R. (Ed.), Synthetics, Mineral Oils, and Bio-Based Lubricants. Chemistry and Technology, Taylor & Francis, CRC Press, PA, USA.

10. Campanella, A., Rustoy, E., Baldessari, A., Baltanas, M.A. 2010. Lubricants from chemically modified vegetable oils. Bioresour. Technol. 101: 245–254.

11. Erhan, S.Z., Asadaukas, S. 2000. Lubricants base stocks from vegetable oils, Ind. Crop Prod. 11: 277–282.

12. Sharma, B.K., Stipanovic, A.J. 2003. Development of a new oxidation stability test method for lubricating oils using high-pressure differential scanning calorimetry, Thermochim. Acta 402: 1–18.

13. Duangkaewmanee, S., Petsom, A. 2011. Synergistic and antagonistic effects on oxidation stability of antioxidants in a synthetic ester based oil Tribol. Int. 44: 266–271.

14. Ming KK, Chandramohan D. 2002. Palm oil industry at crossroad and its future direction, Oil Palm Industry Economic Journal 2: 10–5.

15. Ramli, M. R., Siew, W. L., Cheah, K. Y., 2009. Production of high oleic palm oils on a pilot scale, J. Am. Oil. Chem. Soc. 86: 587-594.
16. Yeong, S. K., Ooi, T. L., Salmiah, A., 2005. Palm-Based Hydraulic Fluid, MPOB, KL.
17. Loh, S. K., Choo, Y. M., 2006. Food-Grade Palm-Based Industrial Lubricants, MPOB, KL.
18. Derawi, D., Salimon, J., 2010. Optimization on epoxidation of palm olein by using performic acid, E-J.Chem. 7(4):  1440-1448.
19. Emery, 1983. Emery Analytical Testing Procedures, Emery Industries, USA.
20. Fox, N.J., Stachowiak, G.W. 2007. Vegetable oil-based lubricants—A review of oxidation, Tribology International 40: 1035–1046.
21. Stachowiak, G. W., Batchelor, A. W. 2005. Engineering Tribology, Elsevier Inc., UK.
22. ISO 3448, 1975. International Standard, Industrial Liquid Lubricants, ISO Viscosity Classification.
23. Kalin, M., Velkavrh, I., Vizintin, J. 2009. The Stribeck curve and lubrication design for non-fully wetted surfaces, Wear 267: 1232-1240.
24. Coussot, P., Tocquer, L., Lanos, C., Ovarlez, G., 2009. Macroscopic vs local rheology of yield stress fluids. J. Non-Newtonian Fluid Mech., 158: 85-90.
25. Gunstone, F.D. 2004. The Chemistry of Oils and Fats: Sources, Composition, Properties and Uses, Blackwell Publishing Ltd., U.K.
26. Wade, L. G., 2006. Organic Chemistry, 6th ed., Pearson Prentice Hall, United States.
27. Derawi, D., Salimon, J. 2011. Effect of Performic Acid Concentration on Epoxidation of Palm Olein, Sains Malaysiana 40(9): 1023-1027
28. Pavia, D. L., Lampman, G. M., Kriz, G. S. 2001. Introduction to spectroscopy, Thomson Learning, Inc., USA.
29. Hironaka, S., 1984. Boundary Lubrication and Lubricants., Three Bond Co. Ltd., Japan.
30. Batchelor, G. 2000. An Introduction to Fluid Mechanics, Cambridge University Press, UK.
