The Malaysian Journal of Analytical Sciences Vol 17 No 1 (2013): 185 – 192

SYNTHESIS OF ESTOLIDE 2-ETHYLHEXYL ESTER FROM 
RICINUS COMMUNIS
(Sintesis Estolida 2-Etilheksil Ester dari Ricinus Communis)

Nazrizawati Ahmad Tajuddin1,2*, Nor Habibah Rosli1, Jumat Salimon2, Mohd Firdaus Mohd Yusoff 2, 
Noraishah Abdullah2
1Department of Chemistry, International Education College, 

UiTM Section 17, 40200 Shah Alam, Selangor, Malaysia

2Oleochemistry Programme, School of Chemical Science and Food Technology, 

Faculty of Science and Technology, 

Universiti Kebangsaan Malaysia,43000 Bangi, Selangor, Malaysia
*Corresponding author: nazriza@salam.uitm.edu.my
Abstract

Estolide 2-ethylhexyl ester synthesized through condensation reaction between ricinoleic acid from castor oil (Ricinus communis) and lauric acid, and then capped with 2-ethylhexyl alcohol. The reaction was continuously conducted under vacuum for 24 hours. Product of 2-ethylhexyl ester was characterized by using Fourier Transform Infrared (FTIR) to determine functional group and Nuclear Magnetic Resonans (NMR) for structure’s determination. The presence of ester group at 1738.23 cm-1 wavenumber indicates that the formation of estolide ester has occurred. The vibration peak of C-O at 1174.60 cm-1 and 1117.10 cm-1 support the formation of ester. The presence of CH2 bending indicated the long-chain compound. The ester methine signal at 3.8669 ppm indicated the estolide linkage in the 1H-NMR spectrum while the 13C-NMR showed two carbonyl signals at 173.41 ppm for acid and 173.56 ppm for ester.

Keywords: Castor oil, ricinoleic acid, estolide ester, biodegradable, biolubricant study
References
1. Lin, J.T. & Chen, G.Q. 2010. Acylglycerols Containing Trihydroxy Fatty Acids in Castor Oil and the Regiospecific Quantification of Triacylglycerols. Journal of the American Oil Chemists' Society. 87:1371-1379
2. Jumat, S., Neeranjini, N., Nadia, S. & Bashar, M.A. 2011. Synthesis and Physical Properties of Estolide Ester Using Saturated Fatty Acid and Ricinoleic Acid. Journal of Automated Methods and Management in Chemistry.2011: 1-4
3. Cermak, S.C. & Isbell, T.A. 2002. Physical prop of saturated estolides and their 2-ethylhexyl ester. Industrial Crops Products. 16: 119-127. 
4. Zaher, F.A. & Nomany, H.M. 1988. Vegetable oils and lubricants. Grases Aceities (Seville). 39: 235-238
5. Becker, R. & Knorr, A. 1996. An evaluation of antioxidants for vegetable oil at elevated temperatures. Lubri. Sci. 8: 95-117. 
6. Asadauskas, S. & Erthan, S.Z. 1999. Depression of pour points of vegetable oils by blending with diluents used for biodegradable lubricants. J.Am.Oil Chem.Soc. 76: 313-316. 
7. Isbell, T.A., Kleiman, R. & Plattner, B.A. 1994. Acid.Catalyzed Condensation of Oleic Acid into Estolides and Polyestolides. J.Am.Oil Chem.Soc: 71.  
8. Isbell, T.A. & Kleiman, R. 1994. Characterization of Estolides Produced from the Acid-Catalyzed Condensation of Oleic Acid. New Crops Research. 71:379-383. 
9. Cermak, S.C. & Isbell, T.A. 2001. Synthesis of estolides from oleic and saturated fatty acids. J.Am.Oil.Chem.Soc. 78: 557-565. 
10. Cermak, S.C. & Isbell, T.A. 2003. Synthesis physical properties of estolide-based functional fluids. Industrial Crops Products. 18:183-196.
11. Cermak, S.C., Brandon, K.B. & Isbell, T.A. 2006. Synthesis and physical properties of estolides from lesquerella and castor fatty acid esters.  Industrial Crops Products.23:54-64.
12. Pavia, D.L., Lampman, G.M. & Kriz, G.S. 2001. Introduction to spectroscopy, 3rd ed. America:Thomson Learning.
