The Malaysian Journal of Analytical Sciences Vol 17 No 1 (2013): 30 – 37

DEVELOPMENT OF BIO-BASED PAINT BY USING METHYL ESTERS FROM PALM OIL FOR CORROSION INHIBITOR

(Pembangunan Cat Berasaskan Bio Menggunakan Metil Ester Dari Minyak Sawit Untuk Mengawal Pembentukan Karat)

Mohibah Musa*, Miradatul Najwa Muhd Rodhi, Najmiddin Yaakob,
Ku Halim Ku Hamid, Juferi Idris
Environmental Research Centre, Fakulti Kejuruteraan Kimia, 

Universiti Teknologi MARA, Shah Alam, Selangor, Malaysia

*Corresponding author: mohibah@salam.uitm.edu.my
Abstract

Paint is used as a means of protection to prevent surfaces from being corroded over time.  This research is focused on the development of a Bio-based paint made from palm oil methyl ester (POME) which originated from crude palm oil (CPO). New formulation paint has been developed to protect the pipeline from corrosion thus reducing the cost of the operation. Bio-based paint is made up of four components which are solvent, binder, additives, and pigment. The solvent in the bio-based paint is POME. The additives used are wetting and dispersing agent. The pigment used in the bio-based paint is TiO2. The formulation was developed by using a constant amount of additives and binder but varying the amount of POME at 10 ml, 15 ml, 20 ml, 25 ml and 30 ml with addition of water.  The Standard Testing Methods for measuring the corrosion rate (ASTM G5-94(2011)) was carried out for each sample. In conclusion, it is proven that in the  making of bio-based paint formulation for better corrosion inhibitor; the best amount of binder, additives and de-foam that should be used is 20 ml, 10 ml and 10 ml, respectively. 

Keywords: bio-based paint, additives, crude palm oil, palm oil methyl ester
References

1. Migahed, M.A., Abdul-Raheim, A.M., Atta, A.M., & Brostow, W., (2010). Synthesis and evaluation of a new water soluble corrosion inhibitor from recycled poly(ethylene terphethalate). Mater. Chem. Phys 121: 208 - 214.
2. Malik, M. A., Hashim, M. A., Nabi, F., Al-Thabaiti, S. A., & Khan, Z. (2011). Anti-corrosion Ability of Surfactants: A Review. Int. J. Electrochem. Sci. 6: 1927 - 1948.  
3. Yoo, S. H., Kim, Y. W., Chung, K., Baik, S. Y. &  Kim, J. S.  (2012). Synthesis and corrosion inhibition behaviour of imidazoline derivatives based on vegetable oil. Corrosion Science 59: 42 - 54. 
4. Kalendová, A., Sapurina, I., Stejskal, J., & Vesely, D. (2008). Anticorrosion properties of polyaniline-coated pigments in organic coatings. Corrosion Science 50: 3549 – 3560.
5. Briegel, K. & Kane, R. (2007). Corrosion monitoring technology leads to real-time results for specialty materials: 1-2
6. Orubite-Okorosaye, K, Jack, I R, Ochei, M, & Akaranta, O. (2007). Synergistic Effect of Potassium Iodide on Corrosion Inhibition of Mild Steel in HCl Medium by Extracts of Nypa Fruticans’ Wurmb. J. Appl. Sci. Environ. Manage 11: 27 - 31.
7. Caroline, M.M., Christian, P., Hannes, C.S., Boris, K., & Ilhan A.A., (2008). Inhibition and Promotion of Copper Corrosion by CTAB in a Micro reactor System. Langmuir 24: 14269.
8. El–Maksoud, S.A.Abd, (2008). The Effect of Organic Compounds on the Electrochemical Behaviour of Steel in Acidic Media. A review. Int. J. Electrochem. Sci. 3: 528 - 555.
9. Antonijevic, M. M & Petrovic, M. B (2008). Copper Corrosion Inhibitors: A review. Int. J. Electrochem. Sci. 3:  1-28
10. Kumar, A, (2008). Corrosion Inhibition of Mild Steel in Hydrochloric Acid by Sodium Lauryl Sulfate (SLS). e-Journal of Chemistry 5: 275 - 280. 
11. Maqsood, A.M., Mohammad, A.H., Firdosa, N., Shaeel, A.T., & Zaheer, K. (2011). Anti-corrosion Ability of Surfactants: A Review. Int. J. Electrochem. Sci 6: 1927 - 1948.  
12. Moura, E.F., Neto, A.O.W., Dantas, T.N.C., Scatena, J.H., & Gurgel, A. (2009). Applications of micelle and micro emulsion systems containing aminated surfactants synthesised from ricinoleic acid as carbon-steel corrosion inhibitors. Colloids Surf. A. 340: 199 - 207.
13. Bentley, J & Turner, G.P.A. (1997). Introduction to Paint Chemistry and Principles of Paint Technology. Chapman & Hall, ISBN: 9780412723308, pg 79 - 85.
14. Smith, D. G., Liu, W. H, & Nan-Tou. (2006). Laminated Coconut Palm Oil and Products Thereof, US Patent:20060078666
15. Tiarks, F., Frechen, T., Kirsch, S., Leuninger, J., Melan, M., Pfau, A., Richter, F., Schuler, B., & Zhao, C. L (2003). Formulation effects on the distribution of pigment particles in paints. Progress in Organic Coatings 48: 140 - 152.
16. Environmental Protection Agency’s (EPA), EPA’s Toxics Release Inventory. National Emission Inventory (2006) : pg 23-35
17. Johannes T.P, Derksen, F., Petrus Cuperus, & Peter Kolster, (1996). Renewable Resources in Coatings Technology: A Review. Progress in Organic Coatings 27: 45 - 53. 
18. American Council on Science and Health, (1997) Animal Experiments, Human Cancer Risk and Regulatory.
19. Darnoko, D., & Cheryan, M. (2000). Kinetics of Palm Oil Transesterification in a BatchReactor. Journal: Journal of The American Oil Chemists Society 77: 1263 - 1267.
20. ASTM 1999, G 5-94, Standard Reference Test Method for making Potentiostatic and Potentiodynamic Anodic Polarization Measurements 3.01: 61-72.
