The Malaysian Journal of Analytical Sciences Vol 17 No 1 (2013): 75 – 84
EFFECT OF SODA-ANTHRAQUINONE PULPING CONDITIONS AND BEATING REVOLUTION ON THE MECHANICAL PROPERTIES OF PAPER MADE FROM Gigantochloa scortechinii (SEMANTAN BAMBOO)

(Kesan Faktor-Faktor Pemulpaan Soda-Antrakuinon dan Pemukulan Ke Atas Sifat-Sifat Mekanikal Kertas Gigantochloa Scortechinii (Buluh Semantan))
Nurul Husna Mohd Hassan1*, Suhaimi Muhammed1, Rushdan Ibrahim2

1 Department of Wood Industry, Faculty of Applied Sciences, 

Universiti Teknologi MARA Pahang, 26400 Bandar Tun Abdul Razak, Jengka Pahang

2Pulp and Paper Programme, 

Forest Research Institute Malaysia (FRIM), 52109 Kepong, Selangor

*Corresponding author: afna07@yahoo.com
Abstract

The effect of soda-AQ pulping conditions and beating revolution on the mechanical properties of paper made from Semantan bamboo (Gigantochloa scortechinii) was studied. The bamboo chips were pulped using MK digester pulping unit with 10 to 20% alkali charge and 150 to 170oC cooking temperature. The screened yield varies from 38.7 to 48.4%, and each yield went through beating process at 1000 or 8000 beating revolutions. The bamboo pulp was then made into 60 g/m2 laboratory scale papers and their mechanical properties were assessed conforming to TAPPI standards. The results revealed that tensile index, bursting index, tearing index and folding endurance ranged from 42.04 to 91.09 Nm/g, 2.68 to 7.10 kPa.m2/g, 11.03 to 26.64 mN.m2/g and 30 to 1127 double folds, respectively. The highest paper properties were found from pulping condition of 15% alkali charge and 150oC cooking temperature based on the fibre bonding index, with tensile index at 87.71 Nm/g, bursting index at 6.94 kPa.m2/g, tearing index at 12.72 mN.m2/g and folding endurance at 613 double folds. Such findings indicate that comparable high strength mechanical properties of paper can be produced from Semantan bamboo pulp with more environmentally friendly pulping process compared to the kraft pulping process that had been used in bamboo pulping.

Keywords: soda-AQ pulping, Semantan bamboo, beating, paper mechanical properties
References
1. Azmy, H.M., Norini, H. & Wan Razali, W.M. (1997). Management Guidelines and Economics of Natural Bamboo Stands, FRIM Technical Information Handbook No.15, Forest Research Institute Malaysia, Kepong, pp1.
2. Chen, M.C., Ho, C.C., & Tracy, M.Y.L. (2000). Bonding Moso Bamboo with Copolymer Resins Made of Biomass Residual Extracts with Phenol and Formaldehyde. Forest Prod. J. 50 (9):70-74.
3. Wong, K.M. (1995). The Bamboos of Peninsular Malaysia. Malaysian Forest Records, No. 41.  Forest Research Institute Malaysia. pp 71.
4. Lee, A.W.C & Liu, Y. (2003). Selected Physical Properties of Bamboo Flooring, Forest Prod. J., 53(6):23-25
5. Wong, K.M. (1989). Current and Potential Uses of Bamboo in Peninsular Malaysia, Journal of American Bamboo Society 7(172):1-15.
6. Azmy, H.M. (1989). Perusahaan Membuat Bakul Ikan dan Sayur dan Bakul Arang, FRIM Technical Information No. 8, Forest Research Institute Malaysia, Kepong, pp 6 (In Malay).
7. Rushdan, I. (2003). Structural, Mechanical And Optical Properties Of Recycled Paper Blended With Oil Palm Empty Fruit Bunch Pulp. Journal of Oil Palm Research, Vol. 15, No. 2, December 2003, pp. 28-34.
8. Suphat, K. (2007). Preliminary Study of Anthraquinone in Sweet Bamboo (Dendrocalamus asper Backer) Alkaline Sulfite Pulping, Chiang Mai J. Sci., 34(2) : 235-247.
9. Biermann, C. J. (1993). Essential of pulping and papermaking, California: ACADEMIC PRESS, Inc.
10. Nurul Husna, M.H., Mansur, A. & Rushdan, I. (2010). Enhancement of Mechanical Properties of Semantan Bamboo Pulp by Beating. (Eds.) Gan, K.S., Mahmudin, S., Mohd Nor, M.Y. In Proceedings of the International Symposium on Forestry and Forest Product 2010. Addressing  Global Concerns and Changing Societal Needs, 5 – 7 October 2010, Kuala Lumpur, Malaysia, 91 – 100.
11. Yusoff, M.N.M., Kadir, A.Abd., & Mohamed, A. H. (1992). Utilization of Bamboo for Pulp and Medium Density Board, (Eds.) Mohd W. R.W., and Mohamad A.B., In Proceeding of Seminar Towards the Management, Conservation, Marketing and Utilization of Bamboos, Kuala Lumpur: FRIM, 196 – 205.
12. Sadawarte, N.S., Dharwadkar, A.R., & Veeramani, H. (1982). Pulp strength properties and black liquor viscosity for kraft pulping of bamboo-bagasse blend (70:30), In 1982 Pulping Conference, Book. 1, Atlanta, 197 – 206.
