ISOLATION AND UTILIZATION OF CORN COBS HEMISELLULOSE AS CHELATING AGENT FOR LEAD IONS
Muchlisyam1*, Urip Harahap1, Jansen Silalahi1,  Zul Alfian2

1Facultyof Pharmacy, Universityof Sumatra Utara, Medan, Indonesia.
 2Department of Chemistry Faculty of Mathematics and Natural Sciences University of  Sumatra Utara,Medan, Indonesia

*Corresponding author: muchlisyam@gmail.com

Abstract

Corn cobs is an agricultural byproduct containing polysaccharide composed of cellulose, hemicellulose  and lignin. Hemicellulose has a hydroxyl and carbonyl functional groups   which can be used  as chelating agent for metal ions. The purpose of this study was to isolate and evaluate corncobs hemicellulose as a chelating agent toward lead ion. Graphite furnace spectrofotometry at 283.3  nm was used to determine the residual lead ion in solution.  The research’s result showed that the highest yield of hemicellulose (12.04%) was obtained from delignication with  0,03M NaOH in 60% ethanol and 3% H2O2, hemicellulose isolation with 500 ml of 0.2 M NaOH, and precipitation with 1 : 4 ratio of 10% acetic acid in 95% ethanol.  The 300 mg corn cobs hemicellulose has chelating effect for 40mg lead solution at (39.52 ± 0.1350) mg or  98.80%, that the corn cobs hemicellulose can be used as a chelating agent for lead.
Key words: corn cobs, isolation, hemicellulose, Pb, chelating agent

Abstrak

Tongkol jagung adalah sisa pertanian yang mengandungi polisakarida yang terdiri daripada selulos, hemiselulos dan lignin. Hemiselulos mempunyai gugusan berfungsi karbonil dan hidroksil yang vboleh digunakan sebagai agen pengkelat ion logam. Tujuan kajian ini ialah untuk mengasingkan dan menilai hemiselulos tongkol jagung sebagai agen pengkelat ion plumbum. Spektrofotometri dapur grafit digunakan bagi menentukan plumbum dalam larutan pada 283.3 nm. Hasil kajian menunjukkan hasil hemiselulos tertinggi (12.4%) diperolehi daripada nyahlignin dengan 0,03M NaOH dalam 60% ethanol dan 3% H2O2 dan pengasingan hemilulos dengan 500 ml   0.2 M NaOH,dan pemendekan dengan 1:4 nisbah 10% asid asetik dalam 95% ethanol. Sebanyak 300 mg hemiselulos tongkol jagung menyerap  39.52 ± 0.1350 mg (98.8%) daripada 40 mg Pb, ini menunjukkan hemiselulos tongkol jagung boleh digunakan sebagai agen pengkelat Pb.
Kata kunci: tongkol jagung, hemiselulos, Pb, agen pengkelat.

Introduction

Hemicellulose  is one of most abundant polymer after cellulose. However, its potential has yet to be completely recognized. Hemicellulose comprises a variety of monomers including xylosa, mannose, arabinose, glucose, glukoronic acid having hydroxyl (OH) group on each monomer [1]. In the qualitative chemical analysis of organic compounds, the OH group in both cyclical  aliphatic  will be able to bind metal ions to form complex salts. Hemicellulose applications in the pharmaceutical field could potentially be developed as a dietary supplement or as drug formulation excipients such as binders, disintergrator, thickeners and stabilizers. In addition, several important applications of hemicellulose have been done by making the derivatives which have pharmacological effects such as lowering cholesterol, and inhibitors of HIV [2,3,4].
Corn cobs contains hemicellulose approximately 12.5% ​​and is the largest amount in comparison with other  species [5].  Several reseaches have been performed on the separation of hemicellulose from different plant byproducts with different methods of isolation.  Isolation of hemicellulose by using alkali such as KOH or NaOH at various concentrations have been reported [2,3,5].   
Lead is a toxic element because it tends to undergo a process of bioaccumulation and  potential toxic amount accumulate within sensitive organs and tissues. In humans, poisoning by most of these metals causes severe dysfunction in the kidneys, reproductive system, liver, brain and central nervous system [6,7]. The aim of this study is to isolate hemicelluloses from corn cobs and to test its ability to absorb lead in solution.
Method of Research
Materials
Corn Cobs  were obtained from local Corn  in Medan, Indonesia. Pectin Technical grade (China), NaOH (E.Merck), 35% H2O2 (E.Merck), 96% ethanol (E.Merck),  CH3COOH (E.Merck), Pb(NO3)2 (E.Merck), Lead ion 1000 ppb/ml  (E.Merck), All other chemicals used were of analytical grade.

Isolation of hemisellulose  from corn cobs
The extraction method was modified from the combination methods described by [2,3,5].  The corn cobs powder of 50 grams was added to 500 ml of 0.03 M NaOH in 70% ethanol and heated at 60°C and stirred for 2 hours to dissolve the lignin. The suspension was allowed to cool to room temperature and filtered through Whatman filter paper. The precipitate was added 500 ml of 0.2 M NaOH, and stirred for 8 hours at room temperature to dissolve hemicellulose, and then filtered. The filtrate was heated at a temperature of 65°C, and added 137 ml of 3% H2O2  in stages. Each addition of 1 ml 3% H2O2 to the filtrate and stirred constantly, stirring was performed until the entire 3% H2O2is used, stirring is continued until a clear solution.  Solution of 10% acetic acid in 95% ethanol with a ratio of 1:4 (v / v) was added to the sample solution and left at room temperature for 6 hours until the precipitate formed. The suspension was centrifuged at a rate of 10,000 rpm for 15 minutes, and the filtrate was discarded, the precipitate was washed with 96% ethanol, and dried in vacuum dryer. The washed precipitate is hemicellulose.
Lead absorption
The absorption  method was modified from the methods described by Wong et al. [8]. The hemicellulose  and pectin  respectively weighed 100 mg, 200 mg and 300 mg, Then each dissolved into erlenmeyer containing 25 ml solution 40 mg/ml of lead in 0.1 N nitric acid and the pH adjusted with acid pH performed at pH 2, the solution was stirred with a magnetic stirrer at room temperature for 2 hours. Then each was centrifuged at 10,000 rpm for 30 minutes. The supernatant was taken and diluted with 0.5 ml to 50 ml aquabidest  then 0.25 ml of dilution was taken and diluted to 25 ml with aquabidest and lead levels were measured. The Lead  in the supernatant were estimated using graphite furnace atomic absorption spectroscopy (Hitachi Analyst 100). The results are presented as mean values ± standard deviation.
Results and discussion
Isolation of Hemicellulose

Modified isolation of corn cobs hemicellulose using 500ml of 0:03M NaOH in70% ethanol and precipitation using the solution of 10% acetic acid in 95% ethanol with a ratio of 1:4 (v/v) and corn cobs hemicellulose obtained with levels of 12.03% and in accordance with the results of Ricahana 2006 research that levels of 12:04% [5].  Chelating ability of corn cobs hemicellulose and pectin toward lead ion is shown in Table 1.
Table 1. Chelating effect of Corn Cobs Hemicellulose and Pectin for 40mg/25ml lead ions.
	Chelating agent
	Weight
	Lead content in Chelating agent
(mg)
	Percentage lead ion in Chelating agent (%)


	Hemicellulose


	100 mg
	35.97  ± 0.2461
	89.92

	
	200 mg
	37.33  ± 1.9041
	93.32

	
	300 mg
	39.53  ± 0.1350
	98.82

	Pectin


	100 mg
	21.10  ± 1.0834
	52.75

	
	200 mg
	32.48  ± 0.7152
	81.20

	
	300 mg
	37.39  ± 0.2237
	93.47


Table 2 shows that the administration of chelating agent to bind lead at pH 2, the higher the amount of chelating agent  showed an increase chelating ability, but in hemicellulose from corn cobs the increase was not in proportional with the amount of hemicellulose, it is in accordance with the principle of adsorption that the adsorption process will end if there is equilibrium between the adsorbent, so the weight does not affect a significant absorbance with the increasing amount of  hemicellulose for each treatment. 
From Table 2 can be seen that there is the influence of the type of chelating agent and the weight the chelating agent applied. But in contrast to pectin, that with the addition of pectin concentration will also increase properly strapped to lead ions. On the 100 mg pectin has a binding capacity of (21.10  ± 1.0834)  mglead ion or 52.75%, but the 200 mg pectin will give a greater ability that is (32.48  ± 0.7152) mg lead ion or 81.20%  and 300 mg of pectin bound by an increase of (37.39  ± 0.2237) mg olead ions  or 93.47% and compared to corn cobs hemicellulose increases the ability of the chelating agent average around 4.33% -6.61%, and although the over all number increased holding capacity of pectin is still below the chelating agent means that a chelating effect of the corn cobs hemicellulose has greater than pectin. Absorption characteristics between hemicelluloses and pectin are different where hemicelluloses reacts with lead ions 
This suggests that the hydroxyl group of the hemicellulose causes attraction of lead ions present in solution, thus hemicellulose is more polar and has a better absorption capacity than the less polar substances. Uptake mechanism that occurs between the hydroxyl function from hemicellulose monomer for example xylose group attached to the surface with the positively charged metal ion (cation) is an ion exchange mechanism as follows,
                                                                              

X-O     

X-OH     +     Pb2+                                                                         
    Pb      +    2H+

                                                                                  

X-O

Metal ion in the form of  lead ions, -OH groups are hydroxyl groups present on the C atom of the monomer compound in the hemicellulose and X is a matrix of hemicellulose place the-OH group attached. Interactions between the-OH group with the lead ion is also possible through the mechanism of formation of coordination complexes as atomic oxygen (O)   with -OH group has a lone pair, while the lead  ion has an empty  orbitals. The free electron pair will occupy a empty orbital which is owned by a metal ion, thus forming a compound or complex ion [9]. Chemical bonding that occurs between the active groups in the molecules of organic substances can be explained as the behavior of Lewis acid-base interactions which produce complex on the surface of solids. In the system of binding of metal ion solution, for example the interaction is written in general form, 

  

2[FH]   +     Mz                                 

[F2M(Z-2)]+    +       2H+


with FH is a functional group found in organic matter, and M is the ion of z valency. This means that the in-vitro hemicellulose which is an organic compound having a hydroxyl group can bind to metal of two valency in the dissolved state and acidic conditions.

Conclusion
The modified method for isolation of corn cobs hemicelluloses gave a yield of 12.03%. Corn cobs hemicelluloses have the ability to bind lead at pH2 and the capacity was influenced by the weight and the highest was shown by the 300mg corn cobs hemicelluloses with binding capacity at 39.52 ± 0.1350 mg  to 40mg of lead solution, or 98.80%. Corn cobs Hemicelluloses can be used as a chelating agent for lead. 
References
1.   Dumitriu, S. (2005). Polysaccharides: Structural Diversity and Functional Versatility. New York: Marcel Dekker.
2. Karssalan, A. M., Tshabalala, M. A., & Buschle, D. G.  (2010). Wood Hemisellulose/Chitosan-Basedsemi-Interpenetrating  Networks  Hydrogels: Mechanical, Swelling And  Control  Drug  Release  Properties,   J. BioResources 5(2): 1036 - 1054.
3.  Yadav, M. P., Johnston, D. B., Hotchkiss, A. T., & Hicks, K. B. (2007). Corn Fiber Gum: A Potential Gum Arabic Replacer For Beverage Flavor Emulsificatio,  Food  Hydrocolloids : 1022 – 1030.
4.   Saha, C. B. (2003). Hemicellulose bioconversion. J. Microbiol. Biotech. 30 (16): 279 - 291.
5.  Richana, N., Irawadi, T. T., & Nur, A. M. (2007).  Ekstraksi Hemiselulosa Dari Tongkol Jagung.  J. Pascapanen 4(1):38-43.
6. Casas, S. J & Sordo, J. (2006). Lead  Chemistry, Analytical Aspects, Environmental Impact and Health Effects. Amsterdam:  Elsevier.   
7.   Jickel, S. &  Negrusz, A. (2008).Clarke’s Analytical Forensic Toxicology. Chichago, USA.
8.  Wong, W. W., Abbas, F. M. A., Liong, M. T. & Azhar, M. E. (2008). Modification of durian ring  for improved biosorbent ability, Int. Food Res. J. 15(3): 363 - 365.

9.   Pearson, R. G. (2005). Chemical hardness and density functional theory.  J. Chem. Sci. 117(5): 369 – 377.

