The Malaysian Journal of Analytical Sciences Vol 17 No 2 (2013): 244 – 254

SORPTION OF Au (III) AND Ag (I) ON AMINO- AND MERCAPTO-SILICA HYBRID COLUMNS

(Jerapan Au (III) dan Ag (I) pada Turus Hibrid Amino- dan Merkapto-silika)

Nuryono1*, Nurma Y. Indriyanti2, Julita B. Manuhutu3, Narsito1, Shunitz Tanaka4
1Department of Chemistry, Faculty of Mathematics and Natural Sciences 

Universitas Gadjah Mada, Sekip Utara, Yogyakarta 55281, Indonesia

2Study Program of Chemical education, Faculty of Teacher Training and Education 

Universitas Sebelas Maret Surakarta 57126, Indonesia

3Study Program of Chemistry, Faculty of Educational Sciences 

Universitas Pattimura Ambon, Indonesia

4Division of Environmental material Science, Faculty of Environmental Earth Science, 

Hokkaido University, Japan
*Corresponding author: nuryono_mipa@ugm.ac.id

Abstract

Adsorption-desorption of Au(III) and Ag(I) ion on amino-silica hybrid (ASH) and mercapto-silica hybrid (MSH) in a column system has been studied. Adsorption was conducted in a 0.5-g adsorbent packed column passing through 30 mL solution of Au(III)/Ag(I)/Cu(II) ions 10 mg/L for MSH and Au(III)/Ag(I)/Ni(II) for ASH with three repetitions. Desorption used eluent of thiourea in HCl solution with volume of 10 mL each. Concentration of metal ions in the eluent was analyzed with flame atomic absorption spectroscopy and the amount of metal ions desorbed was calculated. The results showed that metal ions loaded in the columns were adsorbed completely in both adsorbents. However, the amount of metal ions desorbed for first three fractions is depended on the concentration of eluent. Thiourea 1M in 1M HCl solution eluted 96.7% and 59.1% of Au(III) ion from MSH and ASH, respectively; and Ag(I) was desorbed 79.2% from MSH and 97.6% from ASH. Metal ions of Cu(II) and Ni(II) are not easily eluted with that eluent; only 45.8%  of Cu(II) was eluted from MSH and 5.0% of Ni(II) from ASH. Repetition of process in three-time use indicates the highly stability of the adsorbents; hence those are potential for solid phase extraction application.

Keywords:  sorption, gold, silver, silica, rice hull ash
References

1. Goswami A.,  & Singh,  A. K., (2002).1,8-Dihydroxyanthraquinone anchored on silica gel: synthesis and application as solid phase extractant for lead(II), zinc(II) and cadmium(II) prior to their determination by ﬂame atomic absorption spectrometry, Talanta, 58, 669 - 678. 

2. Ramesh, A., Hasegawa, H., Sugimoto, W., Maki, T. & Ueda, K. (2008). Adsorption of gold(III), platinum(IV) and palladium(II) ontoglycine modiﬁed crosslinked chitosan resin, Bioresource Technology, 99: 3801 – 3809.

3. Zih-Pere ´nyi, K., Lasztity, A., Horvath, Z., Levai, A. (1998). Use of a new type of 8-hydroxyquinoline-5-sulphonic acid cellulose (sulphoxine cellulose) for the preconcentration of trace metals from highly mineralised water prior their GFAAS determination, Talanta, 47: 673 - 679.

4. Kasahara, I., Willie, S. N., Sturgeon, R. E., Berman, S. S., Taguchi, S., Goto, K. (1993). Preparation of 8-quinolinol immobilized adsorbents with minimum contamination for the preconcentration of trace metals in water, Bunseki Kagaku, 42: 107-110.

5. Sarkar, A. R., Datta, P. K. & Sarkar, M. (1996). Sorption recovery of metal ions using silica gel modified with salicylaldoxime, Talanta, 43: 1857-1862.

6. Zaporozhets, O. A.,  Nadzhafova, O. Y.,  Zubenko, A. I. & Sukhan, V. V. (1994). Analytical Application of Silica Gel Modified with Didecylaminoethyl-β-Tridecylammonium Iodide, Talanta, 41, 2067 - 2071.

7. Zaporozhets, O.,  Petruniock, N. and Sukhan, V. (1999). Determination of Ag(I), Hg(II) and Pb(II) by using silica gel loaded with dithizone and zinc dithizonate, Talanta, 50: 865 - 872.

8. Kocjan, R. (1999). Retention of Some Metal Ions and Their Separation on Silica Gel Modified with Acid Red 88, Microchim. Acta, 131: 153-158.

9. Ferreira, S. L. C., & de Brito, C. F. (1999). Separation and Preconcentration of Cobalt after Sorption onto Amberlite XAD-2 Loaded with 2-(2-Thiazolylazo)-p-cresol, Anal. Sci., 15: 189 - 192.

10. Zaporozhets, O., Petruniock, N., Bessarabova, O., Sukhan, V. (1999). Determination of Cu(II) and Zn(II) using silica gel loaded with 1-(2-thiasolylazo)-2-naphthol, Talanta, 49: 899 - 906.

11. Tong, A., Akama, Y. & Tanaka, S. (1990). Pre-concentration of copper, cobalt and nickel with 3-methyl-1-phenyl-4-stearoyl-5-pyrazolone loaded on silica gel,  Analyst, 115: 947 - 949.

12. Mahmoud, M. E. & Soliman , E. M. (1997). Silica-immobilized formylsalicylic acid as a selective phase for the extraction of iron(III), Talanta, 44: 15 - 22.

13. P. Liu, Q. Pu, Z. Su, (2000), Synthesis of silica gel immobilized thiourea and its application to the on-line preconcentration and separation of silver, gold and palladium, Analyst, 125: 147 - 150.

14. Liu, P., Pu, Q. & Su, Z. (1998). Application of 2-mercaptobenzothiazole-modified silica gel to on-line preconcentration and separation of silver for its atomic absorption spectrometric determination,  Analyst, 123: 239 - 243.

15. Mahmoud, M. E. (1999). Selective solid phase extraction of mercury(II) by silica gel-immobilized-dithiocarbamate derivatives, Anal. Chim. Acta, 398: 297 - 302.

16. Kubota, L. T., Moreira, J. C., Gushikem, Y. (1989). Adsorption of metal ions from ethanol on an iminosalicyl-modified silica gel, Analyst, 114: 1385 - 1388.

17. Garg, B. S., Sharma, R. K.,  Bist, J. S., Bhojak, N. & Mittal, S. (1999). Separation and preconcentration of metal ions and their estimation in vitamin, steel and milk samples using o-vanillin-immobilized silica, Talanta, 48 (1): 49 - 55.

18. Kim, J. S. & Yi, J. (1999). The Removal of Copper Ions from Aqueous Solutions Using Silica Supports Immobilized with 2-Hydroxy-5-nonylacetophenoneoxime, Sep. Sci. Technol., 34: 2957 – 2971.

19. Pu, Q. S., Su, Z. X., Hu, Z. H., Chang, X. J. & Yang, M. J. (1998).  2-Mercaptobenzothiazole-bonded silica gel as selective adsorbent for preconcentration of gold, platinum and palladium prior to their simultaneous inductively coupled plasma optical emission spectrometric determination, Journal of Analytical Atomic Spectrometry, 13: 249 – 253.

20. Liu, P., Pu, Q. S., & Su, Z. X. (2000) Synthesis of silica gel immobilized thiourea and its application to the on-line preconcentration and separation of silver, gold and palladium, Analyst (London), 125: 147 – 150. 

21. Gentscheva, G., Tzvetkova, P., Vassileva, P., Lakov, L., Peshev, O. & Ivanova, E. (2007). Analytical characterization of a silica gel sorbent with thioethericsites, Mikrochimica Acta, 156: 303 – 306. 

22. Bozkurt, S. S. & Merdivan, M. (2009). Solid phase extraction of gold(III) on silica gel modiﬁed with benzoylthiourea prior to its etermination by ﬂame atomic absorption spectrometry,  Environ Monit Assess, 158: 5 – 21.

23. Sakti, S.C.W., Siswanta, D. & Nuryono (2013), Adsorption of Gold(III) on Ionic Imprinted Amino-Silica Hybrid Prepared from Rice Hull Ash, Pure Appl. Chem., 85 (1): 211 - 223.

24. Bonnemann, H., Endruschat, U., Tesche, B., Ruﬁnska, A., Lehmann, C. W., Wagner, F. E., Filoti, G., Parvulescu, V. and Parvulescu,  V. I. (2000) An SiO2-Embedded Nanoscopic Pd/Au Alloy Colloid, Eur. J. Inorg. Chem., 5: 819 - 822.

25. Xie, Y. W., Quinlivan S. & Asefa, T. (2008). Tuning Metal Nanostructures in Mesoporous Silica by a Simple Change of Metal Complexes and by Reduction with Grafted Imines and Hemiaminals,  J. Phys. Chem. 112: 9996 - 10003.

26. Hall, S. R., Davis S. A. & Mann, S. (2000). Cocondensation of Organosilica Hybrid Shells on Nanoparticle Templates:  A Direct Synthetic Route to Functionalized Core−Shell Colloids, Langmuir, 16: 1454 - 1456.

27. Kalapathy, U., Proctor, A. &  Shultz, J. (2000). A simple method for production of pure silica from rice hull ash, Bioresource Technology, 73: 257 - 262.

28. Nuryono, Bassir, M., Setyaningsih, A. & Narsito (2007). Synthesis of Amino-Silica Hybrid from Rice Hull Ash for Heavy Metal Ion Adsorption, Presented at International Conference of Chemical Sciences (ICCS) Held by Department of Chemistry, Universitas Gadjah Mada and School of Chemistry, University Sains Malaysia on 24-25 May 2007, In Yogyakarta, Indonesia.
29. Hamdiani, S., Nuryono, Rusdiarso, B. & Sakti,  S. C. W. (2010).   Kajian Adsorpsi-Desorpsi Au(III) Pada Hibrida Merkapto Silika (HMS), Prosiding Seminar Nasional Penelitian, 15 Mei 2010 (Indonesian)

30. Mujiyanti, D. R., Nuryono & Kunarti, E.S. (2007). Simultaneous Adsorption Of Ag(I), Pb(II), Cu(II), Cr(III), And Ni(II) On Mercapto Immobilized Rice Hull Ash Silica, Presented at International Conference of Chemical Sciences (ICCS) Held by Department of Chemistry, Universitas Gadjah Mada and School of Chemistry, University Sains Malaysia on 24-25 May 2007, In Yogyakarta, Indonesia.
31. Lam, K. F., Fong,  C. M., Yeung, K. L. & Mckay, G. (2008). Selective adsorption of gold from complex mixtures using mesoporous adsorbent, J. Chem. Eng., 145: 185 – 195
32. Groenewald, T. (1976). The Solution of Gold in Acidic Solutions Thiourea, Hydrometallurgy,1: 277 - 290.

33. Martell, E.A. & Hancock, R.D. (1996). Metal Complexes in Aqueos Solution, Plenum Press, New York.

34. Lacoste-Bouchet, P., Deschenes, G. and Ghali E. (1998). Thiourea Leaching of a Copper-Gold Ore Using Statistical Design, Hydrometallurgy, 47: 189 - 203. 

35. Ertan, E. & Gulfen, M. (2009). Separation of Gold(III) from Copper(II) and Zinc(II) Ions Using Thiourea-Formaldehyde or Urea-Formaldehyde Chelating Resins.  J. Appl Polym Sci., 111: 2798 – 2805.

36. Puddephat, R. J., (1978), The Chemistry of Gold, Elsevier Scientific Publishing Company, Amsterdam.

