Malaysian Journal of Analytical Sciences Vol 17 No 3 (2013): 394 – 402

DETERMINATION OF ANILINE DEGRADED FROM SUDAN I IN CLOTHS

(Penentuan Anilin Yang Terurai Daripada Sudan I Dalam Kain)

Chong Kian Wei*, Loke Chui Fung and Chan Kar Men

Department of Chemistry and Biology, 

Faculty of Applied Sciences and Computing, 

Tunku Abdul Rahman University College, Jalan Genting Kelang, Setapak, 53300 Kuala Lumpur, Malaysia

*Corresponding author: chongkw@acd.tarc.edu.my
Abstract

A method development for the determination of an aromatic amine degraded from an azo dye in cloths was carried out. Sodium dithionite was used to cleave the azo bond of Sudan I into its aromatic amines, and the amines, mainly aniline were analyzed using high performance liquid chromatography (HPLC) with UV detection. The efficiency of the reduction process of Sudan I, based on the degree of decolorization of dye, was measured using the spectrophotometer. The optimized values of the reduction process was found effective when 1:1 ratio  of 0.30% sodium dithionite to Sudan I (dit/Sud) was used at pH 8. The recovery percentage and relative standard deviation (R.S.D.) of this method was found to be 62.9 – 88.4% and 7.6 – 21.5%, respectively. The proposed method was tested on self-dyed cloth samples with Sudan I. Aniline released from the reduction of Sudan I was detected in the self-dyed cloth samples. The results of this study demonstrate the applicability of sodium dithionite for the reduction of the azo dye in the cloth samples.

Keywords: aniline, Sudan I, sodium dithionite, azo dye

References

1. Garrigós, M.C., Reche, F., Marin, M.L., & Jiménez, A. (2002). Determination of Aromatic Amines Formed from Azo Colorants in Toy Products. J. Chromatogr. A. 976, 309-317.

2. Li, H., Xiong, Z., Dai, X., & Zeng, Q. (2012). The Effect of Perspiration on Photo-induced Chemical Reaction of Azo Dyes and The Determination of Aromatic Amine Products. Dyes pigments. 94, 55-59.

3. Ahlström, L.H., Eskilsson, C.S., & Björklund, E. (2005). Determination of Banned Azo Dyes in Consumer Goods. Trend Anal. Chem.. 24(1), 49-56.

4. Rodrigues, C.S.D., Madeira, L.M., & Boaventura, A.R. (2008). Optimization of The Azo Dye Procion Red H-EXL Degradation by Fenton’s Reagent Using Experimental Design. J. Hazard. Mater. 164, 987-994.

5. Pielesz, A., Baranowska, I., Rybak, A., & Wlochowicz, A. (2002). Detection and Determination of Aromatic Amines as Products of Reductive Splitting from Selected Azo Dyes. Ecotoxicol. Environ. Saf. 53, 42-47.

6. Gómez, J.L., León, G., Hidalgo, A.M., Gómez, M., Murcia, M.D., & Griñàn, G. (2009). Application of Reverse Osmosis to Remove Aniline from Wastewater. Desalination. 245, 687-693.

7. International Agency for Research on Cancer. (1975). Monographs on The Evaluation of Carcinogenic Risks to Humans and Their Supplements. IARC. 8, 225–241.

8. International Agency for Research on Cancer. (1987). IARC Monographs on The Evaluation of The Carcinogenic Risks to Humans. Overall Evaluations of Carcinogenicity: An Updating of IARC Monographs Volumes 1 to 42. Supplement 7. France; IARC.

9. Eskilsson, C.S., Davidsson, R., & Mathiasson, L. (2002). Harmful Azo Colorants in Leather. Determination Based on Their Cleavage and Extraction of Corresponding Carcinogenic Aromatic Amines Using Modern Extraction Techniques. J. Chromatogr. A. 955, 215-227.

10. Pricelius, S., Held, C., Sollner, S., Deller, S., Murkovic, M., Ullrich, R., Hofrichter, M., Cavaco-Paulo, A., Macheroux, P., & Guebitz, G.M. (2007). Enzymatic Reduction and Oxidation of Fiber-bound Azo-dyes. Enzyme Microb. Technol. 40, 1732-1738.

11. Shu, H.Y., Chang, M.C., & Fan, H.J. (2004). Decolorization of Azo Dye Acid Black I byThe UV/H2O2 Process and Optimization of Operating Parameters. J. Hazard. Mater. B113, 201-208.  
12. Lui, G., Zhou, J., Wang, J., Zhou. M., Lu, H., & Jin, R. (2009). Acceleration of Azo Dye Decolorization by Using Quinone Reductase Activity of Azoreductase and Quinone Redox Mediator. Bioresour. Technol. 100, 2791-2795.

13. Zille, A., Górnacka, B., Rehorek, A., & Cavaco-Paulo, A. (2005). Degradation of Azo Dyes by Trametes villosa Laccase Over Long Periods of Oxidative Conditions. Appl. Environ. Microbiol. 71(11), 6711-6718.

14. Bhaskar, M., Gnanamani, A., Ganeshjeevan, R.J., Chandrasekar, R., Sadulla, S., & Radhakrishnan, G. (2003). Analyses of Carcinogenic Aromatic Amines Released from Harmful Azo Colorants by Streptomyces SP. SS07. J. Chromatogr. A. 1018, 117-123.

15. Ji, Q., Lui, G., Zhou, J., Wang, J., Jin, R., & Lv, H. (2012). Removal of Water-insoluble Sudan Dyes by Shewanella oneidensis MR-1. Bioresour. Technol. 114, 144-148.

16. Lister, M. W. & Garvie, R. C., (1959) Sodium Dithionite, Decomposition in Aqueous Solution and in The Solid State. Can. J. Chem. 37, 1567-1574.
