Malaysian Journal of Analytical Sciences Vol 17 No 3 (2013): 422 – 429
PREPARATION AND ACTIVATION OF SPIROPYRAN-MEROCYANINE SYSTEM
(Penyediaan dan Pengaktifan bagi Sistem Spiropiran-Merosianin)
Rumaisa Nordin, Azwani Mat Lazim, Atisya Rohadi, Siti Aishah Hasbullah*

School of Chemical Sciences and Food Technology, 

Faculty of Science and Technology

Universiti Kebangsaan Malaysia, 43600 Bangi

*Corresponding author: aishah80@ukm.my

Abstract

A benzospiropyran derivative has been prepared by the condensation of the precursor, methylene indoline derivative with 2,3-dihydroxylbenzaldehye in 1:1 mole ratio. The product, spiro [2H-1-benzopyran-2, 2’-(8’-hydroxy-1’, 3’, 3’-trimethylindoline)] was able to undergo molecular rearrangement when exposed to UV light, producing an open form merocyanine. Both opened (MC) and closed form (SP) of benzospiropyran were characterized and distinguished by NMR spectroscopy, ATR Infrared and UV-vis absorption. In addition, complexation of metal ions with benzospiropyran in ethanol solution gives rise to colour changes that are visible to the naked eye. Hence, hypsochromic shift in the absorption bands were observed due to the metal ion binding (MC-M). 

Keywords: benzospiropyran, photochromic, merocyanine and hypsochromic shift
References

1. Jiang, G., Song, Y., Guo, X., Zhang, D. & Zhu, D. (2008). Organic Functional Molecules towards Information Processing and High-Density Information Storage. Journal of Advanced Materials, 20 (15):2888 – 2898.
2. Young, D. D. & Deiters, A. (2003). Light-Regulated RNA–Small Molecule Interactions. Journal of Chemistry BioChemistry, 9(8): 1225–1228.
3. Raymo, F. M. & Giodani, S. (2001). Signals Processing at the Molecular Level. Journal of the American Chemical Society, 123: 4651 – 4652.
4. Zhu, M. Q., Zhu, L., Han, J. J., Wu, W., Hurst, J. K.& Li, A. D. Q. (2005). Spiropyran-based Photochromic Polymer Nanoparticles with Optically Switchable Luminescence. Journal of the American Chemical Society, 128: 4303 – 4309.
5. Wang, S., Song, Y. & Jiang, L. (2007). Photoresponsive surfaces with controllable wettability. Journal of Photochemistry and Photobiology C: Photochemistry Reviews, 8:18 – 29.
6. Ercole, F., Davis, T. P. & Evans, R. A. (2009). Photo-responsive Systems and Biomaterials: Photochromic Polymers, light-triggered Self-assembly, Surface modification, fluorescence modulation and beyond. Polymer Chemistry, 1: 37 – 54.
7. Maurer, M. K., Lednev, I. K. & Asher, S. A. (2005). Photoswitchable Spirobenzopyran- Based Photochemically Controlled Photonic Crystals. Journal of Advanced Functional Materials, 15 (9):1401–1406.
8. Anzai, J. I. & Osa, T. (2010). Photosensitive artificial membranes based on azobenzene and spirobenzopyran derivatives. Journal of Tetrahedron, 50 (14): 4039 – 4070.
9. Berkovic, G., Krongauz, V. & Weiss, V. (2000). Spiropyran and Spirooxazines for Memories and Switches. Journal of Chemical Review, 100 (5): 1741 – 1754.
10. Bowden, S. L., Harris, S. A., Heller, H. G. & Hewlins, M. J. E. (1992). Photochromic heterocyclic fulgides. Part 6. Base-catalysed cyclizations of 1-(2, 5-dimethyl-3-furyl and 2, 5-dimethyl-3-thienyl) ethylidene (isopropylidene) succinic anhydrides and related compounds. Journal of the Chemical Society, Perkin Transactions 1, 6: 725 – 728.
11. Oda, H. (1991). Photostabilisation of colorants for imaging and data recording systems: Effects of metal carboxylates on the lightfastness of colour formers. Journal of Dyes and Pigments, 16:1 – 10.
12. Shao, N., Zhang, Y., Cheung, S. M., Yang, R. H., Chan, W. H., Mo, T., Li, K. A. & Liu, F. (2005). Copper Ion-selective Fluorescent Sensor based on the inner filter effect using a spiropyran derivative. Journal of Analytical Chemistry, 77 (22): 7294 – 7303.
13. Winkler, J. D., Bowen, C. M., and Michelet, V. (1998). Photodynamic Fluorescent metal ion sensors with parts per billion sensitivity. Journal of the American Chemical Society, 120:3237 – 3242. 
14. Ren, J. & Tian, H. (2007). Thermally Stable Merocyanine Form of Photochromic Spiropyran with Aluminium ions as a reversible photo-driven sensor in aqueous solution. Sensors 7:3166 – 3178. 
15. Oda, H. (1998). New Developments in the stabilization of Photochromic dyes: counter-ion effects on the light fatigue resistance of spiropyrans. Journal of Dyes and Pigments, 38 (4): 243 – 254.
16. Yagi, S., Maeda, K. & Nakazumi, H. (1999). Photochromic properties of cationic merocyanine dyes. Thermal stability of the spiropyran form produced by irradiation with visible light. Journal of Materials Chemistry, 9: 2991 – 2997.
17. Han, S. & Chen, Y. (2010). Mercury ion induced activation of the C-O bond in a photo-responsive spiropyran. Journal of Dyes and Pigments, 88: 235 – 239.
18. Zakhs, E. R., Zvenigorodskaya, L. A., Leshenyuk, N. G. & Martynova, V. P. (1978). Bromination of spiropyrans and reduction of their nitro derivatives. Plenum Publishing Corporation, 10: 1320 – 1326.
19. Scarmagnani, S. (2010). Development of New Adaptive Materials Based On Spiropyran Molecular Photoswitches. PhD Thesis. Dublin City University, 32-34.
20. Hecht, S. (2011). Introduction to the Synthesis of Photochromes: Spiropyran and Diarylethenes. SFB Kolluquium. Humboldt-Universitat zu Berlin
21. Macuil, R. D., Lopez, M. R., Martinez, M. B. & Pernas, V. C. (2008). ATR‐FTIR Spectroscopy and their Applications in the Ring‐Opening Reaction of Spiropyran Polymers. AIP Conference Proceedings, 992: 1237 – 1241.
22. Keum, S. R., Choi, Y. K., Lee, M. J. & Kim, S. H. (2001). Synthesis and properties of thermo- and photochromic bisindolinobenzospiropyrans linked by thio- and carbonyl groups. Journal of Dyes and Pigments, 50: 171-176.
23. Zou, W. X., Huang, H. M., Gao, Y., Matsuura, T. & Meng, J. B. (2004). Structures of Two Spiropyrans in the Open and Closed Form. Journal of Structural Chemistry, 15 (4):  317 – 321.
24. Keum, S. R., Choi Y. K., Kim, S. H. & Yoon, C. M. (1999). Symmetric and unsymmetric indolinobenzospiropuran dimmers: synthesis and characterization. Journal of Dyes and Pigments, 41:41 – 47.
25. Preigh, M. J., Stauffer, M. T., Lin, F. T. & Weber, S. G. (1996). Anodic oxidation mechanism of a Spiropyran. Journal of Chemical Society Faraday Trans, 92 (20):3991 – 3996.
26. Natali, M., Aakeröy, C., Desper, J. & Giordani, S. (2010). The role of metal ions and counterions in the switching behavior of a carboxylic acid functionalized spiropyran. Dalton Trans, 39:8269 – 8277.
27. Shiraishi, Y., Itoh, M. & Hirai, T. (2010). Thermal isomerization of spiropyran to merocyanine in aqueous media and its application to colorimetric temperature indication. Physical Chemistry Chemical Physics, 12: 13731 – 13745.
28. Nikolaeva, O. G., Tsukanov, A. V., Shepelenko, E. N., Lukyanov, B. S., Metelitsa, A. V., Kostyrina, O. Y., Dubonosov, A. D., Bren, V. A. & Minkin, V. I. (2009). Synthesis of Novel Iono- and Photochromic Spiropyrans Derived from 6, 7-Dihydroxy-8-Formyl-4-Methyl-2H-Chromene-2-One. International Journal of Photoenergy 2009: 1 – 6
