Malaysian Journal of Analytical Sciences Vol 18 No 1 (2014): 78 – 84

A STUDY ON ADSORPTION OF CADMIUM BY USING CHEMICALLY MODIFIED SALVINIA
(Kajian Penjerapan Kadmium Dengan Menggunakan Salvinia Yang Diubah Suai Secara Kimia)

Anies Suhaida Mohd Naspu1,2*, Mohd Lias Kamal2, Zaini Hamzah1, Sharizal Hasan2

1Faculty of Applied Science, 

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia
2Faculty of Applied Science, 

Universiti Teknologi MARA, 02600 Arau, Perlis, Malaysia
*Corresponding author: anies_suhaida@yahoo.com
Abstract

Salvinia was collected at the Tasik Melati, Perlis, Malaysia and it was modified using citric acid to increase the performance in removing heavy metals from standard heavy metal solution. Fourier Transform Infrared (FTIR) and Field Emission Scanning Electron Microscope (FESEM) were used to characterize Salvinia before and after chemical modification. Cadmium (Cd2+) removal studies were carried out by using modified Salvinia and the effect of various parameters such as contact time, initial heavy metal concentration and biosorbent dosage were studied. The adsorption study was investigated by using Inductively Coupled Plasma Mass Spectrometry (ICP-MS) to determine the removing of heavy metal concentration from the standard Cd2+ solution. From the study, FTIR analysis was shown the increasing of intensity on hydroxyl group after modification. A clear and smooth surface morphology of Salvinia after treatment were observed by using FESEM. The adsorption of cadmium was increased as contact time and biosorbent dosage increased. In contrast, the percent of adsorption was slightly decreased when initial concentration of Cd2+ increased.

Keywords: Salvinia, biosorbent, citric acid, cadmium and adsorption

References

1. Vargas, K., Cerro-Lopez, M., Reyna-Tellez, S., Bandala E. R. & Sanchez-Salas, J. L. (2012). Biosorption of heavy metals in polluted water, using different waste fruit cortex.Physics and Chemistry of the Earth, 37-39:  26-29.

2. Li, Q., Chai L. & Qin, W. (2012). Cadmium(II) adsorption on esterified spent grain: Equilibrium modeling and possible mechanisms. Chemical Engineering Journal, 197: 173-180.

3. Vimala, R. & Das, N. (2011). Mechanism of Cd(II) adsorption by macro fungus Pleurotus platypus. Journal of Environmental Sciences, 23(2): 288-293.

4. Espinoza-Quiñones, F. R., Módenes, A. N., Thomé, L. P., Palácio, S. M., Trigueros, D. E. G., Oliveira, A. P. & Szymanski, N. (2009). Study of the bioaccumulation kinetic of lead by living aquatic macro phyte Salvinia auriculata. Chemical Engineering Journal, 150(2–3): 316-322.

5. Xiong, C. H. & Yao, C. P. (2009). Study on the adsorption of cadmium (II) from aqueous solution by D152 resin. Journal of Hazardous Materials, 166(2–3), 815-820.

6. Zhu, B., Fan T. & Zhang, D. (2008). Adsorption of copper ions from aqueous solution by citric acid modified soybean straw. Journal of Hazardous Materials, 153 (1-2): 300-308.
7. Sabdono, A. (2009). An Assessment of Heavy Metal Concentrations in the Scleractinian Coral Tisue of Karimunjawa Archipelago, Indonesia. Journal of Coastal Development, 13 (1): 9-17.
8. Reddy, D. H. K., Harinath, Y., Seshaiash, K. & Reddy, A. V. R. (2010). Biosorption of Pb(II) from aqueous solutions using chemically modified Moringaoleifera tree leaves. Chemical Engineering Journal, 162 (2): 626-634.
9. Baral, S. S., Das, S. N., Roy Chaudhury, G., Swamy, Y. V. & Rath, P. (2008). Adsorption of Cr(VI) using thermally activated weed Salvinia cucullata. Chemical Engineering Journal, 139 (2): 245-255.
10. Chen, Y.-n., Nie, J.-x., Chen, M. & Zhang, D.-c. (2009). Biosorptional removal of lead and cadmium from water by waste material. Paper presented at the International Conference on Management and Service Science:Wuhan.
11. Sajab, M. S., Chia, C.  H., Zakaria, S., Jani, S. M., Ayob, M. K., Chee, K.  L., Khiew, P. S. & Chiu, W. S. (2011). Citric acid modified kenaf core fibres for removal of methylene blue from aqueous solution. Bioresource Technology, 102 (15): 7237-7243.
12. Leyva-Ramos, R., Landin-Rodriguez, L. E., Leyva-Ramos, S.  & Medellin-Castill, N. A. (2012). Modification of corncob with citric acid to enhance its capacity for adsorbing cadmium(II) from water solution. Chemical Engineering Journal, 180: 113-120.
13. Reddy, D. H. K., Seshaiah, K., Reddy, A. V. R. & Lee, S. M. (2012). Optimazation of Cd(II), Cu(II) and Ni(II) biosorption by chemically modified Moringa oleifera leaves powder. Carbohydrate Polymers, 88 (3): 1077-1086.
14. Lasheen, M. R., Ammar, N. S. & Ibrahim, H. S. (2012). Adsorption /desorption of Cd(II), Cu(II) and Pb(II) using chemically modified orange peel: Equilibrium and kinetic studies. Solid State Sciences, 14 (2): 202-210.
15. Chubbar, N., Carvolho, J.R. & Correia, M. J. N.  (2003). Cork biomass as biosorbent for Cu(II), Zn(II) and Ni(II).  Colloid and Surface A:Physicochemical and Engineering Aspects, 230 (1-3): 57-65.
16. Karthikeyan, S., Balasubramanian, R. & Iyer, C. S. P. (2007). Evaluation of marine algae Ulva fasciataand Sargassum sp. for the biosorption of Cu(II) from aqueous solution. Bioresource Technology, 98 (2): 452-455.
17. King, P., Srinivas, P., Kumar, Y. P. & Prasad, V. S. R. K. (2006). Sorption of copper(II) ion from aqueous solution by Tectona grandis (teak leaves powder). Journal of  Hazardous Material, 136 (3): 560-566.
