Malaysian Journal of Analytical Sciences Vol 18 No 1 (2014): 107 – 115

HYDROGEN PEROXIDE IMPEDIMETRIC DETECTION ON POLY-ORTHO-PHENYLENEDIAMINE MODIFIED PLATINUM DISK MICROELECTRODE

(Pengesanan Hidrogen Peroksida Secara Impedimetrik Di Atas Elektrod Mikro Cakera Platinum Yang Di Ubah Suai Dengan Poli-Orto-Fenilinadiamina)

Zainiharyati Mohd Zain* and Norazreen Zakaria
Faculty of Applied Sciences, 

Universiti Teknologi MARA, 40450 Shah Alam,  Selangor, Malaysia
*Corresponding author: zainihar@salam.uitm.edu.my
Abstract

This work describes the development of hydrogen peroxide detection based on Poly-ortho-phenylenediamine modified Platinum disk microelectrode (50 µm in diameter).  The electrochemical performances of H2O2 detection were studied using Chronoamperometry, Cyclic Voltammetry (CV) and Electrochemical Impedance Spectroscopy (EIS) techniques in Phosphate Buffer Solution (PBS) pH 7.4.  Effect of potential, electrode size, and various concentrations of H2O2, among others, were investigated by tracking the impedance changes at a specific perturbation frequency. To obtain the Charge transfer resistance (Rct) values, a modified Randles Equivalent Circuit was modelled and fitted to Nyquist Plot. Then, this sensor was further applied in the detection of H2O2 in antiseptic mouthwash with percent recovery of 97% ± 0.14 (x103 kΩ).

Keywords:   Electrochemical Impedance Spectroscopy, Platinum microelectrode,  hydrogen peroxide, poly-ortho-phenylen-diamine
References
1. Chiu, M. H., Kumar, A. S., Sornambikai, S., Chen, P.Y., Shih, Y. & Zen, J. M. (2011). Cosmetic  Silver Electrode. Int. J. Electrochem. Sci, 6: 2352- 2365.

2. Li,G. Wang, Y. & Xu, H. (2007).  A Hydrogen Peroxide Sensor Prepared by Electropolymerization of Pyrolle based on Screen printed Carbon Paste Electrodes.  Sensors, 7: 239-250.

3. Ansari, A. A., Solanki, P. R. & Malhotra, B. D.( 2009). Hydrogen peroxide sensor based on horseradish peroxidase immobilized nanostructured cerium oxide film.  Biotechnology, 142: 179- 184.

4. Chai, X.S., Hou, Q. X., Luo, Q. & Zhu, J.Y. (2004). Rapid determination of hydrogen peroxide in the wood pulp bleaching streams by a dual-wavelength spectroscopic method.  Analytica  Chimica  Acta, 507: 281-284.

5. Shamsipur, M., Asgari, M., Maragheh, M. G. & Moosavi-Movahedi A. A. (2012). A novel impedimetric nanobiosensor for low level determination of hydrogen peroxide based on biocatalysis of catalase.  Bioelectrochemistry, 83: 31-37.
6. C.F. Sanchez, C. J. McNeil, and K. Rawson, Trends. Anal. Chem., 2005, 24, 37.

7. Shervedani, R. K., Mehrjardi, A. H. & Zamiri, N. (2006). A novel method for glucose determination based on electrochemical impedance spectroscopy using glucose oxidase self-assembled biosensor. Bioelectrochem,69: 201- 208

8. Daniels, J. S. & Pourmand, N. (2007). Label-Free Impedance Biosensors: Opportunities and Challenges. Electroanalysis, 12: 1239- 1257.

9. Bard, A. J. & Faulkner, L. R. (2001). Electrochemical Methods: Fundamentals and Applications, Second edition. John Wiley and Sons, New York, Chichester, Brisbane, Toronto.
10.  Zhang, L., Yin, H. B., Luo, J. J., Yang, P. H. & Cai, J. Y. (2013). Construction of Electrochemical Impedance Sensor Based on Poly Dopamine- Hyaluronic Acid Composite Membrane for Detection of Hydrogen Peroxide. Chinese Journal of Analytical Chemistry, 41(4): 534-539. 
11. Aziah, A. A., O’ Neill, R .D.,  Yahya, M. Z. A. & Zainiharyati, M. Z. (2012). Electropolymerization of ortho-Phenylenediamine and its Use for Detection on Hydrogen Peroxide and Ascorbic Acid by Electrochemical Impedance Spectroscopy.  International Journal  of  Electrochemical Science, 7:10154-10163.
12. Rothwell, S. A., Killoran, S. J. & O’Neill, R. D. Enzyme Immobilization Strategies and Electropolymerization Conditions to Control Sensitivity and Selectivity Parameters of a Polymer-Enzyme Composite Glucose Biosensor. Sensor, 10: 6439- 6462.
13. Zhou, D. M., Dai, Y. Q. & Shiu, K. K. (2010). Poly(phenylenediamine) film for the construction of glucose biosensors based on platinized glassy carbon electrode. J. Appl. Electrochem, 40: 1997-2003.
14. Rothwell, S. A., . Killoran, S. J.,  Neville, E. M. A., Crotty, M. & O’Neill, R . D. (2008). Poly(o-phenylenediamine) electrosynthesized in the absence of added background electrolyte provides a new permselectivity benchmark for biosensor applications. Electrochemistry  Communications, 10: 1078-1081.
15. Rothwell, S. A., McMahon, C. P. & O’Neill, R. D. (2010). Effects of polymerization potential on the permselectivity of poly(o-phenylenediamine) coatings deposited on Pt–Ir electrodes for biosensor applications. Electrochimica  Acta, 55: 1051-1060.
16. Han, J. H., Boo, H., Park, S. & Chung, T. D. (2006). Electrochemical oxidation of hydrogen peroxide at nanoporous platinum electrodes and the application to glutamate microsensor. Electrochimica Acta., 52:  1788- 1791.
17. Miao, X. M., Yuan, R., Chai, Y. Q., Shi, Y. T . & Yuan,  Y. Y. (2008). Direct electrocatalytic reduction of hydrogen peroxide based on Nafion and copper oxide nanoparticles modified Pt electrode. Journal of Electroanalytical Chemistry, 612: 157- 163.
18. Upadhyay, A. K., Chen, S. M., Ting, T . W. & Peng, Y. Y. (2011). A Biosensor for Hydrogen Peroxide Based on Single walled Carbon Nanotube and Metal Oxide Modified Indium Tin Oxide Electrode. International Journal of  Electrochemical Science, 6:  3466- 3482.
19. Zainiharyati, M. Z., O’Neill, R. D.,  Lowry, J. P., Pierce, K. W.,  Tricklebank, M., Dewa, A. & Sulaiman, A. G. (2010). Development of an implantable d-serine biosensor for in vivo monitoring using mammalian d-amino acid oxidase on a poly (o-phenylenediamine) and Nafion-modified platinum–iridium disk electrode. Biosensors and Bioelectronics 25,  1454 – 1459.
20. Wahnono, N., Qin, S., Oomen, P., Cremers, T. I. F., Vries, M. G. D. & Westerink, B. H. C.(2012). Evaluation of permselective membranes for optimization of intracerebral amperometric glutamate biosensors. Biosensors and Bioelectronics 33, 260- 266. 
21. Aldeen. E. (1999). The Electrochemical Oxidation Of Hydrogen Peroxide On Platinum Electrodes At Phosphate Buffer Solutions.  Massey University, Palmerston North New Zealand.
22. Jacabson. T (2002) Complex impedance method for AC circuits. Supplement, Phy273. University of Marylan.
23. Ghica, M. E., Brett, M. A. & Goncalves, A. R. (2010). Preparation and characterisation of poly(3,4-ethylenedioxythiophene) and poly(3,4-ethylenedioxythiophene)/poly(neutral red) modified carbon film electrodes, application as sensor for hydrogen peroxide. Electrochimica Acta, 10: 1016.
24. Kartika, S. H.,  Zainiharyati, M. Z., Mohamed, H. I. A., Jafri, M. A. & O’Neill, R. D. (2013). Development of a Brain Glutamate Microbiosensor. World Academy of Sciences, Engineering and Technology, 78.
25. Ahmed, R. & Reifsnider, K. (2011).  Study of Influence of Electrode Geometry on Impedance Spectroscopy. International Journal of Electrochemical Science. 6: 1159 – 1174.
26. Orazem, M. & Tribollet, B. (2008). Electrochemical Impedance Spectroscopy. John Wiley and Sons, Inc., Hoboken, New Jersey.
27. Katz, E. & Willner, I. (2003). Probing Biomolecular Interactions at Conductive and Semiconductive Surfaces by Impedance Spectroscopy: Routes to Impedimetric Immunosensors, DNA-Sensors, and Enzyme Biosensors. Electroanlysis,  15: 11.
28. Babaei, A., Garret, D. J. & Downard, A. J. (2012). Electrochemical Investigations on a Third Generation Biosensor for Determination of Hydrogen Peroxide Based on Immobilization of Myoglobin on a Novel Platinum Nanoparticle/Carbon Nanotube/Ionic Liquid/Nafion Composite. International Journal of Electrochemical Science, 7: 3141- 3154.
29. Kirwan, S. M., Rocchitta, G., McMahon C. P.,  , Craig, J. D.,  Killoran, S. J.,  O’Brien, K. B., Serra,  P. A., Lowry, J. P. & O’Neill, R. D. (2007). Modifications of Poly(o-phenylenediamine) Permselective Layer on Pt-Ir for Biosensor Application in Neurochemical Monitoring. Sensors, 7: 420-437.
