Malaysian Journal of Analytical Sciences Vol 18 No 1 (2014): 204 - 211
EFFECT OF RICE STRAW EXTRACT AND ALKALI LIGNIN ON THE CORROSION INHIBITION OF CARBON STEEL
(Kesan Ekstrak Jerami Padi dan Alkali Lignin Terhadap Perencatan Kakisan Keluli Karbon)
Rabiahtul Zulkafli1, Norinsan Kamil Othman1*, Irman Abdul Rahman1, Azman Jalar2

1School of Applied Physics, Faculty of Science and Technology,

2Institute of Micro Engineering and Nanoelectronics (IMEN), 

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor,  Malaysia

*Corresponding author: insan@ukm.my

Abstract

A paddy residue based corrosion inhibitor was prepared by treating finely powdered rice straw with aqueous ethanol under acid catalyst (0.01M H2SO4). Commercial alkali lignin was obtained from Sigma-Aldrich. Prior to the corrosion test, the extraction yield and alkali lignin was characterized via FTIR to determine the functional group. The effect of paddy residue extract and commercial alkali lignin on the corrosion inhibition of carbon steel in 1M HCl was investigated through the weight loss method, potentiodynamic polarization technique and scanning electron microscopy (SEM). The corrosion inhibition efficiency of the extract and alkali lignin at different immersion times (3h, 24h and 42h) was evaluated. The results show that the paddy waste extract exhibited lesser weight loss of carbon steel in the acidic medium in comparison to the commercial alkali lignin, suggesting that the paddy residue extract is more effective than the commercial alkali lignin in terms of its corrosion inhibition properties. The results obtained proves that the extract from paddy residue could serve as an effective inhibitor for carbon steel in acidic mediums.

Keywords: Rice straw extract, corrosion, carbon steel, inhibition
References

1. Satar, M. Z. M., Noor, M. F. M., Samsudin, M. W., & Othman, M. R. (2012). Corrosion Inhibition of Aluminum by Using Nipah (Nypa Fruticans) Extract Solutions in Hydrochloric Acid (HCl) Media. Int. J. Electrochem. Sci., 7: 1958 – 1967.
2. Obot, I. B.,Umoren, S. A Umoren & Obi-Egbedi N.O. (2011). Corrosion Inhibition and Adsorption Behaviour for Aluminuim by Extract of Aningeria Robusta in HCl Solution: Synergistic Effect of Iodide Ions. J. Mater. Environ. Sci. 2 (1): 60-71.
3. Anvar, U., Buranov, & Mazza, G. (2008). Review-Lignin in Straw of Herbaceous Crops. Industrial Crops and Products 28: 237–259.
4. Dafalla, S.B., Mukhtar, H., & Shaharun, M.S. (2010). Characterisation of Adsorbent Developed from Rice Husk: Effect of Surface Functional Group on Phenol Adsorption. J. Appl. Sci. 10 (12): 1060-1067.

5. Sastri, V.S. (1998). Chemical Aspects of Corrosion Inhibition in Corrosion Inhibitors. Principles and Applications. John Wiley & Sons, Ltd. Exerter : 110.
6. El-Eltre, A.Y., Abdallah, M. & El-Tantawy, Z.E. (2005). Corrosion Inhibition of Some Metals using Lawsonia Extract. Corrosion Science 47: 385 - 395. 

7. Olusegun K. A. & James A.O (2010). The Effects of Aloe vera Extract on Corrosion and Kinetics of Corrosion Process of Zinc in HCl Solution. Corrosion Science 52: 661–664.
8. Afidah A. R., Emmanuel R., Jean Steinmetz, M. Jain K., & M. Sani Ibrahim. (2007). Mangrove Tannins and their Flavonoid Monomers as Alternative Steel Corrosion Inhibitors in Acidic Medium. Corrosion Science 49: 402-417.

9. Radojčić, I., Berković, K., & Vorkapić-Furač, J.(2008),. Natural Honey and Black Radish Juice as Tin Corrosion Inhibitors. Corrosion Science 50: 1489-1505.
10. Orubite, K.O. & Oforka, N.C. (2004). Inhibition of The Corrosion Of Mild Steel in Hydrochloric Acid Solutions by The Extract of Leaves Of Nypa Fruiticans Wurmb. Materials Letters 58: 1768-1772.
11. Hortling, B., Tamminen, T. & Kentta, E. (1997). Determination of Carboxyl and Non-Conjugated Carbonyl Groups in Dissolved and Residual Lignins by IR Spectroscopy. Holzforschung, 51: 405–410.
12. Abiola O. K. & Oforka N. C., (2003). Corrosion Inhibition Effect of Cocos Nuciferal Juice on Mild Steel in 5% Hydrochloric Acid Solution. Scientia Africa.2: 82 

13. Sun, X. F., Xu F., Sun R. C.,Fowder P., & Baird M. S. (2005). Characteristics of Degraded Cellulose Obtained from Steam-Exploded Wheat Straw. Carbohydrate Resource 340:97-106.
14. Adapa, P. K., Karunakaran C., Tabil L. G., & Schoenau G. J. (2009). Potential Applications of Infrared and Raman Spectromicroscopy for Agricultural Biomass. Agricultural Engineering International 1081: 1-25.
15. Robert Baboian  (2005). Corrosion Tests And Standards: Application And Interpretation. ASTM International: 295.
16. Sakakibara, I., Katsuhara, T., Ikeya, Y., Hayashi, K. & Mitsuhashi, H. (1991). Cannabisin A, An Arylnaphthalene Lignanamide from fruits of Cannabis sativa. Phytochemistry 30 (9): 3013-3016.

17. Vanquez, G., Antorrena, G., Gonzalez, J. & Freire, S. (1997). FTIR, H—1 and C-13 NMR Characterization of Acetosolv-Soloubilized Pine and Eucalyptus Lignins. Holzforschung 51 (2): 158-166.
18. Sun, Y. L., Zhang, Q., Schwab, J. J., Demerjian, K. L. Chen, W. N., Bae, M.S., Hung, H. M. Hogrefe, O., Frank, B., Rattigan, O. V. &. Lin, Y. C. Characterization Of The Sources And Processes Of Organic And Inorganic Aerosols In New York City With A High-Resolution Time-Of-ﬂight Aerosol Mass Apectrometer. Atmospheric Chemistry and Physics 11(4): 1581-1602.
19. Freeman, R. A & Silverman, D. C. (1992). Error Propagation in Coupon Immersion Tests. Corrosion 48 (6). 1992: 463.
20. Tebbiji, K., Oudda, H., Hammouti, B., Benkaddour, M., El Kodadi, M., Malek, F., & Ramdani, A. (2005). Inhibitive Action of Two Bipyrazolic Isomers Towards Corrosion of Steel in 1 M HCl Solution. Applied Surface Science 241: 326-334.
21. Ashassi-Sorkhabi, H., Majidi, M. R. & Seyyedi K. (2004). Investigation of Inhibition Effect of Some Amino Acids Against Steel Corrosion in HCl Solution. Applied Surface Science 225:176-185.

22. O. L. Riggs Jr. (1973), Corrosion Science, Second ed., C. C Nathan, Houston, Texas.
