Malaysian Journal of Analytical Sciences Vol 18 No 1 (2014): 221 - 225
DIGESTION STUDY OF WATER LEACH PURIFICATION (WLP) RESIDUE FOR POSSIBILITY OF THORIUM EXTRACTION

(Kajian Penghadaman Residu Pemurnian Larut Resap Air (WLP) Untuk Kebarangkalian Pengekstrakan Torium)

Wadeeah M. AL-Areqi*, Amran Ab. Majid, Sukiman Sarmani

Nuclear Science Programme, School of Chemical Sciences & Food Technology,

Faculty of Science and Technology, 

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: walareqi@yahoo.com
Abstract

Water leach purification (WLP) is the main residue being produced by Lynas Advanced Materials Plant (LAMP). During rare earths elements extraction process, thorium is removed completely to WLP. The objective of this study was to extract thorium from WLP in order to reduce the level of radioactivity and to store Th for future nuclear fuel. Alkali and concentrated acids process was used to recover the Th from WLP. The concentration of Th and U in WLP was determined by Instrumental Neutron Activation Analysis (INAA) and found to be 1952.9 ± 17.6 mg/kg and 17.2 ± 2.4 mg/kg respectively. Digestion process of WLP via sodium hydroxide, concentrated nitric and sulphuric acids using different time and temperature has been tested. The Th concentrations in liquid phrase were determined by Inductively Coupled Plasma-Mass Spectroscopy (ICP-MS). In both processes less than 5% recovery of Th has been achieved. This study showed that very low Th recovery was achieved due to thorium was probably converted into refractory and insoluble form through the calcination stage of LAMP processing. Therefore different techniques should be used to recover the thorium.

Keywords: thorium, digestion, WLP, Th recovery
References
1. AEA. (2005). Thorium fuel cycle- Potential benefits and challenges. IAEA-TECDOC-1450.

2. Mathieu, L., Heuer D., Brissot , R., Garzenne, C., Le Brun, C., Lecarpentier, D., Liatard, E., Loiseaux, J.-M., Me´plan, O., Merle-Lucotte, E., Nuttin , A., Walle, E. & Wilson, J. (2006). The thorium molten salt reactor: Moving on from the MSBR. Progress in Nuclear Energy 48: 664-679.

3. Hania, P.R. & Klaassen, F.C. (2012). Thorium Oxide Fuel. Comprehensive nuclear material 3: 87–108.

4. Csom G., Reiss, T., Fehér, S.& Czifrus, S.(2012). Thorium as an alternative fuel for SCWRs. Annals of Nuclear Energy 41: 67–78.

5. Björk, K. I., Fhager, V. & Demazière, C. (2011). Comparison of thorium-based fuels with different fissile components in existing boiling water reactors. Progress in Nuclear Energy 53: 618- 625

6. Lehto, J. & Hou, X. (2011).  Chemistry and Analysis of Radionuclides: Laboratory Techniques and Methodology. Wiley-VCH Verlag & Co. KGaA 
7. USGS. (2012). U.S. Geological Survey, Mineral Commodity Summaries, January 2012.
8. Kabata-Pendias, A. and Mukherjee, A. B. (2007). Trace Elements from Soil to Human. Berlin : Springer.

9. Cordier, D.J. (2012). U.S. Geological Survey. Mineral Commodity Summaries. (703) 648-7723, dcordier@usgs.gov. 

10. Hughes, K.C. & Singh, R. (1980). The isolation of thorium from monazite by solvent extraction. Hydrometallurgy 6: 25-33.

11. Wickleder, M. S.  Fourest, B. & Dorhout,P. K. (2010). The Chemistry of the Actinide and Transactinide Elements, chapter three:  Thorium.

12. Abrao, A., Alves de Freitas, A., & Sequeira de Carvalho, F. M. (2001). Preparation of highly pure thorium nitrate via thorium sulfate and thorium Peroxide. Journal of Alloys and Compounds 323–324: 53- 56.

13. RIA (2011). Radiological impact Assessmant of Lynas Advanced Materials Plant 2011: Exective Summary, Rev   4, November (2011).

14. IAEA (2011). Radiation Protection and NORM Residue Management in the Production of Rare Earths from Thorium Containing Minerals, Safety Reports Series No. 68. 

15. Ali, A.M.I. El-Nadi, Y.a. Daoud, J.a.& Aly, H.F. (2007). Recovery of thorium (IV) from leached monazite solutions using counter-current extraction. International Journal of Mineral Processing 81: 217-223.

16. Cardarelli, F. (2008).  Materials Handbook: A Concise Desktop Reference, 2nd Edition. 
