Malaysian Journal of Analytical Sciences Vol 18 No 1 (2014): 28 – 36

THE EFFECT OF TEMPERATURE ON MILD STEEL CORROSION IN 

1 M HCl BY SCHIFF BASES

(Kesan Suhu Terhadap Kakisan Keluli Lembut Dalam 1 M HCl oleh Ligan Bes Schiff)
Nor Zakiah Nor Hashim1* and Karimah Kassim1, 2
1Faculty of Applied Sciences, 

 2Institute of Sciences, 

Universiti Teknologi MARA,40450, Shah Alam, Selangor, Malaysia

*Corresponding author: norzakiah21@gmail.com
Abstract

The temperature effects in the range of 25 to 55oC on the inhibition efficiency of three Schiff bases which were (E)-N1-benzylidene-N4-phenylbenzene-1,4-diamine (K1), N-[(E)-4-chlorobenzylidene-N’-phenylbenzene-1,4-diamine (K2), and N-[(E)-4-methoxybenzylidene-N’-phenylbenzene-1,4-diamine (K3) against mild steel in 1 M hydrochloric acid (HCl) solution were studied using polarization method. Thermodynamic adsorption parameter suggests that the inhibitors under study were mixed type inhibitors dominated by anodic reaction and it was found that from all of the three inhibitors, K2 having the highest corrosion inhibition efficiency.

Keywords: 1 M HCl, mild steel, Schiff base, temperature, corrosion
References

1. Haleem, S.M.A.E., Wanees, S.A., Aal, E.E.A.E. and Farouk, A. (2013). Factors affecting the corrosion behaviour of aluminium in acid solutions. I. Nitrogen and/or sulphur-containing organic compounds as corrosion inhibitors for Al in HCl solutions. Corrosion Science 68: 1-13.

2. Goulart, C.M., Souza, A.E., Huitle, C.A.M., Rodrigues, C.J.F., Maciel, M.A.M. and Echevarria, A. (2013). Experimental and theoretical evaluation of semicarbazones and thiosemicarbazones as organic corrosion inhibitors. Corrosion Science 67: 281-291.

3. Ju, H., Kai, Z.P. and Li,Y. 2008. Aminic nitrogen-bearing polydentate Schiﬀ base compounds as corrosion inhibitors for iron in acidic media: A quantum chemical calculation. Corrosion Science 50: 865-871.

4. Mallaiya, K., Subramaniam, R., Srikandan, S.S., Gowri, S., Rajasekaran, N. and Selvaraj, A. (2011). Electrochemical characterization of the protective ﬁlm formed by the unsymmetrical Schiff’s base on the mild steel surface in acid media. Electrochimica Acta 56: 3857-3863.

5. Hashim, N.Z.N., Kassim, K. and Yamin, B.M. (2010). N-[(E)-4-Chlorobenzylidene]-N’-phenylbenzene-1,4-diamine. Acta Crystallographica E66: o2039.

6. Hassan, H.H., Abdelghani, E. and Amin, M.A. (2007). Inhibition of mild steel corrosion in hydrochloric acid solution by triazole derivatives Part I. Polarization and EIS studies. Electrochimica Acta 52: 6359-6366.

7. Amin, M.A., Ahmed, M.A., Arida, H.A., Arslan, T., Saracoglu, M. and Kandermirli, F. (2011). Monitoring corrosion and corrosion control of iron in HCl by non-ionic surfactants of the TRITON- X series- Part II. Temperature effect, activation energies and thermodynamics of adsorption. Corrosion Science 53: 540-548.

8. Bentiss, F., Traisnel, M., Gengembre, L. and Lagrenée. (1999). A new triazole derivative as inhibitor of the acid corrosion of mild steel: electrochemical studies, weight loss 
determination, SEM and XPS. Applied Surface Science 152: 237-249.

9. Aljourani, J. Raeissi, K. and Golozar, M.A. (2009). Benzimidazole and its derivatives as corrosion inhibitors for mild steel in 1M HCl solution. Corrosion Science 51: 1836-1843.

10. Radovici, O. (1965). Proceedings of the Second European Symposium on Corrosion Inhibitors. Ferrara, p 178.

11. Hasan, B.O. and Sadek, S.A. (2014). The effect of temperature and hydrodynamics on carbon steel corrosion and its inhibition in oxygenated acid-salt solution, Journal of Industrial and Engineering Chemistry 20: 297-307.
12. Vračar, L.M. and Dražić, D.M. (2002).  Adsorption and corrosion inhibitive properties of some organic molecules on iron electrode in sulfuric acid. Corrosion Science 44:1669-1680.
13. Sorkhabi, H.A. Shaabani, B. and Seifzadeh, D. (2005). Corrosion inhibition of mild steel by some schiff base compounds in hydrochloric acid. Applied Surface Science 239: 154-164.

14. Antonijevic, M.M. and Petrovic, M.B. Copper Corrosion Inhibitors. A review. International Journal of Electrochemical Science 3: 1-28.

15. Obot, I.B., Egbedi, N.O.O. and Umoren, S.A. 2009. Antifungal drugs as corrosion inhibitors for aluminium in 0.1 M HCl. Corrosion Science 51:1868-1875.

16. Emregül, K.C. and Hayvali, M. 2006. Studies on the eﬀect of a newly synthesized Schiﬀ base compound from phenazone and vanillin on the corrosion of steel in 2 M HCl. Corrosion Science 48: 797-812. 

17. Nasser, A.J.A. and Sathiq, M.A. (2012). Comparative study of N-[(4-methoxyphenyl) (morpholin-4-yl)methyl]acetamide (MMPA) and N-[morpholin-4 yl(phenyl)methyl]acetamide (MPA) as corrosion inhibitors for mild steel in sulfuric acid solution. Arabian Journal of Chemistry. 
http://dx.doi.org/10.1016/j.arabjc.2012.07.032
18. Kandias, D., Bundjali, B. and Wahyuningrum, D. 2011. Curcuminoid compounds isolated from curcuma domestica val. as corrosion inhibitor towards carbon steel in 1 % NaCl solution. 
Sains Malaysiana 40: 1013-1018.
