
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 343 – 350

THE EFFECT OF BLEND RATIO ON PROPERTIES OF RECYCLED POLYPROPYLENE/RECYCLED HIGH DENSITY
POLYETHYLENE GEO- COMPOSITES
(Kesan Nisbah Adunan Ke Atas Sifat-Sifat Geo-Komposit Polipropilena Kitar Semula/Polietilena Ketumpatan Tinggi Kitar Semula)

A.A.S Mariam Atiqah, H.Salmah*, Z. Firuz, D.N.U. Lan
School of Materials Engineering,

Universiti Malaysia Perlis,Taman Muhibah, Jejawi, 02600 Arau, Perlis,Malaysia

*Corresponding author: irsalmah@unimap.edu.my

Abstract

The effect of blends ratio of Recycled Polypropylene (rPP) and Recycled High Density Polyethylene (rHDPE) on tensile properties of rPP/rHDPE geo-composites were studied. The increasing of rHDPE ratios has decreased the tensile strength and elongation at break of rPP/rHDPE geo-composites, but the modulus of elasticity increased. The effects of rPP ratios have enhance the tensile strength and modulus of elasticity of geo-composites. The elongation of break of rPP/rHDPE was decreased with increasing the rPP content. At similar blends ratio, the rPP/rHDPE geo-composites higher tensile strength and modulus of elasticity compared to rHDPE/rPP geo-composites. The MFI value of rPP/rHDPE higher than rHDPE/rPP blends. The SEM micrograph showed that rPP/rHDPE has smooth failure surface. 
Keywords: recycled polypropylene, recycled high density polyethylene, tensile properties, blends, geo-composites.
Abstrak

Kesan nisbah adunan ke atas sifat- sifat tegangan geo komposit polipropilena kitar semula (rPP)/ polietilena ketumpatan tinggi kitar semula (rHDPE) telah dikaji. Peningkatan nisbah rHDPE telah mengurangkan kekuatan tegangan dan  rPP/rHDPE tetapi meningkatkan ketegangan modulus. Kesan nisbah rPP telah meningkatkan kekuatan tegangan dan pemanjangan geo- komposit. Pemanjagan rPP/rHDPE telah menurun dengan peningkatan kandungan rPP. Pada campuran nisbah yang sama, rPP/rHDPE geo-komposit kekuatan tegangan modulus tinggi berbanding rHDPE/rPP geo-komposit. Nilai MFI adunan rPP/rHDPE lebih tinggi berbanding adunan rHDPE/rPP. Mikrograf SEM menunjukkan rPP/rHDPE mempunyai permukaan yang licin. 
Kata kunci: polipropilena kitar semula, polietilena ketumpatan tinggi kitar semula, sifat-sifat tegangan, adunan, geo-komposit
References
1. Rahman M.M., Islam M.A., Ahmed M. (2012). Recycling of Waste Polymeric Materials as a Partial Replacement for Aggregate in Concrete. International Conference on Chemical, Environmental and Biological Sciences (ICCEBS’2012), Penang, Malaysia.
2. Sukunya C. A study of compatibilization and properties of recycled high densitypolyethylene/polyethylene teraphthalate blends. Institute of Engineering, Polymer Engineering, Suranaree University of Technology, (2007) MSc Thesis.
3. Albano L. & Sanchez G. (1999). Study of the Mechanical, Thermal and Thermodegradative Properties of Virgin PP with Recycled and Non Recycled HDPE. PolymerEngineering and Science. 39(8): 1456-1462.
4. La Mantia F. (2002). Handbook of Plastic Recycling. Rapra Technology Ltd., Shropshire,UK, London. pg.132-167
5. Oza S.,Wang R., Lu N. (2011). Thermal and Mechanical Properties of Recycled High Density Polyethylene/hemp Fiber  Composites. International Journal of Applied Science and Technology,1 (5), 31-36.
6. Batayney M., Marie I., Asi I. (2007). Use of selected waste materials in concrete mixes. Faculty of Engineering, Civil Engineering Department, The Hashemite Univeristy, Jordan. Waste Management, 27: 1870-1876. 
7. Siddique R., Khatib J., Kaur I. (2008). Use of Recycled plastic in concrete: A review. Waste Management, 28: 1835-1852.
8. Fasanella E.L., Jackson E.K., Kellas S. (2007). Soft Soil Impact testing and Simulation of Aerospace Structures. NASA langley Research Center, Hampton, Virginia, US.
9. Palmeira E.M., Tatsuoka F., Bathurst R.J., Stevenson P.E., Zornberg J.G. (2008). Advances in Geosynthesis Materials and Applications for Soil Reinforcement and Environmental Protection Works. Electronic Journal of Geothecnical Engineering: 1 - 38.
10. Vijay C., John S.K.,Thomas J., George   J.N. (2010). World’s First Thermoplastic Bridges. Parsons Brinckerhoff Inc.  New York. 
11. Pan B., Ning N., Liu J.,Bai L., Fu Q. (2009). Mechanical Properties of SMC Whisker Reinforced High Density Polyethylene Composites. Chinese Journal of Polymer Science, 27 (2), 267 – 274.
12. Lei Y.,Wu Q.,Yao F.,Xu Y. (2007). Preparation and Properties of recycled HDPE/natural fiber composites. Composites: Part A, 38, 1664-1674.
13.  Shenoy A.V., Saini D.R., Nadkarni V.M. (1984). Melt rheology of polymer blends from melt flow index. International Journal of Polymeric Materials and Polymeric Biomaterials, 10,231-235.
14. Utracki L.A. (1983). Melt flow of polymer blends. Polymer Engineering and Sciences: Polymer Blends. 23(11), 602-609.
