
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 368 – 375

MECHANICAL AND MORPHOLOGY PROPERTIES OF FEATHER FIBER COMPOSITE FOR DENTAL POST APPLICATION

(Sifat- Sifat Mekanikal dan Morfologi Komposit Serat Bulu Untuk Aplikasi Pos Pergigian)

Siti Maizatul Farhain Salehuddin1, Mat Uzir Wahit2*, Mohammed Rafiq Abdul Kadir3, Eshamsul Sulaiman4,
 Noor Hayaty Abu Kasim4

1Department of Polymer Engineering, Faculty of Chemical Engineering,

2Center of Composite, Faculty of Mechanical Engineering,

3Medical Implant Technology Group, Faculty of Biosciences & Medical Engineering,

Universiti Teknologi Malaysia, 81310 UTM Skudai, Johor Bahru, Malaysia

4Department of Restorative Dentistry, Faculty of Dentistry Building,

Universiti Malaya, Kuala Lumpur, Malaysia

*Corresponding author: mat.uzir@cheme.utm.my

Abstract

Feather/plastic composite material was fabricated from polymethyl methacrylate (PMMA), feather fiber (FF) and  montmorillonite (MMT) using brabender internal mixer. PMMA based composites were produced with 1, 3, 5, 7 and 10 phr composite of mass feather fiber with and without 4 % of montmorillonite (MMT). Alkali treatment was used to improve the interfacial adhesion among the feather fiber (FF) and the PMMA. Flexural properties of FF/PMMA and FF/PMMA/MMT composites were investigated. Composites were analyzed by Scanning Electron (SEM) and Fourier Transform Infra Red (FTIR) spectroscopy techniques. The result showed that, the addition of FF significantly increased the flexural strength of the composites. The hydrophobic nature of feather fiber displayed an excellent compatibility among fibers and PMMA matrix. 

Keywords: PMMA, Feather Fiber, alkali treatment
Abstrak

Dalam kajian ini, bulu / bahan komposit plastik telah diperbuat daripada polimetil metakrilat (PMMA), serat bulu (FF) montmorilonit (MMT) menggunakan brabender percampuran dalaman. PMMA komposit dihasilkan berasaskan dengan 1, 3, 5, 7 dan 10 phr komposit berat serat bulu dengan dan tanpa 4% daripada MMT. Kaedah rawatan alkali telah digunakan untuk meningkatkan lekatan antara muka antara serat bulu dan PMMA. Sifat mekanik FF/PMMA dan FF /PMMA/ MMT komposit kekuatan lenturan itu telah disiasat. Spesimen yang diperolehi dianalisis dengan mikroskop imbasan elektron (SEM) dan teknik spektroskopi FTIR. Keputusan menunjukkan bahawa penambahan FF meningkatkan kekuatan lenturan bahan komposit ini. Sifat hidrofobik serat menunjukkan satu keserasian yang baik antara gentian dan matrik PMMA.

Kata kunci: PMMA, serat bulu, rawatan alkali
References

1. Kock J. W. (2006). Physical and Mechanical Properties of Chicken Feather Materials. Master School of Civil and Environmental Engineering, Georgia Institute of Technology.

2. Alberts, B.,  Bray, D.,  Lewis, J., Raff, M., Robert, K., & Watson, J. D. (1994). Molecular Biology of the Cell. 3rd edition. Garland Press. New York. 
3. Jeffrey, W. K. (2006). Physical and Mechanical Properties of Chicken Feather Material. Master of Science. Georgia Institute of Technology.
4. Ananda R.V., Alok, S., & Mirsha, S. C. (2007). Polymer Composites Reinforced with Short Fibers Obtained from Poultry Feathers. Proceedings of International and INCCOM-6 Conference.
5. Unemori, M., Matsuya, Y., Matsuya, S., Akashi, A., & Akamine, A. (2003). Water Absorption of Poly(methyl methacrylate) Containing 4-methacryloxyethyl Trimellitic Anhydride. Biomaterials. 24(8): 1381-1387.
6. Nidal, W. E. (2006). Mechanical and Enviroment Properties of Denture Base Poly(methylmethacrylate) Filled by Brium Titanate. Master of Science. Universiti Sains Malaysia (USM).
7. Ramanaiah. K, Ratna Prasad. A. V., & Hema Chandra Reddy, K. (2012). Effect of Fiber Loading on Mechanical Properties of Borassus Seed Shoot Fiber Reinforced Polyester Composites.  Journal of Material Environment Science. 3(3): 374-378. 
8. Mishra, S. C., Nayak, N. B., & Satapathy, A. (2010). Investigation on Bio-waste Reinforced Epoxy Composites. Journal of Reinforced Plastics and Composites. 29(19): 3016-3020. 
9. Madejova, J. (2003). FTIR Techniques in clay Mineral studies. Vibrational Spectroscopy 31: 1-10.
10. Barone, J. R., & Schmidt, W. F. (2005). Polyethylene Reinforced with Keratin Fibers Obtained from Chicken Feathers. Composites Science and Technology. 65(2): 173-181.
11. Murayama-Arai K., Takahashi R., Yokote Y., Akahane K. (1983). Amino acid sequence of feather keratin from fowl. European Journal of Biochemistry. 132: 501 - 507.
12. Castano V.M., Martinez-Harnandez A. L., Velasco-Santos C., & De-Icaza M. (2007). Dynamical- mechanical and thermal analysis of polymeric composites reinforced with keratin biofibers from chicken feathers, Composites B. 38(3): 405-410.
13. Martínez-Hernández, A. L., Velasco-Santos, C., Icaza, M. d., & Castaño, V. M. (2005). Mechanical Properties Evaluation of New Composites with Protein Biofibers Reinforcing Poly(methyl methacrylate). Polymer. 46(19): 8233-8238. 
