
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 376 – 384

CARBOXYMETHYL CELLULOSE FROM KENAF REINFORCED COMPOSITE POLYMER ELECTROLYTES BASED 49% POLY(METHYL METHACRYLATE)-GRAFTED NATURAL RUBBER 

(Komposit Polimer Elektrolit Berasaskan 49% Poli(metil metakrilat)-cangkukan Getah Asli Diperkuat Karboksimetil Selulosa Daripada Kenaf)

Serawati Jafirin1, Ishak Ahmad1,2*,  Azizan Ahmad1,2

1School of Chemical Sciences and Food Technology,

2Polymer Research Centre (PORCE), 

Faculty of Science and Technology

Universiti Kebangsaan Malaysia, 43600, Bangi, Selangor Darul Ehsan, Malaysia

*Corresponding author: gading@ukm.edu.my

Abstract

Composite polymer electrolytes based 49% poly(methyl methacrylate)-grafted natural rubber (MG49) incorporating lithium triflate (LiCF3SO3) were prepared. The study mainly focuses on the ionic conductivity performances and mechanical properties. Prior to that, carboxymethyl cellulose was synthesized from kenaf fiber. The films were characterized by electrochemical impedance (EIS) spectroscopy, linear sweep voltammetry (LSV), universal testing machine and scanning electron microscopy (SEM). The conductivity was found to increase with carboxymethyl cellulose loading. The highest conductivity value achieved was 6.5 × 10-6 Scm-1 upon addition of 6 wt% carboxymethyl cellulose. LSV graph shows the stability of this film was extended to 2.7 V at room temperature. The composition with 6 wt% carboxymethyl cellulose composition showed the highest tensile strength value of 7.9 MPa and 273 MPa of Young’s modulus. The morphology of the electrolytes showed a smooth surface of films after addition of salt and filler indicating amorphous phase in electrolytes system. Excellent mechanical properties and good ionic conductivity are obtained, enlightening that the film is suitable for future applications as thin solid polymer electrolytes in lithium batteries.

Keywords: carboxymethyl cellulose, ionic conductivity, mechanical properties, polymer electrolytes

Abstrak

Komposit polimer elekrolit berasaskan 49% poli(metil metakrilat)-cangkukan getah asli (MG49) dengan penambahan garam triflat (LiCF3SO3) telah disediakan. Kajian ini lebih menumpukan kepada ciri-ciri kekonduksian ion dan kekuaan sifat mekanik sistem elektolit yang dihasilkan. Sebelum itu, karboksimetil selulosa daripada kenaf disediakan terlebih dahulu. Filem yang dihasilkan dicirikan menggunakan spekroskopi impedans (EIS), voltametri sapuan linear (LSV), mesin pengujian universal dan mikroskopi imbasan elektron (SEM). Nilai kekonduksian ion didapati meningkat dengan penambahan karboksimetil selulosa. Kekonduksian ion tertinggi diperolehi dengan nilai 6 ×10-6 Scm-1 pada penambahan 6 bt% karboksimetil selulosa. Graf LSV menunjukkan kestabilan filem yang dihasilkan mencapai sehingga 2.7 V pada suhu bilik. 6 bt.% karboksimetil selulosa menunjukkan 7.9 MPa kekuatan regangan dan 273 MPa modulus young. Morpologi permukaan elektrolit mempamerkan permukaan lebih licin selepas penambahan garam dan pengisi yang menunjukkan kawasan amorfus pada sistem elektrolit. Kekuatan regangan dan kekonduksian ion memberansangkan yang diperolehi menunjukkan filem yang dihasilkan sesuai digunakan sebagai filem pepejal elektrolit polimer dalam bateri litium.

Kata kunci: karboksimetil selulosa, kekonduksian ion, sifat mekanik, polimer elektrolit
References

1. Su’ait, M. S., Ahmad, A. & Rahman, M. Y. A. (2009). Ionic Conductivity Studies of 49% poly(methyl methacrylate)-grafted Natural Rubber-based Solid Polymer Electrolytes.Ionics, 15 (4): 497 - 500.
2. Chiappone, A., Nair, J. R., Gerbaldi, C., Jabbour, L., Bongiovanni, R., Zeno, E., Beneventi, D. & Penazzi, N. (2011). Microfibrillated Cellulose as Reinforcement for Li-ion Battery Polymer Electrolytes with Excellent Mechanical Stability.Journal of Power Sources, 196: 10280 - 10288.
3. Alloin, F., D’Apreaa, A., Kissi, N. E., Dufresne, A. & Bossard, F. (2010). Nanocomposite Polymer Electrolyte Based on Whisker or Microfibrils Polyoxyethylene Nanocomposites.Electrochimica Acta, 55 (18): 5186 – 5194.

4. Adinugraha, M. P., Marseno, D. W. & Haryadi. (2005). Synthesis and Characterization of Sodium Carboxymethylcellulose from Cavendish Banana Pseudo Stem (Musa cavendishii LAMBERT).Carbohydrate Polymers, 62 (2): 164 - 169.
5. Mobarak, N. N., Ahmad, A., Abdullah, M. P., Ramli, N. & Rahman, M. Y. A. (2013). Conductivity Enhancement via Chemical Modification of Chitosan Based Green Polymer Electrolyte. Electrochimica Acta, 92: 161 - 167.
6. Yaacob, B., Mohd Amin, M. C. I., Hashim, K. & Abu Bakar, B. (2011). Optimization of Reaction Condition for Carboxymethylated Sago Starch.Iranian Polymer Journal, 20 (3): 195 - 204.
7. Kargarzadeh, H., Ahmad, I., Abdullah, I., Dufresne, A., Zainudin, S. Y. & Sheltami, R. M. (2012). Effects of Hydrolysis Conditions on the Morphology, Crystallinity, and Thermal Stability of Cellulose Nanocrystals Extracted from Kenaf Bast Fibers.Cellulose, 19 (13): 855 - 866.
8. Bono, A., Ying, P. H., Yan, F. Y., Muei, C. L., Sarbatly, R. & Krishnaiah, D. (2009). Synthesis and Characterization of Carboxymethyl Cellulose from Palm Kernel Cake.Advances in Natural & Applied Sciences, 3 (11): 5 - 11.
9. Low, S. P., Ahmad, A., Hamzah, H. & Rahman, M. Y. A. (2011). Nanocomposite Solid Polymeric electrolytes of 49% poly(methyl methacrylate)-grafted Natural Rubber-titanium Dioxide-lithium Tetrafluoroborate (MG49-TiO2-LiBF4).Journal of Solid State Electrochemistry, 15 (11-12): 2611 - 2618.
10. Chang H. P, Kim, D. W.,  Prakash, J. & Sun, Y. K. (2003). Electrochemical Stability and Conductivity Enhancement of Composite Polymer Electrolytes. Solid State Ionics, 159 (1-2): 111 - 119.
11. Azizi Samir, M. A. S., Mateos, A. M., Alloin, F., Sanchez, J. Y., and Dufresne, A. (2004). Plasticized Nanocomposite Polymer Blectrolytes based on Poly(oxyethylene) and Cellulose Whiskers.Electrochimica Acta, 49 (26): 4667 - 4677.

12. Nair, J. R., Chiapponea, A., Gerbaldia, C., Ijeri, V. S., Zenod, E., Bongiovannia, R., Bodoardoa, S. & Penazzia, N. (2011). Novel Cellulose Reinforcement for Polymer Electrolyte Membranes with Outstanding Mechanical Properties.Electrochimica Acta, 57: 104 - 111.
13. Nair, J. R., Gerbaldi, C., Chiappone, A., Zeno, E., Bongiovanni, R., Bodoardo, S. & Penazzi, N. (2009). UV-cured Polymer Electrolyte Membranes for Li-cells: Improved Mechanical Properties by a Novel Cellulose Reinforcement.Electrochemistry Communications, 11 (9): 1796 - 1798.
14. Schroers, M., Kokil, A., & Weder, C. (2004). Solid Polymer Electrolytes based on Nanocomposites of Ethylene oxide-epichlorohydrin Copolymers and Cellulose Whiskers.Journal of Applied Polymer Science, 93 (6): 2883 - 2888.
