
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 385 - 390

EFFECT OF FERMENTED CHITIN NANOWHISKERS ON PROPERTIES OF POLYLACTIC ACID BIOCOMPOSITE FILMS

(Kesan Kitin Terfermentasi Terhadap Sifat Filem Biokomposit Asid Poli Laktik)

Syazeven Effatin Azma Mohd Asri1, Zainoha Zakaria1*, Azman Hassan2,  M. K. Mohamad Haafiz2,3
1Department of Chemistry, Faculty of Science,

2Department of Polymer Engineering, Faculty of Chemical Engineering, 

Universiti Teknologi Malaysia 81310 Skudai, Johor, Malaysia

3School of Industrial Technology, 

Universiti Sains Malaysia, 11800 USM Penang, Malaysia

*Corresponding author: zainoha@kimia.fs.utm.my
Abstract

The fermented chitin nanowhiskers (FCNW) filled polylactic acid (PLA) biocomposite films were successfully produced using solution casting method. The biocomposite films were characterized in terms of tensile properties. The Young’s modulus increased with increasing FCNW content while the tensile strength increased and reached the maximum value at 4 phr FCNW loading. Therefore it can be concluded that the optimum loading of FCNW is at 4 phr and further addition of FCNW may lead to agglomeration resulting in a decrease in tensile strength. The elongation at break of the biocomposite films decreased rapidly upon addition of FCNW into PLA. From the Atomic Force Microscopy, the surface morphology of the PLA changed upon addition of FCNW and tendency for agglomeration of FCNW at high loading was observed.

Keywords: chitin, nanowhiskers, polylactide, film, solution casting

Abstrak

Kitin nanowisker daripada kitin terfermentasi (FCNW) yang memenuhi filem biokomposit asid poli laktik (PLA) telah berjaya dihasilkan melalui kaedah tuangan larutan. Filem biokomposit itu kemudiannya dicirikan berdasarkan sifat kekuatan tensilnya. Modulus Young meningkat seiring dengan peningkatan kandungan FCNW manakala kekuatan tensil meningkat dan mencapai nilai maksimum pada 4 phr. Oleh yang demikian, boleh disimpulkan bahawa pengisian optimum FCNW adalah pada 4 phr dan penambahan berterusan FCNW mungkin akan membawa kepada penggumpalan yang mengakibatkan penurunan dalam kekuatan tensil. Ciri pemanjangan takat putus filem biokomposit menurun secara mendadak dengan penambahan FCNW ke dalam PLA. Daripada mikroskop daya atom, morfologi permukaan PLA berubah setelah ditambah dengan FCNW dan potensi kepada penggumpalan pada pengisian tinggi FCNW telah diperhatikan.

Kata kunci: kitin, nanowisker, asid poli-laktik, filem, tuangan larutan
References
1. Yu, L. et al. (2006). Polymer Blends and Composites from Renewable resources. Progress in Polymer Science, 31: 576-602. 

2. Nampoothiri, K. M, Nair, N. R., & John, R. P. (2010). An overview of the recent developments in polylactide (PLA) research.  Bioresource Technology, 101: 8493-850.
3. Rizvi, R., Cochrane, B., Naguib, H & Lee, P.C. (2011). Fabrication and characterization of polylactide-chitin composites and their foams. Journal of Cellular Plastics 47: 283-300.
4. Chaussard, G. & Domard, A. (2004). New Aspects of the Extraction of Chitin from Squid Pens.  Biomacromolecules. 5, 559-564. 
5. Chandumpaia, A., Singhpibulpornb, N., Faroongsarngc, D. & Sornprasita, P. (2004). Preparation and physico-chemical characterization of chitin and chitosan from the pens of squid species. Loligo lessoniana and Loligo formosana, Carbohydrate Polymers. 58: 467-474.
6. Struszczyk, M.H. (2006). Global Requirements for Medical Applications of Chitin and its Derivatives.  Polish Chitin Society, Monograph XI, 95-102.
7. Rinaudo, M. (2006). Chitin and chitosan: Properties and applications. Progress in Polymer Science. 31: 603-632.
8. Nishino, T., Matsui, R. & Nakamae, K., (1999). Elastic Modulus of the crystalline regions of chitin and chitosan. J. Polymer Science Part B. 37: 1191-1196.
9. Nor, N.M., Zakaria, Z., Manaf, M.S.A. & Salleh, M.,M. (2011). The Effect of Partial Replacement of Dietary Fishmeal with Fermented Prawn Waste Liquor on Juvenile Sea Bass Growth.  Journal of Applied Aquaculture 23: 51-57.
10. Nair G.K., & Dufresne A. (2003). Crab Shell chitin whisker reinforced natural rubber nanocomposites. 1. Processing and Swelling Behavior Biomacromolecules, 4: 657-665.

11. Haafiz, M.K.M., Hassan, A., Zakaria, Z., Inuwa, I.M., Islam, M.S. & Jawaid, M. (2013). Properties of polylactic acid composites reinforced with oil palm biomass microcrystalline cellulose. Carbohydrate Polymer 98:139-145.
12. Cheng, Q., Wang, S., & Rials, T.G. (2009). Poly (vinyl alcohol) nanocomposites reinforced with cellulose fibrils isolated by high intensity ultrasonication. Composites: Part A, 40: 218-224.
13. Bulota, M., Vesterinen, A.H., Hughes, & Seppälä, J. (2013).  Mechanical Behavior, Structure, and Reinforcement Processes of TEMPO-Oxidized Cellulose Reinforced Poly(lactic) Acid.  Polymer Composites.  34:173-179.
14. Wang, Y., Cao, X. & Zhang, L. (2006).  Effects of Cellulose Whiskers on Properties of Soy Protein Thermoplastics.  Macromolecule Biosciences. 6: 524-531.
