
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 405 – 414

EFFECT OF REAGENTS CONCENTRATION AND RATIO ON DEGRADATION OF NATURAL RUBBER LATEX IN ACIDIC MEDIUM

(Kesan Kepekatan dan Nisbah Reagen ke Atas Pendegradasian Lateks Getah Asli dalam Media Berasid)

Suhawati Ibrahim*, Asrul Mustafa

Fine Chemicals and Biomaterials Programme,

 Bahagian Teknologi dan Kejuruteraan, 

Lembaga Getah Malaysia, 47000 Sungai Buloh, Selangor, Malaysia

*Corresponding author: suhawati@lgm.gov.my
Abstract

The molecular weight of natural rubber (NR) was reduced via degradation to liquid natural rubber (LNR) using hydrogen peroxide and sodium nitrite as reagents in latex solution. In this study, the reaction was carried out in an acidic medium at 70oC at various ratio and concentration of reagents. Results showed that the properties of degraded product i.e. LNR depends on the concentration and ratio of the reagents added into reaction mixtures. Increasing the concentration of hydrogen peroxide and sodium nitrite as reagents at 1 to 1 ratio efficiently reduced the molecular weight of LNR, but the gel content increased when reagents were added more than 0.2 mol. Hydrogen peroxide was found to have greater effect on degradation reaction compared to sodium nitrite when excessive amount of hydrogen peroxide showed further reduction in molecular weight of LNR. The degradation reaction also resulted in the formation of certain functional groups such as hydroxyl and carbonyl as shown from spectroscopy microstructure analysis.

Keywords: Liquid natural rubber (LNR), OH radical, redox reaction 

Abstrak

Berat molekul getah asli (NR) telah diturunkan secara pendegradasian kepada getah asli cecair (LNR) menggunakan hidrogen peroksida dan natrium nitrit sebagai reagen-reagen dalam lateks. Dalam kajian ini, tindak balas dilakukan dalam media berasid pada suhu 70oC pada nisbah dan kepekatan reagen yang berbeza. Keputusan menunjukkan bahawa sifat hasil pendegradasian iaitu LNR bergantung kepada kepekatan dan nisbah reagen yang digunakan semasa tindak balas. Penambahan kepekatan reagen pada nisbah 1:1 menurunkan berat molekul LNR dengan berkesan, tetapi kandungan gel meningkat bila kepekatan reagen lebih dari 0.2 mol digunakan. Hidrogen peroksida didapati memberikan pengaruh yang lebih besar ke atas tindak balas pendegradasian berbanding natrium nitrit bila berat molekul LNR terus menunjukkan penurunan bila jumlah berlebihan digunakan. Tindak balas pendegradasian juga menghasilkan kumpulan berfungsi yang tertentu seperti hidroksi dan karbonil seperti ditunjukkan dari analisa spektroskopi.

Kata kunci: Getah asli cecair (LNR), radikal OH, tindak balas redoks
References
1. Mathew V. S, Sinturel C, George S. C, & Thomas S (2010). Epoxy resin/liquid natural rubber system: Secondary phase separation and its impact on mechanical properties. J Mater Sci 45: 1769-1781. 

2. Wayakron Phetphaisit C, Bumee R, Namahoot J, Ruamcharoen J, & Ruamcharoen P (2012). Polyurethane polyester elastomer: Innovative environmental friendly wood adhesive from modified PETs and hydroxyl liquid natural rubber polyols. Int J Adhes Adhes 41: 127-131.

3. Dileep U, & Avirah S. A (2003). Studies on carboxy-terminated natural rubber in filled NR and NR latex vulcanizates. Iranian Polymer Journal (English Edition) 12: 441-448.

4. Abdullah I. (1992). Liquid natural rubber as a compatibilizer in the blending of natural rubber with polypropylene. Mater Forum 16: 353-357.

5. Ahmad S, Abdullah I, Sulaiman C. S, Kohjiya S, & Yoon J. R (1994). Natural rubber -HDPE blends with liquid natural rubber as a compatibilizer. I. Thermal and mechanical properties. J Appl Polym Sci 51: 1357-1363.

6. Srilathakutty R, Noushad V, Joseph R, & George K. E (1996). Studies on the properties of microcellular soles based on NBR/PVC blends. Polymer - Plastics Technology and Engineering 35: 97-119.

7. Dahlan H. M, Zaman M..D..K, & Ibrahim A. (2002). Liquid natural rubber (LNR) as a compatibiliser in NR/LLDPE blends - II: The effects of electron-beam (EB) irradiation. Radiat Phys Chem 64: 429-436.

8. Paul C. J, Gopinathan Nair M. R, Neelakantan N. R, Koshy P, Idage B. B, & Bhelhekar A. A (1998). Segmented block copolymers of natural rubber and 1, 3-butanediol-toluene diisocyanate oligomers. Polymer 39: 6861-6874.

9. Gopakumar S, & Gopinathan Nair M. R (2006). Natural rubber-polyurethane block copolymers: Nonlinear structural variations with NCO/OH ratio. Polym Eng Sci 46: 1812-1821.

10. Nair M. N. R, Sukumar P., Jayashree V, & Nair M. R. G (2010). Mechanical properties and fractography of block copolymers based on NR and MDI-based polyurethanes. Polymer Bulletin 65: 83-96.

11. Kébir N, Campistron I, Laguerre A, Pilard J, & Bunel C. (2011). New crosslinked polyurethane elastomers with various physical properties from natural rubber derivatives. J Appl Polym Sci 122: 1677-1687.

12. Saetung A, Kaenhin L, Klinpituksa P, Rungvichaniwat A, Tulyapitak T, Munleh S, Campistron I, & Pilard J (2012). Synthesis, characteristic, and properties of waterborne polyurethane based on natural rubber. J Appl Polym Sci 124: 2742-2752.

13. Kaenhin L, Klinpituksa P, Rungvichaniwat A, & Pilard J. F (2012). Waterborne polyurethane: Effect of functional groups in aromatic isocyanate and the chain length of hydroxyl terminated natural rubber. Advanced Materials Research 415-417: 2032-2035
14. Saetung A, Rungvichaniwat A, Campistron I, Klinpituksa P, Laguerre A, Phinyocheep P, & Pilard J. F (2010) Controlled degradation of natural rubber and modification of the obtained telechelic oligoisoprenes: Preliminary study of their potentiality as polyurethane foam precursors. J Appl Polym Sci 117: 1279-1289. 

15. Ravindran T, Nayar M..R..G, & Francis D. J (1988). Production of hydroxyl-terminated liquid natural rubber mechanism of photochemical depolymerization and hydroxylation. J Appl Polym Sci 35: 1227-1239.

16. Lemoine A. J (1988)  Production of Liquid Natural Rubber on a Pilot Scale. Proceedings of International Rubber Technology Conference  Kuala Lumpur
17. Gopakumar S, Paul C. J, & Gopinathan Nair M. R (2005) Segmented block copolymers of natural rubber and 1,4-butanediol-toluene diisocyanate oligomers. Materials Science- Poland 23: 227-245.

18. Maier G, Knopfova V, Voit B, Ly P. H, Dung B. T, & Thanh D. B (2004). Synthesis and characterization of segmented block copolymers based on hydroxyl-terminated liquid natural rubber and α,ω-diisocyanato telechelics. Macromolecular Materials and Engineering 289: 927-932.

19. Paul C. J, Nair M. R. G, Koshy P, & Idage B. B (1999). Segmented block copolymers of natural rubber and bisphenol A-toluene diisocyanate oligomers. J Appl Polym Sci 74: 706-721. 

20. Ha T. H, Nguyen T. N, Le Q. H, & Chu N. S (1996). Depolymerization of Natural Rubber Latex using Phenylhydrazine-FeCl2 System. Pure Applied Chemistry: 1923-1930.

21. Gazeley K. F, & Mente P. G (1990). Method for reducing the molecular weight of rubber latex. Malaysian Patent 1,00304-A
22. Phinyocheep P, Phetphaisit C. W, Derouet D, Campistron I, & Brosse J. C (2005) Chemical degradation of epoxidized natural rubber using periodic acid: Preparation of epoxidized liquid natural rubber. J Appl Polym Sci 95: 6-15.

23. Phetphaisit C. W, & Phinyocheep P (2003). Kinetics and Parameters Affecting Degradation of Purified Natural Rubber. J Appl Polym Sci 90: 3546-3555
24. Kodama S, Nishi K, & Furukawa M (2003). Preparation of low molecular weight natural rubber by ozonolysis of high ammonia latex. Journal of Rubber Research 6: 153-163
25. Suhawati I (2012). Preparation of Liquid natural rubber via chemical degradation of natural rubber latex and preparation of LNR-based polyurethane. MSc Thesis
26. Kébir N, Campistron I, Laguerre A, Pilard J, Bunel C, Couvercelle J-, & Gondard C (2005). Use of hydroxytelechelic cis-1,4-polyisoprene (HTPI) in the synthesis of polyurethanes (PUs). Part 1. Influence of molecular weight and chemical modification of HTPI on the mechanical and thermal properties of PUs. Polymer 46: 6869-6877
27. Sakdapipanich J. T, Suksawad P, Insom K, Kawahara S (2005). Preparation of functionalized low molecular weight natural rubber latex using solid nanometric TiO2 film as a photocatalyst. Rubber Chemistry and Technology 78: 597-605.

28. Pavia D. L, Lampman G. M, Kriz G. S, & Vyvyan J. A (2009) Introduction to Spectroscopy, 4th edn. Cengage Learning, Brooks/Cole
29. Halfpenny E, & Robinson P. L (1952) Pernitrous acid. The reaction between hydrogen peroxide and nitrous acid, and the properties of an intermediate product. Journal of the Chemical Society (Resumed): 928-938
30. Solanky S. S, & Singh R (2003) Functional and group determination in photo-degraded liquid rubbers. . Journal of Rubber Research 6: 1-11. 
