
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 415 - 422

SYNTHESIS OF CHITOSAN-GRAFTED-POLY(METHYL METHACRYLATE) WITH FENTON’S REAGENT (Fe2+ - H2O2) AS A REDOX INITIATOR

(Sintesis Kitosan-Cangkuk-Poli(Metil Metakrilat) Dengan Reagen Fenton (Fe2 + - H2O2) Sebagai Pemula Redoks)

Nur Azmyra Abdul Aziz*, Aznizam Abu Bakar, Azman Hassan, Nurulhusna Azmi 

Enhanced Polymer Research Group (ENPRO),

Department of Polymer Engineering, Faculty of Chemical Engineering,

Universiti Teknologi Malaysia, 81310 UTM Skudai, Johor, Malaysia.

*Corresponding author: azmyra_aziz@yahoo.com
Abstract

Graft copolymerization of poly(methyl methacrylate)(PMMA) onto chitosan fiber has been successfully carried out using Fenton’s Reagent which is consisted of hydrogen peroxide(H2O2) as initiator and ferrous ammonium sulphate(FAS) as co-catalyst under inert atmosphere in an aqueous medium. The PMMA homopolymer formed during the reaction was removed from the grafted copolymer by Soxhlet extraction using acetone as the solvent. The grafting percentage and efficiency obtained were 449.16% and 85.94%, respectively. The maximum grafting percentage and efficiency were achieved when 0.3 g chitosan copolymerized with 3 mL monomer at 70oC for 120 minutes with [FAS] = 6 x 10-5 M, [H2O2] = 6 x 10-3 M and 8 mL water. The grafted copolymers were characterized by using FTIR, DSC, TGA and SEM analysis. The presence of absorbance band at 1724 cm-1 provided strong evidence of grafting.

Keywords: graft copolymers, chitosan, monomers, radical polymerization

Abstrak

Pengkopolimeran cangkuk poli(metil metakrilat)(PMMA) terhadap gentian kitosan telah berjaya dilakukan dengan menggunakan Reagen Fenton yang terdiri daripada hidrogen peroksida (H2O2) sebagai pemula dan ferus ammonium sulfat (FAS) sebagai ko-mangkin pada persekitaran atmosfera lengai dalam medium berair. Homopolimer PMMA terbentuk semasa tindakbalas telah disingkirkan daripada kopolimer cangkuk melalui kaedah pengekstrakan Soxhlet dengan menggunakan aseton sebagai pelarut. Peratusan pencangkukan dan peratusan kecekapan pencangkukan yang diperolehi masing-masing ialah 449.16% dan 85.94%. Peratusan maksima pencangkukan dan kecekapan pencangkukan diperolehi apabila 0.3 g kitosan dikopolimer dengan 3 mL monomer pada 70oC selama 120 minit dengan mengunakan [FAS] = 6 x 10-5 M, [H2O2] = 6 x 10-3 M dan 8 ml air. Kopolimer tercangkuk telah dicirikan dengan menggunakan analisis FTIR, DSC, TGA dan SEM. Kehadiran kumpulan penyerapan pada 1724 cm-1 menunjukkan bukti kukuh berlakunya pencangkukan.

Kata kunci: kopolimer cangkuk, kitosan, monomer, radikal pempolimeran
References
1. Liu, Z., Wu, G. & Liu, Y. (2006). Graft copolymerization of methyl acrylate onto chitosan initiated by potassium diperiodatoargentate (III). Journal of Applied Polymer Science. 101 (1): 799-804.
2. Flores-Ramirez, N., Luna-Barcenas, G., Vasquez-Garcia, S., Munoz-Saldana, J., Elizalde-Pena, E., Gupta, R., Sanchez, I., Gonzalez-Hernandez, J., Garcia-Gaitan, B. & Villasenor-Ortega, F. (2008). Hybrid natural-synthetic chitosan resin: thermal and mechanical behavior. Journal of Biomaterials Science, Polymer Edition. 19 (2): 259-273.
3. Radhakumary, C., Nair, P. D., Mathew, S. & Nair, C. P. R. (2005). Biopolymer composite of chitosan and methyl methacrylate for medical applications. Trends Biomater. Artif. Organs. 18 (2): 117-124.
4. Bledzki, A. K., Reihmane, S. & Gassan, J. (1996). Properties and modification methods for vegetable fibers for natural fiber composites. Journal of Applied Polymer Science. 59 (8): 1329-1336.
5. Prashanth, K. V. H. & Tharanathan, R. N. (2003). Studies on graft copolymerization of chitosan with synthetic monomers. Carbohydrate Polymers. 54 (3): 343-351.
6. Gupta, K., Sahoo, S. & Khandekar, K. (2002). Graft copolymerization of ethyl acrylate onto cellulose using ceric ammonium nitrate as initiator in aqueous medium. Biomacromolecules. 3 (5): 1087-1094.
7. Lagos, A. & Reyes, J. (1988). Grafting onto chitosan. I. Graft copolymerization of methyl methacrylate onto chitosan with Fenton's reagent (Fe2+−H2O2) as a redox initiator. Journal of Polymer Science Part A: Polymer Chemistry. 26 (4): 985-991.
8. Prashanth, K. & Tharanathan, R. (2003). Studies on graft copolymerization of chitosan with synthetic monomers. Carbohydrate Polymers. 54 (3): 343-351.
9. Harish Prashanth, K., Lakshman, K., Shamala, T. & Tharanathan, R. (2005). Biodegradation of chitosan-graft-polymethylmethacrylate films. International Biodeterioration & Biodegradation. 56 (2): 115-120.
10. Abu Bakar, A., Nik Mat, N. S. & Isnin, M. K. (2008). Optimized conditions for the grafting reaction of poly (methyl methacrylate) onto oil-palm empty fruit bunch fibers. Journal of Applied Polymer Science. 110 (2): 847-855.
11. Das, R. K., Basu, D. & Banerjee, A. (1999). Study of methyl-methacrylate-viscose fiber graft copolymerization and the effect of grafting on thermal properties. Journal of Applied Polymer Science. 72 (1): 135-140.
