
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 434 - 443

MECHANICAL PROPERTIES OF STARCH FILLED POLYPROPYLENE UNDER EXPOSURE OF HYGROTHERMAL CONDITIONS

(Sifat-sifat Mekanikal Bagi Komposit Polipropilena Terisi Kanji di Bawah Pendedahan Higroterma)

Wan Zakaria Wan Nor*, Nor Azura Abdul Rahim, Hakimah Osman and Muthmirah Ibrahim
School of Materials Engineering, 

Universiti Malaysia Perlis, Kompleks Pengajian Jejawi, Jejawi 2, 02600 Arau, Perlis, Malaysia.

*Corresponding author: wanzakariawannor@gmail.com
Abstract

The hygrothermal properties of starch filled polypropylene (PP) composites with different types of starches; sago, tapioca, and corn content at 20 wt% were studied. The PP composites were compounded using Brabender Plasticoder machine and the composites samples were prepared through by compression molding technique. The hygrothermal absorption test was conducted out to investigate the moisture absorption at different temperatures (i.e. room temperature, 40°C and 70°C). Thus, the flexural test was carried out to study the effect of hygrothermal conditions on mechanical properties and scanning electron microscopy (SEM) used to verify the obtained results through morphological study. The results revealed that the mechanical properties of PP composites deteriorate after a period of immersion time and the hygrothermal aging of composites was accelerated as the temperature increased. 

Keywords: polypropylene composites, starch filled polypropylene, hygrothermal absorption, mechanical properties

Abstrak

Sifat-sifat higroterma bagi komposit polipropilena (PP) terisi kanji; sagu, ubi kayu, dan jagung yang terkandung 20% berat telah dikaji. Komposit-komposit PP telah disebatikan menggunakan mesin Brabender Plasticoder dan sampel-sampel komposit disediakan menggunakan teknik pengacuanan mampatan. Ujian penyerapan higroterma telah dijalankan untuk menyiasat kadar serapan lembapan pada beberapa suhu yang berbeza (suhu bilik, 40°C, dan 70°C). Seterusnya, ujian lenturan telah dijalankan untuk menkaji kesan keadaan higroterma ke atas sifat-sifat mekanikal dan mikroskopi pengimbasan electron (SEM) digunakan untuk mengesahkan keputusan yang diperolehi melalui kajian morfologi. Keputusan menunjukkan bahawa sifat-sifat mekanikal bagi komposit-komposit PP merosot selepas direndam untuk suatu tempoh masa dan kadar penuaan higroterma bagi komposit-komposit telah dipercepatkan apabila suhu meningkat.

Kata kunci: komposit polipropilena, polipropilena terisi kanji, serapan higroterma, sifat-sifat mekanikal
References

1. Potts, J., R. Clendinning, W. Ackart, and W. Niegisch. (1973), The Biodegradability of Synthetic Polymers. Springer. 61-79. US.

2. Gaffney, S. (2008). Corn Refiners Association 1. Journal of Agricultural & Food Information, 9 (2): 94-100.

3. Pedroso, A.G. and D.d.S. Rosa. (2005). Mechanical, thermal and morphological characterization of recycled LDPE/corn starch blends. Carbohydrate Polymers, 59 (1): 1-9.

4. Haque, M.M., M. Hasan, M.S. Islam, and M.E. Ali. (2009). Physico-mechanical properties of chemically treated palm and coir fiber reinforced polypropylene composites. Bioresource technology, 100 (20): 4903-4906.

5. Ramkumar, D., U. Vaidya, M. Bhattacharya, M. Hakkarainen, A.-C. Albertsson, and S. Karlsson. (1996). Properties of injection moulded starch/synthetic polymer blends—I. Effect of processing parameters on physical properties. European polymer journal, 32 (8): 999-1010.

6. Svensson, E. and A.-C. Eliasson. (1995). Crystalline changes in native wheat and potato starches at intermediate water levels during gelatinization. Carbohydrate Polymers, 26 (3): 171-176.

7. Liu, H., F. Xie, L. Yu, L. Chen, and L. Li. (2009). Thermal processing of starch-based polymers. Progress in Polymer Science, 34 (12): 1348-1368.

8. Zullo, R. and S. Iannace. (2009). The effects of different starch sources and plasticizers on film blowing of thermoplastic starch: Correlation among process, elongational properties and macromolecular structure. Carbohydrate Polymers, 77 (2): 376-383.

9. Guimarães, J., F. Wypych, C. Saul, L. Ramos, and K. Satyanarayana. (2010). Studies of the processing and characterization of corn starch and its composites with banana and sugarcane fibers from Brazil. Carbohydrate Polymers, 80 (1): 130-138.

10. Garg, S. and A.K. Jana. (2007). Studies on the properties and characteristics of starch–LDPE blend films using cross-linked, glycerol modified, cross-linked and glycerol modified starch. European polymer journal, 43 (9): 3976-3987.

11. Kim, M. and S.-J. Lee. (2002). Characteristics of crosslinked potato starch and starch-filled linear low-density polyethylene films. Carbohydrate Polymers, 50 (4): 331-337.

12. Kuniak, L. and R. Marchessault. (1972). Study of the crosslinking reaction between epichlorohydrin and starch. Starch‐Stärke, 24 (4): 110-116.

13. Delval, F., G. Crini, S. Bertini, C. Filiatre, and G. Torri. (2005). Preparation, characterization and sorption properties of crosslinked starch-based exchangers. Carbohydrate Polymers, 60 (1): 67-75.

14. Leman, Z., S. Sapuan, A. Saifol, M. Maleque, and M. Ahmad. (2008). Moisture absorption behavior of sugar palm fiber reinforced epoxy composites. Materials & Design, 29 (8): 1666-1670.

15. Berthé, V., L. Ferry, J. Bénézet, and A. Bergeret. (2010). Ageing of different biodegradable polyesters blends mechanical and hygrothermal behavior. Polymer Degradation and Stability, 95 (3): 262-269.

16. Haghighi-Yazdi, M., J.K. Tang, and P. Lee-Sullivan. (2011). Moisture uptake of a polycarbonate blend exposed to hygrothermal aging. Polymer Degradation and Stability, 96 (10): 1858-1865.

17. Mohd Ishak, Z. and J. Berry. (1994). Effect of moisture absorption on the dynamic mechanical properties of short carbon fiber reinforced nylon 6, 6. Polymer composites, 15 (3): 223-230.

18. Hu, R.-H., M.-y. Sun, and J.-K. Lim. (2010). Moisture absorption, tensile strength and microstructure evolution of short jute fiber/polylactide composite in hygrothermal environment. Materials & Design, 31 (7): 3167-3173.

19. Phua, Y., W. Chow, and Z. Mohd Ishak. (2011). The hydrolytic effect of moisture and hygrothermal aging on poly (butylene succinate)/organo-montmorillonite nanocomposites. Polymer Degradation and Stability, 96 (7): 1194-1203.

20. Boubakri, A., K. Elleuch, N. Guermazi, and H. Ayedi. (2009). Investigations on hygrothermal aging of thermoplastic polyurethane material. Materials & Design, 30 (10): 3958-3965.

21. Mohd Ishak, Z., U. Ishiaku, and J. Karger-Kocsis. (2000). Hygrothermal aging and fracture behavior of short-glass-fiber-reinforced rubber-toughened poly (butylene terephthalate) composites. Composites Science and technology, 60 (6): 803-815.

22. Duanmu, J., E.K. Gamstedt, and A. Rosling. (2007). Hygromechanical properties of composites of crosslinked allylglycidyl-ether modified starch reinforced by wood fibres. Composites Science and technology, 67 (15): 3090-3097.

23. Yew, G., A. Mohd Yusof, Z. Mohd Ishak, and U. Ishiaku. (2005). Water absorption and enzymatic degradation of poly (lactic acid)/rice starch composites. Polymer Degradation and Stability, 90 (3): 488-500.

24. Nielsen, L.E. (1974), Mechanical properties of polymers and composites. Vol. 2. Dekker New York

25. Preechawong, D., M. Peesan, P. Supaphol, and R. Rujiravanit. (2004). Characterization of starch/poly (ε-caprolactone) hybrid foams. Polymer testing, 23 (6): 651-657.

26. Thakore, I., S. Desai, B. Sarawade, and S. Devi. (2001). Studies on biodegradability, morphology and thermo-mechanical properties of LDPE/modified starch blends. European polymer journal, 37 (1): 151-160.

27. Wang, W., M. Sain, and P. Cooper. (2006). Study of moisture absorption in natural fiber plastic composites. Composites Science and technology, 66 (3): 379-386.

28. Ke, T., S.X. Sun, and P. Seib. (2003). Blending of poly (lactic acid) and starches containing varying amylose content. Journal of applied polymer science, 89 (13): 3639-3646.

29. Athijayamani, A., M. Thiruchitrambalam, U. Natarajan, and B. Pazhanivel. (2009). Effect of moisture absorption on the mechanical properties of randomly oriented natural fibers/polyester hybrid composite. Materials Science and Engineering: A, 517 (1): 344-353.

30. Mohd Ishak, Z., A. Ariffin, and R. Senawi. (2001). Effects of hygrothermal aging and a silane coupling agent on the tensile properties of injection molded short glass fiber reinforced poly (butylene terephthalate) composites. European polymer journal, 37 (8): 1635-1647.

31. Vlasveld, D., J. Groenewold, H. Bersee, and S. Picken. (2005). Moisture absorption in polyamide-6 silicate nanocomposites and its influence on the mechanical properties. Polymer, 46 (26): 12567-12576.

32. Huang, G. and H. Sun. (2007). Effect of water absorption on the mechanical properties of glass/polyester composites. Materials & Design, 28 (5): 1647-1650.
