
Malaysian Journal of Analytical Sciences Vol 18 No 2 (2014): 245 – 250

POTENTIAL OF PALM OLEIN AS GREEN LUBRICANT SOURCE: LUBRICATION ANALYSIS AND CHEMICAL CHARACTERISATION 

(Potensi Minyak Sawit Olein Sebagai Sumber Lubrikan Hijau: Analisis Pelinciran dan Pencirian Kimia)

Darfizzi Derawi* and Jumat Salimon
School of Chemical Sciences and Food Technology, 

Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 Bangi, Selangor, Malaysia

*Corresponding author: darfizzi@ukm.edu.my
Abstract

Palm olein (POo) is widely used as edible oil in tropical countries. The lubrication properties and chemical compositions of POo being considered to be used as renewable raw material for biolubricant synthesis. POo is suitable to be used directly as biolubricant for medium temperature industrial applications. Palm olein has good viscosity index, oxidative stability, flash and fire point as a lubricant source. POo contains unsaturated triacylglycerols (TAG): Palmitin-Olein-Olein, POO (33.3 %), Palmitin-Olein-Palmitin, POP (29.6 %), which are very important to produce good lubricant properties. This unsaturated bond is preferable in chemical modification to produce biolubricant. The chemical compositions of POo were tested by using high performance liquid chromatography (HPLC) and gas chromatography (GC) techniques. 
Keywords: Palm olein, Renewable Source, Lubrication Analysis, Biolubricant 
Abstrak

Minyak sawit olein (POo) digunakan secara meluas sebagai minyak masak  bagi negara-negara beriklim tropika. Sifat-sifat pelinciran dan komposisi kimia POo dinilai untuk digunakan sebagai bahan mentah dalam sintesis biolubrikan. POo sesuai digunakan secara terus sebagai biolubrikan untuk aplikasi industri bersuhu sederhana. Minyak sawit olein adalah baik sebagai sumber lubrikan berdasarkan indeks kelikatan, kestabilan oksidatif, takat kilat dan api. POo mengandungi triasilgliserida tak tepu (TAG): POO (33.3 %), POP (29.6 %) iaitu sangat pnting untuk menghasilkan  sifat-sifat lubrikan yang baik. Ikatan tak tepu diperlukan dalam modifikasi kimia untuk menghasilkan biolubrikan. Komposisi kimia POo diuji menggunakan teknik kromatografi cecair berprestasi tinggi (HPLC) dan kromatografi gas (GC). 

Kata kunci: Minyak Sawit Olein, Sumber Boleh Diperbaharui, Analisisi Pelinciran, Biolubrikan
References
1. Derawi, D. & Salimon, J. (2010). Optimization on Epoxidation of Palm Olein by Using Performic Acid.E-Journal of Chemistry, 7 (4): 1440 – 1448.
2. Gunsotne, F. D. (2004). The Chemistry of Oils and Fats, Sources, Composition, Properties and Uses, Blackwell Publishing Ltd., UK.

3. Gunstone, F. D. & Padley, F. B. (1997). Lipid Technologies and Applications, Marcel Dekker, Inc., New York.

4. O’Brien, R. D. (1998). Fats and Oils: Formulating and Processing for Applications, Technomic Publishing AG., Switzerland.

5. Gunstone, F. D., Harwood, J. L. & Padley, F. B. (1994). The Lipid Handbook, 2nd ed. Chapman & Hall, UK.

6. Salimon, J., Said, M., Ramli, S. & Mat Lazim, M. A. S. (2006). Oils and Fats Analysis, Penerbit UKM, Bangi.

7. Emery (1983). Emery Analytical Testing Procedures, Emery Industries, USA.

8. Salih, N. Salimon, J. Yousif E. & Abdullah, B. M. (2013). Biolubricant basestocks from chemically modified plant oils: ricinoleic acid based-tetraesters, Chemistry Central Journal, 7 (128).
9. Salimon, J. Abdullah, B.M. & Salih, N. (2012). Diesters biolubricant base oils: synthesis, optimization, characterization and physicochemical characteristics, International Journal of Chemical Engineering, Article ID 896598.
10. Stachowiak, G. W. & Batchelor, A. W. (2005). Engineering Tribology, 3rd ed. Elsevier Inc., UK.

11. ISO 3448 (1975). International Standard, Industrial Liquid Lubricants, ISO Viscosity Classification. ISO International Standards, US.
12. Ramli, M. R., Siew, W. L. & Cheah, K. Y. (2008). Properties of high-oleic palm oils derived by fractional crystallization. Journal of Food Science, 73 (3): 1750 – 3841.

13. Uniqema (2006). Oleochemical Ester Base Fluids for European Eco-label Compliant Lubricant Formulations, Uniqema Inc, USA.

14. Hironaka, S. (1984). Boundary Lubrication and Lubricants, Three Bond Co. Ltd., Japan.
