The Malaysian Journal of Analytical Sciences, Vol 18 No 3 (2014): 522 - 526
Azlin et al:  Synthesis of Nanocrystalline Olivine LiNiPO4 Powder Prepared by Sol-Gel Method: Thermal Analysis and XRD Studies

[image: image1.png]



Synthesis of Nanocrystalline Olivine LiNiPO4
Powder Prepared by Sol-Gel Method: Thermal Analysis and XRD Studies

(Penyediaan Serbuk Nanokristal LiNiPO4 dengan Struktur Olivin Melalui Kaedah Sol-Gel: Analisis Terma dan Kajian XRD)
Azlin Sanusi1,2,3*, Shanti Navaratnam2,3, Wan Jeffrey Basirun4
1INTEC Education College, 
Jalan Senangin Satu 17/2A, Seksyen 17, 40200 Shah Alam, Selangor, Malaysia

2Faculty of Applied Sciences,
 3Institue of Science, 
Universiti Teknologi Mara,40450 Shah Alam , Selangor Malaysia

4Chemistry Department, Faculty of Science, 
University of Malaya,50732 Kuala Lumpur, Malaysia

*Corresponding author: azlin457@salam.uitm.edu.my
Abstract

LiMPO4 have attracted much attention as potential cathode material as it does not liberate oxygen on decomposition unlike lithium transition metal oxides (LMO). In this work, LiNiPO4  powder was prepared by sol gel method using  LiOH, Ni(CH3COO)2, NH4H2(PO4) and  tartaric acid  as chelating agent .The precursor powders were studied by thermogravimetric analysis (TGA). Based on the TGA results, the sample was calcined at 1000oC in air. The TGA/DTGA studies have been employed to analyse the reaction of raw materials during the formation of LiNiPO4 .The formation mechanism for the synthesis of LiNiPO4  and the overall decomposition equation for the precursor were proposed from the TGA/DTGA analysis. The calculated total weight loss from the overall proposed decomposition process which is 66.4% shows agreement with the percentage weight loss from the TGA curves which is 68%.  The X-ray diffraction analysis was carried out to confirm the formation of LiNiPO4. The precursors and the calcined powders were characterized by X-ray diffraction (XRD). Analysis of the synthesized LiNiPO4 using XRD demonstrated the formation of a pure LiNiPO4 phase powder. 

Keywords: lithium nickel phosphate, sol-gel, mechanism

Abstrak

LiMPO4  telah menarik banyak minat terhadap potensinya sebagai bahah katod untuk bateri litium. kerana tidak seperti  litium oksida logam peralihan (LMO) bahan ini tidak melepaskan oksigen ketika proses penguraian. Didalam kajian ini LiNiPO4 telah disintisis dengan mencampurkan LiOH, Ni(CH3COO)2, NH4H2(PO4) dan asid tartarik  dengan menggunakan kaedah sol-gel. Analisis TGA telah dilakukan keatas prapenanda LiNiPO4 untuk menetukan suhu pembakaran dan didapati suhu yang sesuai adalah 10000C. Unjuran persamaan bagi penguraian prapenanda LiNiPO4 telah diperolehi dengan menggunakan lekok TGA/DTGA. Pengiraan peratus penurunan berat menggunakan persamaan unjuran (66.4%) dan lekok TGA (68%) adalah hampir sama. Spektrum belauan sinar –X (XRD) menunjukkan bahan sampel LiNiPO4 adalah tulin. 

Kata kunci: litium nikel fosfat, kaedah sol-gel, mekanisme

Introduction

In recent years, lithium metal phosphate (LiMPO4) with the olivine structure has received a lot of attention to be a potential candidate for cathode materials in lithium ion batteries [1-4]. Unlike lithium transition metal oxides (LMO), LiMPO4 does not liberate oxygen on decomposition. In addition, LiMPO4 is cheaper, benign, and environmentally friendly and has greater stability than LMO. Various methods have been used to synthesize LiMPO4 cathode material such as solid-state [1], sol-gel [2-4], hydrothermal [5-7] and aqueous precipitation [8].  Many of the sol-gel method reported used citric acid as chelating agent and argon or nitrogen ambient during calcinations of precursor powders.

This paper reports the synthesis and characterization of LiNiPO4 (lithium nickel phosphate) which belongs to the olivine structure. In this work, LiNiPO4 was prepared by the sol-gel method with tartaric acid and calcined in air. Sol-gel has considerable advantages of good mixing of the starting materials and good chemical homogeneity of the product. To the best of our knowledge, reports on LiMnPO4 nanocrystalline structured powders prepared by tartaric acid and calcined in air are rare.

The resulting LiNiPO4 powders obtained were then characterized by thermogravimetric analysis (TGA),) and X-ray diffraction (XRD). The formation mechanism for the synthesis of LiNiPO4 are also discussed in this paper.

Materials and Methods

Sample preparation

Stoichiometric amounts of lithium hydroxide (LiOH.H2O, Ajax), nickel acetate (Ni(CH3COO)2 .4H2O, Ajax) and ammonium dihydrogen phosphate NH4H2PO4(AR grade) were weighed and dissolved in distilled and deionised  water separately with 1:1:1 mole ratio. The aqueous solutions were mixed together and stirred constantly. A 1.0 M tartaric acid solution was slowly added to the mixture as the chelating agent.  Ammonium hydroxide was added carefully into the mixture until a pH value of 5-7 was achieved. The mixtures were mixed and stirred thoroughly until a greenish gel was obtained. The gels were left for drying in an oven at 600C  for 3 days. 

Characterization of sample synthesized

Thermogravimetric analysis (TGA) and differential thernogravimetric analysis (DTGA) analysis of the LiNiPO4 powders were performed in order to examine the thermal decomposition behaviour of the gel precursor. The heating rate was 100C min-1and the precursor was heated at 300C-10000C in nitrogen atmosphere. 

The structure and phase of the product was identified by X-ray powder diffraction (XRD) analysis. The measurements were made with Siemens D5000 X-ray diffractometer with CuKα radiation at room temperature.
Results and Discussion

The TGA/DTGA analysis of the greenish gel obtained in this work is shown in Fig 1. The TGA thermogram of the precursors revealed that there are four significant weight loss regions as shown in Figure 1. A weight loss about 1.1 % ocurred slowly as the temperature was increased to about 150 oC, due to the  evaporation of residual water  which are still present in the sample. Rapid weight loss occurred around the temperature range between 150 oC -275 oC and  is associated with a 34.1 % weight loss. The decomposition process is attributed to the decomposition of unreacted ammonium dihydrogen phosphate as it was one of the reactant materials in the sample. The removal of tartaric acid is also assigned to this region. The weight loss is also due to the decomposition of the Li-Ni acetate gel formed in the experiment. The decomposition process of the precursor is also accompanied by a sharp peak at about  237 oC as seen  on the DTGA thermogram in Figure 1. The peak is probably due to the decomposition of ammonium dihydrogen phosphate which is an endothermic process. 
The third weight loss occurred at the temperature range from 275 to 325 oC. This decomposition was associated with a weight loss of 8.8 % and can be attributed to the burning out of organic residues which resulted from the Li-Ni acetate complex decomposition. The final decomposition step which is associated with 23.9 % weight loss occurred in the temperature range from 325 oC to 725 oC. The weight loss is attributed to the decomposition of nickel acetate and lithium hydroxide. Nickel acetate steadily decomposed in the temperature range from 272 oC to 400 oC . 

The DTGA thermogram reveals a sharp peak at 354 oC indicating the rapid decomposition of  nickel acetate. The weight is constant after 725 oC indicating that no heat is used for evaporation or decomposition processes and that LiNiPO4 can be obtained by firing the precursor at temperatures above 750 oC. The tartaric acid is likely to act as a fuel in the pyrolysis and expedite the process of decomposition of acetate ions .The corresponding weight loss, temperature ranges and their assignment are summarized in Table 1.
[image: image2.emf]0

20

40

60

80

100

120

30 230 430 630 830

Temperature (

o

C)

Weight loss (%)

-3

-2.5

-2

-1.5

-1

-0.5

0

0.5

First derivative % C

-1

TGA

DTGA

275

729

150

325

1 st weight loss (1.1%)

4 th weight loss (23.9%)

3rd weight loss (8.8%)

2nd weight loss (34.1%)


Figure 1. TG-DTGA curves of the precursor

Table1. TG/DTGA results of the LiNiPO4 precursor

	Sample
	Temperature range
	Weight loss(%)
	Assignment

	LiNiPO4 from LiOH, Ni(CH3COO)2 and (NH4)H2PO4 with tartaric acid.
	30-150
	1.1
	Evaporation of absorbed water.

	
	150-275
	34.1
	Decomposition of (NH4)H2PO4 and evaporation of tartaric acid. Li-Ni acetate gel(precursor) decomposition

	
	275-325
	8.8
	Burning out organic residues resulted from the complex decomposition 

	
	325-725
	23.9
	Decomposition of Ni(CH3COO)2. and LiOH. Structural OH bond broken 

	
	725-900
	-
	Formation of LiNiPO4

	Total weight loss
	
	67.9
	


The reaction mechanism for the synthesis of LiNiPO4 has been proposed as shown below.     When tartaric acid (C4H6O6) was added to the mixture, it reacted with (NH4)H2PO4 and LiOH according to the following equations:
	2(NH4)H2PO4
	+
	C4H6O6
	→
	H3PO4
	+
	H 2PO4 -  
	+
	( (NH4)2C4H5O6) ) +           
	 (1)



	LiOH
	+
	C4H6O6
	→
	Li(C4H5O6)
	+
	H2O
	
	  
	 (2)




LiOH also reacted with H3PO4 produced in equation (1) according to the following,

	 LiOH
	+
	H3PO4
	→
	LiH2PO4  
	+
	H2O
	
	
	(3)




On heating,

	2(Ni(CH3COO)2)
	+
	2 C4H6O6  
	+  
	8O 2                    
	→
	2(Ni C4H4O6 )  
	+
	8CO2
	+
	8H2O  
	(4)




and

	H 2PO4 -
	+
	((NH4) 2C4H5O6)+
	+
	C4H6O6
	+
	C4H6O6
	+
	[image: image4.png]*/



 O2
	→
	
	(5)


	((H 2PO4 )(NH4) 2C4H5O6 ) 
	+
	4CO2
	+
	3H2O
	
	
	
	
	
	
	


 Therefore overall reaction is given as,
	2(NH4) H2PO4  
	+
	2LiOH
	+
	(Ni(CH3COO)2)
	+
	5C4H6O6
	+
	[image: image6.png]


 O2
	→
	
	(6)


	LiH 2PO4  
	+
	Li(C4H5O6)
	+
	((H 2PO4 )(NH4) 2C4H5O6 )
	+
	2(NiC4H4O6)  
	+

	12CO2  
	+
	13H2O     


Equation (6) suggests that the dried gel precursor is composed of  Li((H2PO4 )2(NH4) 2C4H5O6)  LiC4H5O6 . (NiC4H4O6 )2

Therefore the overall proposed decomposition equation for the precursor in air atmosphere i.e. during firing is,    

	Li((H2PO4)2(NH4) 2C4H5O6)  Li C4H5O6 . (Ni C4H4O6 )2  
	+
	10O2
	→


	(7)

	2LiNiPO4
	+
	16CO2
	+
	12H2O 
	+
	2NH3


Based on equation (7), the percentage weight loss is 66.4 %.The total weight loss of the decomposition process from the TGA curves as shown in Table 1 is 67.9 % which agrees closely with the calculated values based on Equation (7). The discrepancy could be due to the absorbed water from the ambient.


[image: image7.png]o
S
R

o
S
=]

o o o
g8 8 8
8 ¢ R
(ne) Aysuayu

o
S
S

o
3

IS

15 20 25 30 35 40 45 50 55 60
2 8(degrees)

10





Figure 2. XRD Patterns of the LiNiPO4 sample                                           

The XRD pattern of the sample fired at 1000 o C for 24 hours exhibits the characteristic diffraction lines of LiNiPO4 without any impurities and matches the orthorhombic structure listed in JCPDS pattern number 32-0578. The XRD of this sample also agrees with the results of Ruffo and co-workers (2005). The above observations confirmed that a pure compound of LiNiPO4 was successfully synthesized in the present work. 
The crystallite size (L) was estimated using the conventional Scherrer equation below.

	           [image: image8.png]_ 084
= Bcoso





	  (8)


Here ( is the X-ray wavelength 1.5406 Å and Br is the FWHM of the peak representing the (111) plane. The full width at half maximum (FWHM) of the (111) reflection plane was determined since the peak at 2( =25.9 0 has the highest intensity. The average crystallite size of the prepared pure LiNiPO4 is 66 nm.  
Conclusion

The olivine LiNiPO4 powders were successfully synthesized by the sol-gel method with tartaric acid as the chelating agent. TGA/DTGA results showed that the LiNiPO4 powders can be obtained by calcining the precursor at temperature above 750oC. The sample prepared at 1000oC showed that the position of peaks and the variation in intensity matches the pattern shown in the standard JCPDS data.  The weight loss obtained from the thermogram supports the mechanism of reactions proposed. The percentage weight loss is 66.4 % while the total weight loss of the decomposition process from the TGA curves is 67.9 % which agrees closely with the calculated values based on the proposed equation. By using information obtained from the FWHM, the crystallite size of the LiNiPO4 is ~ 66 nm.
References

1. Liu, H., Li C., Zhang, H. P., Fu, L. Wu, Y. P., and H.Q. Wu (2006). Kinetic study on LiFePO4/C nanocomposites synthesized by solid state technique, Journal Power Sources 159: 717-720.

2. Kuei-Feng H., Sun-Yuan T. and Bing-Joe H., (2005). Physical and electrochemical properties of LiFePO4/carbon composite synthesized at various pyrolysis periods, Journal Power Sources 146: 529-533.

3. Piana, M., Cushing, B. L., Goodenough, J. B. and Penazzi, N. (2004). A new promising sol–gel synthesis of phospho-olivines as environmentally friendly cathode materials for Li-ion cells, Solid State Ion. 175: 233-237.

4. Jingsi Y. and Jun John X, (2004). Nonaqueous Sol-Gel Synthesis of High-Performance LiFePO4. Electrochem. Solid-State Lett. 7: 515-A518.

5. Jaewon L., and Amy S. T. (2006). Synthesis of LiFePO4 Micro and Nanoparticles in Supercritical Water, Mater Lett, 60: 2105-109.

6. Jiajun C. and M Stanley W. (2006). Hydrothermal synthesis of lithium iron phosphate, Electrochemistry Communications 8: 855-858.

7. Shigehisa T., Yosuke I., Kazuyoshi U., Kenji T., Mineo S. (2004) Enhanced electrochemical performance of LiFePO4 prepared by hydrothermal reaction, Solid State Ion. 175: 287-290.

8. Arnold, G. Garche, J., Hemmer, R., Strobe, S., Volgler, C., and Wohlfart-Mehrens M. (2003). Fine-particle lithium iron phosphate LiFePO4 synthesized by a new low-cost aqueous precipitation technique, Journal Power Sources 119-121:247-251.
526
525

_1477382374.xls
Chart1

		10

		10.02

		10.04

		10.06

		10.08

		10.1

		10.12

		10.14

		10.16

		10.18

		10.2

		10.22

		10.24

		10.26

		10.28

		10.3

		10.32

		10.34

		10.36

		10.38

		10.4

		10.42

		10.44

		10.46

		10.48

		10.5

		10.52

		10.54

		10.56

		10.58

		10.6

		10.62

		10.64

		10.66

		10.68

		10.7

		10.72

		10.74

		10.76

		10.78

		10.8

		10.82

		10.84

		10.86

		10.88

		10.9

		10.92

		10.94

		10.96

		10.98

		11

		11.02

		11.04

		11.06

		11.08

		11.1

		11.12

		11.14

		11.16

		11.18

		11.2

		11.22

		11.24

		11.26

		11.28

		11.3

		11.32

		11.34

		11.36

		11.38

		11.4

		11.42

		11.44

		11.46

		11.48

		11.5

		11.52

		11.54

		11.56

		11.58

		11.6

		11.62

		11.64

		11.66

		11.68

		11.7

		11.72

		11.74

		11.76

		11.78

		11.8

		11.82

		11.84

		11.86

		11.88

		11.9

		11.92

		11.94

		11.96

		11.98

		12

		12.02

		12.04

		12.06

		12.08

		12.1

		12.12

		12.14

		12.16

		12.18

		12.2

		12.22

		12.24

		12.26

		12.28

		12.3

		12.32

		12.34

		12.36

		12.38

		12.4

		12.42

		12.44

		12.46

		12.48

		12.5

		12.52

		12.54

		12.56

		12.58

		12.6

		12.62

		12.64

		12.66

		12.68

		12.7

		12.72

		12.74

		12.76

		12.78

		12.8

		12.82

		12.84

		12.86

		12.88

		12.9

		12.92

		12.94

		12.96

		12.98

		13

		13.02

		13.04

		13.06

		13.08

		13.1

		13.12

		13.14

		13.16

		13.18

		13.2

		13.22

		13.24

		13.26

		13.28

		13.3

		13.32

		13.34

		13.36

		13.38

		13.4

		13.42

		13.44

		13.46

		13.48

		13.5

		13.52

		13.54

		13.56

		13.58

		13.6

		13.62

		13.64

		13.66

		13.68

		13.7

		13.72

		13.74

		13.76

		13.78

		13.8

		13.82

		13.84

		13.86

		13.88

		13.9

		13.92

		13.94

		13.96

		13.98

		14

		14.02

		14.04

		14.06

		14.08

		14.1

		14.12

		14.14

		14.16

		14.18

		14.2

		14.22

		14.24

		14.26

		14.28

		14.3

		14.32

		14.34

		14.36

		14.38

		14.4

		14.42

		14.44

		14.46

		14.48

		14.5

		14.52

		14.54

		14.56

		14.58

		14.6

		14.62

		14.64

		14.66

		14.68

		14.7

		14.72

		14.74

		14.76

		14.78

		14.8

		14.82

		14.84

		14.86

		14.88

		14.9

		14.92

		14.94

		14.96

		14.98

		15

		15.02

		15.04

		15.06

		15.08

		15.1

		15.12

		15.14

		15.16

		15.18

		15.2

		15.22

		15.24

		15.26

		15.28

		15.3

		15.32

		15.34

		15.36

		15.38

		15.4

		15.42

		15.44

		15.46

		15.48

		15.5

		15.52

		15.54

		15.56

		15.58

		15.6

		15.62

		15.64

		15.66

		15.68

		15.7

		15.72

		15.74

		15.76

		15.78

		15.8

		15.82

		15.84

		15.86

		15.88

		15.9

		15.92

		15.94

		15.96

		15.98

		16

		16.02

		16.04

		16.06

		16.08

		16.1

		16.12

		16.14

		16.16

		16.18

		16.2

		16.22

		16.24

		16.26

		16.28

		16.3

		16.32

		16.34

		16.36

		16.38

		16.4

		16.42

		16.44

		16.46

		16.48

		16.5

		16.52

		16.54

		16.56

		16.58

		16.6

		16.62

		16.64

		16.66

		16.68

		16.7

		16.72

		16.74

		16.76

		16.78

		16.8

		16.82

		16.84

		16.86

		16.88

		16.9

		16.92

		16.94

		16.96

		16.98

		17

		17.02

		17.04

		17.06

		17.08

		17.1

		17.12

		17.14

		17.16

		17.18

		17.2

		17.22

		17.24

		17.26

		17.28

		17.3

		17.32

		17.34

		17.36

		17.38

		17.4

		17.42

		17.44

		17.46

		17.48

		17.5

		17.52

		17.54

		17.56

		17.58

		17.6

		17.62

		17.64

		17.66

		17.68

		17.7

		17.72

		17.74

		17.76

		17.78

		17.8

		17.82

		17.84

		17.86

		17.88

		17.9

		17.92

		17.94

		17.96

		17.98

		18

		18.02

		18.04

		18.06

		18.08

		18.1

		18.12

		18.14

		18.16

		18.18

		18.2

		18.22

		18.24

		18.26

		18.28

		18.3

		18.32

		18.34

		18.36

		18.38

		18.4

		18.42

		18.44

		18.46

		18.48

		18.5

		18.52

		18.54

		18.56

		18.58

		18.6

		18.62

		18.64

		18.66

		18.68

		18.7

		18.72

		18.74

		18.76

		18.78

		18.8

		18.82

		18.84

		18.86

		18.88

		18.9

		18.92

		18.94

		18.96

		18.98

		19

		19.02

		19.04

		19.06

		19.08

		19.1

		19.12

		19.14

		19.16

		19.18

		19.2

		19.22

		19.24

		19.26

		19.28

		19.3

		19.32

		19.34

		19.36

		19.38

		19.4

		19.42

		19.44

		19.46

		19.48

		19.5

		19.52

		19.54

		19.56

		19.58

		19.6

		19.62

		19.64

		19.66

		19.68

		19.7

		19.72

		19.74

		19.76

		19.78

		19.8

		19.82

		19.84

		19.86

		19.88

		19.9

		19.92

		19.94

		19.96

		19.98

		20

		20.02

		20.04

		20.06

		20.08

		20.1

		20.12

		20.14

		20.16

		20.18

		20.2

		20.22

		20.24

		20.26

		20.28

		20.3

		20.32

		20.34

		20.36

		20.38

		20.4

		20.42

		20.44

		20.46

		20.48

		20.5

		20.52

		20.54

		20.56

		20.58

		20.6

		20.62

		20.64

		20.66

		20.68

		20.7

		20.72

		20.74

		20.76

		20.78

		20.8

		20.82

		20.84

		20.86

		20.88

		20.9

		20.92

		20.94

		20.96

		20.98

		21

		21.02

		21.04

		21.06

		21.08

		21.1

		21.12

		21.14

		21.16

		21.18

		21.2

		21.22

		21.24

		21.26

		21.28

		21.3

		21.32

		21.34

		21.36

		21.38

		21.4

		21.42

		21.44

		21.46

		21.48

		21.5

		21.52

		21.54

		21.56

		21.58

		21.6

		21.62

		21.64

		21.66

		21.68

		21.7

		21.72

		21.74

		21.76

		21.78

		21.8

		21.82

		21.84

		21.86

		21.88

		21.9

		21.92

		21.94

		21.96

		21.98

		22

		22.02

		22.04

		22.06

		22.08

		22.1

		22.12

		22.14

		22.16

		22.18

		22.2

		22.22

		22.24

		22.26

		22.28

		22.3

		22.32

		22.34

		22.36

		22.38

		22.4

		22.42

		22.44

		22.46

		22.48

		22.5

		22.52

		22.54

		22.56

		22.58

		22.6

		22.62

		22.64

		22.66

		22.68

		22.7

		22.72

		22.74

		22.76

		22.78

		22.8

		22.82

		22.84

		22.86

		22.88

		22.9

		22.92

		22.94

		22.96

		22.98

		23

		23.02

		23.04

		23.06

		23.08

		23.1

		23.12

		23.14

		23.16

		23.18

		23.2

		23.22

		23.24

		23.26

		23.28

		23.3

		23.32

		23.34

		23.36

		23.38

		23.4

		23.42

		23.44

		23.46

		23.48

		23.5

		23.52

		23.54

		23.56

		23.58

		23.6

		23.62

		23.64

		23.66

		23.68

		23.7

		23.72

		23.74

		23.76

		23.78

		23.8

		23.82

		23.84

		23.86

		23.88

		23.9

		23.92

		23.94

		23.96

		23.98

		24

		24.02

		24.04

		24.06

		24.08

		24.1

		24.12

		24.14

		24.16

		24.18

		24.2

		24.22

		24.24

		24.26

		24.28

		24.3

		24.32

		24.34

		24.36

		24.38

		24.4

		24.42

		24.44

		24.46

		24.48

		24.5

		24.52

		24.54

		24.56

		24.58

		24.6

		24.62

		24.64

		24.66

		24.68

		24.7

		24.72

		24.74

		24.76

		24.78

		24.8

		24.82

		24.84

		24.86

		24.88

		24.9

		24.92

		24.94

		24.96

		24.98

		25

		25.02

		25.04

		25.06

		25.08

		25.1

		25.12

		25.14

		25.16

		25.18

		25.2

		25.22

		25.24

		25.26

		25.28

		25.3

		25.32

		25.34

		25.36

		25.38

		25.4

		25.42

		25.44

		25.46

		25.48

		25.5

		25.52

		25.54

		25.56

		25.58

		25.6

		25.62

		25.64

		25.66

		25.68

		25.7

		25.72

		25.74

		25.76

		25.78

		25.8

		25.82

		25.84

		25.86

		25.88

		25.9

		25.92

		25.94

		25.96

		25.98

		26

		26.02

		26.04

		26.06

		26.08

		26.1

		26.12

		26.14

		26.16

		26.18

		26.2

		26.22

		26.24

		26.26

		26.28

		26.3

		26.32

		26.34

		26.36

		26.38

		26.4

		26.42

		26.44

		26.46

		26.48

		26.5

		26.52

		26.54

		26.56

		26.58

		26.6

		26.62

		26.64

		26.66

		26.68

		26.7

		26.72

		26.74

		26.76

		26.78

		26.8

		26.82

		26.84

		26.86

		26.88

		26.9

		26.92

		26.94

		26.96

		26.98

		27

		27.02

		27.04

		27.06

		27.08

		27.1

		27.12

		27.14

		27.16

		27.18

		27.2

		27.22

		27.24

		27.26

		27.28

		27.3

		27.32

		27.34

		27.36

		27.38

		27.4

		27.42

		27.44

		27.46

		27.48

		27.5

		27.52

		27.54

		27.56

		27.58

		27.6

		27.62

		27.64

		27.66

		27.68

		27.7

		27.72

		27.74

		27.76

		27.78

		27.8

		27.82

		27.84

		27.86

		27.88

		27.9

		27.92

		27.94

		27.96

		27.98

		28

		28.02

		28.04

		28.06

		28.08

		28.1

		28.12

		28.14

		28.16

		28.18

		28.2

		28.22

		28.24

		28.26

		28.28

		28.3

		28.32

		28.34

		28.36

		28.38

		28.4

		28.42

		28.44

		28.46

		28.48

		28.5

		28.52

		28.54

		28.56

		28.58

		28.6

		28.62

		28.64

		28.66

		28.68

		28.7

		28.72

		28.74

		28.76

		28.78

		28.8

		28.82

		28.84

		28.86

		28.88

		28.9

		28.92

		28.94

		28.96

		28.98

		29

		29.02

		29.04

		29.06

		29.08

		29.1

		29.12

		29.14

		29.16

		29.18

		29.2

		29.22

		29.24

		29.26

		29.28

		29.3

		29.32

		29.34

		29.36

		29.38

		29.4

		29.42

		29.44

		29.46

		29.48

		29.5

		29.52

		29.54

		29.56

		29.58

		29.6

		29.62

		29.64

		29.66

		29.68

		29.7

		29.72

		29.74

		29.76

		29.78

		29.8

		29.82

		29.84

		29.86

		29.88

		29.9

		29.92

		29.94

		29.96

		29.98

		30

		30.02

		30.04

		30.06

		30.08

		30.1

		30.12

		30.14

		30.16

		30.18

		30.2

		30.22

		30.24

		30.26

		30.28

		30.3

		30.32

		30.34

		30.36

		30.38

		30.4

		30.42

		30.44

		30.46

		30.48

		30.5

		30.52

		30.54

		30.56

		30.58

		30.6

		30.62

		30.64

		30.66

		30.68

		30.7

		30.72

		30.74

		30.76

		30.78

		30.8

		30.82

		30.84

		30.86

		30.88

		30.9

		30.92

		30.94

		30.96

		30.98

		31

		31.02

		31.04

		31.06

		31.08

		31.1

		31.12

		31.14

		31.16

		31.18

		31.2

		31.22

		31.24

		31.26

		31.28

		31.3

		31.32

		31.34

		31.36

		31.38

		31.4

		31.42

		31.44

		31.46

		31.48

		31.5

		31.52

		31.54

		31.56

		31.58

		31.6

		31.62

		31.64

		31.66

		31.68

		31.7

		31.72

		31.74

		31.76

		31.78

		31.8

		31.82

		31.84

		31.86

		31.88

		31.9

		31.92

		31.94

		31.96

		31.98

		32

		32.02

		32.04

		32.06

		32.08

		32.1

		32.12

		32.14

		32.16

		32.18

		32.2

		32.22

		32.24

		32.26

		32.28

		32.3

		32.32

		32.34

		32.36

		32.38

		32.4

		32.42

		32.44

		32.46

		32.48

		32.5

		32.52

		32.54

		32.56

		32.58

		32.6

		32.62

		32.64

		32.66

		32.68

		32.7

		32.72

		32.74

		32.76

		32.78

		32.8

		32.82

		32.84

		32.86

		32.88

		32.9

		32.92

		32.94

		32.96

		32.98

		33

		33.02

		33.04

		33.06

		33.08

		33.1

		33.12

		33.14

		33.16

		33.18

		33.2

		33.22

		33.24

		33.26

		33.28

		33.3

		33.32

		33.34

		33.36

		33.38

		33.4

		33.42

		33.44

		33.46

		33.48

		33.5

		33.52

		33.54

		33.56

		33.58

		33.6

		33.62

		33.64

		33.66

		33.68

		33.7

		33.72

		33.74

		33.76

		33.78

		33.8

		33.82

		33.84

		33.86

		33.88

		33.9

		33.92

		33.94

		33.96

		33.98

		34

		34.02

		34.04

		34.06

		34.08

		34.1

		34.12

		34.14

		34.16

		34.18

		34.2

		34.22

		34.24

		34.26

		34.28

		34.3

		34.32

		34.34

		34.36

		34.38

		34.4

		34.42

		34.44

		34.46

		34.48

		34.5

		34.52

		34.54

		34.56

		34.58

		34.6

		34.62

		34.64

		34.66

		34.68

		34.7

		34.72

		34.74

		34.76

		34.78

		34.8

		34.82

		34.84

		34.86

		34.88

		34.9

		34.92

		34.94

		34.96

		34.98

		35

		35.02

		35.04

		35.06

		35.08

		35.1

		35.12

		35.14

		35.16

		35.18

		35.2

		35.22

		35.24

		35.26

		35.28

		35.3

		35.32

		35.34

		35.36

		35.38

		35.4

		35.42

		35.44

		35.46

		35.48

		35.5

		35.52

		35.54

		35.56

		35.58

		35.6

		35.62

		35.64

		35.66

		35.68

		35.7

		35.72

		35.74

		35.76

		35.78

		35.8

		35.82

		35.84

		35.86

		35.88

		35.9

		35.92

		35.94

		35.96

		35.98

		36

		36.02

		36.04

		36.06

		36.08

		36.1

		36.12

		36.14

		36.16

		36.18

		36.2

		36.22

		36.24

		36.26

		36.28

		36.3

		36.32

		36.34

		36.36

		36.38

		36.4

		36.42

		36.44

		36.46

		36.48

		36.5

		36.52

		36.54

		36.56

		36.58

		36.6

		36.62

		36.64

		36.66

		36.68

		36.7

		36.72

		36.74

		36.76

		36.78

		36.8

		36.82

		36.84

		36.86

		36.88

		36.9

		36.92

		36.94

		36.96

		36.98

		37

		37.02

		37.04

		37.06

		37.08

		37.1

		37.12

		37.14

		37.16

		37.18

		37.2

		37.22

		37.24

		37.26

		37.28

		37.3

		37.32

		37.34

		37.36

		37.38

		37.4

		37.42

		37.44

		37.46

		37.48

		37.5

		37.52

		37.54

		37.56

		37.58

		37.6

		37.62

		37.64

		37.66

		37.68

		37.7

		37.72

		37.74

		37.76

		37.78

		37.8

		37.82

		37.84

		37.86

		37.88

		37.9

		37.92

		37.94

		37.96

		37.98

		38

		38.02

		38.04

		38.06

		38.08

		38.1

		38.12

		38.14

		38.16

		38.18

		38.2

		38.22

		38.24

		38.26

		38.28

		38.3

		38.32

		38.34

		38.36

		38.38

		38.4

		38.42

		38.44

		38.46

		38.48

		38.5

		38.52

		38.54

		38.56

		38.58

		38.6

		38.62

		38.64

		38.66

		38.68

		38.7

		38.72

		38.74

		38.76

		38.78

		38.8

		38.82

		38.84

		38.86

		38.88

		38.9

		38.92

		38.94

		38.96

		38.98

		39

		39.02

		39.04

		39.06

		39.08

		39.1

		39.12

		39.14

		39.16

		39.18

		39.2

		39.22

		39.24

		39.26

		39.28

		39.3

		39.32

		39.34

		39.36

		39.38

		39.4

		39.42

		39.44

		39.46

		39.48

		39.5

		39.52

		39.54

		39.56

		39.58

		39.6

		39.62

		39.64

		39.66

		39.68

		39.7

		39.72

		39.74

		39.76

		39.78

		39.8

		39.82

		39.84

		39.86

		39.88

		39.9

		39.92

		39.94

		39.96

		39.98

		40

		40.02

		40.04

		40.06

		40.08

		40.1

		40.12

		40.14

		40.16

		40.18

		40.2

		40.22

		40.24

		40.26

		40.28

		40.3

		40.32

		40.34

		40.36

		40.38

		40.4

		40.42

		40.44

		40.46

		40.48

		40.5

		40.52

		40.54

		40.56

		40.58

		40.6

		40.62

		40.64

		40.66

		40.68

		40.7

		40.72

		40.74

		40.76

		40.78

		40.8

		40.82

		40.84

		40.86

		40.88

		40.9

		40.92

		40.94

		40.96

		40.98

		41

		41.02

		41.04

		41.06

		41.08

		41.1

		41.12

		41.14

		41.16

		41.18

		41.2

		41.22

		41.24

		41.26

		41.28

		41.3

		41.32

		41.34

		41.36

		41.38

		41.4

		41.42

		41.44

		41.46

		41.48

		41.5

		41.52

		41.54

		41.56

		41.58

		41.6

		41.62

		41.64

		41.66

		41.68

		41.7

		41.72

		41.74

		41.76

		41.78

		41.8

		41.82

		41.84

		41.86

		41.88

		41.9

		41.92

		41.94

		41.96

		41.98

		42

		42.02

		42.04

		42.06

		42.08

		42.1

		42.12

		42.14

		42.16

		42.18

		42.2

		42.22

		42.24

		42.26

		42.28

		42.3

		42.32

		42.34

		42.36

		42.38

		42.4

		42.42

		42.44

		42.46

		42.48

		42.5

		42.52

		42.54

		42.56

		42.58

		42.6

		42.62

		42.64

		42.66

		42.68

		42.7

		42.72

		42.74

		42.76

		42.78

		42.8

		42.82

		42.84

		42.86

		42.88

		42.9

		42.92

		42.94

		42.96

		42.98

		43

		43.02

		43.04

		43.06

		43.08

		43.1

		43.12

		43.14

		43.16

		43.18

		43.2

		43.22

		43.24

		43.26

		43.28

		43.3

		43.32

		43.34

		43.36

		43.38

		43.4

		43.42

		43.44

		43.46

		43.48

		43.5

		43.52

		43.54

		43.56

		43.58

		43.6

		43.62

		43.64

		43.66

		43.68

		43.7

		43.72

		43.74

		43.76

		43.78

		43.8

		43.82

		43.84

		43.86

		43.88

		43.9

		43.92

		43.94

		43.96

		43.98

		44

		44.02

		44.04

		44.06

		44.08

		44.1

		44.12

		44.14

		44.16

		44.18

		44.2

		44.22

		44.24

		44.26

		44.28

		44.3

		44.32

		44.34

		44.36

		44.38

		44.4

		44.42

		44.44

		44.46

		44.48

		44.5

		44.52

		44.54

		44.56

		44.58

		44.6

		44.62

		44.64

		44.66

		44.68

		44.7

		44.72

		44.74

		44.76

		44.78

		44.8

		44.82

		44.84

		44.86

		44.88

		44.9

		44.92

		44.94

		44.96

		44.98

		45

		45.02

		45.04

		45.06

		45.08

		45.1

		45.12

		45.14

		45.16

		45.18

		45.2

		45.22

		45.24

		45.26

		45.28

		45.3

		45.32

		45.34

		45.36

		45.38

		45.4

		45.42

		45.44

		45.46

		45.48

		45.5

		45.52

		45.54

		45.56

		45.58

		45.6

		45.62

		45.64

		45.66

		45.68

		45.7

		45.72

		45.74

		45.76

		45.78

		45.8

		45.82

		45.84

		45.86

		45.88

		45.9

		45.92

		45.94

		45.96

		45.98

		46

		46.02

		46.04

		46.06

		46.08

		46.1

		46.12

		46.14

		46.16

		46.18

		46.2

		46.22

		46.24

		46.26

		46.28

		46.3

		46.32

		46.34

		46.36

		46.38

		46.4

		46.42

		46.44

		46.46

		46.48

		46.5

		46.52

		46.54

		46.56

		46.58

		46.6

		46.62

		46.64

		46.66

		46.68

		46.7

		46.72

		46.74

		46.76

		46.78

		46.8

		46.82

		46.84

		46.86

		46.88

		46.9

		46.92

		46.94

		46.96

		46.98

		47

		47.02

		47.04

		47.06

		47.08

		47.1

		47.12

		47.14

		47.16

		47.18

		47.2

		47.22

		47.24

		47.26

		47.28

		47.3

		47.32

		47.34

		47.36

		47.38

		47.4

		47.42

		47.44

		47.46

		47.48

		47.5

		47.52

		47.54

		47.56

		47.58

		47.6

		47.62

		47.64

		47.66

		47.68

		47.7

		47.72

		47.74

		47.76

		47.78

		47.8

		47.82

		47.84

		47.86

		47.88

		47.9

		47.92

		47.94

		47.96

		47.98

		48

		48.02

		48.04

		48.06

		48.08

		48.1

		48.12

		48.14

		48.16

		48.18

		48.2

		48.22

		48.24

		48.26

		48.28

		48.3

		48.32

		48.34

		48.36

		48.38

		48.4

		48.42

		48.44

		48.46

		48.48

		48.5

		48.52

		48.54

		48.56

		48.58

		48.6

		48.62

		48.64

		48.66

		48.68

		48.7

		48.72

		48.74

		48.76

		48.78

		48.8

		48.82

		48.84

		48.86

		48.88

		48.9

		48.92

		48.94

		48.96

		48.98

		49

		49.02

		49.04

		49.06

		49.08

		49.1

		49.12

		49.14

		49.16

		49.18

		49.2

		49.22

		49.24

		49.26

		49.28

		49.3

		49.32

		49.34

		49.36

		49.38

		49.4

		49.42

		49.44

		49.46

		49.48

		49.5

		49.52

		49.54

		49.56

		49.58

		49.6

		49.62

		49.64

		49.66

		49.68

		49.7

		49.72

		49.74

		49.76

		49.78

		49.8

		49.82

		49.84

		49.86

		49.88

		49.9

		49.92

		49.94

		49.96

		49.98

		50

		50.02

		50.04

		50.06

		50.08

		50.1

		50.12

		50.14

		50.16

		50.18

		50.2

		50.22

		50.24

		50.26

		50.28

		50.3

		50.32

		50.34

		50.36

		50.38

		50.4

		50.42

		50.44

		50.46

		50.48

		50.5

		50.52

		50.54

		50.56

		50.58

		50.6

		50.62

		50.64

		50.66

		50.68

		50.7

		50.72

		50.74

		50.76

		50.78

		50.8

		50.82

		50.84

		50.86

		50.88

		50.9

		50.92

		50.94

		50.96

		50.98

		51

		51.02

		51.04

		51.06

		51.08

		51.1

		51.12

		51.14

		51.16

		51.18

		51.2

		51.22

		51.24

		51.26

		51.28

		51.3

		51.32

		51.34

		51.36

		51.38

		51.4

		51.42

		51.44

		51.46

		51.48

		51.5

		51.52

		51.54

		51.56

		51.58

		51.6

		51.62

		51.64

		51.66

		51.68

		51.7

		51.72

		51.74

		51.76

		51.78

		51.8

		51.82

		51.84

		51.86

		51.88

		51.9

		51.92

		51.94

		51.96

		51.98

		52

		52.02

		52.04

		52.06

		52.08

		52.1

		52.12

		52.14

		52.16

		52.18

		52.2

		52.22

		52.24

		52.26

		52.28

		52.3

		52.32

		52.34

		52.36

		52.38

		52.4

		52.42

		52.44

		52.46

		52.48

		52.5

		52.52

		52.54

		52.56

		52.58

		52.6

		52.62

		52.64

		52.66

		52.68

		52.7

		52.72

		52.74

		52.76

		52.78

		52.8

		52.82

		52.84

		52.86

		52.88

		52.9

		52.92

		52.94

		52.96

		52.98

		53

		53.02

		53.04

		53.06

		53.08

		53.1

		53.12

		53.14

		53.16

		53.18

		53.2

		53.22

		53.24

		53.26

		53.28

		53.3

		53.32

		53.34

		53.36

		53.38

		53.4

		53.42

		53.44

		53.46

		53.48

		53.5

		53.52

		53.54

		53.56

		53.58

		53.6

		53.62

		53.64

		53.66

		53.68

		53.7

		53.72

		53.74

		53.76

		53.78

		53.8

		53.82

		53.84

		53.86

		53.88

		53.9

		53.92

		53.94

		53.96

		53.98

		54

		54.02

		54.04

		54.06

		54.08

		54.1

		54.12

		54.14

		54.16

		54.18

		54.2

		54.22

		54.24

		54.26

		54.28

		54.3

		54.32

		54.34

		54.36

		54.38

		54.4

		54.42

		54.44

		54.46

		54.48

		54.5

		54.52

		54.54

		54.56

		54.58

		54.6

		54.62

		54.64

		54.66

		54.68

		54.7

		54.72

		54.74

		54.76

		54.78

		54.8

		54.82

		54.84

		54.86

		54.88

		54.9

		54.92

		54.94

		54.96

		54.98

		55

		55.02

		55.04

		55.06

		55.08

		55.1

		55.12

		55.14

		55.16

		55.18

		55.2

		55.22

		55.24

		55.26

		55.28

		55.3

		55.32

		55.34

		55.36

		55.38

		55.4

		55.42

		55.44

		55.46

		55.48

		55.5

		55.52

		55.54

		55.56

		55.58

		55.6

		55.62

		55.64

		55.66

		55.68

		55.7

		55.72

		55.74

		55.76

		55.78

		55.8

		55.82

		55.84

		55.86

		55.88

		55.9

		55.92

		55.94

		55.96

		55.98

		56

		56.02

		56.04

		56.06

		56.08

		56.1

		56.12

		56.14

		56.16

		56.18

		56.2

		56.22

		56.24

		56.26

		56.28

		56.3

		56.32

		56.34

		56.36

		56.38

		56.4

		56.42

		56.44

		56.46

		56.48

		56.5

		56.52

		56.54

		56.56

		56.58

		56.6

		56.62

		56.64

		56.66

		56.68

		56.7

		56.72

		56.74

		56.76

		56.78

		56.8

		56.82

		56.84

		56.86

		56.88

		56.9

		56.92

		56.94

		56.96

		56.98

		57

		57.02

		57.04

		57.06

		57.08

		57.1

		57.12

		57.14

		57.16

		57.18

		57.2

		57.22

		57.24

		57.26

		57.28

		57.3

		57.32

		57.34

		57.36

		57.38

		57.4

		57.42

		57.44

		57.46

		57.48

		57.5

		57.52

		57.54

		57.56

		57.58

		57.6

		57.62

		57.64

		57.66

		57.68

		57.7

		57.72

		57.74

		57.76

		57.78

		57.8

		57.82

		57.84

		57.86

		57.88

		57.9

		57.92

		57.94

		57.96

		57.98

		58

		58.02

		58.04

		58.06

		58.08

		58.1

		58.12

		58.14

		58.16

		58.18

		58.2

		58.22

		58.24

		58.26

		58.28

		58.3

		58.32

		58.34

		58.36

		58.38

		58.4

		58.42

		58.44

		58.46

		58.48

		58.5

		58.52

		58.54

		58.56

		58.58

		58.6

		58.62

		58.64

		58.66

		58.68

		58.7

		58.72

		58.74

		58.76

		58.78

		58.8

		58.82

		58.84

		58.86

		58.88

		58.9

		58.92

		58.94

		58.96

		58.98

		59

		59.02

		59.04

		59.06

		59.08

		59.1

		59.12

		59.14

		59.16

		59.18

		59.2

		59.22

		59.24

		59.26

		59.28

		59.3

		59.32

		59.34

		59.36

		59.38

		59.4

		59.42

		59.44

		59.46

		59.48

		59.5

		59.52

		59.54

		59.56

		59.58

		59.6

		59.62

		59.64

		59.66

		59.68

		59.7

		59.72

		59.74

		59.76

		59.78

		59.8

		59.82

		59.84

		59.86

		59.88

		59.9

		59.92

		59.94

		59.96

		59.98

		60



2 θ(degrees)

Intensity (a.u)

6.6683

5.668

3.6675

5.0012

5.0012

6.3349

5.668

5.3346

7.3351

6.6683

6.0014

4.6678

6.0014

4.3344

6.6683

5.3346

5.668

4.6678

7.3351

5.0012

3.3341

4.6678

7.0017

6.6683

5.3346

4.001

4.3344

4.6678

5.668

7.3351

6.3349

4.6678

6.0014

5.3346

5.668

5.0012

5.0012

4.6678

5.3346

5.3346

5.3346

5.3346

4.001

4.6678

6.0014

4.001

3.0007

5.0012

3.6675

3.3341

5.0012

7.0017

5.0012

5.668

6.0014

7.6685

7.6685

5.3346

4.3344

4.001

5.0012

7.0017

6.6683

6.0014

7.0017

5.668

4.6678

5.3346

6.0014

6.6683

2.6673

5.668

5.668

4.6678

3.6675

7.0017

3.3341

5.668

5.3346

4.6678

5.668

3.3341

4.3344

5.0012

5.668

5.3346

7.6685

4.001

7.0017

5.0012

4.6678

3.3341

4.6678

3.0007

8.3353

6.3349

5.0012

4.3344

7.6685

5.3346

4.001

4.001

4.3344

6.3349

5.668

5.0012

4.001

3.6675

4.6678

4.001

4.6678

3.6675

3.6675

3.0007

6.3349

4.001

3.0007

3.6675

4.3344

5.3346

4.001

4.001

4.3344

6.0014

6.3349

5.0012

3.6675

4.3344

4.001

4.3344

5.668

5.668

3.3341

4.3344

4.001

2.3339

4.3344

4.6678

3.0007

5.3346

2.3339

4.6678

5.3346

5.0012

5.3346

4.3344

6.0014

6.3349

5.0012

5.668

5.3346

5.0012

4.6678

5.668

6.0014

5.0012

4.3344

6.0014

6.3349

4.3344

7.0017

5.0012

8.0019

3.3341

6.6683

3.3341

5.0012

7.6685

4.001

4.6678

6.6683

5.0012

3.3341

4.001

5.3346

3.3341

4.6678

3.6675

5.3346

4.3344

5.3346

4.6678

3.6675

3.0007

5.668

5.668

7.0017

4.3344

4.6678

3.0007

5.3346

3.6675

5.0012

3.6675

4.001

4.001

2.3339

4.6678

7.6685

8.6687

4.6678

4.6678

3.6675

4.001

5.3346

5.3346

6.0014

6.0014

5.668

6.0014

4.001

4.6678

4.3344

5.3346

5.668

4.6678

8.3353

4.6678

5.0012

3.6675

4.3344

7.0017

6.3349

5.3346

4.6678

5.0012

6.0014

5.3346

5.0012

4.3344

5.3346

4.3344

7.6685

5.668

3.6675

5.0012

4.3344

4.3344

5.3346

5.3346

4.001

5.0012

3.0007

4.001

7.6685

3.3341

5.668

5.0012

4.001

7.3351

6.0014

4.001

3.3341

5.668

3.6675

5.0012

3.6675

2.6673

5.668

3.3341

9.0022

5.668

3.3341

5.3346

5.3346

5.668

4.001

4.6678

5.0012

3.3341

2.6673

5.0012

4.001

4.001

5.3346

3.3341

4.3344

5.0012

3.6675

7.3351

4.6678

5.668

4.3344

3.6675

4.001

6.3349

7.0017

6.3349

5.3346

4.6678

8.3353

5.668

4.3344

4.3344

5.3346

5.0012

4.3344

4.6678

5.3346

4.3344

9.0022

4.001

3.0007

7.6685

7.6685

4.6678

7.6685

4.6678

6.6683

4.3344

4.001

7.6685

3.6675

5.3346

5.3346

4.001

4.3344

5.0012

4.3344

5.3346

7.3351

6.6683

3.3341

3.6675

4.001

4.6678

6.0014

5.3346

6.6683

6.0014

5.3346

6.0014

5.3346

5.3346

3.3341

6.6683

4.001

4.3344

5.668

6.3349

4.6678

5.0012

5.3346

5.668

5.3346

6.0014

5.3346

2.6673

5.668

3.0007

5.3346

6.0014

6.0014

5.668

4.001

3.6675

4.6678

4.6678

4.001

4.001

5.3346

2.0005

5.668

6.3349

5.3346

4.001

5.3346

5.0012

6.0014

6.6683

5.3346

6.6683

6.0014

4.3344

4.6678

7.6685

7.0017

7.6685

6.3349

6.3349

8.0019

9.0022

12.003

24.673

50.012

93.022

232.72

362.09

445.77

340.08

239.72

129.36

54.346

17.004

19.338

16.671

12.003

12.003

9.669

8.6687

7.0017

8.0019

5.668

7.0017

6.3349

6.6683

6.0014

4.6678

6.3349

7.3351

5.0012

5.3346

4.001

3.3341

5.0012

4.6678

5.3346

5.3346

4.001

4.3344

8.6687

6.6683

5.3346

3.3341

6.3349

3.3341

7.3351

5.3346

6.0014

4.6678

8.0019

7.6685

5.668

3.6675

5.0012

7.0017

4.3344

4.6678

7.0017

5.3346

6.0014

5.668

3.3341

4.001

4.6678

6.6683

6.0014

4.6678

6.6683

4.3344

5.0012

4.3344

4.3344

5.3346

4.001

3.3341

5.3346

6.0014

5.0012

5.3346

3.6675

3.6675

6.3349

5.0012

3.3341

3.0007

5.668

5.668

4.3344

5.0012

2.6673

6.3349

6.6683

3.3341

6.6683

9.0022

11.003

6.6683

7.6685

7.3351

5.3346

5.3346

5.0012

3.6675

5.3346

5.0012

6.6683

3.6675

5.3346

4.3344

5.3346

7.6685

4.6678

4.001

6.3349

6.3349

4.6678

5.0012

3.6675

4.001

7.6685

4.3344

3.0007

6.3349

8.6687

5.3346

5.668

6.6683

7.0017

5.668

5.668

6.6683

5.0012

8.6687

4.6678

5.0012

6.0014

5.668

4.3344

6.6683

7.6685

4.6678

4.6678

4.3344

3.3341

4.3344

4.001

5.668

6.0014

4.6678

4.6678

5.0012

3.3341

8.3353

7.3351

6.0014

8.6687

4.001

6.3349

8.0019

7.3351

7.0017

12.003

11.003

16.337

24.006

34.008

37.676

88.355

110.36

174.04

351.75

372.76

219.72

212.72

136.7

52.012

24.006

18.671

14.67

13.67

13.003

8.0019

5.668

5.3346

10.336

4.3344

6.3349

8.0019

4.6678

7.0017

6.0014

6.3349

4.6678

6.0014

7.0017

7.3351

6.6683

5.668

4.6678

4.001

5.668

3.6675

9.669

4.6678

5.668

5.0012

5.668

5.3346

7.0017

5.0012

6.6683

5.0012

2.3339

3.0007

4.3344

5.3346

2.6673

5.3346

5.3346

3.6675

6.3349

4.6678

4.6678

6.6683

4.001

3.3341

4.3344

4.001

3.3341

9.669

5.668

4.3344

6.3349

5.3346

4.3344

5.668

8.0019

4.3344

6.6683

6.6683

5.3346

7.0017

5.3346

5.0012

4.6678

5.0012

6.6683

6.3349

6.0014

5.3346

6.0014

4.3344

6.0014

4.6678

3.0007

5.3346

4.001

6.0014

4.001

4.001

5.0012

5.3346

4.6678

3.6675

6.0014

4.6678

5.668

6.6683

4.3344

3.6675

8.0019

7.3351

3.0007

5.3346

7.3351

7.3351

7.0017

8.3353

5.3346

7.3351

7.0017

6.0014

9.669

10.336

16.337

18.671

29.007

53.013

71.684

108.36

165.04

174.38

114.36

97.023

87.688

37.342

15.004

9.0022

11.336

13.003

7.6685

8.3353

7.6685

6.3349

6.6683

7.6685

4.001

5.3346

3.6675

8.0019

5.3346

3.0007

3.6675

5.668

4.3344

5.0012

7.0017

6.0014

7.3351

6.3349

7.0017

7.3351

5.3346

5.668

4.001

6.0014

4.001

6.3349

4.6678

7.3351

5.3346

6.0014

6.3349

7.3351

5.3346

6.6683

10.002

8.3353

22.339

36.675

66.683

82.353

50.345

50.679

56.013

31.341

12.003

11.336

8.0019

6.6683

7.3351

5.0012

7.0017

4.001

5.668

9.669

5.0012

5.3346

5.3346

6.3349

4.6678

7.6685

5.668

6.6683

6.6683

7.0017

6.0014

5.0012

5.0012

6.6683

6.0014

4.3344

5.3346

6.6683

4.3344

7.3351

2.6673

7.6685

5.668

4.6678

6.6683

4.6678

6.0014

5.0012

7.3351

7.6685

6.0014

4.001

7.0017

7.0017

6.3349

6.0014

4.3344

7.3351

5.668

3.0007

5.3346

4.001

9.669

6.3349

8.0019

6.0014

6.0014

6.6683

6.0014

9.3356

7.3351

8.6687

6.6683

9.3356

15.004

15.337

18.004

19.005

25.673

39.009

58.681

106.69

219.39

317.08

371.42

371.42

294.4

254.39

251.73

157.7

78.352

49.012

40.676

27.006

21.672

15.004

11.336

10.669

10.669

9.0022

7.0017

10.669

9.0022

7.0017

7.0017

5.668

8.3353

7.3351

8.3353

8.3353

9.669

6.3349

4.6678

4.6678

6.3349

5.668

4.3344

4.6678

4.6678

6.3349

7.3351

2.6673

5.3346

6.6683

5.3346

5.0012

5.0012

4.6678

7.0017

4.001

5.668

4.6678

6.0014

5.3346

8.0019

5.3346

5.0012

7.3351

6.3349

4.6678

5.0012

7.6685

6.3349

6.3349

5.3346

6.0014

5.3346

3.3341

5.3346

4.001

3.3341

2.6673

5.668

5.0012

5.3346

3.0007

4.6678

3.3341

6.3349

4.6678

5.3346

5.668

4.6678

5.0012

7.3351

5.668

8.0019

7.3351

4.6678

5.668

5.668

4.3344

7.0017

6.0014

4.6678

5.3346

4.3344

6.6683

7.3351

5.668

10.669

8.3353

8.0019

7.3351

6.6683

7.3351

9.669

5.0012

8.3353

5.3346

6.6683

5.0012

6.6683

3.6675

5.0012

6.3349

6.6683

6.6683

4.001

6.0014

5.668

9.3356

5.668

3.6675

5.668

6.3349

9.3356

5.3346

7.3351

3.6675

6.6683

3.3341

3.0007

5.3346

8.3353

5.3346

5.668

6.0014

3.3341

6.6683

4.3344

6.0014

7.3351

6.0014

8.0019

5.668

6.3349

4.3344

7.0017

5.3346

6.3349

8.6687

8.6687

7.0017

5.668

5.3346

5.3346

4.3344

7.0017

8.6687

4.001

5.668

4.3344

6.0014

7.0017

5.3346

6.3349

6.3349

5.668

6.0014

7.3351

4.6678

5.0012

7.3351

7.3351

5.3346

6.3349

3.6675

8.6687

8.3353

7.3351

5.3346

5.3346

4.001

5.668

4.3344

6.0014

4.6678

6.0014

6.0014

3.6675

6.0014

5.3346

7.6685

5.3346

5.0012

7.6685

8.6687

5.3346

6.3349

6.0014

5.0012

6.0014

6.3349

6.0014

3.3341

7.3351

6.0014

7.0017

7.6685

7.6685

6.3349

5.3346

7.6685

11.003

13.67

14.337

22.005

30.674

51.679

35.008

24.006

23.339

27.34

29.007

26.006

23.339

31.674

44.677

49.345

70.017

127.36

261.4

463.11

434.1

300.41

257.06

268.73

241.06

139.7

68.683

41.677

28.674

27.34

21.672

15.004

11.003

14.337

14.67

8.6687

9.0022

6.6683

6.0014

7.0017

8.6687

10.002

8.3353

7.6685

5.3346

8.6687

8.3353

7.0017

7.0017

7.6685

6.3349

5.0012

6.6683

6.3349

7.6685

8.0019

7.0017

7.6685

5.3346

6.3349

8.0019

3.3341

7.0017

6.6683

4.3344

4.6678

6.3349

7.0017

3.6675

6.3349

6.0014

5.0012

6.6683

5.0012

4.6678

4.6678

8.6687

5.3346

4.6678

5.3346

6.3349

3.6675

4.6678

4.6678

5.668

5.3346

4.001

4.3344

4.6678

6.0014

6.0014

3.0007

4.6678

6.3349

5.3346

5.668

4.3344

4.6678

4.6678

8.6687

5.3346

8.6687

5.668

7.0017

4.001

6.0014

5.3346

5.3346

3.6675

3.3341

4.6678

4.3344

3.6675

6.0014

5.668

4.6678

5.668

3.6675

5.0012

6.6683

3.3341

4.6678

7.6685

6.0014

7.6685

5.668

8.6687

9.0022

8.3353

8.6687

7.6685

7.0017

16.004

20.005

36.675

64.349

93.022

90.022

85.687

81.353

61.348

61.681

44.677

38.676

20.672

18.004

11.003

12.336

10.002

9.0022

5.668

4.001

6.6683

6.0014

7.6685

7.0017

6.0014

6.0014

5.3346

5.3346

5.668

4.6678

4.6678

8.0019

7.3351

6.6683

6.0014

5.668

6.6683

6.3349

3.3341

6.0014

5.3346

8.0019

5.0012

4.6678

4.6678

3.6675

5.3346

4.3344

4.6678

8.0019

4.6678

5.3346

7.3351

3.0007

5.3346

6.6683

5.3346

5.668

5.0012

6.3349

6.0014

4.3344

6.6683

3.3341

4.3344

7.3351

4.3344

6.0014

5.3346

4.001

5.668

7.0017

5.0012

5.668

4.001

6.0014

5.668

6.6683

4.3344

5.0012

5.0012

5.3346

5.0012

4.001

6.6683

4.3344

6.3349

3.3341

4.001

4.6678

2.3339

5.0012

3.3341

4.6678

4.001

4.001

6.6683

6.6683

5.3346

4.001

6.6683

5.0012

5.0012

4.3344

6.3349

4.001

5.0012

6.6683

4.6678

4.001

5.668

4.6678

5.0012

4.6678

4.6678

5.3346

4.6678

3.0007

4.3344

7.0017

4.6678

3.6675

5.3346

5.0012

7.6685

7.0017

8.0019

7.6685

7.0017

5.3346

6.3349

5.3346

8.0019

25.673

40.343

25.673

15.337

16.004

23.339

24.339

14.337

10.669

7.3351

8.6687

5.3346

4.3344

4.3344

10.002

8.0019

6.3349

5.668

6.3349

8.6687

6.0014

6.3349

7.6685

5.0012

7.0017

5.3346

8.3353

9.0022

7.3351

7.6685

7.3351

10.336

10.336

11.669

11.669

13.67

13.337

16.004

17.337

22.005

32.675

36.675

53.013

114.69

197.05

282.4

500.12

606.48

439.77

254.39

246.06

308.07

286.4

179.04

90.022

51.346

33.341

20.338

14.67

23.672

16.337

11.336

9.669

7.6685

10.669

6.6683

8.0019

9.0022

6.3349

6.6683

7.3351

11.669

6.0014

10.669

5.668

9.0022

9.0022

8.6687

10.669

9.0022

7.0017

9.0022

6.3349

11.336

13.003

8.6687

12.336

14.337

15.004

26.34

38.343

59.014

122.36

281.73

355.42

206.72

111.36

112.03

184.04

189.05

96.356

44.344

23.339

16.671

11.669

14.003

11.336

11.003

8.6687

10.002

7.6685

6.6683

4.3344

10.669

8.3353

5.668

4.001

6.0014

5.668

3.6675

6.6683

5.3346

5.668

6.0014

6.6683

4.3344

7.0017

6.0014

6.6683

5.3346

7.3351

3.6675

6.0014

3.3341

2.6673

5.668

6.3349

5.3346

6.3349

6.6683

5.0012

3.6675

4.6678

6.0014

7.6685

7.0017

4.001

3.0007

6.3349

7.0017

11.336

12.336

11.003

7.6685

5.3346

5.0012

12.67

9.3356

2.3339

4.001

6.0014

2.6673

9.0022

4.3344

5.0012

7.0017

4.001

4.3344

8.6687

4.001

5.668

5.0012

6.0014

8.3353

14.337

19.338

31.007

31.674

37.342

59.348

58.014

43.01

24.339

29.34

33.675

32.341

20.005

11.336

8.3353

6.6683

7.6685

8.6687

7.0017

5.3346

8.3353

5.3346

6.3349

6.0014

7.6685

12.003

14.003

20.005

32.008

36.342

53.346

66.349

44.011

27.006

24.339

26.673

29.007

21.338

14.67

6.0014

7.0017

4.3344

4.3344

6.3349

7.3351

5.3346

3.6675

7.0017

5.3346

4.6678

5.0012

6.6683

3.6675

6.0014

2.0005

3.6675

5.3346

4.6678

6.3349

2.6673

8.3353

6.3349

6.3349

3.6675

5.3346

8.3353

8.0019

5.0012

6.3349

5.668

6.0014

6.0014

7.3351

6.6683

6.3349

13.337

15.337

24.006

33.008

49.345

74.351

76.352

50.679

32.675

34.008

47.678

51.012

37.676

20.672

29.34

47.011

51.346

55.013

45.344

40.01

46.344

34.675

37.676

33.341

24.339

20.338

11.336

4.6678

7.6685

6.3349

6.3349

8.6687

5.668

4.3344

5.668

6.3349

4.6678

6.0014

4.6678

4.6678

5.668

5.3346

4.001

4.3344

4.001

4.6678

5.0012

4.001

2.6673

5.0012

5.3346

5.3346

3.3341

4.6678

4.6678

4.6678

5.0012

4.6678

4.3344

5.3346

5.3346

4.001

5.0012

4.6678

5.0012

6.3349

3.0007

6.6683

5.0012

4.6678

5.668

4.3344

6.3349

5.668

4.3344

5.3346

6.0014

4.001

4.6678

5.0012

3.6675

3.3341

3.3341

7.0017

6.0014

6.3349

3.6675

4.001

7.6685

3.6675

5.0012

4.6678

6.6683

6.3349

6.3349

6.6683

7.0017

9.3356

9.3356

12.003

10.669

14.003

17.004

25.006

44.011

65.682

79.686

122.03

211.72

309.41

306.07

139.7

81.353

94.023

150.37

170.04

118.7

39.343

16.671

10.336

8.6687

11.336

8.6687

8.3353

7.6685

4.6678

8.6687

5.0012

7.3351

5.0012

5.3346

8.6687

6.0014

6.0014

4.001

4.001

5.0012

6.3349

9.3356

3.6675

8.6687

5.668

6.6683

6.0014

7.0017

5.3346

5.3346

6.0014

6.0014

6.0014

2.6673

4.001

6.0014

5.3346

4.6678

5.668

4.3344

3.0007

5.668

5.668

3.6675

5.3346

6.0014

4.6678

5.668

6.6683

4.3344

7.0017

3.3341

2.0005

5.0012

2.0005

5.0012

3.6675

4.001

5.668

3.3341

3.6675

6.0014

5.0012

4.001

4.6678

3.0007

6.0014

4.6678

4.3344

4.3344

3.3341

5.3346

4.001

4.001

5.0012

7.3351

5.0012

3.0007

5.0012

4.3344

4.3344

3.6675

4.6678

5.0012

6.6683

4.6678

5.0012

4.3344

4.001

4.001

3.3341

4.6678

4.001

4.6678

5.668

4.6678

4.3344

3.6675

3.6675

5.0012

3.3341

4.6678

5.0012

3.3341

4.001

3.6675

5.0012

5.668

6.0014

7.0017

3.6675

6.0014

3.6675

5.3346

5.3346

5.668

3.3341

5.0012

5.0012

3.3341

6.6683

3.0007

5.668

5.668

5.3346

5.0012

5.3346

6.3349

4.6678

4.6678

5.668

7.0017

11.003

18.671

19.671

26.006

17.004

12.67

11.669

13.67

15.337

16.004

16.004

10.336

9.3356

6.6683

7.3351

5.0012

5.0012

4.3344

4.001

4.6678

5.0012

4.001

4.001

4.001

5.3346

7.3351

2.3339

4.001

4.3344

5.0012

5.3346

6.3349

3.3341

5.3346

3.0007

4.6678

4.3344

4.3344

3.6675

4.6678

5.0012

4.6678

5.668

3.3341

4.001

5.0012

5.0012

6.0014

5.0012

3.0007

4.001

6.0014

4.6678

4.3344

3.6675

6.0014

3.3341

3.6675

4.001

5.0012

3.6675

4.6678

3.6675

5.3346

3.0007

5.668

1.6671

4.3344

2.6673

3.0007

3.3341

2.6673

4.3344

5.668

6.3349

4.001

5.3346

4.6678

4.6678

6.6683

4.001

3.3341

4.6678

6.3349

4.001

6.3349

2.6673

3.3341

3.0007

5.3346

4.3344

4.001

5.0012

5.3346

5.3346

4.6678

6.3349

10.336

10.336

6.3349

4.6678

5.0012

7.0017

7.3351

5.668

6.0014

4.001

6.0014

4.001

4.001

5.0012

9.0022

5.668

8.6687

14.67

9.0022

8.0019

7.0017

6.6683

5.3346

7.3351

8.6687

10.336

7.3351

4.6678

6.6683

6.6683

5.3346

4.001

5.668

8.3353

4.6678

4.6678

4.3344

4.6678

3.3341

7.0017

5.3346

3.0007

3.6675

4.3344

4.6678

4.001

3.6675

2.0005

5.668

4.6678

3.0007

2.6673

3.6675

5.668

2.0005

5.668

4.3344

3.0007

4.6678

6.0014

3.0007

5.668

3.6675

3.6675

4.6678

5.3346

2.6673

3.0007

4.3344

4.001

5.0012

4.001

5.3346

5.0012

3.6675

6.6683

4.3344

2.6673

4.3344

3.0007

4.3344

4.001

6.0014

7.3351

4.3344

3.3341

6.6683

5.0012

5.668

4.6678

3.3341

4.001

4.001

6.3349

4.001

5.668

5.668

6.6683

5.668

6.3349

6.6683

6.0014

4.001

4.6678

6.3349

5.3346

5.0012

5.0012

3.6675

4.001

6.3349

5.668

6.0014

5.3346

7.0017

7.0017

6.3349

4.6678

8.3353

13.003

8.0019

8.6687

14.67

25.339

43.344

64.015

56.347

40.01

22.005

19.671

22.005

32.008

35.342

25.339

19.338

11.336

11.003

5.3346

8.6687

5.3346

8.0019

6.6683

4.6678

3.3341

5.3346

4.001

5.0012

3.0007

5.0012

3.0007

3.3341

5.0012

4.001

6.3349

5.0012

4.6678

4.6678

4.6678

3.6675

5.3346

3.6675

5.668

7.3351

7.6685

6.6683

10.002

14.337

15.67

12.67

14.003

10.002

8.3353

8.3353

11.336

10.336

7.3351

6.3349

6.6683

5.0012

7.6685

4.3344

6.6683

6.3349

4.001

7.0017

4.3344

5.0012

5.3346

5.0012

4.3344

4.6678

4.6678

4.3344

3.0007

5.3346

4.6678

5.3346

8.6687

5.0012

5.668

7.0017

8.0019

10.336

9.669

15.004

20.338

31.007

59.348

69.35

71.35

60.348

37.009

24.006

28.674

40.343

46.678

40.676

36.675

22.672

14.003

10.002

13.003

12.336

13.337

12.67

16.337

28.007

30.674

32.675

26.34

25.673

25.339

14.003

18.004

20.672

18.338

19.338

17.337

11.336

12.336

9.0022

8.6687

6.6683

7.3351

6.0014

6.0014

6.0014

4.3344

4.6678

6.3349

4.001

6.0014

5.0012

4.3344

4.001

5.668

3.3341

2.6673

3.6675

6.6683

5.0012

5.0012

4.001

5.3346

4.001

3.6675

7.6685

5.0012

4.001

6.0014

4.6678

5.668

6.0014

4.001

6.3349

6.0014

6.6683

6.0014

6.6683

11.669

6.6683

3.6675

6.6683

5.668

8.3353

8.3353

9.0022

11.669

13.67

13.337

15.337

15.67

20.005

26.34

35.342

62.682

116.03

178.38

218.05

184.04

95.356

69.017

61.681

84.687

105.36

139.03

126.36

76.018

62.015

40.01

31.674

24.339

22.339

17.671

22.672

18.004

21.338

10.002

13.337

10.669

5.0012

9.0022

11.336

7.3351

4.6678

7.0017

6.6683

7.0017

8.0019

7.3351

7.0017

9.3356

16.671

22.672

26.006

23.672

25.339

18.338

10.669

9.3356

12.003

12.67

19.005

13.003

15.004

8.0019

4.3344

8.3353

6.3349

7.0017

5.668

7.0017

9.0022

6.0014

5.0012

2.6673

3.6675

5.0012

4.3344

5.3346

5.0012

3.0007

5.3346

5.3346

8.0019

7.0017

4.6678

7.0017

5.0012

8.0019

11.003

4.6678

8.0019

9.3356

9.3356

12.003

6.0014

7.3351

7.6685

7.0017

8.3353

8.6687

9.3356

8.0019

7.0017

5.3346

5.668

4.6678

7.6685

6.6683

5.3346

5.668

5.3346

6.3349

7.3351

3.6675

7.0017

3.0007

4.001

5.668

3.0007

2.3339

4.001

4.6678

5.668

6.0014

4.3344

5.3346

4.3344

3.3341

6.3349

5.0012

6.0014

5.0012

6.0014

4.3344

9.669

6.0014

7.0017

7.3351

4.001

4.6678

6.3349

10.002

11.336

15.337

25.673

38.676

41.677

42.343

42.01

31.007

20.338

18.338

19.671

25.673

28.34

18.671

20.005

18.338

9.669

9.0022

8.3353

3.6675

3.6675

5.0012

5.3346

4.3344

4.3344

5.0012

4.3344

6.3349

4.3344

6.3349

8.0019

4.6678

3.3341

4.6678

4.6678

7.0017

5.668

5.0012

8.3353

7.6685

5.3346

5.3346

5.3346

5.0012

2.6673

5.668

3.6675

4.6678

7.0017

2.6673

6.3349

3.6675

4.3344

5.3346

4.3344

6.3349

5.3346

6.3349

4.6678

7.3351

7.0017

10.669

7.3351

8.6687

9.669

13.67

19.005

26.006

31.007

40.343

53.013

48.012

31.341

24.339

21.338

19.005

20.338

26.673

25.339

28.674

16.337

12.003

9.669

8.0019

6.6683

6.6683

6.6683

7.3351

7.3351

7.0017

7.6685

8.0019

6.3349

3.3341

5.0012

6.6683

4.6678

5.668

9.0022

5.668

7.3351

6.3349

5.668

7.0017

7.0017

10.336

14.67

13.003

14.67

13.003

23.006

27.006

45.678

77.018

82.353

83.687

57.681

31.341

29.34

23.006

35.342

42.01

46.344

41.343

27.34

18.671

13.67

12.67

9.669

9.669

10.002

8.0019

6.6683

8.0019

6.0014

7.0017

5.0012

7.6685

5.0012

8.6687

4.001

6.0014

4.3344

7.0017

7.3351

6.3349

6.0014

5.0012

3.3341

4.3344

6.0014

3.6675

3.3341

5.0012

4.001

7.3351

4.6678

4.3344

3.6675

5.3346

6.0014

5.668

7.3351

4.6678

10.002

11.336

8.6687

6.6683

4.001

6.3349

6.6683

8.3353

8.0019

7.0017

4.3344

5.3346

4.3344

4.3344

5.668

6.0014

5.3346

5.3346

5.3346

4.001

3.3341

3.3341

6.0014

3.0007

5.668

3.6675

6.3349

4.6678

5.668

5.0012

8.3353

4.3344

3.3341

5.668

8.0019

5.3346

6.0014

7.3351

7.0017

11.336

12.336

11.336



B

		; C:\DIFFDAT1\JF-Wan Jeffrey\Azlin-B5.raw(Diffrac Plus V1.01 file) converted by XCH V1.0

		_FILEVERSION=2

		_SITE='Kuala Lumpur, Malaysia'

		_USER='Jabatan Fizik'

		_SAMPLE_CHANGER_CODE=0

		_ATTACHMENTS_CODE=0

		_GONIOMETER_RADIUS=200.500000

		_FIXED_DIVSLIT=1.000000

		_FIXED_SAMPLESLIT=1.000000

		_SOLLER_SLITS='Y'

		_FIXED_DETSLIT=0.100000

		_MONOCHROMATOR=0

		; None

		_THIN_FILM='N'

		_BETA_FILTER='Y'

		_FIXED_ANTISLIT=1.000000

		_ANALYZER_CODE=0

		; None

		_DATEMEASURED='28-Jun-2006 11:30:50'

		_WL_UNIT='A'

		_WL1=1.540600

		_WL2=1.544390

		_WL3=1.392220

		_WLRATIO=0.500000

		_ANODE='Cu'

		; (Data for Range number 1)

		_DRIVE='COUPLED'

		_STEPTIME=2.000000

		_STEPSIZE=0.030000

		_STEPMODE='C'

		_START=5.000000

		_THETA=2.500000

		_2THETA=5.000000

		_KHI=0.000000

		_PHI=0.000000

		_X=0.000000

		_Y=0.000000

		_Z=0.000000

		_DIVERGENCE=0.000000

		_ANTISCATTER=0.000000

		_DETECTOR=1

		; S.C.

		_HV=856.000000

		_GAIN=2.000000

		_LLD=0.400000

		_ULD=1.700000

		_DETECTORSLIT='unkn'

		_AUX1=0.000000

		_AUX2=0.000000

		_AUX3=0.000000

		_TIMESTARTED=14.000000

		_TEMP_RATE=-1.000000

		_TEMP_DELAY=-1.000000

		_KV=40

		_MA=40

		_RANGE_WL=1.540600

		_3DPLANE=0

		_2THETACPS						B1						B2						B3						B4

		5		21.5				5		21.5				5		16.5				5		10				10		6.6683

		5.03		16.5				5.03		16.5				5.03		14				5.03		8.5				10.02		5.668

		5.06		14				5.06		14				5.06		22				5.06		10				10.04		3.6675

		5.09		17.5				5.09		17.5				5.09		16.5				5.09		3.5				10.06		5.0012

		5.12		22				5.12		22				5.12		16				5.12		11				10.08		5.0012

		5.15		14.5				5.15		14.5				5.15		16.5				5.15		5.5				10.1		6.3349

		5.18		17				5.18		17				5.18		14				5.18		6				10.12		5.668

		5.21		18.5				5.21		18.5				5.21		18				5.21		7				10.14		5.3346

		5.24		18.5				5.24		18.5				5.24		14.5				5.24		10				10.16		7.3351

		5.27		20.5				5.27		20.5				5.27		13				5.27		7				10.18		6.6683

		5.3		17				5.3		17				5.3		16.5				5.3		10				10.2		6.0014

		5.33		16.5				5.33		16.5				5.33		20				5.33		9				10.22		4.6678

		5.36		17.5				5.36		17.5				5.36		13				5.36		7.5				10.24		6.0014

		5.39		19				5.39		19				5.39		13.5				5.39		7.5				10.26		4.3344

		5.42		15.5				5.42		15.5				5.42		16				5.42		6.5				10.28		6.6683

		5.45		17				5.45		17				5.45		17.5				5.45		8.5				10.3		5.3346

		5.48		19.5				5.48		19.5				5.48		16				5.48		7				10.32		5.668

		5.51		20				5.51		20				5.51		15.5				5.51		5.5				10.34		4.6678

		5.54		15				5.54		15				5.54		20.5				5.54		7				10.36		7.3351

		5.57		23				5.57		23				5.57		16.5				5.57		10				10.38		5.0012

		5.6		18.5				5.6		18.5				5.6		18				5.6		7.5				10.4		3.3341

		5.63		18				5.63		18				5.63		19.5				5.63		5				10.42		4.6678

		5.66		19				5.66		19				5.66		13				5.66		11				10.44		7.0017

		5.69		17.5				5.69		17.5				5.69		20				5.69		10				10.46		6.6683

		5.72		21				5.72		21				5.72		12.5				5.72		6				10.48		5.3346

		5.75		14				5.75		14				5.75		12.5				5.75		7.5				10.5		4.001

		5.78		18.5				5.78		18.5				5.78		18				5.78		10				10.52		4.3344

		5.81		19				5.81		19				5.81		15.5				5.81		7.5				10.54		4.6678

		5.84		21.5				5.84		21.5				5.84		18				5.84		10.5				10.56		5.668

		5.87		13.5				5.87		13.5				5.87		14				5.87		4				10.58		7.3351

		5.9		17.5				5.9		17.5				5.9		17.5				5.9		9				10.6		6.3349

		5.93		19				5.93		19				5.93		15				5.93		6.5				10.62		4.6678

		5.96		20.5				5.96		20.5				5.96		14				5.96		7.5				10.64		6.0014

		5.99		15				5.99		15				5.99		14				5.99		6				10.66		5.3346

		6.02		11				6.02		11				6.02		15				6.02		6.5				10.68		5.668

		6.05		16.5				6.05		16.5				6.05		17				6.05		4				10.7		5.0012

		6.08		14.5				6.08		14.5				6.08		17.5				6.08		4.5				10.72		5.0012

		6.11		16.5				6.11		16.5				6.11		16.5				6.11		8				10.74		4.6678

		6.14		15				6.14		15				6.14		16				6.14		6.5				10.76		5.3346

		6.17		14.5				6.17		14.5				6.17		10.5				6.17		7.5				10.78		5.3346

		6.2		13.5				6.2		13.5				6.2		15.5				6.2		8.5				10.8		5.3346

		6.23		14				6.23		14				6.23		11				6.23		7				10.82		5.3346

		6.26		15.5				6.26		15.5				6.26		17.5				6.26		6.5				10.84		4.001

		6.29		15				6.29		15				6.29		18.5				6.29		8				10.86		4.6678

		6.32		16				6.32		16				6.32		19				6.32		5.5				10.88		6.0014

		6.35		12.5				6.35		12.5				6.35		13.5				6.35		3.5				10.9		4.001

		6.38		15				6.38		15				6.38		12.5				6.38		6				10.92		3.0007

		6.41		16.5				6.41		16.5				6.41		17				6.41		4				10.94		5.0012

		6.44		12.5				6.44		12.5				6.44		8.5				6.44		4.5				10.96		3.6675

		6.47		9.5				6.47		9.5				6.47		16				6.47		6				10.98		3.3341

		6.5		15				6.5		15				6.5		13.5				6.5		6				11		5.0012

		6.53		17.5				6.53		17.5				6.53		10.5				6.53		6.5				11.02		7.0017

		6.56		18				6.56		18				6.56		12				6.56		5				11.04		5.0012

		6.59		12.5				6.59		12.5				6.59		12.5				6.59		7				11.06		5.668

		6.62		13.5				6.62		13.5				6.62		18.5				6.62		4				11.08		6.0014

		6.65		11				6.65		11				6.65		11.5				6.65		8.5				11.1		7.6685

		6.68		18.5				6.68		18.5				6.68		16				6.68		3.5				11.12		7.6685

		6.71		15				6.71		15				6.71		17.5				6.71		6				11.14		5.3346

		6.74		15				6.74		15				6.74		12				6.74		7				11.16		4.3344

		6.77		11.5				6.77		11.5				6.77		8				6.77		4.5				11.18		4.001

		6.8		19.5				6.8		19.5				6.8		16				6.8		7.5				11.2		5.0012

		6.83		15.5				6.83		15.5				6.83		15.5				6.83		6				11.22		7.0017

		6.86		19				6.86		19				6.86		8.5				6.86		6				11.24		6.6683

		6.89		13				6.89		13				6.89		14				6.89		8.5				11.26		6.0014

		6.92		17				6.92		17				6.92		14				6.92		6				11.28		7.0017

		6.95		17				6.95		17				6.95		17				6.95		4				11.3		5.668

		6.98		12.5				6.98		12.5				6.98		13				6.98		6				11.32		4.6678

		7.01		13				7.01		13				7.01		15				7.01		5.5				11.34		5.3346

		7.04		12.5				7.04		12.5				7.04		10				7.04		4.5				11.36		6.0014

		7.07		16				7.07		16				7.07		15				7.07		4.5				11.38		6.6683

		7.1		13				7.1		13				7.1		9.5				7.1		3				11.4		2.6673

		7.13		18.5				7.13		18.5				7.13		14.5				7.13		6.5				11.42		5.668

		7.16		11.5				7.16		11.5				7.16		14.5				7.16		4				11.44		5.668

		7.19		11.5				7.19		11.5				7.19		10.5				7.19		6.5				11.46		4.6678

		7.22		14.5				7.22		14.5				7.22		13.5				7.22		7				11.48		3.6675

		7.25		12.5				7.25		12.5				7.25		12.5				7.25		7				11.5		7.0017

		7.28		14				7.28		14				7.28		10.5				7.28		5.5				11.52		3.3341

		7.31		9				7.31		9				7.31		16.5				7.31		7.5				11.54		5.668

		7.34		13.5				7.34		13.5				7.34		12				7.34		5				11.56		5.3346

		7.37		15.5				7.37		15.5				7.37		12.5				7.37		7.5				11.58		4.6678

		7.4		13				7.4		13				7.4		16				7.4		3.5				11.6		5.668

		7.43		15.5				7.43		15.5				7.43		11.5				7.43		3				11.62		3.3341

		7.46		17.5				7.46		17.5				7.46		12				7.46		4.5				11.64		4.3344

		7.49		19				7.49		19				7.49		15				7.49		6.5				11.66		5.0012

		7.52		6				7.52		6				7.52		19				7.52		5				11.68		5.668

		7.55		10.5				7.55		10.5				7.55		14.5				7.55		3.5				11.7		5.3346

		7.58		14.5				7.58		14.5				7.58		9.5				7.58		8				11.72		7.6685

		7.61		15.5				7.61		15.5				7.61		13.5				7.61		6.5				11.74		4.001

		7.64		17				7.64		17				7.64		11.5				7.64		7				11.76		7.0017

		7.67		13.5				7.67		13.5				7.67		14				7.67		3.5				11.78		5.0012

		7.7		9.5				7.7		9.5				7.7		10				7.7		3.5				11.8		4.6678

		7.73		13				7.73		13				7.73		13				7.73		7.5				11.82		3.3341

		7.76		12				7.76		12				7.76		11.5				7.76		7				11.84		4.6678

		7.79		11				7.79		11				7.79		17				7.79		6.5				11.86		3.0007

		7.82		17.5				7.82		17.5				7.82		12				7.82		4				11.88		8.3353

		7.85		11				7.85		11				7.85		12				7.85		5.5				11.9		6.3349

		7.88		11.5				7.88		11.5				7.88		14				7.88		4.5				11.92		5.0012

		7.91		13				7.91		13				7.91		14.5				7.91		5				11.94		4.3344

		7.94		8.5				7.94		8.5				7.94		12.5				7.94		3.5				11.96		7.6685

		7.97		9				7.97		9				7.97		15.5				7.97		5				11.98		5.3346

		8		9				8		9				8		17.5				8		5				12		4.001

		8.03		13.5				8.03		13.5				8.03		14				8.03		3				12.02		4.001

		8.06		13				8.06		13				8.06		10				8.06		5				12.04		4.3344

		8.09		9				8.09		9				8.09		11				8.09		7				12.06		6.3349

		8.12		14				8.12		14				8.12		14				8.12		7				12.08		5.668

		8.15		16				8.15		16				8.15		14				8.15		1.5				12.1		5.0012

		8.18		11.5				8.18		11.5				8.18		15				8.18		5.5				12.12		4.001

		8.21		12.5				8.21		12.5				8.21		12.5				8.21		2				12.14		3.6675

		8.24		11				8.24		11				8.24		11.5				8.24		3				12.16		4.6678

		8.27		12.5				8.27		12.5				8.27		12.5				8.27		8.5				12.18		4.001

		8.3		10				8.3		10				8.3		10				8.3		5.5				12.2		4.6678

		8.33		11				8.33		11				8.33		14.5				8.33		5				12.22		3.6675

		8.36		11				8.36		11				8.36		11.5				8.36		6.5				12.24		3.6675

		8.39		15.5				8.39		15.5				8.39		11.5				8.39		2				12.26		3.0007

		8.42		12				8.42		12				8.42		11				8.42		4				12.28		6.3349

		8.45		12.5				8.45		12.5				8.45		11.5				8.45		6				12.3		4.001

		8.48		17.5				8.48		17.5				8.48		12				8.48		4.5				12.32		3.0007

		8.51		13				8.51		13				8.51		11				8.51		3.5				12.34		3.6675

		8.54		13				8.54		13				8.54		10				8.54		6				12.36		4.3344

		8.57		10.5				8.57		10.5				8.57		15.5				8.57		4				12.38		5.3346

		8.6		15.5				8.6		15.5				8.6		16				8.6		6				12.4		4.001

		8.63		13.5				8.63		13.5				8.63		13.5				8.63		3.5				12.42		4.001

		8.66		10				8.66		10				8.66		10				8.66		2				12.44		4.3344

		8.69		14.5				8.69		14.5				8.69		10.5				8.69		4.5				12.46		6.0014

		8.72		15				8.72		15				8.72		12.5				8.72		2				12.48		6.3349

		8.75		7				8.75		7				8.75		12.5				8.75		2.5				12.5		5.0012

		8.78		11				8.78		11				8.78		10.5				8.78		4				12.52		3.6675

		8.81		14				8.81		14				8.81		12.5				8.81		3.5				12.54		4.3344

		8.84		13				8.84		13				8.84		12				8.84		4				12.56		4.001

		8.87		17				8.87		17				8.87		13.5				8.87		4				12.58		4.3344

		8.9		12.5				8.9		12.5				8.9		14				8.9		4				12.6		5.668

		8.93		10.5				8.93		10.5				8.93		15.5				8.93		4				12.62		5.668

		8.96		12				8.96		12				8.96		10.5				8.96		3.5				12.64		3.3341

		8.99		9.5				8.99		9.5				8.99		14				8.99		4				12.66		4.3344

		9.02		8.5				9.02		8.5				9.02		13				9.02		3				12.68		4.001

		9.05		11.5				9.05		11.5				9.05		11.5				9.05		3.5				12.7		2.3339

		9.08		12				9.08		12				9.08		14.5				9.08		3				12.72		4.3344

		9.11		12.5				9.11		12.5				9.11		12				9.11		4				12.74		4.6678

		9.14		15				9.14		15				9.14		13.5				9.14		1.5				12.76		3.0007

		9.17		13.5				9.17		13.5				9.17		13.5				9.17		1.5				12.78		5.3346

		9.2		14.5				9.2		14.5				9.2		10.5				9.2		5				12.8		2.3339

		9.23		8.5				9.23		8.5				9.23		9.5				9.23		2.5				12.82		4.6678

		9.26		11.5				9.26		11.5				9.26		18				9.26		3.5				12.84		5.3346

		9.29		12				9.29		12				9.29		15.5				9.29		2.5				12.86		5.0012

		9.32		12.5				9.32		12.5				9.32		11.5				9.32		4.5				12.88		5.3346

		9.35		11.5				9.35		11.5				9.35		10.5				9.35		3.5				12.9		4.3344

		9.38		10				9.38		10				9.38		11				9.38		4				12.92		6.0014

		9.41		8				9.41		8				9.41		13				9.41		2				12.94		6.3349

		9.44		13				9.44		13				9.44		12.5				9.44		2.5				12.96		5.0012

		9.47		15.5				9.47		15.5				9.47		13				9.47		4				12.98		5.668

		9.5		10.5				9.5		10.5				9.5		16				9.5		2.5				13		5.3346

		9.53		8				9.53		8				9.53		15				9.53		3				13.02		5.0012

		9.56		8.5				9.56		8.5				9.56		15				9.56		4.5				13.04		4.6678

		9.59		10				9.59		10				9.59		12				9.59		5.5				13.06		5.668

		9.62		10.5				9.62		10.5				9.62		12.5				9.62		4				13.08		6.0014

		9.65		8				9.65		8				9.65		14				9.65		2				13.1		5.0012

		9.68		7				9.68		7				9.68		16.5				9.68		3.5				13.12		4.3344

		9.71		9.5				9.71		9.5				9.71		13.5				9.71		2.5				13.14		6.0014

		9.74		9				9.74		9				9.74		10.5				9.74		1				13.16		6.3349

		9.77		13				9.77		13				9.77		14.5				9.77		3.5				13.18		4.3344

		9.8		13.5				9.8		13.5				9.8		11				9.8		2				13.2		7.0017

		9.83		9.5				9.83		9.5				9.83		14				9.83		2.5				13.22		5.0012

		9.86		8.5				9.86		8.5				9.86		10				9.86		2.5				13.24		8.0019

		9.89		9				9.89		9				9.89		10.5				9.89		5				13.26		3.3341

		9.92		9.5				9.92		9.5				9.92		13.5				9.92		1.5				13.28		6.6683

		9.95		12.5				9.95		12.5				9.95		12.5				9.95		3.5				13.3		3.3341

		9.98		13.5				9.98		13.5				9.98		14.5				9.98		1.5				13.32		5.0012

		10.01		10.5				10.01		10.5				10.01		14.5				10.01		2.5				13.34		7.6685

		10.04		12.5				10.04		12.5				10.04		13				10.04		1.5				13.36		4.001

		10.07		12				10.07		12				10.07		9.5				10.07		1.5				13.38		4.6678

		10.1		10.5				10.1		10.5				10.1		13				10.1		1.5				13.4		6.6683

		10.13		8				10.13		8				10.13		10.5				10.13		3.5				13.42		5.0012

		10.16		8				10.16		8				10.16		10.5				10.16		3.5				13.44		3.3341

		10.19		8.5				10.19		8.5				10.19		14				10.19		2.5				13.46		4.001

		10.22		7.5				10.22		7.5				10.22		13.5				10.22		2.5				13.48		5.3346

		10.25		10				10.25		10				10.25		9				10.25		2.5				13.5		3.3341

		10.28		10.5				10.28		10.5				10.28		10.5				10.28		2				13.52		4.6678

		10.31		11.5				10.31		11.5				10.31		15				10.31		2				13.54		3.6675

		10.34		11				10.34		11				10.34		13				10.34		4				13.56		5.3346

		10.37		11				10.37		11				10.37		13.5				10.37		4				13.58		4.3344

		10.4		3.5				10.4		3.5				10.4		12				10.4		1.5				13.6		5.3346

		10.43		10.5				10.43		10.5				10.43		11				10.43		2.5				13.62		4.6678

		10.46		10.5				10.46		10.5				10.46		15				10.46		3.5				13.64		3.6675

		10.49		14.5				10.49		14.5				10.49		12				10.49		2				13.66		3.0007

		10.52		9				10.52		9				10.52		12				10.52		1.5				13.68		5.668

		10.55		10.5				10.55		10.5				10.55		11				10.55		1.5				13.7		5.668

		10.58		10				10.58		10				10.58		12				10.58		3				13.72		7.0017

		10.61		8.5				10.61		8.5				10.61		12				10.61		3				13.74		4.3344

		10.64		9				10.64		9				10.64		12				10.64		3.5				13.76		4.6678

		10.67		16.5				10.67		16.5				10.67		13.5				10.67		3				13.78		3.0007

		10.7		13				10.7		13				10.7		13.5				10.7		4.5				13.8		5.3346

		10.73		10				10.73		10				10.73		12				10.73		4.5				13.82		3.6675

		10.76		13				10.76		13				10.76		13.5				10.76		3.5				13.84		5.0012

		10.79		6.5				10.79		6.5				10.79		8				10.79		2				13.86		3.6675

		10.82		11.5				10.82		11.5				10.82		12				10.82		4				13.88		4.001

		10.85		14				10.85		14				10.85		9.5				10.85		3.5				13.9		4.001

		10.88		9.5				10.88		9.5				10.88		14				10.88		1				13.92		2.3339

		10.91		14				10.91		14				10.91		14				10.91		3.5				13.94		4.6678

		10.94		13				10.94		13				10.94		11.5				10.94		3				13.96		7.6685

		10.97		10				10.97		10				10.97		16.5				10.97		2				13.98		8.6687

		11		10.5				11		10.5				11		11.5				11		2.5				14		4.6678

		11.03		12.5				11.03		12.5				11.03		9.5				11.03		0.5				14.02		4.6678

		11.06		7				11.06		7				11.06		12				11.06		2				14.04		3.6675

		11.09		12				11.09		12				11.09		16				11.09		2				14.06		4.001

		11.12		12				11.12		12				11.12		11.5				11.12		1.5				14.08		5.3346

		11.15		9				11.15		9				11.15		18.5				11.15		4				14.1		5.3346

		11.18		8.5				11.18		8.5				11.18		15				11.18		1.5				14.12		6.0014

		11.21		10				11.21		10				11.21		14				11.21		5				14.14		6.0014

		11.24		17.5				11.24		17.5				11.24		12.5				11.24		1				14.16		5.668

		11.27		14.5				11.27		14.5				11.27		15				11.27		3.5				14.18		6.0014

		11.3		6				11.3		6				11.3		17.5				11.3		0				14.2		4.001

		11.33		11.5				11.33		11.5				11.33		11.5				11.33		2				14.22		4.6678

		11.36		7.5				11.36		7.5				11.36		11.5				11.36		3.5				14.24		4.3344

		11.39		12.5				11.39		12.5				11.39		11.5				11.39		3				14.26		5.3346

		11.42		7				11.42		7				11.42		16				11.42		2				14.28		5.668

		11.45		9.5				11.45		9.5				11.45		11				11.45		3.5				14.3		4.6678

		11.48		15.5				11.48		15.5				11.48		15				11.48		1.5				14.32		8.3353

		11.51		13.5				11.51		13.5				11.51		12				11.51		4				14.34		4.6678

		11.54		12.5				11.54		12.5				11.54		10				11.54		1.5				14.36		5.0012

		11.57		7				11.57		7				11.57		15				11.57		1				14.38		3.6675

		11.6		9				11.6		9				11.6		12.5				11.6		3.5				14.4		4.3344

		11.63		9				11.63		9				11.63		12.5				11.63		2.5				14.42		7.0017

		11.66		10.5				11.66		10.5				11.66		12				11.66		1				14.44		6.3349

		11.69		8.5				11.69		8.5				11.69		16.5				11.69		2				14.46		5.3346

		11.72		6.5				11.72		6.5				11.72		13				11.72		2				14.48		4.6678

		11.75		7.5				11.75		7.5				11.75		16.5				11.75		2.5				14.5		5.0012

		11.78		10.5				11.78		10.5				11.78		13				11.78		2				14.52		6.0014

		11.81		9.5				11.81		9.5				11.81		12.5				11.81		2				14.54		5.3346

		11.84		10				11.84		10				11.84		10				11.84		1.5				14.56		5.0012

		11.87		6.5				11.87		6.5				11.87		16				11.87		1.5				14.58		4.3344

		11.9		7.5				11.9		7.5				11.9		12.5				11.9		2				14.6		5.3346

		11.93		13				11.93		13				11.93		15.5				11.93		1.5				14.62		4.3344

		11.96		13.5				11.96		13.5				11.96		18.5				11.96		3				14.64		7.6685

		11.99		10				11.99		10				11.99		11				11.99		1				14.66		5.668

		12.02		8				12.02		8				12.02		14				12.02		1.5				14.68		3.6675

		12.05		10.5				12.05		10.5				12.05		11				12.05		0.5				14.7		5.0012

		12.08		9.5				12.08		9.5				12.08		17				12.08		1.5				14.72		4.3344

		12.11		8.5				12.11		8.5				12.11		16.5				12.11		1				14.74		4.3344

		12.14		10.5				12.14		10.5				12.14		16				12.14		3				14.76		5.3346

		12.17		9.5				12.17		9.5				12.17		11.5				12.17		2.5				14.78		5.3346

		12.2		13.5				12.2		13.5				12.2		13.5				12.2		3				14.8		4.001

		12.23		7.5				12.23		7.5				12.23		8.5				12.23		1				14.82		5.0012

		12.26		11.5				12.26		11.5				12.26		12				12.26		2.5				14.84		3.0007

		12.29		12.5				12.29		12.5				12.29		17				12.29		2				14.86		4.001

		12.32		12				12.32		12				12.32		20.5				12.32		0.5				14.88		7.6685

		12.35		12				12.35		12				12.35		13				12.35		1.5				14.9		3.3341

		12.38		11				12.38		11				12.38		7.5				12.38		1				14.92		5.668

		12.41		13				12.41		13				12.41		15.5				12.41		1.5				14.94		5.0012

		12.44		9.5				12.44		9.5				12.44		14				12.44		1.5				14.96		4.001

		12.47		7.5				12.47		7.5				12.47		15.5				12.47		2.5				14.98		7.3351

		12.5		10.5				12.5		10.5				12.5		12.5				12.5		0.5				15		6.0014

		12.53		9				12.53		9				12.53		18.5				12.53		3				15.02		4.001

		12.56		14				12.56		14				12.56		14				12.56		3				15.04		3.3341

		12.59		11.5				12.59		11.5				12.59		7.5				12.59		1				15.06		5.668

		12.62		12				12.62		12				12.62		8				12.62		3				15.08		3.6675

		12.65		11				12.65		11				12.65		16.5				12.65		2				15.1		5.0012

		12.68		10				12.68		10				12.68		13.5				12.68		2.5				15.12		3.6675

		12.71		14				12.71		14				12.71		18				12.71		1.5				15.14		2.6673

		12.74		9				12.74		9				12.74		14				12.74		3				15.16		5.668

		12.77		5.5				12.77		5.5				12.77		19				12.77		1.5				15.18		3.3341

		12.8		7.5				12.8		7.5				12.8		16				12.8		2				15.2		9.0022

		12.83		12.5				12.83		12.5				12.83		13				12.83		2.5				15.22		5.668

		12.86		12				12.86		12				12.86		14				12.86		1.5				15.24		3.3341

		12.89		10				12.89		10				12.89		14				12.89		2.5				15.26		5.3346

		12.92		15				12.92		15				12.92		12				12.92		1.5				15.28		5.3346

		12.95		8.5				12.95		8.5				12.95		15.5				12.95		3				15.3		5.668

		12.98		17				12.98		17				12.98		12				12.98		0.5				15.32		4.001

		13.01		11				13.01		11				13.01		11				13.01		2				15.34		4.6678

		13.04		19.5				13.04		19.5				13.04		18.5				13.04		1.5				15.36		5.0012

		13.07		15.5				13.07		15.5				13.07		17.5				13.07		2				15.38		3.3341

		13.1		14				13.1		14				13.1		16.5				13.1		6.5				15.4		2.6673

		13.13		9.5				13.13		9.5				13.13		19.5				13.13		3				15.42		5.0012

		13.16		12.5				13.16		12.5				13.16		9.5				13.16		1.5				15.44		4.001

		13.19		12.5				13.19		12.5				13.19		13.5				13.19		3				15.46		4.001

		13.22		9.5				13.22		9.5				13.22		14				13.22		1.5				15.48		5.3346

		13.25		13				13.25		13				13.25		13				13.25		2				15.5		3.3341

		13.28		10.5				13.28		10.5				13.28		14.5				13.28		3				15.52		4.3344

		13.31		7.5				13.31		7.5				13.31		14				13.31		0.5				15.54		5.0012

		13.34		11				13.34		11				13.34		13.5				13.34		0.5				15.56		3.6675

		13.37		12				13.37		12				13.37		14.5				13.37		1				15.58		7.3351

		13.4		11.5				13.4		11.5				13.4		14				13.4		2				15.6		4.6678

		13.43		10				13.43		10				13.43		14				13.43		0.5				15.62		5.668

		13.46		8.5				13.46		8.5				13.46		7.5				13.46		2				15.64		4.3344

		13.49		8.5				13.49		8.5				13.49		12.5				13.49		3.5				15.66		3.6675

		13.52		6.5				13.52		6.5				13.52		13.5				13.52		1				15.68		4.001

		13.55		9.5				13.55		9.5				13.55		17				13.55		1				15.7		6.3349

		13.58		9.5				13.58		9.5				13.58		15.5				13.58		2.5				15.72		7.0017

		13.61		10				13.61		10				13.61		19				13.61		2				15.74		6.3349

		13.64		14.5				13.64		14.5				13.64		22				13.64		0.5				15.76		5.3346

		13.67		10				13.67		10				13.67		13.5				13.67		2				15.78		4.6678

		13.7		10				13.7		10				13.7		14				13.7		3.5				15.8		8.3353

		13.73		14				13.73		14				13.73		9.5				13.73		2.5				15.82		5.668

		13.76		9				13.76		9				13.76		11				13.76		1.5				15.84		4.3344

		13.79		7.5				13.79		7.5				13.79		17				13.79		0.5				15.86		4.3344

		13.82		7				13.82		7				13.82		11				13.82		0.5				15.88		5.3346

		13.85		5.5				13.85		5.5				13.85		10.5				13.85		4.5				15.9		5.0012

		13.88		8.5				13.88		8.5				13.88		14				13.88		3				15.92		4.3344

		13.91		10				13.91		10				13.91		8.5				13.91		2.5				15.94		4.6678

		13.94		5.5				13.94		5.5				13.94		16				13.94		2				15.96		5.3346

		13.97		9				13.97		9				13.97		10				13.97		2				15.98		4.3344

		14		9				14		9				14		10.5				14		1.5				16		9.0022

		14.03		11.5				14.03		11.5				14.03		11				14.03		2.5				16.02		4.001

		14.06		9.5				14.06		9.5				14.06		10.5				14.06		1				16.04		3.0007

		14.09		11				14.09		11				14.09		13				14.09		1.5				16.06		7.6685

		14.12		7				14.12		7				14.12		11				14.12		1				16.08		7.6685

		14.15		12.5				14.15		12.5				14.15		8				14.15		1.5				16.1		4.6678

		14.18		12				14.18		12				14.18		16				14.18		1				16.12		7.6685

		14.21		10.5				14.21		10.5				14.21		13.5				14.21		2.5				16.14		4.6678

		14.24		7				14.24		7				14.24		9.5				14.24		1.5				16.16		6.6683

		14.27		7.5				14.27		7.5				14.27		15.5				14.27		3				16.18		4.3344

		14.3		12.5				14.3		12.5				14.3		10.5				14.3		2				16.2		4.001

		14.33		9.5				14.33		9.5				14.33		18				14.33		1				16.22		7.6685

		14.36		9				14.36		9				14.36		9				14.36		2				16.24		3.6675

		14.39		9.5				14.39		9.5				14.39		9.5				14.39		2				16.26		5.3346

		14.42		6				14.42		6				14.42		11				14.42		2				16.28		5.3346

		14.45		12				14.45		12				14.45		14				14.45		4				16.3		4.001

		14.48		10				14.48		10				14.48		9				14.48		4				16.32		4.3344

		14.51		12				14.51		12				14.51		12				14.51		1				16.34		5.0012

		14.54		6.5				14.54		6.5				14.54		12.5				14.54		1				16.36		4.3344

		14.57		12.5				14.57		12.5				14.57		11				14.57		1.5				16.38		5.3346

		14.6		9				14.6		9				14.6		12				14.6		1.5				16.4		7.3351

		14.63		10				14.63		10				14.63		14				14.63		0				16.42		6.6683

		14.66		8.5				14.66		8.5				14.66		16				14.66		2				16.44		3.3341

		14.69		12				14.69		12				14.69		13.5				14.69		2				16.46		3.6675

		14.72		8				14.72		8				14.72		11.5				14.72		1				16.48		4.001

		14.75		9				14.75		9				14.75		7				14.75		1				16.5		4.6678

		14.78		6.5				14.78		6.5				14.78		14				14.78		3.5				16.52		6.0014

		14.81		7				14.81		7				14.81		15				14.81		1.5				16.54		5.3346

		14.84		11.5				14.84		11.5				14.84		16				14.84		1				16.56		6.6683

		14.87		10				14.87		10				14.87		12.5				14.87		1				16.58		6.0014

		14.9		10.5				14.9		10.5				14.9		14.5				14.9		4				16.6		5.3346

		14.93		9.5				14.93		9.5				14.93		9.5				14.93		2				16.62		6.0014

		14.96		10.5				14.96		10.5				14.96		12.5				14.96		1.5				16.64		5.3346

		14.99		6				14.99		6				14.99		19				14.99		1.5				16.66		5.3346

		15.02		10.5				15.02		10.5				15.02		15				15.02		1.5				16.68		3.3341

		15.05		10				15.05		10				15.05		13				15.05		2.5				16.7		6.6683

		15.08		9				15.08		9				15.08		18				15.08		1				16.72		4.001

		15.11		12				15.11		12				15.11		13.5				15.11		3				16.74		4.3344

		15.14		13.5				15.14		13.5				15.14		12.5				15.14		1.5				16.76		5.668

		15.17		9.5				15.17		9.5				15.17		16				15.17		1.5				16.78		6.3349

		15.2		12				15.2		12				15.2		13				15.2		3				16.8		4.6678

		15.23		9				15.23		9				15.23		9.5				15.23		0.5				16.82		5.0012

		15.26		9				15.26		9				15.26		11.5				15.26		2				16.84		5.3346

		15.29		7.5				15.29		7.5				15.29		14				15.29		1.5				16.86		5.668

		15.32		9				15.32		9				15.32		16				15.32		2.5				16.88		5.3346

		15.35		9				15.35		9				15.35		6.5				15.35		3				16.9		6.0014

		15.38		10				15.38		10				15.38		17.5				15.38		1				16.92		5.3346

		15.41		5				15.41		5				15.41		9.5				15.41		0.5				16.94		2.6673

		15.44		7				15.44		7				15.44		14				15.44		1				16.96		5.668

		15.47		8				15.47		8				15.47		12				15.47		2				16.98		3.0007

		15.5		10.5				15.5		10.5				15.5		15.5				15.5		1				17		5.3346

		15.53		7.5				15.53		7.5				15.53		11				15.53		1				17.02		6.0014

		15.56		8				15.56		8				15.56		11.5				15.56		1				17.04		6.0014

		15.59		7				15.59		7				15.59		11.5				15.59		0.5				17.06		5.668

		15.62		5				15.62		5				15.62		7.5				15.62		1.5				17.08		4.001

		15.65		6.5				15.65		6.5				15.65		15.5				15.65		3				17.1		3.6675

		15.68		6.5				15.68		6.5				15.68		17.5				15.68		0.5				17.12		4.6678

		15.71		7				15.71		7				15.71		8.5				15.71		3.5				17.14		4.6678

		15.74		10.5				15.74		10.5				15.74		10				15.74		0				17.16		4.001

		15.77		6.5				15.77		6.5				15.77		4.5				15.77		1.5				17.18		4.001

		15.8		10.5				15.8		10.5				15.8		12.5				15.8		1				17.2		5.3346

		15.83		9				15.83		9				15.83		12.5				15.83		4.5				17.22		2.0005

		15.86		7				15.86		7				15.86		9				15.86		0.5				17.24		5.668

		15.89		7.5				15.89		7.5				15.89		13				15.89		1.5				17.26		6.3349

		15.92		7				15.92		7				15.92		10				15.92		1.5				17.28		5.3346

		15.95		9.5				15.95		9.5				15.95		12				15.95		1				17.3		4.001

		15.98		11				15.98		11				15.98		11.5				15.98		4.5				17.32		5.3346

		16.01		9.5				16.01		9.5				16.01		10.5				16.01		2				17.34		5.0012

		16.04		8.5				16.04		8.5				16.04		10				16.04		1.5				17.36		6.0014

		16.07		8.5				16.07		8.5				16.07		11.5				16.07		2				17.38		6.6683

		16.1		9				16.1		9				16.1		12				16.1		1.5				17.4		5.3346

		16.13		5				16.13		5				16.13		11				16.13		1.5				17.42		6.6683

		16.16		5.5				16.16		5.5				16.16		9				16.16		0				17.44		6.0014

		16.19		7.5				16.19		7.5				16.19		7.5				16.19		0.5				17.46		4.3344

		16.22		8.5				16.22		8.5				16.22		10.5				16.22		1				17.48		4.6678

		16.25		9				16.25		9				16.25		12.5				16.25		1				17.5		7.6685

		16.28		10				16.28		10				16.28		4.5				16.28		1				17.52		7.0017

		16.31		6				16.31		6				16.31		11.5				16.31		2				17.54		7.6685

		16.34		12				16.34		12				16.34		11.5				16.34		1.5				17.56		6.3349

		16.37		8.5				16.37		8.5				16.37		7				16.37		1				17.58		6.3349

		16.4		7.5				16.4		7.5				16.4		9				16.4		1				17.6		8.0019

		16.43		10				16.43		10				16.43		8.5				16.43		1				17.62		9.0022

		16.46		7				16.46		7				16.46		13.5				16.46		1				17.64		12.003

		16.49		4				16.49		4				16.49		10.5				16.49		1				17.66		24.673

		16.52		9				16.52		9				16.52		6				16.52		3				17.68		50.012

		16.55		5.5				16.55		5.5				16.55		8				16.55		2				17.7		93.022

		16.58		10				16.58		10				16.58		13				16.58		1.5				17.72		232.72

		16.61		10				16.61		10				16.61		16.5				16.61		1				17.74		362.09

		16.64		6.5				16.64		6.5				16.64		5.5				16.64		2				17.76		445.77

		16.67		10				16.67		10				16.67		8				16.67		2				17.78		340.08

		16.7		7.5				16.7		7.5				16.7		11.5				16.7		1.5				17.8		239.72

		16.73		9.5				16.73		9.5				16.73		10.5				16.73		3				17.82		129.36

		16.76		10.5				16.76		10.5				16.76		8				16.76		2				17.84		54.346

		16.79		9				16.79		9				16.79		12.5				16.79		2				17.86		17.004

		16.82		15				16.82		15				16.82		15				16.82		1				17.88		19.338

		16.85		10.5				16.85		10.5				16.85		14.5				16.85		1.5				17.9		16.671

		16.88		15.5				16.88		15.5				16.88		17				16.88		0.5				17.92		12.003

		16.91		19				16.91		19				16.91		14				16.91		3				17.94		12.003

		16.94		11				16.94		11				16.94		19				16.94		2				17.96		9.669

		16.97		13.5				16.97		13.5				16.97		8				16.97		7				17.98		8.6687

		17		7				17		7				17		13				17		3.5				18		7.0017

		17.03		12.5				17.03		12.5				17.03		8				17.03		3.5				18.02		8.0019

		17.06		7.5				17.06		7.5				17.06		13				17.06		3.5				18.04		5.668

		17.09		8				17.09		8				17.09		9.5				17.09		1.5				18.06		7.0017

		17.12		7.5				17.12		7.5				17.12		12.5				17.12		2.5				18.08		6.3349

		17.15		10				17.15		10				17.15		16				17.15		3				18.1		6.6683

		17.18		10				17.18		10				17.18		8.5				17.18		2				18.12		6.0014

		17.21		6.5				17.21		6.5				17.21		11.5				17.21		2				18.14		4.6678

		17.24		11				17.24		11				17.24		12				17.24		1				18.16		6.3349

		17.27		11.5				17.27		11.5				17.27		15				17.27		1				18.18		7.3351

		17.3		15.5				17.3		15.5				17.3		14.5				17.3		1				18.2		5.0012

		17.33		16				17.33		16				17.33		12				17.33		1				18.22		5.3346

		17.36		14.5				17.36		14.5				17.36		9.5				17.36		1.5				18.24		4.001

		17.39		18.5				17.39		18.5				17.39		16				17.39		1.5				18.26		3.3341

		17.42		33.5				17.42		33.5				17.42		25				17.42		4				18.28		5.0012

		17.45		32				17.45		32				17.45		29				17.45		2				18.3		4.6678

		17.48		41.5				17.48		41.5				17.48		43.5				17.48		3				18.32		5.3346

		17.51		55.5				17.51		55.5				17.51		54.5				17.51		1.5				18.34		5.3346

		17.54		79				17.54		79				17.54		64				17.54		4				18.36		4.001

		17.57		118				17.57		118				17.57		87.5				17.57		3				18.38		4.3344

		17.6		137				17.6		137				17.6		113				17.6		19				18.4		8.6687

		17.63		97.5				17.63		97.5				17.63		104				17.63		29.5				18.42		6.6683

		17.66		59				17.66		59				17.66		95.5				17.66		55				18.44		5.3346

		17.69		40.5				17.69		40.5				17.69		64				17.69		83				18.46		3.3341

		17.72		17.5				17.72		17.5				17.72		27				17.72		54.5				18.48		6.3349

		17.75		14				17.75		14				17.75		14.5				17.75		24				18.5		3.3341

		17.78		10.5				17.78		10.5				17.78		11				17.78		8.5				18.52		7.3351

		17.81		6				17.81		6				17.81		10.5				17.81		2.5				18.54		5.3346

		17.84		7				17.84		7				17.84		12.5				17.84		1.5				18.56		6.0014

		17.87		14.5				17.87		14.5				17.87		11.5				17.87		2.5				18.58		4.6678

		17.9		7				17.9		7				17.9		8				17.9		1.5				18.6		8.0019

		17.93		13				17.93		13				17.93		7.5				17.93		3				18.62		7.6685

		17.96		9				17.96		9				17.96		8.5				17.96		2				18.64		5.668

		17.99		6.5				17.99		6.5				17.99		12.5				17.99		1				18.66		3.6675

		18.02		12				18.02		12				18.02		11.5				18.02		1				18.68		5.0012

		18.05		6.5				18.05		6.5				18.05		9.5				18.05		1.5				18.7		7.0017

		18.08		8				18.08		8				18.08		6.5				18.08		2.5				18.72		4.3344

		18.11		9.5				18.11		9.5				18.11		10.5				18.11		0.5				18.74		4.6678

		18.14		8				18.14		8				18.14		12				18.14		0.5				18.76		7.0017

		18.17		10.5				18.17		10.5				18.17		7				18.17		0.5				18.78		5.3346

		18.2		5				18.2		5				18.2		9.5				18.2		1.5				18.8		6.0014

		18.23		8				18.23		8				18.23		9				18.23		2.5				18.82		5.668

		18.26		8				18.26		8				18.26		7				18.26		1.5				18.84		3.3341

		18.29		6				18.29		6				18.29		11.5				18.29		1.5				18.86		4.001

		18.32		4				18.32		4				18.32		9.5				18.32		2				18.88		4.6678

		18.35		8				18.35		8				18.35		4.5				18.35		1				18.9		6.6683

		18.38		5.5				18.38		5.5				18.38		8.5				18.38		2				18.92		6.0014

		18.41		6				18.41		6				18.41		5				18.41		0.5				18.94		4.6678

		18.44		6.5				18.44		6.5				18.44		10.5				18.44		1.5				18.96		6.6683

		18.47		6.5				18.47		6.5				18.47		12.5				18.47		2.5				18.98		4.3344

		18.5		6.5				18.5		6.5				18.5		9.5				18.5		3				19		5.0012

		18.53		3.5				18.53		3.5				18.53		10				18.53		0.5				19.02		4.3344

		18.56		6.5				18.56		6.5				18.56		8				18.56		0.5				19.04		4.3344

		18.59		4.5				18.59		4.5				18.59		11.5				18.59		0.5				19.06		5.3346

		18.62		7				18.62		7				18.62		8				18.62		1				19.08		4.001

		18.65		8				18.65		8				18.65		10.5				18.65		0.5				19.1		3.3341

		18.68		6.5				18.68		6.5				18.68		9				18.68		2				19.12		5.3346

		18.71		11				18.71		11				18.71		11				18.71		0.5				19.14		6.0014

		18.74		5.5				18.74		5.5				18.74		8.5				18.74		1.5				19.16		5.0012

		18.77		7				18.77		7				18.77		7.5				18.77		2				19.18		5.3346

		18.8		7				18.8		7				18.8		7				18.8		2.5				19.2		3.6675

		18.83		8				18.83		8				18.83		7				18.83		2.5				19.22		3.6675

		18.86		4.5				18.86		4.5				18.86		7				18.86		1.5				19.24		6.3349

		18.89		3.5				18.89		3.5				18.89		7				18.89		1.5				19.26		5.0012

		18.92		5				18.92		5				18.92		6				18.92		1.5				19.28		3.3341

		18.95		4				18.95		4				18.95		9				18.95		1				19.3		3.0007

		18.98		4				18.98		4				18.98		9				18.98		1				19.32		5.668

		19.01		5				19.01		5				19.01		11				19.01		1				19.34		5.668

		19.04		5				19.04		5				19.04		7				19.04		1				19.36		4.3344

		19.07		6.5				19.07		6.5				19.07		12				19.07		0.5				19.38		5.0012

		19.1		3.5				19.1		3.5				19.1		8				19.1		0.5				19.4		2.6673

		19.13		6.5				19.13		6.5				19.13		9.5				19.13		1.5				19.42		6.3349

		19.16		4				19.16		4				19.16		8.5				19.16		0.5				19.44		6.6683

		19.19		5				19.19		5				19.19		12				19.19		3				19.46		3.3341

		19.22		4				19.22		4				19.22		7				19.22		1				19.48		6.6683

		19.25		6.5				19.25		6.5				19.25		8.5				19.25		0.5				19.5		9.0022

		19.28		4.5				19.28		4.5				19.28		12				19.28		2.5				19.52		11.003

		19.31		5				19.31		5				19.31		3.5				19.31		1				19.54		6.6683

		19.34		4.5				19.34		4.5				19.34		7.5				19.34		2				19.56		7.6685

		19.37		5.5				19.37		5.5				19.37		4.5				19.37		2				19.58		7.3351

		19.4		3.5				19.4		3.5				19.4		9				19.4		3				19.6		5.3346

		19.43		4.5				19.43		4.5				19.43		3.5				19.43		2				19.62		5.3346

		19.46		6				19.46		6				19.46		6				19.46		2				19.64		5.0012

		19.49		6.5				19.49		6.5				19.49		9.5				19.49		1				19.66		3.6675

		19.52		5				19.52		5				19.52		4.5				19.52		3				19.68		5.3346

		19.55		6				19.55		6				19.55		8.5				19.55		1				19.7		5.0012

		19.58		5				19.58		5				19.58		5				19.58		1.5				19.72		6.6683

		19.61		9.5				19.61		9.5				19.61		5				19.61		0.5				19.74		3.6675

		19.64		3				19.64		3				19.64		5				19.64		0.5				19.76		5.3346

		19.67		7				19.67		7				19.67		7				19.67		2				19.78		4.3344

		19.7		8				19.7		8				19.7		9.5				19.7		2.5				19.8		5.3346

		19.73		5.5				19.73		5.5				19.73		5.5				19.73		1				19.82		7.6685

		19.76		7.5				19.76		7.5				19.76		4				19.76		1.5				19.84		4.6678

		19.79		12				19.79		12				19.79		7.5				19.79		1.5				19.86		4.001

		19.82		8				19.82		8				19.82		6				19.82		1				19.88		6.3349

		19.85		12				19.85		12				19.85		6				19.85		1				19.9		6.3349

		19.88		4				19.88		4				19.88		8.5				19.88		2.5				19.92		4.6678

		19.91		7				19.91		7				19.91		10				19.91		2.5				19.94		5.0012

		19.94		10				19.94		10				19.94		5.5				19.94		2				19.96		3.6675

		19.97		6				19.97		6				19.97		8				19.97		1				19.98		4.001

		20		5.5				20		5.5				20		11				20		0.5				20		7.6685

		20.03		6				20.03		6				20.03		6				20.03		2				20.02		4.3344

		20.06		8				20.06		8				20.06		6.5				20.06		0				20.04		3.0007

		20.09		6				20.09		6				20.09		4				20.09		2				20.06		6.3349

		20.12		6.5				20.12		6.5				20.12		5.5				20.12		0.5				20.08		8.6687

		20.15		6.5				20.15		6.5				20.15		4.5				20.15		1				20.1		5.3346

		20.18		6				20.18		6				20.18		8				20.18		1.5				20.12		5.668

		20.21		7.5				20.21		7.5				20.21		8.5				20.21		1				20.14		6.6683

		20.24		4				20.24		4				20.24		10				20.24		0.5				20.16		7.0017

		20.27		9				20.27		9				20.27		8.5				20.27		2.5				20.18		5.668

		20.3		9				20.3		9				20.3		8.5				20.3		1				20.2		5.668

		20.33		11				20.33		11				20.33		6				20.33		0				20.22		6.6683

		20.36		11				20.36		11				20.36		6.5				20.36		1				20.24		5.0012

		20.39		9				20.39		9				20.39		7				20.39		2				20.26		8.6687

		20.42		10.5				20.42		10.5				20.42		7.5				20.42		1				20.28		4.6678

		20.45		17.5				20.45		17.5				20.45		7.5				20.45		2				20.3		5.0012

		20.48		15				20.48		15				20.48		6.5				20.48		1				20.32		6.0014

		20.51		7				20.51		7				20.51		11				20.51		4.5				20.34		5.668

		20.54		11.5				20.54		11.5				20.54		7				20.54		3				20.36		4.3344

		20.57		14				20.57		14				20.57		10				20.57		0.5				20.38		6.6683

		20.6		14.5				20.6		14.5				20.6		17.5				20.6		2				20.4		7.6685

		20.63		20				20.63		20				20.63		10.5				20.63		1				20.42		4.6678

		20.66		21				20.66		21				20.66		16				20.66		3				20.44		4.6678

		20.69		26.5				20.69		26.5				20.69		22.5				20.69		1				20.46		4.3344

		20.72		47				20.72		47				20.72		30.5				20.72		3				20.48		3.3341

		20.75		62.5				20.75		62.5				20.75		46.5				20.75		1				20.5		4.3344

		20.78		87.5				20.78		87.5				20.78		59				20.78		1.5				20.52		4.001

		20.81		120.5				20.81		120.5				20.81		92.5				20.81		4				20.54		5.668

		20.84		166.5				20.84		166.5				20.84		128.5				20.84		11.5				20.56		6.0014

		20.87		179				20.87		179				20.87		168.5				20.87		18				20.58		4.6678

		20.9		145.5				20.9		145.5				20.9		180.5				20.9		39.5				20.6		4.6678

		20.93		89.5				20.93		89.5				20.93		177.5				20.93		88.5				20.62		5.0012

		20.96		51				20.96		51				20.96		106.5				20.96		183				20.64		3.3341

		20.99		19.5				20.99		19.5				20.99		56.5				20.99		102				20.66		8.3353

		21.02		13				21.02		13				21.02		23.5				21.02		82.5				20.68		7.3351

		21.05		13				21.05		13				21.05		12.5				21.05		16.5				20.7		6.0014

		21.08		6				21.08		6				21.08		6.5				21.08		4.5				20.72		8.6687

		21.11		11.5				21.11		11.5				21.11		10.5				21.11		6.5				20.74		4.001

		21.14		7.5				21.14		7.5				21.14		12				21.14		3				20.76		6.3349

		21.17		6				21.17		6				21.17		8.5				21.17		3.5				20.78		8.0019

		21.2		10				21.2		10				21.2		7.5				21.2		4.5				20.8		7.3351

		21.23		7.5				21.23		7.5				21.23		8.5				21.23		3				20.82		7.0017

		21.26		12				21.26		12				21.26		3.5				21.26		0				20.84		12.003

		21.29		7				21.29		7				21.29		9.5				21.29		0.5				20.86		11.003

		21.32		8				21.32		8				21.32		4.5				21.32		1.5				20.88		16.337

		21.35		6.5				21.35		6.5				21.35		6.5				21.35		2				20.9		24.006

		21.38		6.5				21.38		6.5				21.38		9				21.38		2				20.92		34.008

		21.41		7				21.41		7				21.41		7.5				21.41		1.5				20.94		37.676

		21.44		5				21.44		5				21.44		5.5				21.44		0.5				20.96		88.355

		21.47		6				21.47		6				21.47		3.5				21.47		1				20.98		110.36

		21.5		5.5				21.5		5.5				21.5		5				21.5		4				21		174.04

		21.53		6.5				21.53		6.5				21.53		5.5				21.53		2				21.02		351.75

		21.56		4.5				21.56		4.5				21.56		8.5				21.56		2.5				21.04		372.76

		21.59		8				21.59		8				21.59		6				21.59		1				21.06		219.72

		21.62		7				21.62		7				21.62		6.5				21.62		2				21.08		212.72

		21.65		6.5				21.65		6.5				21.65		7.5				21.65		1.5				21.1		136.7

		21.68		4				21.68		4				21.68		7				21.68		1				21.12		52.012

		21.71		6.5				21.71		6.5				21.71		8.5				21.71		2				21.14		24.006

		21.74		8.5				21.74		8.5				21.74		9.5				21.74		1.5				21.16		18.671

		21.77		6				21.77		6				21.77		5				21.77		2				21.18		14.67

		21.8		5				21.8		5				21.8		7				21.8		0.5				21.2		13.67

		21.83		3				21.83		3				21.83		4				21.83		1.5				21.22		13.003

		21.86		6				21.86		6				21.86		7				21.86		1				21.24		8.0019

		21.89		5.5				21.89		5.5				21.89		3.5				21.89		0.5				21.26		5.668

		21.92		7.5				21.92		7.5				21.92		4				21.92		0.5				21.28		5.3346

		21.95		3				21.95		3				21.95		6.5				21.95		2.5				21.3		10.336

		21.98		4.5				21.98		4.5				21.98		2				21.98		1				21.32		4.3344

		22.01		7.5				22.01		7.5				22.01		5.5				22.01		2				21.34		6.3349

		22.04		7.5				22.04		7.5				22.04		7				22.04		3				21.36		8.0019

		22.07		6				22.07		6				22.07		6				22.07		0				21.38		4.6678

		22.1		11				22.1		11				22.1		6				22.1		1.5				21.4		7.0017

		22.13		9				22.13		9				22.13		6				22.13		1.5				21.42		6.0014

		22.16		15				22.16		15				22.16		12				22.16		1				21.44		6.3349

		22.19		17				22.19		17				22.19		11				22.19		1				21.46		4.6678

		22.22		21				22.22		21				22.22		17				22.22		1				21.48		6.0014

		22.25		27				22.25		27				22.25		13.5				22.25		2				21.5		7.0017

		22.28		23.5				22.28		23.5				22.28		20				22.28		2				21.52		7.3351

		22.31		27.5				22.31		27.5				22.31		21.5				22.31		3				21.54		6.6683

		22.34		18				22.34		18				22.34		15.5				22.34		7.5				21.56		5.668

		22.37		8.5				22.37		8.5				22.37		10				22.37		6.5				21.58		4.6678

		22.4		11				22.4		11				22.4		6.5				22.4		2.5				21.6		4.001

		22.43		9.5				22.43		9.5				22.43		8				22.43		3.5				21.62		5.668

		22.46		10				22.46		10				22.46		3				22.46		2.5				21.64		3.6675

		22.49		5				22.49		5				22.49		3.5				22.49		3				21.66		9.669

		22.52		7				22.52		7				22.52		4				22.52		1				21.68		4.6678

		22.55		3.5				22.55		3.5				22.55		8				22.55		0				21.7		5.668

		22.58		3.5				22.58		3.5				22.58		5				22.58		1				21.72		5.0012

		22.61		6				22.61		6				22.61		6				22.61		1				21.74		5.668

		22.64		6				22.64		6				22.64		5.5				22.64		3				21.76		5.3346

		22.67		3.5				22.67		3.5				22.67		6				22.67		0.5				21.78		7.0017

		22.7		5				22.7		5				22.7		6				22.7		1				21.8		5.0012

		22.73		7				22.73		7				22.73		7				22.73		1.5				21.82		6.6683

		22.76		5.5				22.76		5.5				22.76		6.5				22.76		1				21.84		5.0012

		22.79		11.5				22.79		11.5				22.79		9				22.79		3				21.86		2.3339

		22.82		4.5				22.82		4.5				22.82		5				22.82		2.5				21.88		3.0007

		22.85		3.5				22.85		3.5				22.85		4.5				22.85		1.5				21.9		4.3344

		22.88		5.5				22.88		5.5				22.88		6.5				22.88		1.5				21.92		5.3346

		22.91		3.5				22.91		3.5				22.91		6.5				22.91		1				21.94		2.6673

		22.94		10.5				22.94		10.5				22.94		8				22.94		2.5				21.96		5.3346

		22.97		15				22.97		15				22.97		12				22.97		2				21.98		5.3346

		23		12				23		12				23		9				23		3.5				22		3.6675

		23.03		14				23.03		14				23.03		11				23.03		3				22.02		6.3349

		23.06		24				23.06		24				23.06		14				23.06		0				22.04		4.6678

		23.09		31.5				23.09		31.5				23.09		22.5				23.09		0.5				22.06		4.6678

		23.12		46				23.12		46				23.12		27				23.12		1				22.08		6.6683

		23.15		62				23.15		62				23.15		36				23.15		4				22.1		4.001

		23.18		67				23.18		67				23.18		51				23.18		5				22.12		3.3341

		23.21		61				23.21		61				23.21		58				23.21		8				22.14		4.3344

		23.24		98				23.24		98				23.24		83.5				23.24		5.5				22.16		4.001

		23.27		90.5				23.27		90.5				23.27		99				23.27		9				22.18		3.3341

		23.3		94.5				23.3		94.5				23.3		92.5				23.3		21				22.2		9.669

		23.33		59.5				23.33		59.5				23.33		63				23.33		37				22.22		5.668

		23.36		33.5				23.36		33.5				23.36		45.5				23.36		67.5				22.24		4.3344

		23.39		18.5				23.39		18.5				23.39		23				23.39		57				22.26		6.3349

		23.42		19.5				23.42		19.5				23.42		10				23.42		27.5				22.28		5.3346

		23.45		10				23.45		10				23.45		11				23.45		11				22.3		4.3344

		23.48		7.5				23.48		7.5				23.48		7				23.48		5				22.32		5.668

		23.51		4.5				23.51		4.5				23.51		8.5				23.51		2.5				22.34		8.0019

		23.54		9.5				23.54		9.5				23.54		9				23.54		2.5				22.36		4.3344

		23.57		5.5				23.57		5.5				23.57		7.5				23.57		3.5				22.38		6.6683

		23.6		9				23.6		9				23.6		8				23.6		1				22.4		6.6683

		23.63		4.5				23.63		4.5				23.63		7				23.63		2				22.42		5.3346

		23.66		7.5				23.66		7.5				23.66		4.5				23.66		1				22.44		7.0017

		23.69		7.5				23.69		7.5				23.69		5.5				23.69		0.5				22.46		5.3346

		23.72		5.5				23.72		5.5				23.72		7				23.72		0.5				22.48		5.0012

		23.75		5.5				23.75		5.5				23.75		3.5				23.75		1.5				22.5		4.6678

		23.78		6				23.78		6				23.78		5.5				23.78		2				22.52		5.0012

		23.81		5.5				23.81		5.5				23.81		4.5				23.81		0.5				22.54		6.6683

		23.84		3				23.84		3				23.84		7				23.84		0.5				22.56		6.3349

		23.87		6.5				23.87		6.5				23.87		11				23.87		0.5				22.58		6.0014

		23.9		3.5				23.9		3.5				23.9		4.5				23.9		2.5				22.6		5.3346

		23.93		3.5				23.93		3.5				23.93		7				23.93		0.5				22.62		6.0014

		23.96		3.5				23.96		3.5				23.96		7.5				23.96		1				22.64		4.3344

		23.99		6				23.99		6				23.99		3.5				23.99		2.5				22.66		6.0014

		24.02		7.5				24.02		7.5				24.02		5.5				24.02		3.5				22.68		4.6678

		24.05		8				24.05		8				24.05		8				24.05		1				22.7		3.0007

		24.08		6.5				24.08		6.5				24.08		4.5				24.08		1				22.72		5.3346

		24.11		10.5				24.11		10.5				24.11		12.5				24.11		0.5				22.74		4.001

		24.14		17.5				24.14		17.5				24.14		11				24.14		0.5				22.76		6.0014

		24.17		15.5				24.17		15.5				24.17		13.5				24.17		0				22.78		4.001

		24.2		30				24.2		30				24.2		21				24.2		1.5				22.8		4.001

		24.23		29.5				24.23		29.5				24.23		26.5				24.23		2				22.82		5.0012

		24.26		43				24.26		43				24.26		38.5				24.26		2				22.84		5.3346

		24.29		45				24.29		45				24.29		43.5				24.29		4				22.86		4.6678

		24.32		28				24.32		28				24.32		37.5				24.32		12.5				22.88		3.6675

		24.35		20				24.35		20				24.35		20.5				24.35		19.5				22.9		6.0014

		24.38		13				24.38		13				24.38		16				24.38		17.5				22.92		4.6678

		24.41		7				24.41		7				24.41		10.5				24.41		13.5				22.94		5.668

		24.44		2				24.44		2				24.44		7.5				24.44		7.5				22.96		6.6683

		24.47		4.5				24.47		4.5				24.47		9.5				24.47		6				22.98		4.3344

		24.5		6.5				24.5		6.5				24.5		7				24.5		4.5				23		3.6675

		24.53		6.5				24.53		6.5				24.53		9.5				24.53		3.5				23.02		8.0019

		24.56		6				24.56		6				24.56		6				24.56		1.5				23.04		7.3351

		24.59		12.5				24.59		12.5				24.59		6.5				24.59		4				23.06		3.0007

		24.62		14				24.62		14				24.62		7.5				24.62		0				23.08		5.3346

		24.65		13.5				24.65		13.5				24.65		9.5				24.65		1				23.1		7.3351

		24.68		15.5				24.68		15.5				24.68		12.5				24.68		2.5				23.12		7.3351

		24.71		24.5				24.71		24.5				24.71		15.5				24.71		1.5				23.14		7.0017

		24.74		27.5				24.74		27.5				24.74		18				24.74		2.5				23.16		8.3353

		24.77		20				24.77		20				24.77		22				24.77		1				23.18		5.3346

		24.8		17				24.8		17				24.8		21.5				24.8		2				23.2		7.3351

		24.83		10				24.83		10				24.83		24.5				24.83		2.5				23.22		7.0017

		24.86		6.5				24.86		6.5				24.86		11				24.86		3.5				23.24		6.0014

		24.89		4				24.89		4				24.89		16				24.89		6				23.26		9.669

		24.92		5				24.92		5				24.92		6				24.92		4				23.28		10.336

		24.95		3.5				24.95		3.5				24.95		6.5				24.95		1.5				23.3		16.337

		24.98		4.5				24.98		4.5				24.98		6				24.98		2.5				23.32		18.671

		25.01		6.5				25.01		6.5				25.01		6				25.01		2				23.34		29.007

		25.04		6				25.04		6				25.04		4				25.04		1				23.36		53.013

		25.07		4				25.07		4				25.07		1.5				25.07		2.5				23.38		71.684

		25.1		2				25.1		2				25.1		4.5				25.1		2.5				23.4		108.36

		25.13		6.5				25.13		6.5				25.13		7				25.13		1.5				23.42		165.04

		25.16		4				25.16		4				25.16		5.5				25.16		2				23.44		174.38

		25.19		7				25.19		7				25.19		6.5				25.19		1				23.46		114.36

		25.22		5.5				25.22		5.5				25.22		6				25.22		1.5				23.48		97.023

		25.25		3.5				25.25		3.5				25.25		5				25.25		1				23.5		87.688

		25.28		3				25.28		3				25.28		4.5				25.28		2				23.52		37.342

		25.31		4				25.31		4				25.31		7.5				25.31		1.5				23.54		15.004

		25.34		3.5				25.34		3.5				25.34		7				25.34		2				23.56		9.0022

		25.37		8.5				25.37		8.5				25.37		6				25.37		1				23.58		11.336

		25.4		5.5				25.4		5.5				25.4		7				25.4		3				23.6		13.003

		25.43		6				25.43		6				25.43		5.5				25.43		1				23.62		7.6685

		25.46		5.5				25.46		5.5				25.46		5				25.46		0.5				23.64		8.3353

		25.49		10				25.49		10				25.49		12				25.49		2.5				23.66		7.6685

		25.52		14.5				25.52		14.5				25.52		7				25.52		0				23.68		6.3349

		25.55		5.5				25.55		5.5				25.55		11				25.55		1.5				23.7		6.6683

		25.58		12				25.58		12				25.58		8.5				25.58		2.5				23.72		7.6685

		25.61		20				25.61		20				25.61		7.5				25.61		0.5				23.74		4.001

		25.64		28.5				25.64		28.5				25.64		13				25.64		5				23.76		5.3346

		25.67		32.5				25.67		32.5				25.67		23				25.67		2.5				23.78		3.6675

		25.7		47.5				25.7		47.5				25.7		31.5				25.7		2				23.8		8.0019

		25.73		70.5				25.73		70.5				25.73		40				25.73		4				23.82		5.3346

		25.76		103				25.76		103				25.76		65.5				25.76		3				23.84		3.0007

		25.79		146				25.79		146				25.79		122.5				25.79		6.5				23.86		3.6675

		25.82		228.5				25.82		228.5				25.82		189				25.82		12.5				23.88		5.668

		25.85		278				25.85		278				25.85		273.5				25.85		16.5				23.9		4.3344

		25.88		290.5				25.88		290.5				25.88		312				25.88		49.5				23.92		5.0012

		25.91		244.5				25.91		244.5				25.91		265.5				25.91		117.5				23.94		7.0017

		25.94		153.5				25.94		153.5				25.94		199				25.94		193.5				23.96		6.0014

		25.97		101				25.97		101				25.97		121.5				25.97		164				23.98		7.3351

		26		61.5				26		61.5				26		88				26		158.5				24		6.3349

		26.03		32				26.03		32				26.03		65				26.03		112.5				24.02		7.0017

		26.06		25.5				26.06		25.5				26.06		48.5				26.06		52.5				24.04		7.3351

		26.09		18				26.09		18				26.09		20				26.09		34.5				24.06		5.3346

		26.12		9				26.12		9				26.12		11.5				26.12		22.5				24.08		5.668

		26.15		9				26.15		9				26.15		11				26.15		12.5				24.1		4.001

		26.18		11.5				26.18		11.5				26.18		7				26.18		7.5				24.12		6.0014

		26.21		12.5				26.21		12.5				26.21		7				26.21		4				24.14		4.001

		26.24		9				26.24		9				26.24		7				26.24		2				24.16		6.3349

		26.27		7				26.27		7				26.27		7.5				26.27		3.5				24.18		4.6678

		26.3		8				26.3		8				26.3		7.5				26.3		2				24.2		7.3351

		26.33		6.5				26.33		6.5				26.33		11				26.33		2.5				24.22		5.3346

		26.36		7				26.36		7				26.36		8.5				26.36		1				24.24		6.0014

		26.39		7.5				26.39		7.5				26.39		12				26.39		1				24.26		6.3349

		26.42		8.5				26.42		8.5				26.42		5.5				26.42		1				24.28		7.3351

		26.45		6.5				26.45		6.5				26.45		4				26.45		2				24.3		5.3346

		26.48		3				26.48		3				26.48		5				26.48		1.5				24.32		6.6683

		26.51		4				26.51		4				26.51		9				26.51		1				24.34		10.002

		26.54		3.5				26.54		3.5				26.54		8				26.54		0				24.36		8.3353

		26.57		6				26.57		6				26.57		5				26.57		1.5				24.38		22.339

		26.6		3				26.6		3				26.6		3.5				26.6		0.5				24.4		36.675

		26.63		8				26.63		8				26.63		1				26.63		0.5				24.42		66.683

		26.66		2.5				26.66		2.5				26.66		3				26.66		2				24.44		82.353

		26.69		4.5				26.69		4.5				26.69		2				26.69		2.5				24.46		50.345

		26.72		4				26.72		4				26.72		3.5				26.72		3				24.48		50.679

		26.75		5				26.75		5				26.75		5				26.75		3				24.5		56.013

		26.78		4				26.78		4				26.78		3				26.78		1				24.52		31.341

		26.81		5				26.81		5				26.81		3				26.81		2				24.54		12.003

		26.84		6				26.84		6				26.84		5.5				26.84		1.5				24.56		11.336

		26.87		6.5				26.87		6.5				26.87		6				26.87		2				24.58		8.0019

		26.9		4.5				26.9		4.5				26.9		6.5				26.9		0				24.6		6.6683

		26.93		5				26.93		5				26.93		7.5				26.93		1.5				24.62		7.3351

		26.96		4.5				26.96		4.5				26.96		5				26.96		1				24.64		5.0012

		26.99		9				26.99		9				26.99		6.5				26.99		1				24.66		7.0017

		27.02		4.5				27.02		4.5				27.02		6.5				27.02		1.5				24.68		4.001

		27.05		5				27.05		5				27.05		9.5				27.05		0.5				24.7		5.668

		27.08		4.5				27.08		4.5				27.08		1.5				27.08		2.5				24.72		9.669

		27.11		3.5				27.11		3.5				27.11		4.5				27.11		1.5				24.74		5.0012

		27.14		6				27.14		6				27.14		4				27.14		1				24.76		5.3346

		27.17		3.5				27.17		3.5				27.17		6				27.17		1.5				24.78		5.3346

		27.2		4				27.2		4				27.2		6.5				27.2		0.5				24.8		6.3349

		27.23		4.5				27.23		4.5				27.23		7				27.23		0.5				24.82		4.6678

		27.26		4				27.26		4				27.26		6				27.26		0.5				24.84		7.6685

		27.29		3.5				27.29		3.5				27.29		3.5				27.29		1				24.86		5.668

		27.32		3				27.32		3				27.32		5.5				27.32		1				24.88		6.6683

		27.35		2				27.35		2				27.35		8				27.35		2.5				24.9		6.6683

		27.38		3				27.38		3				27.38		4.5				27.38		0				24.92		7.0017

		27.41		7				27.41		7				27.41		6.5				27.41		2				24.94		6.0014

		27.44		4				27.44		4				27.44		7				27.44		1.5				24.96		5.0012

		27.47		4.5				27.47		4.5				27.47		4				27.47		1.5				24.98		5.0012

		27.5		7.5				27.5		7.5				27.5		8				27.5		1				25		6.6683

		27.53		6				27.53		6				27.53		5.5				27.53		1.5				25.02		6.0014

		27.56		7				27.56		7				27.56		6.5				27.56		1.5				25.04		4.3344

		27.59		4.5				27.59		4.5				27.59		5.5				27.59		0.5				25.06		5.3346

		27.62		5.5				27.62		5.5				27.62		6.5				27.62		0.5				25.08		6.6683

		27.65		6				27.65		6				27.65		4.5				27.65		1				25.1		4.3344

		27.68		7.5				27.68		7.5				27.68		2				27.68		1				25.12		7.3351

		27.71		10				27.71		10				27.71		6				27.71		1				25.14		2.6673

		27.74		9				27.74		9				27.74		7				27.74		1				25.16		7.6685

		27.77		6.5				27.77		6.5				27.77		7.5				27.77		0				25.18		5.668

		27.8		7				27.8		7				27.8		4				27.8		2				25.2		4.6678

		27.83		5				27.83		5				27.83		6				27.83		0.5				25.22		6.6683

		27.86		5.5				27.86		5.5				27.86		4.5				27.86		1.5				25.24		4.6678

		27.89		6.5				27.89		6.5				27.89		6.5				27.89		2				25.26		6.0014

		27.92		6				27.92		6				27.92		3.5				27.92		2				25.28		5.0012

		27.95		3.5				27.95		3.5				27.95		5.5				27.95		2				25.3		7.3351

		27.98		5.5				27.98		5.5				27.98		6.5				27.98		1.5				25.32		7.6685

		28.01		3.5				28.01		3.5				28.01		3.5				28.01		1.5				25.34		6.0014

		28.04		5.5				28.04		5.5				28.04		5.5				28.04		0.5				25.36		4.001

		28.07		5.5				28.07		5.5				28.07		7				28.07		0.5				25.38		7.0017

		28.1		6				28.1		6				28.1		4				28.1		0.5				25.4		7.0017

		28.13		5				28.13		5				28.13		6.5				28.13		0				25.42		6.3349

		28.16		7.5				28.16		7.5				28.16		7				28.16		1				25.44		6.0014

		28.19		5.5				28.19		5.5				28.19		5.5				28.19		2.5				25.46		4.3344

		28.22		9				28.22		9				28.22		3.5				28.22		2				25.48		7.3351

		28.25		7				28.25		7				28.25		6				28.25		2				25.5		5.668

		28.28		6.5				28.28		6.5				28.28		6				28.28		1				25.52		3.0007

		28.31		7				28.31		7				28.31		3.5				28.31		1.5				25.54		5.3346

		28.34		4				28.34		4				28.34		3.5				28.34		0				25.56		4.001

		28.37		6.5				28.37		6.5				28.37		6.5				28.37		1				25.58		9.669

		28.4		4				28.4		4				28.4		5.5				28.4		2				25.6		6.3349

		28.43		3.5				28.43		3.5				28.43		7				28.43		1				25.62		8.0019

		28.46		2				28.46		2				28.46		5.5				28.46		0				25.64		6.0014

		28.49		3				28.49		3				28.49		7				28.49		0.5				25.66		6.0014

		28.52		4.5				28.52		4.5				28.52		6				28.52		1.5				25.68		6.6683

		28.55		4.5				28.55		4.5				28.55		8				28.55		2				25.7		6.0014

		28.58		4				28.58		4				28.58		6.5				28.58		3				25.72		9.3356

		28.61		4.5				28.61		4.5				28.61		6				28.61		0.5				25.74		7.3351

		28.64		3.5				28.64		3.5				28.64		6.5				28.64		2.5				25.76		8.6687

		28.67		6.5				28.67		6.5				28.67		5.5				28.67		2.5				25.78		6.6683

		28.7		4.5				28.7		4.5				28.7		6.5				28.7		2.5				25.8		9.3356

		28.73		8.5				28.73		8.5				28.73		11				28.73		2				25.82		15.004

		28.76		8.5				28.76		8.5				28.76		7.5				28.76		1				25.84		15.337

		28.79		11				28.79		11				28.79		9.5				28.79		2.5				25.86		18.004

		28.82		6.5				28.82		6.5				28.82		6				28.82		1.5				25.88		19.005

		28.85		6.5				28.85		6.5				28.85		9.5				28.85		2.5				25.9		25.673

		28.88		7.5				28.88		7.5				28.88		6				28.88		2				25.92		39.009

		28.91		4				28.91		4				28.91		6				28.91		3.5				25.94		58.681

		28.94		5.5				28.94		5.5				28.94		8				28.94		2				25.96		106.69

		28.97		7.5				28.97		7.5				28.97		5.5				28.97		2				25.98		219.39

		29		4				29		4				29		5				29		0.5				26		317.08

		29.03		4.5				29.03		4.5				29.03		5				29.03		0.5				26.02		371.42

		29.06		5				29.06		5				29.06		5.5				29.06		2.5				26.04		371.42

		29.09		7.5				29.09		7.5				29.09		7.5				29.09		0.5				26.06		294.4

		29.12		8				29.12		8				29.12		6				29.12		1				26.08		254.39

		29.15		9				29.15		9				29.15		11				29.15		1.5				26.1		251.73

		29.18		8				29.18		8				29.18		8.5				29.18		3.5				26.12		157.7

		29.21		8				29.21		8				29.21		5				29.21		1.5				26.14		78.352

		29.24		6.5				29.24		6.5				29.24		5				29.24		2				26.16		49.012

		29.27		4				29.27		4				29.27		7				29.27		5				26.18		40.676

		29.3		3.5				29.3		3.5				29.3		9.5				29.3		1.5				26.2		27.006

		29.33		3				29.33		3				29.33		7.5				29.33		1.5				26.22		21.672

		29.36		4				29.36		4				29.36		6.5				29.36		3				26.24		15.004

		29.39		6.5				29.39		6.5				29.39		4				29.39		1.5				26.26		11.336

		29.42		7				29.42		7				29.42		8				29.42		2				26.28		10.669

		29.45		7				29.45		7				29.45		6.5				29.45		0.5				26.3		10.669

		29.48		8.5				29.48		8.5				29.48		10.5				29.48		1				26.32		9.0022

		29.51		6				29.51		6				29.51		11.5				29.51		0.5				26.34		7.0017

		29.54		7				29.54		7				29.54		9.5				29.54		2.5				26.36		10.669

		29.57		8.5				29.57		8.5				29.57		8.5				29.57		1				26.38		9.0022

		29.6		10.5				29.6		10.5				29.6		8.5				29.6		2				26.4		7.0017

		29.63		10.5				29.63		10.5				29.63		6.5				29.63		0.5				26.42		7.0017

		29.66		11.5				29.66		11.5				29.66		6				29.66		0.5				26.44		5.668

		29.69		8				29.69		8				29.69		5				29.69		1.5				26.46		8.3353

		29.72		10.5				29.72		10.5				29.72		4.5				29.72		1.5				26.48		7.3351

		29.75		11				29.75		11				29.75		10				29.75		0.5				26.5		8.3353

		29.78		7.5				29.78		7.5				29.78		6				29.78		2.5				26.52		8.3353

		29.81		8				29.81		8				29.81		8.5				29.81		2.5				26.54		9.669

		29.84		9				29.84		9				29.84		7.5				29.84		2				26.56		6.3349

		29.87		7				29.87		7				29.87		10				29.87		1.5				26.58		4.6678

		29.9		8				29.9		8				29.9		8.5				29.9		1.5				26.6		4.6678

		29.93		9.5				29.93		9.5				29.93		9				29.93		2				26.62		6.3349

		29.96		13				29.96		13				29.96		8				29.96		2.5				26.64		5.668

		29.99		10				29.99		10				29.99		8.5				29.99		2.5				26.66		4.3344

		30.02		17.5				30.02		17.5				30.02		14.5				30.02		1				26.68		4.6678

		30.05		17				30.05		17				30.05		11.5				30.05		2.5				26.7		4.6678

		30.08		24.5				30.08		24.5				30.08		17.5				30.08		2				26.72		6.3349

		30.11		29.5				30.11		29.5				30.11		21.5				30.11		3.5				26.74		7.3351

		30.14		53.5				30.14		53.5				30.14		32.5				30.14		3				26.76		2.6673

		30.17		47				30.17		47				30.17		34				30.17		5.5				26.78		5.3346

		30.2		37				30.2		37				30.2		45.5				30.2		16				26.8		6.6683

		30.23		33				30.23		33				30.23		33				30.23		24				26.82		5.3346

		30.26		37.5				30.26		37.5				30.26		32.5				30.26		16.5				26.84		5.0012

		30.29		42				30.29		42				30.29		34				30.29		15.5				26.86		5.0012

		30.32		65.5				30.32		65.5				30.32		47.5				30.32		12				26.88		4.6678

		30.35		97				30.35		97				30.35		88				30.35		11.5				26.9		7.0017

		30.38		132.5				30.38		132.5				30.38		125				30.38		4.5				26.92		4.001

		30.41		163				30.41		163				30.41		176.5				30.41		8.5				26.94		5.668

		30.44		215.5				30.44		215.5				30.44		299				30.44		19.5				26.96		4.6678

		30.47		196				30.47		196				30.47		295.5				30.47		39.5				26.98		6.0014

		30.5		146.5				30.5		146.5				30.5		220				30.5		95				27		5.3346

		30.53		99				30.53		99				30.53		148				30.53		85.5				27.02		8.0019

		30.56		73.5				30.56		73.5				30.56		53.5				30.56		76.5				27.04		5.3346

		30.59		39.5				30.59		39.5				30.59		25.5				30.59		65.5				27.06		5.0012

		30.62		24.5				30.62		24.5				30.62		14.5				30.62		38				27.08		7.3351

		30.65		18				30.65		18				30.65		13				30.65		22.5				27.1		6.3349

		30.68		15				30.68		15				30.68		18				30.68		8.5				27.12		4.6678

		30.71		19.5				30.71		19.5				30.71		13.5				30.71		4.5				27.14		5.0012

		30.74		5				30.74		5				30.74		12.5				30.74		3				27.16		7.6685

		30.77		9				30.77		9				30.77		9.5				30.77		4.5				27.18		6.3349

		30.8		7.5				30.8		7.5				30.8		6.5				30.8		4				27.2		6.3349

		30.83		10				30.83		10				30.83		9.5				30.83		3.5				27.22		5.3346

		30.86		6				30.86		6				30.86		7.5				30.86		0.5				27.24		6.0014

		30.89		4.5				30.89		4.5				30.89		10.5				30.89		2				27.26		5.3346

		30.92		5.5				30.92		5.5				30.92		11				30.92		2.5				27.28		3.3341

		30.95		6.5				30.95		6.5				30.95		8.5				30.95		2.5				27.3		5.3346

		30.98		3				30.98		3				30.98		10.5				30.98		0.5				27.32		4.001

		31.01		10.5				31.01		10.5				31.01		3.5				31.01		2.5				27.34		3.3341

		31.04		2.5				31.04		2.5				31.04		5				31.04		1.5				27.36		2.6673

		31.07		5				31.07		5				31.07		8				31.07		1				27.38		5.668

		31.1		4				31.1		4				31.1		4.5				31.1		3				27.4		5.0012

		31.13		3.5				31.13		3.5				31.13		7.5				31.13		1				27.42		5.3346

		31.16		3				31.16		3				31.16		3.5				31.16		1.5				27.44		3.0007

		31.19		3				31.19		3				31.19		6.5				31.19		1				27.46		4.6678

		31.22		6.5				31.22		6.5				31.22		5.5				31.22		2				27.48		3.3341

		31.25		4				31.25		4				31.25		3				31.25		0.5				27.5		6.3349

		31.28		4.5				31.28		4.5				31.28		3.5				31.28		1				27.52		4.6678

		31.31		3.5				31.31		3.5				31.31		5.5				31.31		0.5				27.54		5.3346

		31.34		3				31.34		3				31.34		6				31.34		1.5				27.56		5.668

		31.37		3.5				31.37		3.5				31.37		4.5				31.37		1.5				27.58		4.6678

		31.4		2				31.4		2				31.4		6				31.4		1				27.6		5.0012

		31.43		3.5				31.43		3.5				31.43		6.5				31.43		2.5				27.62		7.3351

		31.46		5.5				31.46		5.5				31.46		5				31.46		0.5				27.64		5.668

		31.49		6.5				31.49		6.5				31.49		5				31.49		1.5				27.66		8.0019

		31.52		5				31.52		5				31.52		5.5				31.52		1				27.68		7.3351

		31.55		6				31.55		6				31.55		6				31.55		3				27.7		4.6678

		31.58		4				31.58		4				31.58		5				31.58		1.5				27.72		5.668

		31.61		3.5				31.61		3.5				31.61		2.5				31.61		1.5				27.74		5.668

		31.64		5.5				31.64		5.5				31.64		7.5				31.64		1.5				27.76		4.3344

		31.67		5				31.67		5				31.67		6				31.67		2				27.78		7.0017

		31.7		3				31.7		3				31.7		5				31.7		1				27.8		6.0014

		31.73		3.5				31.73		3.5				31.73		5				31.73		0				27.82		4.6678

		31.76		2.5				31.76		2.5				31.76		2.5				31.76		0.5				27.84		5.3346

		31.79		5				31.79		5				31.79		5				31.79		1.5				27.86		4.3344

		31.82		5				31.82		5				31.82		7				31.82		0.5				27.88		6.6683

		31.85		2.5				31.85		2.5				31.85		4				31.85		1.5				27.9		7.3351

		31.88		3				31.88		3				31.88		6				31.88		0.5				27.92		5.668

		31.91		3.5				31.91		3.5				31.91		7				31.91		0				27.94		10.669

		31.94		4				31.94		4				31.94		6				31.94		1.5				27.96		8.3353

		31.97		5.5				31.97		5.5				31.97		5				31.97		0.5				27.98		8.0019

		32		4.5				32		4.5				32		6				32		1				28		7.3351

		32.03		3				32.03		3				32.03		6.5				32.03		0				28.02		6.6683

		32.06		4				32.06		4				32.06		10				32.06		1				28.04		7.3351

		32.09		3.5				32.09		3.5				32.09		6				32.09		1.5				28.06		9.669

		32.12		5.5				32.12		5.5				32.12		6				32.12		1.5				28.08		5.0012

		32.15		4				32.15		4				32.15		6				32.15		0.5				28.1		8.3353

		32.18		7				32.18		7				32.18		6.5				32.18		2				28.12		5.3346

		32.21		6				32.21		6				32.21		4.5				32.21		0.5				28.14		6.6683

		32.24		6				32.24		6				32.24		5.5				32.24		0.5				28.16		5.0012

		32.27		3.5				32.27		3.5				32.27		8.5				32.27		1.5				28.18		6.6683

		32.3		2				32.3		2				32.3		3				32.3		0.5				28.2		3.6675

		32.33		3				32.33		3				32.33		6.5				32.33		0.5				28.22		5.0012

		32.36		2.5				32.36		2.5				32.36		8.5				32.36		1.5				28.24		6.3349

		32.39		4.5				32.39		4.5				32.39		4				32.39		0.5				28.26		6.6683

		32.42		3.5				32.42		3.5				32.42		5				32.42		1.5				28.28		6.6683

		32.45		9				32.45		9				32.45		7.5				32.45		0.5				28.3		4.001

		32.48		6.5				32.48		6.5				32.48		6				32.48		2.5				28.32		6.0014

		32.51		6.5				32.51		6.5				32.51		3				32.51		2.5				28.34		5.668

		32.54		10				32.54		10				32.54		4.5				32.54		2				28.36		9.3356

		32.57		8.5				32.57		8.5				32.57		5				32.57		1				28.38		5.668

		32.6		12.5				32.6		12.5				32.6		5.5				32.6		1.5				28.4		3.6675

		32.63		18.5				32.63		18.5				32.63		11				32.63		3.5				28.42		5.668

		32.66		18.5				32.66		18.5				32.66		12				32.66		1.5				28.44		6.3349

		32.69		25				32.69		25				32.69		17.5				32.69		2.5				28.46		9.3356

		32.72		52				32.72		52				32.72		18.5				32.72		2				28.48		5.3346

		32.75		53				32.75		53				32.75		28.5				32.75		3.5				28.5		7.3351

		32.78		70.5				32.78		70.5				32.78		62.5				32.78		9				28.52		3.6675

		32.81		71				32.81		71				32.81		72				32.81		3.5				28.54		6.6683

		32.84		75				32.84		75				32.84		71.5				32.84		21				28.56		3.3341

		32.87		57				32.87		57				32.87		70				32.87		49.5				28.58		3.0007

		32.9		40				32.9		40				32.9		59.5				32.9		58.5				28.6		5.3346

		32.93		27				32.93		27				32.93		34.5				32.93		36				28.62		8.3353

		32.96		10				32.96		10				32.96		20.5				32.96		27.5				28.64		5.3346

		32.99		10.5				32.99		10.5				32.99		15				32.99		18				28.66		5.668

		33.02		4				33.02		4				33.02		7.5				33.02		13				28.68		6.0014

		33.05		8				33.05		8				33.05		6				33.05		2.5				28.7		3.3341

		33.08		6.5				33.08		6.5				33.08		7.5				33.08		1.5				28.72		6.6683

		33.11		3				33.11		3				33.11		7.5				33.11		1.5				28.74		4.3344

		33.14		6.5				33.14		6.5				33.14		5.5				33.14		2.5				28.76		6.0014

		33.17		5.5				33.17		5.5				33.17		8				33.17		2.5				28.78		7.3351

		33.2		5.5				33.2		5.5				33.2		7.5				33.2		3				28.8		6.0014

		33.23		4				33.23		4				33.23		7				33.23		1				28.82		8.0019

		33.26		3				33.26		3				33.26		5.5				33.26		1.5				28.84		5.668

		33.29		7.5				33.29		7.5				33.29		4.5				33.29		2.5				28.86		6.3349

		33.32		5				33.32		5				33.32		5				33.32		1.5				28.88		4.3344

		33.35		6.5				33.35		6.5				33.35		5				33.35		1				28.9		7.0017

		33.38		2.5				33.38		2.5				33.38		5				33.38		1.5				28.92		5.3346

		33.41		5				33.41		5				33.41		3				33.41		3				28.94		6.3349

		33.44		4				33.44		4				33.44		7				33.44		3				28.96		8.6687

		33.47		3.5				33.47		3.5				33.47		3.5				33.47		1				28.98		8.6687

		33.5		3.5				33.5		3.5				33.5		5				33.5		2				29		7.0017

		33.53		4.5				33.53		4.5				33.53		4				33.53		1				29.02		5.668

		33.56		6.5				33.56		6.5				33.56		4				33.56		1.5				29.04		5.3346

		33.59		5.5				33.59		5.5				33.59		6.5				33.59		0.5				29.06		5.3346

		33.62		4.5				33.62		4.5				33.62		7.5				33.62		0				29.08		4.3344

		33.65		5				33.65		5				33.65		7.5				33.65		1.5				29.1		7.0017

		33.68		5.5				33.68		5.5				33.68		4.5				33.68		2				29.12		8.6687

		33.71		5				33.71		5				33.71		4				33.71		0.5				29.14		4.001

		33.74		7				33.74		7				33.74		6				33.74		3.5				29.16		5.668

		33.77		9.5				33.77		9.5				33.77		10				33.77		1				29.18		4.3344

		33.8		13.5				33.8		13.5				33.8		13.5				33.8		4				29.2		6.0014

		33.83		14				33.83		14				33.83		16.5				33.83		0.5				29.22		7.0017

		33.86		14.5				33.86		14.5				33.86		20.5				33.86		1.5				29.24		5.3346

		33.89		20.5				33.89		20.5				33.89		28				33.89		1.5				29.26		6.3349

		33.92		14.5				33.92		14.5				33.92		26				33.92		2.5				29.28		6.3349

		33.95		8.5				33.95		8.5				33.95		12				33.95		3.5				29.3		5.668

		33.98		5.5				33.98		5.5				33.98		9.5				33.98		1.5				29.32		6.0014

		34.01		8				34.01		8				34.01		6				34.01		2.5				29.34		7.3351

		34.04		5				34.04		5				34.04		5.5				34.04		1.5				29.36		4.6678

		34.07		9				34.07		9				34.07		10				34.07		1				29.38		5.0012

		34.1		6				34.1		6				34.1		5				34.1		1				29.4		7.3351

		34.13		8.5				34.13		8.5				34.13		5.5				34.13		1.5				29.42		7.3351

		34.16		15				34.16		15				34.16		11.5				34.16		1				29.44		5.3346

		34.19		9				34.19		9				34.19		8				34.19		1				29.46		6.3349

		34.22		11				34.22		11				34.22		10				34.22		0.5				29.48		3.6675

		34.25		6.5				34.25		6.5				34.25		7				34.25		1				29.5		8.6687

		34.28		6.5				34.28		6.5				34.28		6				34.28		1.5				29.52		8.3353

		34.31		6.5				34.31		6.5				34.31		8				34.31		2				29.54		7.3351

		34.34		7				34.34		7				34.34		4.5				34.34		1				29.56		5.3346

		34.37		4				34.37		4				34.37		7.5				34.37		2				29.58		5.3346

		34.4		7.5				34.4		7.5				34.4		6				34.4		0.5				29.6		4.001

		34.43		3.5				34.43		3.5				34.43		5.5				34.43		3.5				29.62		5.668

		34.46		6				34.46		6				34.46		4.5				34.46		1				29.64		4.3344

		34.49		7				34.49		7				34.49		2				34.49		1				29.66		6.0014

		34.52		4.5				34.52		4.5				34.52		3.5				34.52		1				29.68		4.6678

		34.55		6				34.55		6				34.55		6				34.55		1				29.7		6.0014

		34.58		7				34.58		7				34.58		11				34.58		3.5				29.72		6.0014

		34.61		10				34.61		10				34.61		5.5				34.61		0				29.74		3.6675

		34.64		7				34.64		7				34.64		9.5				34.64		1.5				29.76		6.0014

		34.67		11.5				34.67		11.5				34.67		5.5				34.67		2				29.78		5.3346

		34.7		7				34.7		7				34.7		13.5				34.7		0.5				29.8		7.6685

		34.73		6.5				34.73		6.5				34.73		14				34.73		3				29.82		5.3346

		34.76		7.5				34.76		7.5				34.76		7.5				34.76		2.5				29.84		5.0012

		34.79		6.5				34.79		6.5				34.79		6				34.79		3				29.86		7.6685

		34.82		6.5				34.82		6.5				34.82		6.5				34.82		1.5				29.88		8.6687

		34.85		4.5				34.85		4.5				34.85		6.5				34.85		1.5				29.9		5.3346

		34.88		3				34.88		3				34.88		4				34.88		1				29.92		6.3349

		34.91		5				34.91		5				34.91		8				34.91		1.5				29.94		6.0014

		34.94		2				34.94		2				34.94		5.5				34.94		1				29.96		5.0012

		34.97		2				34.97		2				34.97		5				34.97		1				29.98		6.0014

		35		2				35		2				35		4.5				35		2.5				30		6.3349

		35.03		3				35.03		3				35.03		6.5				35.03		2				30.02		6.0014

		35.06		3				35.06		3				35.06		4				35.06		1.5				30.04		3.3341

		35.09		4.5				35.09		4.5				35.09		3				35.09		1				30.06		7.3351

		35.12		2.5				35.12		2.5				35.12		4				35.12		1.5				30.08		6.0014

		35.15		3				35.15		3				35.15		5.5				35.15		1				30.1		7.0017

		35.18		4				35.18		4				35.18		5				35.18		1.5				30.12		7.6685

		35.21		2.5				35.21		2.5				35.21		4				35.21		0.5				30.14		7.6685

		35.24		6.5				35.24		6.5				35.24		5.5				35.24		1				30.16		6.3349

		35.27		8.5				35.27		8.5				35.27		8.5				35.27		1				30.18		5.3346

		35.3		7				35.3		7				35.3		6.5				35.3		0.5				30.2		7.6685

		35.33		10				35.33		10				35.33		11				35.33		3				30.22		11.003

		35.36		9				35.36		9				35.36		9.5				35.36		1.5				30.24		13.67

		35.39		10.5				35.39		10.5				35.39		11.5				35.39		0.5				30.26		14.337

		35.42		11.5				35.42		11.5				35.42		8				35.42		3				30.28		22.005

		35.45		12				35.45		12				35.45		12.5				35.45		4				30.3		30.674

		35.48		13.5				35.48		13.5				35.48		10.5				35.48		4.5				30.32		51.679

		35.51		12				35.51		12				35.51		9				35.51		3				30.34		35.008

		35.54		11.5				35.54		11.5				35.54		12.5				35.54		4				30.36		24.006

		35.57		8				35.57		8				35.57		6.5				35.57		2				30.38		23.339

		35.6		8.5				35.6		8.5				35.6		6				35.6		5.5				30.4		27.34

		35.63		8				35.63		8				35.63		9				35.63		2				30.42		29.007

		35.66		13.5				35.66		13.5				35.66		8				35.66		1				30.44		26.006

		35.69		9				35.69		9				35.69		6.5				35.69		0				30.46		23.339

		35.72		8				35.72		8				35.72		6				35.72		2.5				30.48		31.674

		35.75		4.5				35.75		4.5				35.75		6				35.75		2				30.5		44.677

		35.78		8				35.78		8				35.78		9.5				35.78		2				30.52		49.345

		35.81		10.5				35.81		10.5				35.81		7				35.81		6.5				30.54		70.017

		35.84		13.5				35.84		13.5				35.84		7.5				35.84		3				30.56		127.36

		35.87		10				35.87		10				35.87		6				35.87		1.5				30.58		261.4

		35.9		7				35.9		7				35.9		7.5				35.9		1.5				30.6		463.11

		35.93		14.5				35.93		14.5				35.93		8				35.93		2.5				30.62		434.1

		35.96		16				35.96		16				35.96		13				35.96		0				30.64		300.41

		35.99		14.5				35.99		14.5				35.99		16				35.99		4				30.66		257.06

		36.02		22.5				36.02		22.5				36.02		10.5				36.02		2				30.68		268.73

		36.05		22				36.05		22				36.05		10.5				36.05		2				30.7		241.06

		36.08		28				36.08		28				36.08		17				36.08		4.5				30.72		139.7

		36.11		46.5				36.11		46.5				36.11		24				36.11		5				30.74		68.683

		36.14		55.5				36.14		55.5				36.14		34.5				36.14		3.5				30.76		41.677

		36.17		84				36.17		84				36.17		42.5				36.17		7.5				30.78		28.674

		36.2		117				36.2		117				36.2		66				36.2		10				30.8		27.34

		36.23		187.5				36.23		187.5				36.23		122.5				36.23		10.5				30.82		21.672

		36.26		244				36.26		244				36.26		213				36.26		12.5				30.84		15.004

		36.29		309				36.29		309				36.29		371.5				36.29		23.5				30.86		11.003

		36.32		332.5				36.32		332.5				36.32		450				36.32		46.5				30.88		14.337

		36.35		304				36.35		304				36.35		431				36.35		126.5				30.9		14.67

		36.38		229.5				36.38		229.5				36.38		360				36.38		200				30.92		8.6687

		36.41		140				36.41		140				36.41		236.5				36.41		134				30.94		9.0022

		36.44		81				36.44		81				36.44		128.5				36.44		91.5				30.96		6.6683

		36.47		53.5				36.47		53.5				36.47		61.5				36.47		106.5				30.98		6.0014

		36.5		32				36.5		32				36.5		29				36.5		75				31		7.0017

		36.53		17.5				36.53		17.5				36.53		23				36.53		29				31.02		8.6687

		36.56		15.5				36.56		15.5				36.56		12.5				36.56		8.5				31.04		10.002

		36.59		12				36.59		12				36.59		13.5				36.59		11				31.06		8.3353

		36.62		11.5				36.62		11.5				36.62		13.5				36.62		8				31.08		7.6685

		36.65		11				36.65		11				36.65		14.5				36.65		3.5				31.1		5.3346

		36.68		12.5				36.68		12.5				36.68		7				36.68		4				31.12		8.6687

		36.71		10.5				36.71		10.5				36.71		9.5				36.71		1.5				31.14		8.3353

		36.74		12				36.74		12				36.74		12				36.74		3				31.16		7.0017

		36.77		9.5				36.77		9.5				36.77		11.5				36.77		2.5				31.18		7.0017

		36.8		9.5				36.8		9.5				36.8		17				36.8		0.5				31.2		7.6685

		36.83		8				36.83		8				36.83		10				36.83		0				31.22		6.3349

		36.86		10				36.86		10				36.86		9				36.86		1				31.24		5.0012

		36.89		15				36.89		15				36.89		7				36.89		1.5				31.26		6.6683

		36.92		13.5				36.92		13.5				36.92		5				36.92		1				31.28		6.3349

		36.95		13				36.95		13				36.95		9.5				36.95		2.5				31.3		7.6685

		36.98		18.5				36.98		18.5				36.98		11.5				36.98		2				31.32		8.0019

		37.01		24				37.01		24				37.01		13				37.01		2.5				31.34		7.0017

		37.04		37				37.04		37				37.04		14.5				37.04		2.5				31.36		7.6685

		37.07		46				37.07		46				37.07		21				37.07		3				31.38		5.3346

		37.1		49				37.1		49				37.1		35.5				37.1		6				31.4		6.3349

		37.13		79				37.13		79				37.13		41.5				37.13		5.5				31.42		8.0019

		37.16		101				37.16		101				37.16		61.5				37.16		3.5				31.44		3.3341

		37.19		122				37.19		122				37.19		108				37.19		7.5				31.46		7.0017

		37.22		144.5				37.22		144.5				37.22		127.5				37.22		19.5				31.48		6.6683

		37.25		140				37.25		140				37.25		150.5				37.25		53				31.5		4.3344

		37.28		118.5				37.28		118.5				37.28		132				37.28		88.5				31.52		4.6678

		37.31		84.5				37.31		84.5				37.31		95				37.31		53.5				31.54		6.3349

		37.34		68.5				37.34		68.5				37.34		66				37.34		45				31.56		7.0017

		37.37		40.5				37.37		40.5				37.37		41.5				37.37		58				31.58		3.6675

		37.4		29.5				37.4		29.5				37.4		22.5				37.4		38				31.6		6.3349

		37.43		19.5				37.43		19.5				37.43		17.5				37.43		16.5				31.62		6.0014

		37.46		24.5				37.46		24.5				37.46		13				37.46		8.5				31.64		5.0012

		37.49		14				37.49		14				37.49		13.5				37.49		6				31.66		6.6683

		37.52		14				37.52		14				37.52		11.5				37.52		5				31.68		5.0012

		37.55		12				37.55		12				37.55		7.5				37.55		2				31.7		4.6678

		37.58		7				37.58		7				37.58		4.5				37.58		4.5				31.72		4.6678

		37.61		8.5				37.61		8.5				37.61		10				37.61		2				31.74		8.6687

		37.64		11				37.64		11				37.64		6.5				37.64		3				31.76		5.3346

		37.67		5.5				37.67		5.5				37.67		7				37.67		1				31.78		4.6678

		37.7		5.5				37.7		5.5				37.7		9.5				37.7		2				31.8		5.3346

		37.73		4.5				37.73		4.5				37.73		3				37.73		1.5				31.82		6.3349

		37.76		5				37.76		5				37.76		5.5				37.76		1				31.84		3.6675

		37.79		6				37.79		6				37.79		3.5				37.79		3.5				31.86		4.6678

		37.82		5				37.82		5				37.82		4				37.82		0.5				31.88		4.6678

		37.85		6				37.85		6				37.85		4				37.85		1				31.9		5.668

		37.88		5.5				37.88		5.5				37.88		4.5				37.88		1				31.92		5.3346

		37.91		1				37.91		1				37.91		4				37.91		1				31.94		4.001

		37.94		6.5				37.94		6.5				37.94		3				37.94		2				31.96		4.3344

		37.97		6				37.97		6				37.97		6				37.97		1.5				31.98		4.6678

		38		9				38		9				38		5.5				38		2				32		6.0014

		38.03		9				38.03		9				38.03		4.5				38.03		1				32.02		6.0014

		38.06		6.5				38.06		6.5				38.06		2.5				38.06		1.5				32.04		3.0007

		38.09		3.5				38.09		3.5				38.09		4.5				38.09		0.5				32.06		4.6678

		38.12		6.5				38.12		6.5				38.12		3.5				38.12		1				32.08		6.3349

		38.15		4				38.15		4				38.15		3.5				38.15		1				32.1		5.3346

		38.18		2				38.18		2				38.18		2				38.18		0				32.12		5.668

		38.21		3.5				38.21		3.5				38.21		5				38.21		0.5				32.14		4.3344

		38.24		2.5				38.24		2.5				38.24		5.5				38.24		1				32.16		4.6678

		38.27		4				38.27		4				38.27		6				38.27		1.5				32.18		4.6678

		38.3		9.5				38.3		9.5				38.3		6				38.3		1.5				32.2		8.6687

		38.33		6.5				38.33		6.5				38.33		3				38.33		1				32.22		5.3346

		38.36		8.5				38.36		8.5				38.36		6.5				38.36		2				32.24		8.6687

		38.39		4				38.39		4				38.39		7.5				38.39		3.5				32.26		5.668

		38.42		7.5				38.42		7.5				38.42		6				38.42		3.5				32.28		7.0017

		38.45		5.5				38.45		5.5				38.45		4.5				38.45		4.5				32.3		4.001

		38.48		9.5				38.48		9.5				38.48		6.5				38.48		2				32.32		6.0014

		38.51		4				38.51		4				38.51		8				38.51		2.5				32.34		5.3346

		38.54		3				38.54		3				38.54		5.5				38.54		3.5				32.36		5.3346

		38.57		4.5				38.57		4.5				38.57		5.5				38.57		1.5				32.38		3.6675

		38.6		5				38.6		5				38.6		5				38.6		1				32.4		3.3341

		38.63		3				38.63		3				38.63		3				38.63		0.5				32.42		4.6678

		38.66		5				38.66		5				38.66		4.5				38.66		2				32.44		4.3344

		38.69		5				38.69		5				38.69		5.5				38.69		2				32.46		3.6675

		38.72		5				38.72		5				38.72		4				38.72		2.5				32.48		6.0014

		38.75		7				38.75		7				38.75		6.5				38.75		2.5				32.5		5.668

		38.78		8.5				38.78		8.5				38.78		8				38.78		2.5				32.52		4.6678

		38.81		7.5				38.81		7.5				38.81		4.5				38.81		1.5				32.54		5.668

		38.84		17.5				38.84		17.5				38.84		8				38.84		3.5				32.56		3.6675

		38.87		25				38.87		25				38.87		18.5				38.87		3.5				32.58		5.0012

		38.9		33				38.9		33				38.9		25				38.9		2				32.6		6.6683

		38.93		41.5				38.93		41.5				38.93		38.5				38.93		1.5				32.62		3.3341

		38.96		51.5				38.96		51.5				38.96		55				38.96		7				32.64		4.6678

		38.99		45.5				38.99		45.5				38.99		65.5				38.99		17				32.66		7.6685

		39.02		37.5				39.02		37.5				39.02		68				39.02		43				32.68		6.0014

		39.05		21.5				39.05		21.5				39.05		38				39.05		92				32.7		7.6685

		39.08		17.5				39.08		17.5				39.08		25.5				39.08		56.5				32.72		5.668

		39.11		11				39.11		11				39.11		17				39.11		21				32.74		8.6687

		39.14		11.5				39.14		11.5				39.14		6				39.14		42				32.76		9.0022

		39.17		6				39.17		6				39.17		4				39.17		35				32.78		8.3353

		39.2		3.5				39.2		3.5				39.2		6				39.2		6				32.8		8.6687

		39.23		9				39.23		9				39.23		7				39.23		4				32.82		7.6685

		39.26		7				39.26		7				39.26		5.5				39.26		2				32.84		7.0017

		39.29		8.5				39.29		8.5				39.29		7				39.29		1.5				32.86		16.004

		39.32		11.5				39.32		11.5				39.32		4				39.32		2				32.88		20.005

		39.35		13.5				39.35		13.5				39.35		8				39.35		1				32.9		36.675

		39.38		18				39.38		18				39.38		12.5				39.38		1.5				32.92		64.349

		39.41		31.5				39.41		31.5				39.41		20				39.41		2				32.94		93.022

		39.44		30.5				39.44		30.5				39.44		32.5				39.44		0.5				32.96		90.022

		39.47		30				39.47		30				39.47		27.5				39.47		7				32.98		85.687

		39.5		28				39.5		28				39.5		31				39.5		22.5				33		81.353

		39.53		17.5				39.53		17.5				39.53		29.5				39.53		26.5				33.02		61.348

		39.56		15.5				39.56		15.5				39.56		20				39.56		9				33.04		61.681

		39.59		8				39.59		8				39.59		10.5				39.59		13				33.06		44.677

		39.62		5				39.62		5				39.62		7.5				39.62		15				33.08		38.676

		39.65		5				39.65		5				39.65		6.5				39.65		8				33.1		20.672

		39.68		2.5				39.68		2.5				39.68		5.5				39.68		3.5				33.12		18.004

		39.71		2.5				39.71		2.5				39.71		4				39.71		2				33.14		11.003

		39.74		2				39.74		2				39.74		5.5				39.74		2				33.16		12.336

		39.77		6				39.77		6				39.77		3				39.77		2				33.18		10.002

		39.8		2.5				39.8		2.5				39.8		4.5				39.8		2				33.2		9.0022

		39.83		6				39.83		6				39.83		4.5				39.83		2.5				33.22		5.668

		39.86		7				39.86		7				39.86		3				39.86		1				33.24		4.001

		39.89		3.5				39.89		3.5				39.89		4				39.89		0.5				33.26		6.6683

		39.92		4				39.92		4				39.92		5				39.92		1				33.28		6.0014

		39.95		2.5				39.95		2.5				39.95		3				39.95		1.5				33.3		7.6685

		39.98		2.5				39.98		2.5				39.98		5				39.98		1				33.32		7.0017

		40.01		1.5				40.01		1.5				40.01		3				40.01		0.5				33.34		6.0014

		40.04		7				40.04		7				40.04		3				40.04		2				33.36		6.0014

		40.07		5.5				40.07		5.5				40.07		5				40.07		2				33.38		5.3346

		40.1		4				40.1		4				40.1		5				40.1		0.5				33.4		5.3346

		40.13		4.5				40.13		4.5				40.13		2.5				40.13		1.5				33.42		5.668

		40.16		6.5				40.16		6.5				40.16		5				40.16		0				33.44		4.6678

		40.19		9				40.19		9				40.19		6.5				40.19		1.5				33.46		4.6678

		40.22		9				40.22		9				40.22		4				40.22		2				33.48		8.0019

		40.25		15				40.25		15				40.25		5.5				40.25		1				33.5		7.3351

		40.28		8.5				40.28		8.5				40.28		7				40.28		1.5				33.52		6.6683

		40.31		14.5				40.31		14.5				40.31		12				40.31		1				33.54		6.0014

		40.34		23.5				40.34		23.5				40.34		16.5				40.34		5.5				33.56		5.668

		40.37		30				40.37		30				40.37		30.5				40.37		3				33.58		6.6683

		40.4		42				40.4		42				40.4		41				40.4		4.5				33.6		6.3349

		40.43		55				40.43		55				40.43		63.5				40.43		9.5				33.62		3.3341

		40.46		52				40.46		52				40.46		58				40.46		15.5				33.64		6.0014

		40.49		52.5				40.49		52.5				40.49		71				40.49		35.5				33.66		5.3346

		40.52		42				40.52		42				40.52		54				40.52		76.5				33.68		8.0019

		40.55		39.5				40.55		39.5				40.55		41				40.55		58				33.7		5.0012

		40.58		32.5				40.58		32.5				40.58		27.5				40.58		30.5				33.72		4.6678

		40.61		34				40.61		34				40.61		23				40.61		33.5				33.74		4.6678

		40.64		43				40.64		43				40.64		39.5				40.64		41				33.76		3.6675

		40.67		45				40.67		45				40.67		47.5				40.67		25.5				33.78		5.3346

		40.7		48				40.7		48				40.7		50				40.7		13.5				33.8		4.3344

		40.73		51				40.73		51				40.73		58.5				40.73		34.5				33.82		4.6678

		40.76		48.5				40.76		48.5				40.76		53.5				40.76		35				33.84		8.0019

		40.79		31				40.79		31				40.79		49				40.79		68				33.86		4.6678

		40.82		19				40.82		19				40.82		38.5				40.82		52				33.88		5.3346

		40.85		12				40.85		12				40.85		18.5				40.85		27				33.9		7.3351

		40.88		8.5				40.88		8.5				40.88		12.5				40.88		33				33.92		3.0007

		40.91		10				40.91		10				40.91		5				40.91		26				33.94		5.3346

		40.94		6				40.94		6				40.94		8				40.94		6.5				33.96		6.6683

		40.97		4				40.97		4				40.97		5.5				40.97		2.5				33.98		5.3346

		41		4.5				41		4.5				41		3.5				41		5.5				34		5.668

		41.03		4				41.03		4				41.03		8.5				41.03		0.5				34.02		5.0012

		41.06		3.5				41.06		3.5				41.06		6.5				41.06		1.5				34.04		6.3349

		41.09		3				41.09		3				41.09		6.5				41.09		1				34.06		6.0014

		41.12		4.5				41.12		4.5				41.12		2.5				41.12		1				34.08		4.3344

		41.15		3				41.15		3				41.15		2				41.15		1.5				34.1		6.6683

		41.18		3				41.18		3				41.18		2.5				41.18		1				34.12		3.3341

		41.21		5.5				41.21		5.5				41.21		3				41.21		0.5				34.14		4.3344

		41.24		4.5				41.24		4.5				41.24		2.5				41.24		0.5				34.16		7.3351

		41.27		2.5				41.27		2.5				41.27		4.5				41.27		1				34.18		4.3344

		41.3		2				41.3		2				41.3		3.5				41.3		2.5				34.2		6.0014

		41.33		2.5				41.33		2.5				41.33		4.5				41.33		0.5				34.22		5.3346

		41.36		3				41.36		3				41.36		6.5				41.36		2				34.24		4.001

		41.39		1.5				41.39		1.5				41.39		4				41.39		2				34.26		5.668

		41.42		3.5				41.42		3.5				41.42		5				41.42		1				34.28		7.0017

		41.45		4				41.45		4				41.45		2				41.45		0.5				34.3		5.0012

		41.48		4				41.48		4				41.48		5.5				41.48		1.5				34.32		5.668

		41.51		1				41.51		1				41.51		5				41.51		0				34.34		4.001

		41.54		5				41.54		5				41.54		5.5				41.54		1.5				34.36		6.0014

		41.57		7.5				41.57		7.5				41.57		4.5				41.57		1.5				34.38		5.668

		41.6		4.5				41.6		4.5				41.6		3				41.6		1.5				34.4		6.6683

		41.63		5.5				41.63		5.5				41.63		6				41.63		2				34.42		4.3344

		41.66		6				41.66		6				41.66		4.5				41.66		2.5				34.44		5.0012

		41.69		7.5				41.69		7.5				41.69		5				41.69		0.5				34.46		5.0012

		41.72		5.5				41.72		5.5				41.72		2				41.72		0.5				34.48		5.3346

		41.75		5.5				41.75		5.5				41.75		4				41.75		3.5				34.5		5.0012

		41.78		4.5				41.78		4.5				41.78		4				41.78		0.5				34.52		4.001

		41.81		4.5				41.81		4.5				41.81		5.5				41.81		2				34.54		6.6683

		41.84		4.5				41.84		4.5				41.84		5.5				41.84		1				34.56		4.3344

		41.87		2.5				41.87		2.5				41.87		2				41.87		1.5				34.58		6.3349

		41.9		4				41.9		4				41.9		6.5				41.9		1.5				34.6		3.3341

		41.93		3				41.93		3				41.93		2.5				41.93		0.5				34.62		4.001

		41.96		4.5				41.96		4.5				41.96		4				41.96		1.5				34.64		4.6678

		41.99		3				41.99		3				41.99		2.5				41.99		2				34.66		2.3339

		42.02		6				42.02		6				42.02		3.5				42.02		1.5				34.68		5.0012

		42.05		5.5				42.05		5.5				42.05		5				42.05		0.5				34.7		3.3341

		42.08		2				42.08		2				42.08		7.5				42.08		2.5				34.72		4.6678

		42.11		3.5				42.11		3.5				42.11		3				42.11		1				34.74		4.001

		42.14		3.5				42.14		3.5				42.14		4.5				42.14		1				34.76		4.001

		42.17		5.5				42.17		5.5				42.17		4.5				42.17		0				34.78		6.6683

		42.2		5.5				42.2		5.5				42.2		5				42.2		1.5				34.8		6.6683

		42.23		6.5				42.23		6.5				42.23		6				42.23		3.5				34.82		5.3346

		42.26		7.5				42.26		7.5				42.26		2.5				42.26		2				34.84		4.001

		42.29		6.5				42.29		6.5				42.29		4				42.29		2.5				34.86		6.6683

		42.32		11.5				42.32		11.5				42.32		5.5				42.32		1.5				34.88		5.0012

		42.35		18				42.35		18				42.35		3				42.35		2				34.9		5.0012

		42.38		23.5				42.38		23.5				42.38		14.5				42.38		3.5				34.92		4.3344

		42.41		25				42.41		25				42.41		17				42.41		2.5				34.94		6.3349

		42.44		37.5				42.44		37.5				42.44		38.5				42.44		2.5				34.96		4.001

		42.47		46.5				42.47		46.5				42.47		39				42.47		9				34.98		5.0012

		42.5		63				42.5		63				42.5		51				42.5		12				35		6.6683

		42.53		55				42.53		55				42.53		68				42.53		28.5				35.02		4.6678

		42.56		53				42.56		53				42.56		65.5				42.56		26				35.04		4.001

		42.59		47				42.59		47				42.59		57.5				42.59		25.5				35.06		5.668

		42.62		30.5				42.62		30.5				42.62		43.5				42.62		42				35.08		4.6678

		42.65		17.5				42.65		17.5				42.65		27.5				42.65		35.5				35.1		5.0012

		42.68		15				42.68		15				42.68		17				42.68		19.5				35.12		4.6678

		42.71		11				42.71		11				42.71		11				42.71		13				35.14		4.6678

		42.74		4.5				42.74		4.5				42.74		9				42.74		15.5				35.16		5.3346

		42.77		11.5				42.77		11.5				42.77		9.5				42.77		11.5				35.18		4.6678

		42.8		9				42.8		9				42.8		4.5				42.8		5				35.2		3.0007

		42.83		11				42.83		11				42.83		8.5				42.83		1				35.22		4.3344

		42.86		8.5				42.86		8.5				42.86		9				42.86		2				35.24		7.0017

		42.89		8.5				42.89		8.5				42.89		7.5				42.89		3.5				35.26		4.6678

		42.92		9				42.92		9				42.92		8				42.92		2				35.28		3.6675

		42.95		8				42.95		8				42.95		7				42.95		1.5				35.3		5.3346

		42.98		9.5				42.98		9.5				42.98		9.5				42.98		2				35.32		5.0012

		43.01		17.5				43.01		17.5				43.01		8.5				43.01		2.5				35.34		7.6685

		43.04		17				43.04		17				43.04		9.5				43.04		1.5				35.36		7.0017

		43.07		20				43.07		20				43.07		12				43.07		2				35.38		8.0019

		43.1		37.5				43.1		37.5				43.1		14				43.1		1.5				35.4		7.6685

		43.13		45				43.13		45				43.13		33				43.13		1				35.42		7.0017

		43.16		55				43.16		55				43.16		33				43.16		0.5				35.44		5.3346

		43.19		67.5				43.19		67.5				43.19		36.5				43.19		3				35.46		6.3349

		43.22		71.5				43.22		71.5				43.22		50.5				43.22		3				35.48		5.3346

		43.25		79				43.25		79				43.25		63				43.25		7				35.5		8.0019

		43.28		69.5				43.28		69.5				43.28		61				43.28		8.5				35.52		25.673

		43.31		66.5				43.31		66.5				43.31		68.5				43.31		24.5				35.54		40.343

		43.34		61.5				43.34		61.5				43.34		46				43.34		19.5				35.56		25.673

		43.37		52.5				43.37		52.5				43.37		38				43.37		13				35.58		15.337

		43.4		43				43.4		43				43.4		27.5				43.4		11				35.6		16.004

		43.43		25				43.43		25				43.43		25				43.43		13.5				35.62		23.339

		43.46		20				43.46		20				43.46		15.5				43.46		12.5				35.64		24.339

		43.49		20.5				43.49		20.5				43.49		12.5				43.49		6				35.66		14.337

		43.52		17.5				43.52		17.5				43.52		14				43.52		3.5				35.68		10.669

		43.55		8				43.55		8				43.55		8				43.55		3				35.7		7.3351

		43.58		8				43.58		8				43.58		8.5				43.58		3.5				35.72		8.6687

		43.61		4.5				43.61		4.5				43.61		7.5				43.61		3.5				35.74		5.3346

		43.64		7				43.64		7				43.64		5.5				43.64		3.5				35.76		4.3344

		43.67		8.5				43.67		8.5				43.67		4.5				43.67		1				35.78		4.3344

		43.7		5.5				43.7		5.5				43.7		6				43.7		1.5				35.8		10.002

		43.73		6				43.73		6				43.73		6				43.73		3.5				35.82		8.0019

		43.76		2.5				43.76		2.5				43.76		6				43.76		0.5				35.84		6.3349

		43.79		4.5				43.79		4.5				43.79		4				43.79		0.5				35.86		5.668

		43.82		4				43.82		4				43.82		4.5				43.82		2.5				35.88		6.3349

		43.85		5				43.85		5				43.85		3.5				43.85		1.5				35.9		8.6687

		43.88		4.5				43.88		4.5				43.88		4.5				43.88		3				35.92		6.0014

		43.91		6				43.91		6				43.91		3.5				43.91		1				35.94		6.3349

		43.94		4.5				43.94		4.5				43.94		3.5				43.94		1				35.96		7.6685

		43.97		2				43.97		2				43.97		3.5				43.97		1				35.98		5.0012

		44		5.5				44		5.5				44		3				44		1.5				36		7.0017

		44.03		3				44.03		3				44.03		7				44.03		1.5				36.02		5.3346

		44.06		4				44.06		4				44.06		4				44.06		1.5				36.04		8.3353

		44.09		2				44.09		2				44.09		2				44.09		0.5				36.06		9.0022

		44.12		6.5				44.12		6.5				44.12		7				44.12		1				36.08		7.3351

		44.15		3				44.15		3				44.15		5				44.15		1.5				36.1		7.6685

		44.18		0.5				44.18		0.5				44.18		3				44.18		1.5				36.12		7.3351

		44.21		2				44.21		2				44.21		3.5				44.21		0				36.14		10.336

		44.24		4.5				44.24		4.5				44.24		3				44.24		0.5				36.16		10.336

		44.27		5				44.27		5				44.27		2				44.27		0.5				36.18		11.669

		44.3		2				44.3		2				44.3		3.5				44.3		1.5				36.2		11.669

		44.33		5.5				44.33		5.5				44.33		4				44.33		0.5				36.22		13.67

		44.36		7				44.36		7				44.36		2				44.36		0				36.24		13.337

		44.39		6				44.39		6				44.39		3				44.39		2				36.26		16.004

		44.42		5				44.42		5				44.42		2				44.42		1				36.28		17.337

		44.45		3.5				44.45		3.5				44.45		5.5				44.45		2				36.3		22.005

		44.48		4.5				44.48		4.5				44.48		4.5				44.48		1.5				36.32		32.675

		44.51		4.5				44.51		4.5				44.51		3				44.51		1.5				36.34		36.675

		44.54		2.5				44.54		2.5				44.54		3.5				44.54		1				36.36		53.013

		44.57		2				44.57		2				44.57		4.5				44.57		2				36.38		114.69

		44.6		5.5				44.6		5.5				44.6		3				44.6		1.5				36.4		197.05

		44.63		4				44.63		4				44.63		6				44.63		0.5				36.42		282.4

		44.66		2.5				44.66		2.5				44.66		5				44.66		2				36.44		500.12

		44.69		5				44.69		5				44.69		4.5				44.69		1				36.46		606.48

		44.72		4				44.72		4				44.72		3				44.72		1				36.48		439.77

		44.75		2.5				44.75		2.5				44.75		5.5				44.75		2				36.5		254.39

		44.78		5.5				44.78		5.5				44.78		2.5				44.78		0.5				36.52		246.06

		44.81		4.5				44.81		4.5				44.81		4				44.81		0.5				36.54		308.07

		44.84		1				44.84		1				44.84		3.5				44.84		1.5				36.56		286.4

		44.87		3				44.87		3				44.87		2.5				44.87		1.5				36.58		179.04

		44.9		4				44.9		4				44.9		3				44.9		1				36.6		90.022

		44.93		3				44.93		3				44.93		6				44.93		1.5				36.62		51.346

		44.96		3				44.96		3				44.96		2.5				44.96		0.5				36.64		33.341

		44.99		2.5				44.99		2.5				44.99		3				44.99		1				36.66		20.338

		45.02		1.5				45.02		1.5				45.02		3				45.02		2				36.68		14.67

		45.05		3.5				45.05		3.5				45.05		4.5				45.05		3.5				36.7		23.672

		45.08		4.5				45.08		4.5				45.08		2.5				45.08		0				36.72		16.337

		45.11		5.5				45.11		5.5				45.11		3				45.11		0.5				36.74		11.336

		45.14		6				45.14		6				45.14		6				45.14		2				36.76		9.669

		45.17		4				45.17		4				45.17		4				45.17		2				36.78		7.6685

		45.2		5.5				45.2		5.5				45.2		4				45.2		1				36.8		10.669

		45.23		6				45.23		6				45.23		8				45.23		0				36.82		6.6683

		45.26		5.5				45.26		5.5				45.26		5.5				45.26		1.5				36.84		8.0019

		45.29		8.5				45.29		8.5				45.29		8.5				45.29		2				36.86		9.0022

		45.32		13.5				45.32		13.5				45.32		7				45.32		0.5				36.88		6.3349

		45.35		10				45.35		10				45.35		15.5				45.35		2				36.9		6.6683

		45.38		22.5				45.38		22.5				45.38		16				45.38		4				36.92		7.3351

		45.41		23				45.41		23				45.41		18.5				45.41		10				36.94		11.669

		45.44		16				45.44		16				45.44		23				45.44		14				36.96		6.0014

		45.47		12.5				45.47		12.5				45.47		15.5				45.47		14.5				36.98		10.669

		45.5		15.5				45.5		15.5				45.5		19				45.5		8.5				37		5.668

		45.53		13				45.53		13				45.53		9.5				45.53		7.5				37.02		9.0022

		45.56		7				45.56		7				45.56		4				45.56		4.5				37.04		9.0022

		45.59		4.5				45.59		4.5				45.59		6				45.59		8.5				37.06		8.6687

		45.62		4.5				45.62		4.5				45.62		4				45.62		5				37.08		10.669

		45.65		6.5				45.65		6.5				45.65		4.5				45.65		1				37.1		9.0022

		45.68		3				45.68		3				45.68		5.5				45.68		1.5				37.12		7.0017

		45.71		4				45.71		4				45.71		6				45.71		2				37.14		9.0022

		45.74		5				45.74		5				45.74		3.5				45.74		2.5				37.16		6.3349

		45.77		2.5				45.77		2.5				45.77		3				45.77		1				37.18		11.336

		45.8		4.5				45.8		4.5				45.8		2.5				45.8		1.5				37.2		13.003

		45.83		2.5				45.83		2.5				45.83		4.5				45.83		0.5				37.22		8.6687

		45.86		2.5				45.86		2.5				45.86		2				45.86		0				37.24		12.336

		45.89		3				45.89		3				45.89		2.5				45.89		0.5				37.26		14.337

		45.92		0.5				45.92		0.5				45.92		2.5				45.92		0.5				37.28		15.004

		45.95		2				45.95		2				45.95		3				45.95		1.5				37.3		26.34

		45.98		2				45.98		2				45.98		3.5				45.98		2				37.32		38.343

		46.01		5				46.01		5				46.01		2.5				46.01		1				37.34		59.014

		46.04		1.5				46.04		1.5				46.04		2.5				46.04		1				37.36		122.36

		46.07		2				46.07		2				46.07		1				46.07		0				37.38		281.73

		46.1		5				46.1		5				46.1		1				46.1		2				37.4		355.42

		46.13		1.5				46.13		1.5				46.13		2.5				46.13		2.5				37.42		206.72

		46.16		2				46.16		2				46.16		2.5				46.16		0				37.44		111.36

		46.19		6				46.19		6				46.19		0.5				46.19		2				37.46		112.03

		46.22		3				46.22		3				46.22		1.5				46.22		0				37.48		184.04

		46.25		1.5				46.25		1.5				46.25		4				46.25		1.5				37.5		189.05

		46.28		0.5				46.28		0.5				46.28		1				46.28		2				37.52		96.356

		46.31		3.5				46.31		3.5				46.31		1.5				46.31		1				37.54		44.344

		46.34		1.5				46.34		1.5				46.34		1				46.34		2.5				37.56		23.339

		46.37		0.5				46.37		0.5				46.37		4				46.37		0.5				37.58		16.671

		46.4		2				46.4		2				46.4		4.5				46.4		1				37.6		11.669

		46.43		2.5				46.43		2.5				46.43		3				46.43		1				37.62		14.003

		46.46		2				46.46		2				46.46		5.5				46.46		0.5				37.64		11.336

		46.49		3				46.49		3				46.49		3.5				46.49		2				37.66		11.003

		46.52		1.5				46.52		1.5				46.52		2.5				46.52		1.5				37.68		8.6687

		46.55		3.5				46.55		3.5				46.55		2.5				46.55		1.5				37.7		10.002

		46.58		2.5				46.58		2.5				46.58		3.5				46.58		1				37.72		7.6685

		46.61		2.5				46.61		2.5				46.61		2				46.61		1				37.74		6.6683

		46.64		3.5				46.64		3.5				46.64		2				46.64		1				37.76		4.3344

		46.67		4				46.67		4				46.67		4				46.67		1				37.78		10.669

		46.7		3				46.7		3				46.7		3.5				46.7		0				37.8		8.3353

		46.73		2.5				46.73		2.5				46.73		4.5				46.73		1				37.82		5.668

		46.76		3				46.76		3				46.76		3				46.76		2				37.84		4.001

		46.79		2				46.79		2				46.79		0.5				46.79		1.5				37.86		6.0014

		46.82		5				46.82		5				46.82		2				46.82		1.5				37.88		5.668

		46.85		5				46.85		5				46.85		1				46.85		1				37.9		3.6675

		46.88		5				46.88		5				46.88		5				46.88		1				37.92		6.6683

		46.91		5.5				46.91		5.5				46.91		3.5				46.91		0.5				37.94		5.3346

		46.94		3.5				46.94		3.5				46.94		2				46.94		0.5				37.96		5.668

		46.97		2				46.97		2				46.97		2				46.97		0.5				37.98		6.0014

		47		7				47		7				47		6.5				47		3				38		6.6683

		47.03		3				47.03		3				47.03		3				47.03		0				38.02		4.3344

		47.06		1.5				47.06		1.5				47.06		3.5				47.06		0				38.04		7.0017

		47.09		4				47.09		4				47.09		4				47.09		1				38.06		6.0014

		47.12		3				47.12		3				47.12		2				47.12		0				38.08		6.6683

		47.15		2.5				47.15		2.5				47.15		4				47.15		2				38.1		5.3346

		47.18		2.5				47.18		2.5				47.18		3				47.18		1.5				38.12		7.3351

		47.21		2				47.21		2				47.21		0.5				47.21		0.5				38.14		3.6675

		47.24		3.5				47.24		3.5				47.24		3				47.24		0.5				38.16		6.0014

		47.27		2.5				47.27		2.5				47.27		5				47.27		1.5				38.18		3.3341

		47.3		6				47.3		6				47.3		4				47.3		1.5				38.2		2.6673

		47.33		1.5				47.33		1.5				47.33		4				47.33		1.5				38.22		5.668

		47.36		3.5				47.36		3.5				47.36		3.5				47.36		1				38.24		6.3349

		47.39		3				47.39		3				47.39		3				47.39		3				38.26		5.3346

		47.42		3.5				47.42		3.5				47.42		4.5				47.42		0.5				38.28		6.3349

		47.45		5				47.45		5				47.45		3.5				47.45		0.5				38.3		6.6683

		47.48		6				47.48		6				47.48		4				47.48		1.5				38.32		5.0012

		47.51		5.5				47.51		5.5				47.51		2				47.51		2				38.34		3.6675

		47.54		4				47.54		4				47.54		5				47.54		0.5				38.36		4.6678

		47.57		9				47.57		9				47.57		5.5				47.57		0				38.38		6.0014

		47.6		6.5				47.6		6.5				47.6		8.5				47.6		2.5				38.4		7.6685

		47.63		11				47.63		11				47.63		9.5				47.63		1.5				38.42		7.0017

		47.66		7.5				47.66		7.5				47.66		7.5				47.66		3.5				38.44		4.001

		47.69		9.5				47.69		9.5				47.69		10				47.69		8				38.46		3.0007

		47.72		7.5				47.72		7.5				47.72		10.5				47.72		2				38.48		6.3349

		47.75		7.5				47.75		7.5				47.75		7.5				47.75		2				38.5		7.0017

		47.78		2				47.78		2				47.78		3				47.78		5.5				38.52		11.336

		47.81		3.5				47.81		3.5				47.81		6.5				47.81		4.5				38.54		12.336

		47.84		4.5				47.84		4.5				47.84		4				47.84		4				38.56		11.003

		47.87		2				47.87		2				47.87		6				47.87		3.5				38.58		7.6685

		47.9		4.5				47.9		4.5				47.9		2.5				47.9		4				38.6		5.3346

		47.93		2.5				47.93		2.5				47.93		7.5				47.93		1				38.62		5.0012

		47.96		4.5				47.96		4.5				47.96		3.5				47.96		0.5				38.64		12.67

		47.99		3				47.99		3				47.99		4				47.99		0				38.66		9.3356

		48.02		1				48.02		1				48.02		2.5				48.02		2.5				38.68		2.3339

		48.05		2.5				48.05		2.5				48.05		1.5				48.05		0.5				38.7		4.001

		48.08		2.5				48.08		2.5				48.08		2				48.08		2.5				38.72		6.0014

		48.11		2				48.11		2				48.11		2.5				48.11		0.5				38.74		2.6673

		48.14		3.5				48.14		3.5				48.14		2				48.14		1.5				38.76		9.0022

		48.17		1.5				48.17		1.5				48.17		3.5				48.17		1				38.78		4.3344

		48.2		2.5				48.2		2.5				48.2		1.5				48.2		0.5				38.8		5.0012

		48.23		1				48.23		1				48.23		1				48.23		1				38.82		7.0017

		48.26		1.5				48.26		1.5				48.26		1				48.26		0				38.84		4.001

		48.29		2.5				48.29		2.5				48.29		3.5				48.29		1.5				38.86		4.3344

		48.32		3.5				48.32		3.5				48.32		4				48.32		1.5				38.88		8.6687

		48.35		3				48.35		3				48.35		3.5				48.35		0.5				38.9		4.001

		48.38		4				48.38		4				48.38		2.5				48.38		1.5				38.92		5.668

		48.41		2.5				48.41		2.5				48.41		3.5				48.41		0.5				38.94		5.0012

		48.44		1.5				48.44		1.5				48.44		1.5				48.44		1				38.96		6.0014

		48.47		3.5				48.47		3.5				48.47		3.5				48.47		2				38.98		8.3353

		48.5		1				48.5		1				48.5		2.5				48.5		0				39		14.337

		48.53		1.5				48.53		1.5				48.53		2.5				48.53		1				39.02		19.338

		48.56		2				48.56		2				48.56		3.5				48.56		2				39.04		31.007

		48.59		2				48.59		2				48.59		3				48.59		1				39.06		31.674

		48.62		3.5				48.62		3.5				48.62		1				48.62		1.5				39.08		37.342

		48.65		3.5				48.65		3.5				48.65		4				48.65		2				39.1		59.348

		48.68		3.5				48.68		3.5				48.68		2.5				48.68		0.5				39.12		58.014

		48.71		2.5				48.71		2.5				48.71		1.5				48.71		1				39.14		43.01

		48.74		4.5				48.74		4.5				48.74		2.5				48.74		0.5				39.16		24.339

		48.77		2				48.77		2				48.77		4				48.77		3				39.18		29.34

		48.8		3				48.8		3				48.8		2.5				48.8		0.5				39.2		33.675

		48.83		4				48.83		4				48.83		2				48.83		1.5				39.22		32.341

		48.86		3				48.86		3				48.86		2				48.86		3				39.24		20.005

		48.89		4				48.89		4				48.89		3				48.89		0.5				39.26		11.336

		48.92		2				48.92		2				48.92		4				48.92		1				39.28		8.3353

		48.95		7				48.95		7				48.95		1.5				48.95		2				39.3		6.6683

		48.98		3.5				48.98		3.5				48.98		1.5				48.98		0				39.32		7.6685

		49.01		4				49.01		4				49.01		3.5				49.01		1				39.34		8.6687

		49.04		5.5				49.04		5.5				49.04		3.5				49.04		1				39.36		7.0017

		49.07		4.5				49.07		4.5				49.07		2.5				49.07		1.5				39.38		5.3346

		49.1		3				49.1		3				49.1		3				49.1		0.5				39.4		8.3353

		49.13		3				49.13		3				49.13		3				49.13		0.5				39.42		5.3346

		49.16		6				49.16		6				49.16		3.5				49.16		2				39.44		6.3349

		49.19		6				49.19		6				49.19		3				49.19		2				39.46		6.0014

		49.22		6				49.22		6				49.22		6.5				49.22		1.5				39.48		7.6685

		49.25		7				49.25		7				49.25		5				49.25		1				39.5		12.003

		49.28		6				49.28		6				49.28		6.5				49.28		1				39.52		14.003

		49.31		6				49.31		6				49.31		3				49.31		0.5				39.54		20.005

		49.34		6.5				49.34		6.5				49.34		3.5				49.34		1				39.56		32.008

		49.37		4				49.37		4				49.37		4				49.37		1				39.58		36.342

		49.4		6				49.4		6				49.4		4				49.4		1				39.6		53.346

		49.43		3				49.43		3				49.43		6				49.43		2				39.62		66.349

		49.46		8				49.46		8				49.46		5.5				49.46		0.5				39.64		44.011

		49.49		5				49.49		5				49.49		6.5				49.49		0				39.66		27.006

		49.52		6				49.52		6				49.52		7				49.52		2				39.68		24.339

		49.55		9.5				49.55		9.5				49.55		4				49.55		2				39.7		26.673

		49.58		5.5				49.58		5.5				49.58		3				49.58		2				39.72		29.007

		49.61		9				49.61		9				49.61		5.5				49.61		1				39.74		21.338

		49.64		12				49.64		12				49.64		8.5				49.64		2.5				39.76		14.67

		49.67		12				49.67		12				49.67		14				49.67		1.5				39.78		6.0014

		49.7		23				49.7		23				49.7		17				49.7		3				39.8		7.0017

		49.73		32				49.73		32				49.73		25				49.73		4				39.82		4.3344

		49.76		30.5				49.76		30.5				49.76		42.5				49.76		4				39.84		4.3344

		49.79		40				49.79		40				49.79		39				49.79		7				39.86		6.3349

		49.82		40.5				49.82		40.5				49.82		47.5				49.82		15				39.88		7.3351

		49.85		35				49.85		35				49.85		38				49.85		19				39.9		5.3346

		49.88		28				49.88		28				49.88		32				49.88		14				39.92		3.6675

		49.91		22				49.91		22				49.91		19.5				49.91		8				39.94		7.0017

		49.94		17				49.94		17				49.94		20				49.94		6				39.96		5.3346

		49.97		8.5				49.97		8.5				49.97		17.5				49.97		14				39.98		4.6678

		50		7.5				50		7.5				50		7				50		11.5				40		5.0012

		50.03		4.5				50.03		4.5				50.03		11				50.03		7.5				40.02		6.6683

		50.06		6				50.06		6				50.06		4.5				50.06		1.5				40.04		3.6675

		50.09		6				50.09		6				50.09		4				50.09		1.5				40.06		6.0014

		50.12		4.5				50.12		4.5				50.12		4				50.12		2.5				40.08		2.0005

		50.15		6.5				50.15		6.5				50.15		4.5				50.15		1				40.1		3.6675

		50.18		3				50.18		3				50.18		4				50.18		1.5				40.12		5.3346

		50.21		5.5				50.21		5.5				50.21		4.5				50.21		0.5				40.14		4.6678

		50.24		3.5				50.24		3.5				50.24		2.5				50.24		1.5				40.16		6.3349

		50.27		5				50.27		5				50.27		2.5				50.27		1.5				40.18		2.6673

		50.3		4				50.3		4				50.3		2				50.3		1				40.2		8.3353

		50.33		3				50.33		3				50.33		0.5				50.33		2.5				40.22		6.3349

		50.36		2				50.36		2				50.36		3				50.36		1.5				40.24		6.3349

		50.39		5.5				50.39		5.5				50.39		3				50.39		0				40.26		3.6675

		50.42		4.5				50.42		4.5				50.42		4.5				50.42		2				40.28		5.3346

		50.45		5				50.45		5				50.45		3.5				50.45		1				40.3		8.3353

		50.48		3.5				50.48		3.5				50.48		1.5				50.48		1.5				40.32		8.0019

		50.51		6.5				50.51		6.5				50.51		7.5				50.51		0.5				40.34		5.0012

		50.54		6				50.54		6				50.54		5.5				50.54		0.5				40.36		6.3349

		50.57		10				50.57		10				50.57		9.5				50.57		1				40.38		5.668

		50.6		10.5				50.6		10.5				50.6		12.5				50.6		0.5				40.4		6.0014

		50.63		11.5				50.63		11.5				50.63		13.5				50.63		2.5				40.42		6.0014

		50.66		10				50.66		10				50.66		11.5				50.66		2				40.44		7.3351

		50.69		6.5				50.69		6.5				50.69		9.5				50.69		5.5				40.46		6.6683

		50.72		9				50.72		9				50.72		11				50.72		5				40.48		6.3349

		50.75		6.5				50.75		6.5				50.75		13				50.75		4.5				40.5		13.337

		50.78		6				50.78		6				50.78		6				50.78		2.5				40.52		15.337

		50.81		7.5				50.81		7.5				50.81		8.5				50.81		2				40.54		24.006

		50.84		5				50.84		5				50.84		9.5				50.84		3.5				40.56		33.008

		50.87		4.5				50.87		4.5				50.87		6.5				50.87		3				40.58		49.345

		50.9		3				50.9		3				50.9		8				50.9		1.5				40.6		74.351

		50.93		4				50.93		4				50.93		4.5				50.93		1.5				40.62		76.352

		50.96		2				50.96		2				50.96		6.5				50.96		2				40.64		50.679

		50.99		3.5				50.99		3.5				50.99		4				50.99		3				40.66		32.675

		51.02		4				51.02		4				51.02		4.5				51.02		2.5				40.68		34.008

		51.05		2.5				51.05		2.5				51.05		2.5				51.05		1.5				40.7		47.678

		51.08		5.5				51.08		5.5				51.08		3				51.08		2				40.72		51.012

		51.11		2.5				51.11		2.5				51.11		3.5				51.11		0.5				40.74		37.676

		51.14		4				51.14		4				51.14		3				51.14		0				40.76		20.672

		51.17		5				51.17		5				51.17		3.5				51.17		2.5				40.78		29.34

		51.2		9				51.2		9				51.2		4				51.2		2.5				40.8		47.011

		51.23		5				51.23		5				51.23		5				51.23		1.5				40.82		51.346

		51.26		7.5				51.26		7.5				51.26		3.5				51.26		1.5				40.84		55.013

		51.29		14.5				51.29		14.5				51.29		7				51.29		3				40.86		45.344

		51.32		14				51.32		14				51.32		8.5				51.32		1.5				40.88		40.01

		51.35		21.5				51.35		21.5				51.35		18.5				51.35		1.5				40.9		46.344

		51.38		27.5				51.38		27.5				51.38		26				51.38		2.5				40.92		34.675

		51.41		28.5				51.41		28.5				51.41		35.5				51.41		7				40.94		37.676

		51.44		38.5				51.44		38.5				51.44		36.5				51.44		10				40.96		33.341

		51.47		43				51.47		43				51.47		38				51.47		17				40.98		24.339

		51.5		30				51.5		30				51.5		33.5				51.5		19				41		20.338

		51.53		28				51.53		28				51.53		25				51.53		18				41.02		11.336

		51.56		16.5				51.56		16.5				51.56		21				51.56		9.5				41.04		4.6678

		51.59		19				51.59		19				51.59		11.5				51.59		11.5				41.06		7.6685

		51.62		10.5				51.62		10.5				51.62		8				51.62		15.5				41.08		6.3349

		51.65		11				51.65		11				51.65		5.5				51.65		12				41.1		6.3349

		51.68		12				51.68		12				51.68		8.5				51.68		9				41.12		8.6687

		51.71		13				51.71		13				51.71		8				51.71		4				41.14		5.668

		51.74		17				51.74		17				51.74		7.5				51.74		4.5				41.16		4.3344

		51.77		19				51.77		19				51.77		11.5				51.77		2.5				41.18		5.668

		51.8		22				51.8		22				51.8		18.5				51.8		3				41.2		6.3349

		51.83		31				51.83		31				51.83		34.5				51.83		3.5				41.22		4.6678

		51.86		28.5				51.86		28.5				51.86		42.5				51.86		8.5				41.24		6.0014

		51.89		39.5				51.89		39.5				51.89		42				51.89		15				41.26		4.6678

		51.92		26				51.92		26				51.92		33.5				51.92		14				41.28		4.6678

		51.95		20				51.95		20				51.95		27				51.95		15				41.3		5.668

		51.98		16.5				51.98		16.5				51.98		18				51.98		10				41.32		5.3346

		52.01		17.5				52.01		17.5				52.01		12				52.01		10.5				41.34		4.001

		52.04		5.5				52.04		5.5				52.04		12.5				52.04		10.5				41.36		4.3344

		52.07		6.5				52.07		6.5				52.07		6				52.07		11				41.38		4.001

		52.1		6				52.1		6				52.1		5.5				52.1		10				41.4		4.6678

		52.13		3.5				52.13		3.5				52.13		5.5				52.13		2				41.42		5.0012

		52.16		3				52.16		3				52.16		2				52.16		2				41.44		4.001

		52.19		2.5				52.19		2.5				52.19		2.5				52.19		1.5				41.46		2.6673

		52.22		4				52.22		4				52.22		4.5				52.22		1				41.48		5.0012

		52.25		2				52.25		2				52.25		2.5				52.25		3				41.5		5.3346

		52.28		6.5				52.28		6.5				52.28		2.5				52.28		3				41.52		5.3346

		52.31		3.5				52.31		3.5				52.31		6				52.31		1				41.54		3.3341

		52.34		3.5				52.34		3.5				52.34		3				52.34		1				41.56		4.6678

		52.37		5				52.37		5				52.37		3.5				52.37		1				41.58		4.6678

		52.4		5.5				52.4		5.5				52.4		3.5				52.4		1.5				41.6		4.6678

		52.43		3.5				52.43		3.5				52.43		4.5				52.43		1.5				41.62		5.0012

		52.46		4.5				52.46		4.5				52.46		3				52.46		0.5				41.64		4.6678

		52.49		4				52.49		4				52.49		3.5				52.49		2				41.66		4.3344

		52.52		4.5				52.52		4.5				52.52		4				52.52		0.5				41.68		5.3346

		52.55		2				52.55		2				52.55		2.5				52.55		3.5				41.7		5.3346

		52.58		5				52.58		5				52.58		3				52.58		2				41.72		4.001

		52.61		3.5				52.61		3.5				52.61		2				52.61		0				41.74		5.0012

		52.64		2				52.64		2				52.64		3				52.64		0.5				41.76		4.6678

		52.67		4				52.67		4				52.67		2.5				52.67		0.5				41.78		5.0012

		52.7		3.5				52.7		3.5				52.7		5.5				52.7		4				41.8		6.3349

		52.73		4.5				52.73		4.5				52.73		3.5				52.73		0.5				41.82		3.0007

		52.76		3.5				52.76		3.5				52.76		4.5				52.76		1				41.84		6.6683

		52.79		9				52.79		9				52.79		5				52.79		2.5				41.86		5.0012

		52.82		4				52.82		4				52.82		3				52.82		0.5				41.88		4.6678

		52.85		5				52.85		5				52.85		2				52.85		1				41.9		5.668

		52.88		8				52.88		8				52.88		5				52.88		3				41.92		4.3344

		52.91		6.5				52.91		6.5				52.91		6.5				52.91		0				41.94		6.3349

		52.94		9				52.94		9				52.94		5				52.94		1				41.96		5.668

		52.97		8				52.97		8				52.97		3.5				52.97		1				41.98		4.3344

		53		11.5				53		11.5				53		6				53		3				42		5.3346

		53.03		14				53.03		14				53.03		8.5				53.03		3.5				42.02		6.0014

		53.06		25				53.06		25				53.06		11				53.06		3.5				42.04		4.001

		53.09		28				53.09		28				53.09		16.5				53.09		3				42.06		4.6678

		53.12		36.5				53.12		36.5				53.12		22				53.12		6				42.08		5.0012

		53.15		56				53.15		56				53.15		47.5				53.15		5				42.1		3.6675

		53.18		69.5				53.18		69.5				53.18		68.5				53.18		4				42.12		3.3341

		53.21		99				53.21		99				53.21		99				53.21		10				42.14		3.3341

		53.24		102				53.24		102				53.24		114				53.24		25				42.16		7.0017

		53.27		101				53.27		101				53.27		104				53.27		42.5				42.18		6.0014

		53.3		80.5				53.3		80.5				53.3		95				53.3		57				42.2		6.3349

		53.33		81.5				53.33		81.5				53.33		66.5				53.33		30.5				42.22		3.6675

		53.36		79.5				53.36		79.5				53.36		65.5				53.36		19.5				42.24		4.001

		53.39		59				53.39		59				53.39		61				53.39		25				42.26		7.6685

		53.42		45				53.42		45				53.42		73				53.42		32.5				42.28		3.6675

		53.45		44				53.45		44				53.45		74				53.45		44.5				42.3		5.0012

		53.48		42.5				53.48		42.5				53.48		45				53.48		43				42.32		4.6678

		53.51		25.5				53.51		25.5				53.51		55.5				53.51		38				42.34		6.6683

		53.54		31				53.54		31				53.54		50.5				53.54		19				42.36		6.3349

		53.57		22				53.57		22				53.57		29				53.57		8.5				42.38		6.3349

		53.6		15.5				53.6		15.5				53.6		23.5				53.6		9				42.4		6.6683

		53.63		11.5				53.63		11.5				53.63		18				53.63		22.5				42.42		7.0017

		53.66		10.5				53.66		10.5				53.66		11.5				53.66		13.5				42.44		9.3356

		53.69		5.5				53.69		5.5				53.69		8				53.69		9.5				42.46		9.3356

		53.72		3.5				53.72		3.5				53.72		7				53.72		3.5				42.48		12.003

		53.75		3				53.75		3				53.75		5.5				53.75		4.5				42.5		10.669

		53.78		4.5				53.78		4.5				53.78		6				53.78		2				42.52		14.003

		53.81		7				53.81		7				53.81		4				53.81		2.5				42.54		17.004

		53.84		8				53.84		8				53.84		4				53.84		4				42.56		25.006

		53.87		8				53.87		8				53.87		8.5				53.87		2				42.58		44.011

		53.9		12.5				53.9		12.5				53.9		6.5				53.9		3				42.6		65.682

		53.93		15.5				53.93		15.5				53.93		18.5				53.93		2				42.62		79.686

		53.96		17				53.96		17				53.96		20.5				53.96		3.5				42.64		122.03

		53.99		13.5				53.99		13.5				53.99		15.5				53.99		5.5				42.66		211.72

		54.02		19				54.02		19				54.02		17				54.02		12				42.68		309.41

		54.05		13				54.05		13				54.05		7.5				54.05		9				42.7		306.07

		54.08		8.5				54.08		8.5				54.08		8.5				54.08		6.5				42.72		139.7

		54.11		8				54.11		8				54.11		8				54.11		4				42.74		81.353

		54.14		10				54.14		10				54.14		6.5				54.14		3				42.76		94.023

		54.17		8				54.17		8				54.17		5				54.17		8				42.78		150.37

		54.2		5				54.2		5				54.2		4.5				54.2		3.5				42.8		170.04

		54.23		5				54.23		5				54.23		5				54.23		4				42.82		118.7

		54.26		2.5				54.26		2.5				54.26		2.5				54.26		4.5				42.84		39.343

		54.29		3.5				54.29		3.5				54.29		2.5				54.29		1.5				42.86		16.671

		54.32		3				54.32		3				54.32		3.5				54.32		1				42.88		10.336

		54.35		3				54.35		3				54.35		3				54.35		2.5				42.9		8.6687

		54.38		3.5				54.38		3.5				54.38		2				54.38		0				42.92		11.336

		54.41		3.5				54.41		3.5				54.41		6.5				54.41		2				42.94		8.6687

		54.44		5.5				54.44		5.5				54.44		2.5				54.44		1.5				42.96		8.3353

		54.47		5				54.47		5				54.47		3.5				54.47		1.5				42.98		7.6685

		54.5		5				54.5		5				54.5		6				54.5		1				43		4.6678

		54.53		3				54.53		3				54.53		5				54.53		1.5				43.02		8.6687

		54.56		5.5				54.56		5.5				54.56		3				54.56		0.5				43.04		5.0012

		54.59		7				54.59		7				54.59		2.5				54.59		1				43.06		7.3351

		54.62		7.5				54.62		7.5				54.62		3.5				54.62		2				43.08		5.0012

		54.65		7.5				54.65		7.5				54.65		8				54.65		2				43.1		5.3346

		54.68		7				54.68		7				54.68		4.5				54.68		2				43.12		8.6687

		54.71		4.5				54.71		4.5				54.71		6.5				54.71		1				43.14		6.0014

		54.74		9				54.74		9				54.74		10.5				54.74		3				43.16		6.0014

		54.77		7.5				54.77		7.5				54.77		9.5				54.77		2.5				43.18		4.001

		54.8		8				54.8		8				54.8		12.5				54.8		2.5				43.2		4.001

		54.83		8				54.83		8				54.83		5				54.83		2.5				43.22		5.0012

		54.86		7				54.86		7				54.86		8				54.86		4				43.24		6.3349

		54.89		7.5				54.89		7.5				54.89		7				54.89		5.5				43.26		9.3356

		54.92		4				54.92		4				54.92		5				54.92		1.5				43.28		3.6675

		54.95		5				54.95		5				54.95		6				54.95		2				43.3		8.6687

		54.98		3.5				54.98		3.5				54.98		6.5				54.98		3.5				43.32		5.668

		55.01		4.5				55.01		4.5				55.01		6.5				55.01		2				43.34		6.6683

		55.04		1.5				55.04		1.5				55.04		2				55.04		3.5				43.36		6.0014

		55.07		2.5				55.07		2.5				55.07		1				55.07		1				43.38		7.0017

		55.1		4.5				55.1		4.5				55.1		3				55.1		1.5				43.4		5.3346

		55.13		4				55.13		4				55.13		1.5				55.13		0.5				43.42		5.3346

		55.16		3.5				55.16		3.5				55.16		4.5				55.16		0.5				43.44		6.0014

		55.19		4				55.19		4				55.19		2.5				55.19		1.5				43.46		6.0014

		55.22		4.5				55.22		4.5				55.22		2				55.22		1				43.48		6.0014

		55.25		3.5				55.25		3.5				55.25		3.5				55.25		0.5				43.5		2.6673

		55.28		4				55.28		4				55.28		1.5				55.28		0				43.52		4.001

		55.31		3				55.31		3				55.31		3.5				55.31		1.5				43.54		6.0014

		55.34		5				55.34		5				55.34		6				55.34		1.5				43.56		5.3346

		55.37		3.5				55.37		3.5				55.37		3.5				55.37		1				43.58		4.6678

		55.4		5.5				55.4		5.5				55.4		4.5				55.4		0.5				43.6		5.668

		55.43		3.5				55.43		3.5				55.43		3.5				55.43		1.5				43.62		4.3344

		55.46		1.5				55.46		1.5				55.46		5				55.46		1				43.64		3.0007

		55.49		4				55.49		4				55.49		4				55.49		2.5				43.66		5.668

		55.52		3.5				55.52		3.5				55.52		5.5				55.52		1.5				43.68		5.668

		55.55		5				55.55		5				55.55		5				55.55		1				43.7		3.6675

		55.58		5				55.58		5				55.58		2.5				55.58		1.5				43.72		5.3346

		55.61		6.5				55.61		6.5				55.61		5				55.61		1				43.74		6.0014

		55.64		4				55.64		4				55.64		2				55.64		2.5				43.76		4.6678

		55.67		6.5				55.67		6.5				55.67		8				55.67		2				43.78		5.668

		55.7		9				55.7		9				55.7		6.5				55.7		1				43.8		6.6683

		55.73		11.5				55.73		11.5				55.73		13				55.73		4.5				43.82		4.3344

		55.76		11.5				55.76		11.5				55.76		9.5				55.76		3				43.84		7.0017

		55.79		20.5				55.79		20.5				55.79		19.5				55.79		2				43.86		3.3341

		55.82		32.5				55.82		32.5				55.82		34.5				55.82		4				43.88		2.0005

		55.85		35.5				55.85		35.5				55.85		35.5				55.85		9				43.9		5.0012

		55.88		38				55.88		38				55.88		43.5				55.88		18.5				43.92		2.0005

		55.91		31				55.91		31				55.91		41				55.91		33				43.94		5.0012

		55.94		30				55.94		30				55.94		34.5				55.94		44				43.96		3.6675

		55.97		25				55.97		25				55.97		23.5				55.97		19				43.98		4.001

		56		20.5				56		20.5				56		23				56		7.5				44		5.668

		56.03		11				56.03		11				56.03		20.5				56.03		11.5				44.02		3.3341

		56.06		8				56.06		8				56.06		10.5				56.06		19				44.04		3.6675

		56.09		7				56.09		7				56.09		6.5				56.09		28				44.06		6.0014

		56.12		6.5				56.12		6.5				56.12		10				56.12		8				44.08		5.0012

		56.15		4				56.15		4				56.15		3.5				56.15		4				44.1		4.001

		56.18		4.5				56.18		4.5				56.18		2				56.18		4				44.12		4.6678

		56.21		2.5				56.21		2.5				56.21		3				56.21		2				44.14		3.0007

		56.24		4.5				56.24		4.5				56.24		3.5				56.24		2.5				44.16		6.0014

		56.27		2.5				56.27		2.5				56.27		5.5				56.27		2				44.18		4.6678

		56.3		7.5				56.3		7.5				56.3		3.5				56.3		0.5				44.2		4.3344

		56.33		5.5				56.33		5.5				56.33		4				56.33		0.5				44.22		4.3344

		56.36		4				56.36		4				56.36		3				56.36		0.5				44.24		3.3341

		56.39		1.5				56.39		1.5				56.39		1.5				56.39		1.5				44.26		5.3346

		56.42		5.5				56.42		5.5				56.42		3.5				56.42		1				44.28		4.001

		56.45		3.5				56.45		3.5				56.45		3				56.45		0.5				44.3		4.001

		56.48		2				56.48		2				56.48		3.5				56.48		1				44.32		5.0012

		56.51		5				56.51		5				56.51		2				56.51		1.5				44.34		7.3351

		56.54		2				56.54		2				56.54		4				56.54		0.5				44.36		5.0012

		56.57		1.5				56.57		1.5				56.57		2.5				56.57		1.5				44.38		3.0007

		56.6		4				56.6		4				56.6		2.5				56.6		2.5				44.4		5.0012

		56.63		3				56.63		3				56.63		4.5				56.63		1.5				44.42		4.3344

		56.66		4				56.66		4				56.66		4.5				56.66		2				44.44		4.3344

		56.69		3.5				56.69		3.5				56.69		4.5				56.69		1.5				44.46		3.6675

		56.72		3.5				56.72		3.5				56.72		4.5				56.72		3				44.48		4.6678

		56.75		3.5				56.75		3.5				56.75		1.5				56.75		2				44.5		5.0012

		56.78		5.5				56.78		5.5				56.78		5				56.78		0.5				44.52		6.6683

		56.81		6				56.81		6				56.81		6				56.81		1.5				44.54		4.6678

		56.84		5.5				56.84		5.5				56.84		3				56.84		3				44.56		5.0012

		56.87		6.5				56.87		6.5				56.87		4				56.87		2.5				44.58		4.3344

		56.9		6.5				56.9		6.5				56.9		4				56.9		3				44.6		4.001

		56.93		10.5				56.93		10.5				56.93		4				56.93		0.5				44.62		4.001

		56.96		12				56.96		12				56.96		5				56.96		3				44.64		3.3341

		56.99		7.5				56.99		7.5				56.99		8.5				56.99		3				44.66		4.6678

		57.02		16				57.02		16				57.02		8.5				57.02		3				44.68		4.001

		57.05		22.5				57.05		22.5				57.05		16				57.05		2				44.7		4.6678

		57.08		32.5				57.08		32.5				57.08		16.5				57.08		4.5				44.72		5.668

		57.11		28.5				57.11		28.5				57.11		25				57.11		5.5				44.74		4.6678

		57.14		40				57.14		40				57.14		40				57.14		8				44.76		4.3344

		57.17		46.5				57.17		46.5				57.17		43.5				57.17		11				44.78		3.6675

		57.2		32.5				57.2		32.5				57.2		45				57.2		23.5				44.8		3.6675

		57.23		28.5				57.23		28.5				57.23		40				57.23		19.5				44.82		5.0012

		57.26		24				57.26		24				57.26		34.5				57.26		17				44.84		3.3341

		57.29		25.5				57.29		25.5				57.29		26				57.29		8				44.86		4.6678

		57.32		18				57.32		18				57.32		14				57.32		7				44.88		5.0012

		57.35		13				57.35		13				57.35		17				57.35		8				44.9		3.3341

		57.38		9				57.38		9				57.38		10.5				57.38		14				44.92		4.001

		57.41		7.5				57.41		7.5				57.41		7				57.41		9				44.94		3.6675

		57.44		6.5				57.44		6.5				57.44		9.5				57.44		2				44.96		5.0012

		57.47		7				57.47		7				57.47		4.5				57.47		3.5				44.98		5.668

		57.5		4.5				57.5		4.5				57.5		4.5				57.5		1.5				45		6.0014

		57.53		4				57.53		4				57.53		4.5				57.53		1				45.02		7.0017

		57.56		5				57.56		5				57.56		4				57.56		3.5				45.04		3.6675

		57.59		7.5				57.59		7.5				57.59		3.5				57.59		1				45.06		6.0014

		57.62		6.5				57.62		6.5				57.62		4				57.62		2				45.08		3.6675

		57.65		4				57.65		4				57.65		7.5				57.65		1				45.1		5.3346

		57.68		5				57.68		5				57.68		6.5				57.68		1				45.12		5.3346

		57.71		5.5				57.71		5.5				57.71		5.5				57.71		0.5				45.14		5.668

		57.74		4.5				57.74		4.5				57.74		1.5				57.74		1.5				45.16		3.3341

		57.77		7.5				57.77		7.5				57.77		4				57.77		0				45.18		5.0012

		57.8		7				57.8		7				57.8		3				57.8		3.5				45.2		5.0012

		57.83		8				57.83		8				57.83		7				57.83		2.5				45.22		3.3341

		57.86		11				57.86		11				57.86		5.5				57.86		3.5				45.24		6.6683

		57.89		14				57.89		14				57.89		13				57.89		0				45.26		3.0007

		57.92		18.5				57.92		18.5				57.92		17				57.92		2				45.28		5.668

		57.95		41				57.95		41				57.95		35				57.95		2.5				45.3		5.668

		57.98		51.5				57.98		51.5				57.98		60				57.98		5.5				45.32		5.3346

		58.01		55				58.01		55				58.01		86				58.01		11				45.34		5.0012

		58.04		62.5				58.04		62.5				58.04		98.5				58.04		25.5				45.36		5.3346

		58.07		53.5				58.07		53.5				58.07		100.5				58.07		43.5				45.38		6.3349

		58.1		51.5				58.1		51.5				58.1		60				58.1		41				45.4		4.6678

		58.13		41				58.13		41				58.13		52.5				58.13		24				45.42		4.6678

		58.16		41.5				58.16		41.5				58.16		41.5				58.16		17				45.44		5.668

		58.19		24				58.19		24				58.19		33.5				58.19		15.5				45.46		7.0017

		58.22		19.5				58.22		19.5				58.22		15.5				58.22		24.5				45.48		11.003

		58.25		18.5				58.25		18.5				58.25		13.5				58.25		26				45.5		18.671

		58.28		9.5				58.28		9.5				58.28		8.5				58.28		14.5				45.52		19.671

		58.31		12				58.31		12				58.31		5.5				58.31		11.5				45.54		26.006

		58.34		6				58.34		6				58.34		4.5				58.34		6.5				45.56		17.004

		58.37		8				58.37		8				58.37		6				58.37		4.5				45.58		12.67

		58.4		7.5				58.4		7.5				58.4		3				58.4		4				45.6		11.669

		58.43		3.5				58.43		3.5				58.43		4.5				58.43		2.5				45.62		13.67

		58.46		9				58.46		9				58.46		4.5				58.46		0.5				45.64		15.337

		58.49		8				58.49		8				58.49		3.5				58.49		3.5				45.66		16.004

		58.52		6.5				58.52		6.5				58.52		5.5				58.52		1				45.68		16.004

		58.55		5.5				58.55		5.5				58.55		4				58.55		2.5				45.7		10.336

		58.58		5				58.58		5				58.58		4				58.58		1				45.72		9.3356

		58.61		4.5				58.61		4.5				58.61		3				58.61		2				45.74		6.6683

		58.64		5				58.64		5				58.64		4				58.64		1				45.76		7.3351

		58.67		4				58.67		4				58.67		2.5				58.67		1.5				45.78		5.0012

		58.7		5				58.7		5				58.7		2				58.7		3				45.8		5.0012

		58.73		5.5				58.73		5.5				58.73		1.5				58.73		1.5				45.82		4.3344

		58.76		5				58.76		5				58.76		1.5				58.76		1.5				45.84		4.001

		58.79		3				58.79		3				58.79		2				58.79		1				45.86		4.6678

		58.82		7				58.82		7				58.82		3				58.82		0				45.88		5.0012

		58.85		5				58.85		5				58.85		4				58.85		0.5				45.9		4.001

		58.88		4				58.88		4				58.88		3.5				58.88		2				45.92		4.001

		58.91		6.5				58.91		6.5				58.91		6				58.91		0				45.94		4.001

		58.94		2				58.94		2				58.94		2.5				58.94		1.5				45.96		5.3346

		58.97		4				58.97		4				58.97		3.5				58.97		1				45.98		7.3351

		59		5				59		5				59		3				59		1.5				46		2.3339

		59.03		4.5				59.03		4.5				59.03		4.5				59.03		2				46.02		4.001

		59.06		5.5				59.06		5.5				59.06		4				59.06		1				46.04		4.3344

		59.09		4				59.09		4				59.09		7				59.09		2				46.06		5.0012

		59.12		5				59.12		5				59.12		4				59.12		2.5				46.08		5.3346

		59.15		8.5				59.15		8.5				59.15		7				59.15		5				46.1		6.3349

		59.18		3.5				59.18		3.5				59.18		4				59.18		4.5				46.12		3.3341

		59.21		4.5				59.21		4.5				59.21		5				59.21		1.5				46.14		5.3346

		59.24		4				59.24		4				59.24		5				59.24		4				46.16		3.0007

		59.27		5				59.27		5				59.27		3				59.27		1.5				46.18		4.6678

		59.3		3				59.3		3				59.3		3				59.3		2				46.2		4.3344

		59.33		4				59.33		4				59.33		1.5				59.33		2.5				46.22		4.3344

		59.36		3				59.36		3				59.36		2				59.36		0.5				46.24		3.6675

		59.39		0.5				59.39		0.5				59.39		2.5				59.39		1.5				46.26		4.6678

		59.42		6				59.42		6				59.42		6				59.42		1				46.28		5.0012

		59.45		5.5				59.45		5.5				59.45		5.5				59.45		0				46.3		4.6678

		59.48		2				59.48		2				59.48		3.5				59.48		0				46.32		5.668

		59.51		6				59.51		6				59.51		5.5				59.51		1				46.34		3.3341

		59.54		5				59.54		5				59.54		4.5				59.54		0.5				46.36		4.001

		59.57		4				59.57		4				59.57		4.5				59.57		2.5				46.38		5.0012

		59.6		4				59.6		4				59.6		3				59.6		0				46.4		5.0012

		59.63		5				59.63		5				59.63		3				59.63		1.5				46.42		6.0014

		59.66		5.5				59.66		5.5				59.66		4				59.66		2				46.44		5.0012

		59.69		5				59.69		5				59.69		7.5				59.69		3.5				46.46		3.0007

		59.72		5.5				59.72		5.5				59.72		5				59.72		1				46.48		4.001

		59.75		6.5				59.75		6.5				59.75		5.5				59.75		0				46.5		6.0014

		59.78		11				59.78		11				59.78		8.5				59.78		3				46.52		4.6678

		59.81		10.5				59.81		10.5				59.81		9				59.81		1.5				46.54		4.3344

		59.84		13				59.84		13				59.84		14.5				59.84		2				46.56		3.6675

		59.87		21.5				59.87		21.5				59.87		20				59.87		3.5				46.58		6.0014

		59.9		22.5				59.9		22.5				59.9		25.5				59.9		6.5				46.6		3.3341

		59.93		23.5				59.93		23.5				59.93		45.5				59.93		5.5				46.62		3.6675

		59.96		21				59.96		21				59.96		35.5				59.96		12				46.64		4.001

		59.99		21.5				59.99		21.5				59.99		31.5				59.99		16				46.66		5.0012

		60.02		16.5				60.02		16.5				60.02		21				60.02		13.5				46.68		3.6675

		60.05		18.5				60.05		18.5				60.05		22				60.05		4.5				46.7		4.6678

		60.08		19.5				60.08		19.5				60.08		15.5				60.08		5				46.72		3.6675

		60.11		10				60.11		10				60.11		9				60.11		7				46.74		5.3346

		60.14		11				60.14		11				60.14		4.5				60.14		9				46.76		3.0007

		60.17		6.5				60.17		6.5				60.17		7				60.17		8.5				46.78		5.668

		60.2		3				60.2		3				60.2		5.5				60.2		4				46.8		1.6671

		60.23		3.5				60.23		3.5				60.23		2				60.23		3				46.82		4.3344

		60.26		7.5				60.26		7.5				60.26		4.5				60.26		0				46.84		2.6673

		60.29		3				60.29		3				60.29		4				60.29		2.5				46.86		3.0007

		60.32		6				60.32		6				60.32		2.5				60.32		2.5				46.88		3.3341

		60.35		4				60.35		4				60.35		7				60.35		2				46.9		2.6673

		60.38		9				60.38		9				60.38		5				60.38		2				46.92		4.3344

		60.41		5.5				60.41		5.5				60.41		3				60.41		2				46.94		5.668

		60.44		5				60.44		5				60.44		4.5				60.44		0.5				46.96		6.3349

		60.47		6				60.47		6				60.47		3				60.47		2.5				46.98		4.001

		60.5		6.5				60.5		6.5				60.5		5				60.5		2.5				47		5.3346

		60.53		3.5				60.53		3.5				60.53		3				60.53		1.5				47.02		4.6678

		60.56		4.5				60.56		4.5				60.56		2.5				60.56		1				47.04		4.6678

		60.59		3.5				60.59		3.5				60.59		2				60.59		2				47.06		6.6683

		60.62		3.5				60.62		3.5				60.62		2.5				60.62		1.5				47.08		4.001

		60.65		5.5				60.65		5.5				60.65		2.5				60.65		2				47.1		3.3341

		60.68		2				60.68		2				60.68		3.5				60.68		2				47.12		4.6678

		60.71		2.5				60.71		2.5				60.71		2.5				60.71		1.5				47.14		6.3349

		60.74		2.5				60.74		2.5				60.74		2				60.74		1				47.16		4.001

		60.77		3.5				60.77		3.5				60.77		0.5				60.77		1				47.18		6.3349

		60.8		3.5				60.8		3.5				60.8		5				60.8		1				47.2		2.6673

		60.83		2.5				60.83		2.5				60.83		4.5				60.83		1.5				47.22		3.3341

		60.86		2.5				60.86		2.5				60.86		3				60.86		1				47.24		3.0007

		60.89		2.5				60.89		2.5				60.89		3				60.89		1.5				47.26		5.3346

		60.92		6.5				60.92		6.5				60.92		3.5				60.92		1.5				47.28		4.3344

		60.95		9				60.95		9				60.95		5.5				60.95		1				47.3		4.001

		60.98		10.5				60.98		10.5				60.98		3.5				60.98		1				47.32		5.0012

		61.01		11				61.01		11				61.01		7.5				61.01		1				47.34		5.3346

		61.04		10				61.04		10				61.04		5.5				61.04		1.5				47.36		5.3346

		61.07		7.5				61.07		7.5				61.07		6.5				61.07		2.5				47.38		4.6678

		61.1		8.5				61.1		8.5				61.1		4				61.1		2				47.4		6.3349

		61.13		9.5				61.13		9.5				61.13		4.5				61.13		1.5				47.42		10.336

		61.16		7.5				61.16		7.5				61.16		3				61.16		3				47.44		10.336

		61.19		6.5				61.19		6.5				61.19		4.5				61.19		2				47.46		6.3349

		61.22		6				61.22		6				61.22		2				61.22		2.5				47.48		4.6678

		61.25		6				61.25		6				61.25		2.5				61.25		1.5				47.5		5.0012

		61.28		3				61.28		3				61.28		2				61.28		1.5				47.52		7.0017

		61.31		5.5				61.31		5.5				61.31		2.5				61.31		0.5				47.54		7.3351

		61.34		6.5				61.34		6.5				61.34		1				61.34		2.5				47.56		5.668

		61.37		1.5				61.37		1.5				61.37		4.5				61.37		2				47.58		6.0014

		61.4		5				61.4		5				61.4		4				61.4		0.5				47.6		4.001

		61.43		3				61.43		3				61.43		3.5				61.43		2				47.62		6.0014

		61.46		4.5				61.46		4.5				61.46		2				61.46		0.5				47.64		4.001

		61.49		1				61.49		1				61.49		2.5				61.49		1.5				47.66		4.001

		61.52		1.5				61.52		1.5				61.52		5				61.52		2.5				47.68		5.0012

		61.55		5				61.55		5				61.55		3				61.55		1				47.7		9.0022

		61.58		5				61.58		5				61.58		3				61.58		2				47.72		5.668

		61.61		2				61.61		2				61.61		2				61.61		2				47.74		8.6687

		61.64		3				61.64		3				61.64		2				61.64		1.5				47.76		14.67

		61.67		3				61.67		3				61.67		5.5				61.67		4				47.78		9.0022

		61.7		3.5				61.7		3.5				61.7		2.5				61.7		1				47.8		8.0019

		61.73		2.5				61.73		2.5				61.73		4				61.73		1				47.82		7.0017

		61.76		5				61.76		5				61.76		3				61.76		1				47.84		6.6683

		61.79		6.5				61.79		6.5				61.79		1				61.79		0.5				47.86		5.3346

		61.82		4.5				61.82		4.5				61.82		7				61.82		1.5				47.88		7.3351

		61.85		5				61.85		5				61.85		4				61.85		2				47.9		8.6687

		61.88		3.5				61.88		3.5				61.88		3.5				61.88		1				47.92		10.336

		61.91		8				61.91		8				61.91		5				61.91		0.5				47.94		7.3351

		61.94		4.5				61.94		4.5				61.94		5				61.94		2				47.96		4.6678

		61.97		8				61.97		8				61.97		4.5				61.97		1.5				47.98		6.6683

		62		7.5				62		7.5				62		4.5				62		1.5				48		6.6683

		62.03		7.5				62.03		7.5				62.03		5				62.03		5				48.02		5.3346

		62.06		12				62.06		12				62.06		9.5				62.06		1				48.04		4.001

		62.09		24				62.09		24				62.09		12				62.09		2.5				48.06		5.668

		62.12		22.5				62.12		22.5				62.12		17.5				62.12		3.5				48.08		8.3353

		62.15		32.5				62.15		32.5				62.15		24.5				62.15		6.5				48.1		4.6678

		62.18		36				62.18		36				62.18		32				62.18		7.5				48.12		4.6678

		62.21		29.5				62.21		29.5				62.21		33.5				62.21		15.5				48.14		4.3344

		62.24		23.5				62.24		23.5				62.24		29.5				62.24		17				48.16		4.6678

		62.27		18				62.27		18				62.27		23.5				62.27		18				48.18		3.3341

		62.3		23.5				62.3		23.5				62.3		16				62.3		9				48.2		7.0017

		62.33		16				62.33		16				62.33		20				62.33		3				48.22		5.3346

		62.36		11				62.36		11				62.36		13				62.36		6				48.24		3.0007

		62.39		11				62.39		11				62.39		10.5				62.39		8				48.26		3.6675

		62.42		10.5				62.42		10.5				62.42		10				62.42		10				48.28		4.3344

		62.45		9.5				62.45		9.5				62.45		11.5				62.45		8				48.3		4.6678

		62.48		11				62.48		11				62.48		8.5				62.48		3				48.32		4.001

		62.51		9.5				62.51		9.5				62.51		13.5				62.51		1				48.34		3.6675

		62.54		19				62.54		19				62.54		9.5				62.54		3				48.36		2.0005

		62.57		14				62.57		14				62.57		15.5				62.57		5.5				48.38		5.668

		62.6		14.5				62.6		14.5				62.6		9.5				62.6		4				48.4		4.6678

		62.63		19				62.63		19				62.63		14				62.63		3				48.42		3.0007

		62.66		21				62.66		21				62.66		12.5				62.66		3				48.44		2.6673

		62.69		21				62.69		21				62.69		18				62.69		4				48.46		3.6675

		62.72		27.5				62.72		27.5				62.72		17				62.72		2.5				48.48		5.668

		62.75		29.5				62.75		29.5				62.75		22				62.75		5.5				48.5		2.0005

		62.78		40.5				62.78		40.5				62.78		26.5				62.78		2.5				48.52		5.668

		62.81		40				62.81		40				62.81		25				62.81		9.5				48.54		4.3344

		62.84		35.5				62.84		35.5				62.84		30.5				62.84		8				48.56		3.0007

		62.87		46.5				62.87		46.5				62.87		34				62.87		9.5				48.58		4.6678

		62.9		44				62.9		44				62.9		31				62.9		11.5				48.6		6.0014

		62.93		33.5				62.93		33.5				62.93		40.5				62.93		12.5				48.62		3.0007

		62.96		41				62.96		41				62.96		29.5				62.96		10.5				48.64		5.668

		62.99		34				62.99		34				62.99		36				62.99		23				48.66		3.6675

		63.02		31				63.02		31				63.02		39.5				63.02		13.5				48.68		3.6675

		63.05		26				63.05		26				63.05		18.5				63.05		8				48.7		4.6678

		63.08		20				63.08		20				63.08		23				63.08		8				48.72		5.3346

		63.11		13				63.11		13				63.11		14.5				63.11		6.5				48.74		2.6673

		63.14		17.5				63.14		17.5				63.14		13.5				63.14		7.5				48.76		3.0007

		63.17		12.5				63.17		12.5				63.17		12.5				63.17		8				48.78		4.3344

		63.2		13				63.2		13				63.2		10.5				63.2		6				48.8		4.001

		63.23		11.5				63.23		11.5				63.23		12				63.23		6				48.82		5.0012

		63.26		11.5				63.26		11.5				63.26		9				63.26		3.5				48.84		4.001

		63.29		13.5				63.29		13.5				63.29		14.5				63.29		2				48.86		5.3346

		63.32		23.5				63.32		23.5				63.32		17				63.32		1.5				48.88		5.0012

		63.35		32				63.35		32				63.35		31.5				63.35		3				48.9		3.6675

		63.38		29.5				63.38		29.5				63.38		45.5				63.38		4				48.92		6.6683

		63.41		34				63.41		34				63.41		44.5				63.41		8				48.94		4.3344

		63.44		43				63.44		43				63.44		39				63.44		12.5				48.96		2.6673

		63.47		34				63.47		34				63.47		32.5				63.47		19.5				48.98		4.3344

		63.5		32.5				63.5		32.5				63.5		27				63.5		25				49		3.0007

		63.53		32.5				63.53		32.5				63.53		24				63.53		29				49.02		4.3344

		63.56		25				63.56		25				63.56		21				63.56		22				49.04		4.001

		63.59		23.5				63.59		23.5				63.59		16				63.59		11.5				49.06		6.0014

		63.62		16.5				63.62		16.5				63.62		16				63.62		14				49.08		7.3351

		63.65		19				63.65		19				63.65		13.5				63.65		12.5				49.1		4.3344

		63.68		12				63.68		12				63.68		6				63.68		13.5				49.12		3.3341

		63.71		16.5				63.71		16.5				63.71		8				63.71		19				49.14		6.6683

		63.74		14.5				63.74		14.5				63.74		8.5				63.74		12				49.16		5.0012

		63.77		16.5				63.77		16.5				63.77		8.5				63.77		5				49.18		5.668

		63.8		12				63.8		12				63.8		6				63.8		2.5				49.2		4.6678

		63.83		14.5				63.83		14.5				63.83		6.5				63.83		2.5				49.22		3.3341

		63.86		17				63.86		17				63.86		15				63.86		3				49.24		4.001

		63.89		26				63.89		26				63.89		17				63.89		4				49.26		4.001

		63.92		26.5				63.92		26.5				63.92		24.5				63.92		4.5				49.28		6.3349

		63.95		40				63.95		40				63.95		40.5				63.95		9.5				49.3		4.001

		63.98		50				63.98		50				63.98		57.5				63.98		17.5				49.32		5.668

		64.01		45.5				64.01		45.5				64.01		62				64.01		21.5				49.34		5.668

		64.04		34				64.04		34				64.04		52				64.04		20.5				49.36		6.6683

		64.07		31				64.07		31				64.07		38.5				64.07		17				49.38		5.668

		64.1		20.5				64.1		20.5				64.1		29				64.1		8.5				49.4		6.3349

		64.13		24.5				64.13		24.5				64.13		16				64.13		7.5				49.42		6.6683

		64.16		22.5				64.16		22.5				64.16		20				64.16		9.5				49.44		6.0014

		64.19		16				64.19		16				64.19		19				64.19		8.5				49.46		4.001

		64.22		12.5				64.22		12.5				64.22		10.5				64.22		3				49.48		4.6678

		64.25		11				64.25		11				64.25		6.5				64.25		6				49.5		6.3349

		64.28		14.5				64.28		14.5				64.28		7				64.28		4.5				49.52		5.3346

		64.31		12.5				64.31		12.5				64.31		7.5				64.31		6.5				49.54		5.0012

		64.34		10.5				64.34		10.5				64.34		8.5				64.34		2				49.56		5.0012

		64.37		9				64.37		9				64.37		7				64.37		1.5				49.58		3.6675

		64.4		10				64.4		10				64.4		10				64.4		2				49.6		4.001

		64.43		15				64.43		15				64.43		18.5				64.43		3				49.62		6.3349

		64.46		8				64.46		8				64.46		6.5				64.46		3				49.64		5.668

		64.49		12				64.49		12				64.49		11				64.49		6				49.66		6.0014

		64.52		12				64.52		12				64.52		8				64.52		5				49.68		5.3346

		64.55		9				64.55		9				64.55		9				64.55		5.5				49.7		7.0017

		64.58		11.5				64.58		11.5				64.58		8				64.58		1.5				49.72		7.0017

		64.61		9				64.61		9				64.61		7.5				64.61		1.5				49.74		6.3349

		64.64		8				64.64		8				64.64		4.5				64.64		2				49.76		4.6678

		64.67		5.5				64.67		5.5				64.67		5.5				64.67		2				49.78		8.3353

		64.7		6				64.7		6				64.7		5.5				64.7		3				49.8		13.003

		64.73		5.5				64.73		5.5				64.73		6.5				64.73		2				49.82		8.0019

		64.76		3.5				64.76		3.5				64.76		4.5				64.76		1				49.84		8.6687

		64.79		4				64.79		4				64.79		2				64.79		1.5				49.86		14.67

		64.82		4				64.82		4				64.82		2.5				64.82		1.5				49.88		25.339

		64.85		6				64.85		6				64.85		3				64.85		1				49.9		43.344

		64.88		1.5				64.88		1.5				64.88		2.5				64.88		1.5				49.92		64.015

		64.91		4				64.91		4				64.91		4				64.91		1.5				49.94		56.347

		64.94		5				64.94		5				64.94		5.5				64.94		2				49.96		40.01

		64.97		3				64.97		3				64.97		4.5				64.97		0.5				49.98		22.005

		65		2				65		2				65		5				65		3.5				50		19.671

		65.03		5				65.03		5				65.03		3.5				65.03		1				50.02		22.005

		65.06		2.5				65.06		2.5				65.06		1.5				65.06		2				50.04		32.008

		65.09		2.5				65.09		2.5				65.09		6				65.09		1.5				50.06		35.342

		65.12		3.5				65.12		3.5				65.12		3				65.12		1				50.08		25.339

		65.15		1.5				65.15		1.5				65.15		1.5				65.15		1				50.1		19.338

		65.18		3				65.18		3				65.18		4				65.18		0				50.12		11.336

		65.21		3				65.21		3				65.21		4				65.21		2				50.14		11.003

		65.24		3.5				65.24		3.5				65.24		1				65.24		0				50.16		5.3346

		65.27		2.5				65.27		2.5				65.27		2				65.27		2				50.18		8.6687

		65.3		5				65.3		5				65.3		2.5				65.3		1.5				50.2		5.3346

		65.33		4				65.33		4				65.33		2.5				65.33		1.5				50.22		8.0019

		65.36		4				65.36		4				65.36		2				65.36		1				50.24		6.6683

		65.39		0.5				65.39		0.5				65.39		5				65.39		1				50.26		4.6678

		65.42		3				65.42		3				65.42		3				65.42		1				50.28		3.3341

		65.45		1.5				65.45		1.5				65.45		8				65.45		0.5				50.3		5.3346

		65.48		1.5				65.48		1.5				65.48		4.5				65.48		2				50.32		4.001

		65.51		2.5				65.51		2.5				65.51		2				65.51		0.5				50.34		5.0012

		65.54		4.5				65.54		4.5				65.54		3				65.54		1.5				50.36		3.0007

		65.57		3				65.57		3				65.57		1				65.57		1				50.38		5.0012

		65.6		4.5				65.6		4.5				65.6		1.5				65.6		1.5				50.4		3.0007

		65.63		1.5				65.63		1.5				65.63		5				65.63		3.5				50.42		3.3341

		65.66		4				65.66		4				65.66		3				65.66		1				50.44		5.0012

		65.69		3.5				65.69		3.5				65.69		2				65.69		1				50.46		4.001

		65.72		5				65.72		5				65.72		2.5				65.72		0				50.48		6.3349

		65.75		5				65.75		5				65.75		3				65.75		1				50.5		5.0012

		65.78		2				65.78		2				65.78		3				65.78		1				50.52		4.6678

		65.81		2				65.81		2				65.81		1				65.81		1.5				50.54		4.6678

		65.84		1.5				65.84		1.5				65.84		3				65.84		2				50.56		4.6678

		65.87		5				65.87		5				65.87		3				65.87		1.5				50.58		3.6675

		65.9		3				65.9		3				65.9		3.5				65.9		2				50.6		5.3346

		65.93		5				65.93		5				65.93		2.5				65.93		3.5				50.62		3.6675

		65.96		6				65.96		6				65.96		3.5				65.96		2.5				50.64		5.668

		65.99		3.5				65.99		3.5				65.99		2.5				65.99		3				50.66		7.3351

		66.02		4.5				66.02		4.5				66.02		2				66.02		5				50.68		7.6685

		66.05		1				66.05		1				66.05		5.5				66.05		5.5				50.7		6.6683

		66.08		2.5				66.08		2.5				66.08		3.5				66.08		5				50.72		10.002

		66.11		1.5				66.11		1.5				66.11		3.5				66.11		3				50.74		14.337

		66.14		2.5				66.14		2.5				66.14		3				66.14		0				50.76		15.67

		66.17		2				66.17		2				66.17		4				66.17		0				50.78		12.67

		66.2		4				66.2		4				66.2		3				66.2		2				50.8		14.003

		66.23		4				66.23		4				66.23		4				66.23		1.5				50.82		10.002

		66.26		1				66.26		1				66.26		4				66.26		1.5				50.84		8.3353

		66.29		3.5				66.29		3.5				66.29		2				66.29		2				50.86		8.3353

		66.32		4.5				66.32		4.5				66.32		4.5				66.32		3.5				50.88		11.336

		66.35		5				66.35		5				66.35		6.5				66.35		2				50.9		10.336

		66.38		3				66.38		3				66.38		5				66.38		0.5				50.92		7.3351

		66.41		4				66.41		4				66.41		4.5				66.41		2				50.94		6.3349

		66.44		4				66.44		4				66.44		8				66.44		4				50.96		6.6683

		66.47		4				66.47		4				66.47		3				66.47		3				50.98		5.0012

		66.5		0.5				66.5		0.5				66.5		3.5				66.5		2.5				51		7.6685

		66.53		3				66.53		3				66.53		3.5				66.53		1				51.02		4.3344

		66.56		3.5				66.56		3.5				66.56		3				66.56		1				51.04		6.6683

		66.59		3				66.59		3				66.59		3.5				66.59		2				51.06		6.3349

		66.62		1.5				66.62		1.5				66.62		2.5				66.62		5				51.08		4.001

		66.65		2				66.65		2				66.65		1.5				66.65		1.5				51.1		7.0017

		66.68		3				66.68		3				66.68		2.5				66.68		1				51.12		4.3344

		66.71		3				66.71		3				66.71		3				66.71		0				51.14		5.0012

		66.74		2.5				66.74		2.5				66.74		3				66.74		0.5				51.16		5.3346

		66.77		4				66.77		4				66.77		2.5				66.77		1.5				51.18		5.0012

		66.8		5				66.8		5				66.8		4				66.8		1				51.2		4.3344

		66.83		5				66.83		5				66.83		3				66.83		2.5				51.22		4.6678

		66.86		2.5				66.86		2.5				66.86		2.5				66.86		1.5				51.24		4.6678

		66.89		4				66.89		4				66.89		4				66.89		1				51.26		4.3344

		66.92		2				66.92		2				66.92		2.5				66.92		0.5				51.28		3.0007

		66.95		1				66.95		1				66.95		4				66.95		1				51.3		5.3346

		66.98		1.5				66.98		1.5				66.98		3				66.98		0.5				51.32		4.6678

		67.01		1.5				67.01		1.5				67.01		3.5				67.01		0				51.34		5.3346

		67.04		2.5				67.04		2.5				67.04		4.5				67.04		1.5				51.36		8.6687

		67.07		2.5				67.07		2.5				67.07		1.5				67.07		1.5				51.38		5.0012

		67.1		4.5				67.1		4.5				67.1		4				67.1		0.5				51.4		5.668

		67.13		5				67.13		5				67.13		1.5				67.13		1				51.42		7.0017

		67.16		1.5				67.16		1.5				67.16		5.5				67.16		1				51.44		8.0019

		67.19		4				67.19		4				67.19		2.5				67.19		1.5				51.46		10.336

		67.22		2				67.22		2				67.22		3				67.22		1				51.48		9.669

		67.25		5.5				67.25		5.5				67.25		4.5				67.25		2				51.5		15.004

		67.28		2.5				67.28		2.5				67.28		0.5				67.28		0				51.52		20.338

		67.31		1				67.31		1				67.31		5.5				67.31		0.5				51.54		31.007

		67.34		1				67.34		1				67.34		3				67.34		0				51.56		59.348

		67.37		2.5				67.37		2.5				67.37		2				67.37		0				51.58		69.35

		67.4		3.5				67.4		3.5				67.4		6				67.4		1.5				51.6		71.35

		67.43		8.5				67.43		8.5				67.43		6.5				67.43		1.5				51.62		60.348

		67.46		2.5				67.46		2.5				67.46		5				67.46		0.5				51.64		37.009

		67.49		5				67.49		5				67.49		8				67.49		3				51.66		24.006

		67.52		8				67.52		8				67.52		9.5				67.52		1.5				51.68		28.674

		67.55		11				67.55		11				67.55		9				67.55		2.5				51.7		40.343

		67.58		8				67.58		8				67.58		11.5				67.58		4				51.72		46.678

		67.61		8				67.61		8				67.61		10				67.61		5				51.74		40.676

		67.64		8				67.64		8				67.64		6.5				67.64		5.5				51.76		36.675

		67.67		7				67.67		7				67.67		8				67.67		3.5				51.78		22.672

		67.7		9				67.7		9				67.7		7.5				67.7		1				51.8		14.003

		67.73		8				67.73		8				67.73		5				67.73		3				51.82		10.002

		67.76		9.5				67.76		9.5				67.76		4				67.76		1.5				51.84		13.003

		67.79		6				67.79		6				67.79		6				67.79		2.5				51.86		12.336

		67.82		6.5				67.82		6.5				67.82		3.5				67.82		3.5				51.88		13.337

		67.85		4				67.85		4				67.85		4.5				67.85		1.5				51.9		12.67

		67.88		7.5				67.88		7.5				67.88		3				67.88		3				51.92		16.337

		67.91		7.5				67.91		7.5				67.91		3.5				67.91		3.5				51.94		28.007

		67.94		7.5				67.94		7.5				67.94		5				67.94		1.5				51.96		30.674

		67.97		7				67.97		7				67.97		7				67.97		1.5				51.98		32.675

		68		16				68		16				68		12				68		1.5				52		26.34

		68.03		15				68.03		15				68.03		10.5				68.03		1.5				52.02		25.673

		68.06		17.5				68.06		17.5				68.06		19				68.06		2.5				52.04		25.339

		68.09		18.5				68.09		18.5				68.09		22.5				68.09		5.5				52.06		14.003

		68.12		25				68.12		25				68.12		26				68.12		10				52.08		18.004

		68.15		23				68.15		23				68.15		27.5				68.15		8.5				52.1		20.672

		68.18		19.5				68.18		19.5				68.18		26.5				68.18		11.5				52.12		18.338

		68.21		24				68.21		24				68.21		21.5				68.21		7				52.14		19.338

		68.24		22				68.24		22				68.24		17.5				68.24		4.5				52.16		17.337

		68.27		20				68.27		20				68.27		25				68.27		3.5				52.18		11.336

		68.3		23.5				68.3		23.5				68.3		29.5				68.3		7				52.2		12.336

		68.33		20				68.33		20				68.33		25				68.33		10.5				52.22		9.0022

		68.36		16.5				68.36		16.5				68.36		19.5				68.36		11.5				52.24		8.6687

		68.39		17.5				68.39		17.5				68.39		16.5				68.39		6.5				52.26		6.6683

		68.42		10				68.42		10				68.42		15.5				68.42		6.5				52.28		7.3351

		68.45		5.5				68.45		5.5				68.45		10				68.45		3.5				52.3		6.0014

		68.48		7				68.48		7				68.48		7.5				68.48		3.5				52.32		6.0014

		68.51		10.5				68.51		10.5				68.51		8.5				68.51		6.5				52.34		6.0014

		68.54		6				68.54		6				68.54		9				68.54		3.5				52.36		4.3344

		68.57		10.5				68.57		10.5				68.57		4				68.57		5				52.38		4.6678

		68.6		3.5				68.6		3.5				68.6		3				68.6		6.5				52.4		6.3349

		68.63		3.5				68.63		3.5				68.63		4.5				68.63		4				52.42		4.001

		68.66		4				68.66		4				68.66		3.5				68.66		2				52.44		6.0014

		68.69		4.5				68.69		4.5				68.69		9				68.69		1				52.46		5.0012

		68.72		6				68.72		6				68.72		5				68.72		3.5				52.48		4.3344

		68.75		5				68.75		5				68.75		3				68.75		3				52.5		4.001

		68.78		10.5				68.78		10.5				68.78		5				68.78		1.5				52.52		5.668

		68.81		10.5				68.81		10.5				68.81		5.5				68.81		1				52.54		3.3341

		68.84		7.5				68.84		7.5				68.84		8.5				68.84		2				52.56		2.6673

		68.87		11.5				68.87		11.5				68.87		9.5				68.87		3.5				52.58		3.6675

		68.9		12				68.9		12				68.9		5				68.9		3.5				52.6		6.6683

		68.93		9				68.93		9				68.93		6				68.93		12				52.62		5.0012

		68.96		8				68.96		8				68.96		8				68.96		10.5				52.64		5.0012

		68.99		11				68.99		11				68.99		6				68.99		3.5				52.66		4.001

		69.02		6.5				69.02		6.5				69.02		3				69.02		4				52.68		5.3346

		69.05		2.5				69.05		2.5				69.05		5				69.05		2.5				52.7		4.001

		69.08		5				69.08		5				69.08		4.5				69.08		4				52.72		3.6675

		69.11		6				69.11		6				69.11		5				69.11		2				52.74		7.6685

		69.14		4.5				69.14		4.5				69.14		3				69.14		5.5				52.76		5.0012

		69.17		2.5				69.17		2.5				69.17		4				69.17		5.5				52.78		4.001

		69.2		3.5				69.2		3.5				69.2		3.5				69.2		3.5				52.8		6.0014

		69.23		2.5				69.23		2.5				69.23		2.5				69.23		4.5				52.82		4.6678

		69.26		1.5				69.26		1.5				69.26		2.5				69.26		1.5				52.84		5.668

		69.29		6				69.29		6				69.29		3				69.29		0				52.86		6.0014

		69.32		1				69.32		1				69.32		2.5				69.32		0				52.88		4.001

		69.35		2.5				69.35		2.5				69.35		2				69.35		0.5				52.9		6.3349

		69.38		2				69.38		2				69.38		1.5				69.38		1				52.92		6.0014

		69.41		4				69.41		4				69.41		2				69.41		2				52.94		6.6683

		69.44		3.5				69.44		3.5				69.44		3.5				69.44		0				52.96		6.0014

		69.47		2.5				69.47		2.5				69.47		4.5				69.47		1				52.98		6.6683

		69.5		4				69.5		4				69.5		5.5				69.5		0				53		11.669

		69.53		3				69.53		3				69.53		2.5				69.53		1.5				53.02		6.6683

		69.56		6.5				69.56		6.5				69.56		1.5				69.56		2.5				53.04		3.6675

		69.59		2.5				69.59		2.5				69.59		2				69.59		1.5				53.06		6.6683

		69.62		8.5				69.62		8.5				69.62		2.5				69.62		2				53.08		5.668

		69.65		4				69.65		4				69.65		1				69.65		3				53.1		8.3353

		69.68		3				69.68		3				69.68		2.5				69.68		3.5				53.12		8.3353

		69.71		3				69.71		3				69.71		2				69.71		1				53.14		9.0022

		69.74		4.5				69.74		4.5				69.74		1.5				69.74		2.5				53.16		11.669

		69.77		5				69.77		5				69.77		2				69.77		1				53.18		13.67

		69.8		2.5				69.8		2.5				69.8		3				69.8		1.5				53.2		13.337

		69.83		4				69.83		4				69.83		3.5				69.83		3				53.22		15.337

		69.86		2.5				69.86		2.5				69.86		2.5				69.86		1				53.24		15.67

		69.89		3				69.89		3				69.89		4				69.89		0.5				53.26		20.005

		69.92		1				69.92		1				69.92		5.5				69.92		1				53.28		26.34

		69.95		4				69.95		4				69.95		4.5				69.95		2				53.3		35.342

		69.98		3				69.98		3				69.98		7.5				69.98		1.5				53.32		62.682

		70.01		7.5				70.01		7.5				70.01		4.5				70.01		3.5				53.34		116.03

		70.04		7.5				70.04		7.5				70.04		11.5				70.04		4.5				53.36		178.38

		70.07		6.5				70.07		6.5				70.07		12.5				70.07		7				53.38		218.05

		70.1		4.5				70.1		4.5				70.1		10				70.1		5				53.4		184.04

		70.13		9.5				70.13		9.5				70.13		14				70.13		7.5				53.42		95.356

		70.16		8.5				70.16		8.5				70.16		9.5				70.16		5				53.44		69.017

		70.19		6.5				70.19		6.5				70.19		4				70.19		2.5				53.46		61.681

		70.22		8				70.22		8				70.22		7.5				70.22		1				53.48		84.687

		70.25		6				70.25		6				70.25		7				70.25		1.5				53.5		105.36

		70.28		5.5				70.28		5.5				70.28		7				70.28		3				53.52		139.03

		70.31		4.5				70.31		4.5				70.31		6				70.31		7				53.54		126.36

		70.34		3				70.34		3				70.34		5				70.34		3.5				53.56		76.018

		70.37		6				70.37		6				70.37		3.5				70.37		1.5				53.58		62.015

		70.4		2				70.4		2				70.4		4.5				70.4		2				53.6		40.01

		70.43		3.5				70.43		3.5				70.43		5.5				70.43		1.5				53.62		31.674

		70.46		2.5				70.46		2.5				70.46		2				70.46		1.5				53.64		24.339

		70.49		4.5				70.49		4.5				70.49		2.5				70.49		2.5				53.66		22.339

		70.52		3.5				70.52		3.5				70.52		5.5				70.52		0.5				53.68		17.671

		70.55		7				70.55		7				70.55		5.5				70.55		2.5				53.7		22.672

		70.58		5				70.58		5				70.58		3				70.58		2.5				53.72		18.004

		70.61		5.5				70.61		5.5				70.61		4.5				70.61		3				53.74		21.338

		70.64		12.5				70.64		12.5				70.64		6				70.64		1.5				53.76		10.002

		70.67		4.5				70.67		4.5				70.67		2				70.67		1				53.78		13.337

		70.7		10.5				70.7		10.5				70.7		8.5				70.7		1.5				53.8		10.669

		70.73		16				70.73		16				70.73		6				70.73		2				53.82		5.0012

		70.76		15.5				70.76		15.5				70.76		10.5				70.76		2.5				53.84		9.0022

		70.79		23				70.79		23				70.79		14				70.79		3.5				53.86		11.336

		70.82		26.5				70.82		26.5				70.82		35.5				70.82		8.5				53.88		7.3351

		70.85		30				70.85		30				70.85		36.5				70.85		8.5				53.9		4.6678

		70.88		29				70.88		29				70.88		29				70.88		22				53.92		7.0017

		70.91		26.5				70.91		26.5				70.91		37				70.91		25.5				53.94		6.6683

		70.94		27				70.94		27				70.94		23.5				70.94		17				53.96		7.0017

		70.97		20.5				70.97		20.5				70.97		25.5				70.97		10.5				53.98		8.0019

		71		28				71		28				71		29.5				71		13.5				54		7.3351

		71.03		24.5				71.03		24.5				71.03		29.5				71.03		17.5				54.02		7.0017

		71.06		26				71.06		26				71.06		18				71.06		14				54.04		9.3356

		71.09		24.5				71.09		24.5				71.09		21.5				71.09		15				54.06		16.671

		71.12		16.5				71.12		16.5				71.12		16.5				71.12		20				54.08		22.672

		71.15		13				71.15		13				71.15		12.5				71.15		11.5				54.1		26.006

		71.18		11.5				71.18		11.5				71.18		9.5				71.18		7				54.12		23.672

		71.21		6				71.21		6				71.21		10.5				71.21		6.5				54.14		25.339

		71.24		8.5				71.24		8.5				71.24		9.5				71.24		3				54.16		18.338

		71.27		4				71.27		4				71.27		3.5				71.27		5.5				54.18		10.669

		71.3		3				71.3		3				71.3		6.5				71.3		6				54.2		9.3356

		71.33		3				71.33		3				71.33		3				71.33		4.5				54.22		12.003

		71.36		3				71.36		3				71.36		3.5				71.36		3				54.24		12.67

		71.39		2				71.39		2				71.39		4.5				71.39		1.5				54.26		19.005

		71.42		5				71.42		5				71.42		4.5				71.42		1.5				54.28		13.003

		71.45		4.5				71.45		4.5				71.45		1				71.45		0.5				54.3		15.004

		71.48		3.5				71.48		3.5				71.48		1.5				71.48		1.5				54.32		8.0019

		71.51		2.5				71.51		2.5				71.51		3				71.51		1.5				54.34		4.3344

		71.54		4				71.54		4				71.54		2.5				71.54		0				54.36		8.3353

		71.57		2.5				71.57		2.5				71.57		2.5				71.57		2.5				54.38		6.3349

		71.6		5.5				71.6		5.5				71.6		2.5				71.6		0				54.4		7.0017

		71.63		1.5				71.63		1.5				71.63		2.5				71.63		2				54.42		5.668

		71.66		1.5				71.66		1.5				71.66		1				71.66		0.5				54.44		7.0017

		71.69		2.5				71.69		2.5				71.69		2				71.69		0.5				54.46		9.0022

		71.72		2.5				71.72		2.5				71.72		2.5				71.72		0.5				54.48		6.0014

		71.75		3				71.75		3				71.75		2				71.75		1.5				54.5		5.0012

		71.78		1.5				71.78		1.5				71.78		2				71.78		0				54.52		2.6673

		71.81		2				71.81		2				71.81		1				71.81		1.5				54.54		3.6675

		71.84		4.5				71.84		4.5				71.84		4				71.84		1.5				54.56		5.0012

		71.87		2				71.87		2				71.87		2				71.87		1				54.58		4.3344

		71.9		4				71.9		4				71.9		3.5				71.9		1.5				54.6		5.3346

		71.93		2				71.93		2				71.93		1.5				71.93		2				54.62		5.0012

		71.96		3				71.96		3				71.96		2				71.96		0				54.64		3.0007

		71.99		1				71.99		1				71.99		3.5				71.99		0.5				54.66		5.3346

		72.02		2.5				72.02		2.5				72.02		3				72.02		1.5				54.68		5.3346

		72.05		1.5				72.05		1.5				72.05		2				72.05		1				54.7		8.0019

		72.08		5.5				72.08		5.5				72.08		2.5				72.08		2				54.72		7.0017

		72.11		2				72.11		2				72.11		1.5				72.11		1				54.74		4.6678

		72.14		3				72.14		3				72.14		1.5				72.14		1.5				54.76		7.0017

		72.17		4				72.17		4				72.17		1				72.17		1.5				54.78		5.0012

		72.2		1				72.2		1				72.2		2				72.2		2.5				54.8		8.0019

		72.23		3.5				72.23		3.5				72.23		2				72.23		1				54.82		11.003

		72.26		0.5				72.26		0.5				72.26		4.5				72.26		0.5				54.84		4.6678

		72.29		2				72.29		2				72.29		1.5				72.29		1.5				54.86		8.0019

		72.32		4				72.32		4				72.32		2.5				72.32		1				54.88		9.3356

		72.35		2				72.35		2				72.35		1				72.35		1.5				54.9		9.3356

		72.38		3				72.38		3				72.38		2				72.38		3				54.92		12.003

		72.41		2				72.41		2				72.41		1.5				72.41		4				54.94		6.0014

		72.44		2				72.44		2				72.44		2				72.44		0.5				54.96		7.3351

		72.47		5.5				72.47		5.5				72.47		0.5				72.47		1				54.98		7.6685

		72.5		3				72.5		3				72.5		0.5				72.5		2				55		7.0017

		72.53		2				72.53		2				72.53		2.5				72.53		0				55.02		8.3353

		72.56		2.5				72.56		2.5				72.56		1.5				72.56		1.5				55.04		8.6687

		72.59		1.5				72.59		1.5				72.59		3				72.59		3				55.06		9.3356

		72.62		2.5				72.62		2.5				72.62		2.5				72.62		2.5				55.08		8.0019

		72.65		5.5				72.65		5.5				72.65		3.5				72.65		1				55.1		7.0017

		72.68		5.5				72.68		5.5				72.68		2.5				72.68		1.5				55.12		5.3346

		72.71		3.5				72.71		3.5				72.71		3.5				72.71		3				55.14		5.668

		72.74		7.5				72.74		7.5				72.74		3.5				72.74		0.5				55.16		4.6678

		72.77		2.5				72.77		2.5				72.77		3				72.77		1				55.18		7.6685

		72.8		3.5				72.8		3.5				72.8		3.5				72.8		1				55.2		6.6683

		72.83		4				72.83		4				72.83		2.5				72.83		1				55.22		5.3346

		72.86		3				72.86		3				72.86		4.5				72.86		0				55.24		5.668

		72.89		3.5				72.89		3.5				72.89		4				72.89		2				55.26		5.3346

		72.92		6				72.92		6				72.92		4				72.92		2.5				55.28		6.3349

		72.95		6.5				72.95		6.5				72.95		3.5				72.95		2.5				55.3		7.3351

		72.98		8.5				72.98		8.5				72.98		6.5				72.98		0				55.32		3.6675

		73.01		6.5				73.01		6.5				73.01		6.5				73.01		1.5				55.34		7.0017

		73.04		10.5				73.04		10.5				73.04		9				73.04		3.5				55.36		3.0007

		73.07		15				73.07		15				73.07		9.5				73.07		4.5				55.38		4.001

		73.1		16.5				73.1		16.5				73.1		21				73.1		6				55.4		5.668

		73.13		20				73.13		20				73.13		22.5				73.13		4.5				55.42		3.0007

		73.16		19.5				73.16		19.5				73.16		17.5				73.16		5.5				55.44		2.3339

		73.19		16.5				73.19		16.5				73.19		21.5				73.19		2.5				55.46		4.001

		73.22		13.5				73.22		13.5				73.22		9.5				73.22		5.5				55.48		4.6678

		73.25		13.5				73.25		13.5				73.25		14				73.25		5.5				55.5		5.668

		73.28		21				73.28		21				73.28		12.5				73.28		5.5				55.52		6.0014

		73.31		13.5				73.31		13.5				73.31		19.5				73.31		7				55.54		4.3344

		73.34		13				73.34		13				73.34		16				73.34		8.5				55.56		5.3346

		73.37		11.5				73.37		11.5				73.37		11				73.37		6.5				55.58		4.3344

		73.4		11.5				73.4		11.5				73.4		7				73.4		8.5				55.6		3.3341

		73.43		14				73.43		14				73.43		8				73.43		5				55.62		6.3349

		73.46		7.5				73.46		7.5				73.46		12				73.46		3.5				55.64		5.0012

		73.49		12				73.49		12				73.49		12.5				73.49		7				55.66		6.0014

		73.52		6.5				73.52		6.5				73.52		7.5				73.52		6.5				55.68		5.0012

		73.55		5				73.55		5				73.55		7				73.55		10				55.7		6.0014

		73.58		6.5				73.58		6.5				73.58		4.5				73.58		4.5				55.72		4.3344

		73.61		3				73.61		3				73.61		6.5				73.61		4.5				55.74		9.669

		73.64		2.5				73.64		2.5				73.64		4				73.64		3				55.76		6.0014

		73.67		5.5				73.67		5.5				73.67		6				73.67		3				55.78		7.0017

		73.7		5				73.7		5				73.7		4.5				73.7		3.5				55.8		7.3351

		73.73		2.5				73.73		2.5				73.73		4.5				73.73		5				55.82		4.001

		73.76		3				73.76		3				73.76		1.5				73.76		5.5				55.84		4.6678

		73.79		4.5				73.79		4.5				73.79		1				73.79		3				55.86		6.3349

		73.82		4.5				73.82		4.5				73.82		1.5				73.82		2.5				55.88		10.002

		73.85		4.5				73.85		4.5				73.85		4.5				73.85		0.5				55.9		11.336

		73.88		4				73.88		4				73.88		5				73.88		1.5				55.92		15.337

		73.91		6				73.91		6				73.91		4.5				73.91		1				55.94		25.673

		73.94		4				73.94		4				73.94		5.5				73.94		2				55.96		38.676

		73.97		3.5				73.97		3.5				73.97		3				73.97		2				55.98		41.677

		74		6.5				74		6.5				74		5				74		1.5				56		42.343

		74.03		3.5				74.03		3.5				74.03		2.5				74.03		3				56.02		42.01

		74.06		4				74.06		4				74.06		5				74.06		1				56.04		31.007

		74.09		4.5				74.09		4.5				74.09		3.5				74.09		0.5				56.06		20.338

		74.12		4.5				74.12		4.5				74.12		5.5				74.12		0				56.08		18.338

		74.15		3				74.15		3				74.15		5				74.15		2				56.1		19.671

		74.18		5.5				74.18		5.5				74.18		4				74.18		1				56.12		25.673

		74.21		4.5				74.21		4.5				74.21		3				74.21		3				56.14		28.34

		74.24		5.5				74.24		5.5				74.24		5.5				74.24		2.5				56.16		18.671

		74.27		2				74.27		2				74.27		3				74.27		2.5				56.18		20.005

		74.3		6				74.3		6				74.3		7				74.3		0.5				56.2		18.338

		74.33		7				74.33		7				74.33		8.5				74.33		2.5				56.22		9.669

		74.36		10				74.36		10				74.36		12.5				74.36		1				56.24		9.0022

		74.39		10				74.39		10				74.39		10				74.39		2.5				56.26		8.3353

		74.42		8.5				74.42		8.5				74.42		11.5				74.42		4				56.28		3.6675

		74.45		12				74.45		12				74.45		9.5				74.45		5				56.3		3.6675

		74.48		12.5				74.48		12.5				74.48		12.5				74.48		6				56.32		5.0012

		74.51		13.5				74.51		13.5				74.51		15.5				74.51		5				56.34		5.3346

		74.54		17				74.54		17				74.54		15.5				74.54		2.5				56.36		4.3344

		74.57		16.5				74.57		16.5				74.57		22				74.57		5.5				56.38		4.3344

		74.6		15				74.6		15				74.6		22				74.6		6				56.4		5.0012

		74.63		12				74.63		12				74.63		21.5				74.63		7				56.42		4.3344

		74.66		13				74.66		13				74.66		16				74.66		6				56.44		6.3349

		74.69		11.5				74.69		11.5				74.69		7.5				74.69		5				56.46		4.3344

		74.72		15.5				74.72		15.5				74.72		11.5				74.72		2.5				56.48		6.3349

		74.75		10.5				74.75		10.5				74.75		9.5				74.75		1				56.5		8.0019

		74.78		7.5				74.78		7.5				74.78		10				74.78		1.5				56.52		4.6678

		74.81		9				74.81		9				74.81		6.5				74.81		2.5				56.54		3.3341

		74.84		12				74.84		12				74.84		8				74.84		4				56.56		4.6678

		74.87		4.5				74.87		4.5				74.87		4.5				74.87		3.5				56.58		4.6678

		74.9		7				74.9		7				74.9		2.5				74.9		3.5				56.6		7.0017

		74.93		5.5				74.93		5.5				74.93		3				74.93		2.5				56.62		5.668

		74.96		6				74.96		6				74.96		4.5				74.96		2.5				56.64		5.0012

		74.99		3				74.99		3				74.99		3				74.99		1.5				56.66		8.3353

		75.02		5.5				75.02		5.5				75.02		3.5				75.02		2				56.68		7.6685

		75.05		6				75.05		6				75.05		3.5				75.05		3				56.7		5.3346

		75.08		5.5				75.08		5.5				75.08		3				75.08		2				56.72		5.3346

		75.11		5.5				75.11		5.5				75.11		1.5				75.11		2.5				56.74		5.3346

		75.14		8				75.14		8				75.14		3.5				75.14		0				56.76		5.0012

		75.17		6				75.17		6				75.17		6.5				75.17		1				56.78		2.6673

		75.2		4.5				75.2		4.5				75.2		4.5				75.2		0.5				56.8		5.668

		75.23		6.5				75.23		6.5				75.23		7				75.23		1				56.82		3.6675

		75.26		8				75.26		8				75.26		10				75.26		2				56.84		4.6678

		75.29		13.5				75.29		13.5				75.29		9				75.29		1.5				56.86		7.0017

		75.32		8.5				75.32		8.5				75.32		12.5				75.32		0.5				56.88		2.6673

		75.35		11.5				75.35		11.5				75.35		10				75.35		2.5				56.9		6.3349

		75.38		16				75.38		16				75.38		7				75.38		2.5				56.92		3.6675

		75.41		9.5				75.41		9.5				75.41		9.5				75.41		2				56.94		4.3344

		75.44		17.5				75.44		17.5				75.44		8.5				75.44		2.5				56.96		5.3346

		75.47		10.5				75.47		10.5				75.47		5.5				75.47		2.5				56.98		4.3344

		75.5		9				75.5		9				75.5		7.5				75.5		2				57		6.3349

		75.53		6.5				75.53		6.5				75.53		5.5				75.53		2				57.02		5.3346

		75.56		8				75.56		8				75.56		10.5				75.56		2				57.04		6.3349

		75.59		11				75.59		11				75.59		8.5				75.59		0				57.06		4.6678

		75.62		7.5				75.62		7.5				75.62		6.5				75.62		2				57.08		7.3351

		75.65		9				75.65		9				75.65		5				75.65		3.5				57.1		7.0017

		75.68		3.5				75.68		3.5				75.68		4.5				75.68		4				57.12		10.669

		75.71		4.5				75.71		4.5				75.71		6.5				75.71		0				57.14		7.3351

		75.74		3				75.74		3				75.74		5.5				75.74		1				57.16		8.6687

		75.77		5				75.77		5				75.77		5				75.77		2				57.18		9.669

		75.8		5.5				75.8		5.5				75.8		3.5				75.8		0.5				57.2		13.67

		75.83		5.5				75.83		5.5				75.83		2.5				75.83		0.5				57.22		19.005

		75.86		3.5				75.86		3.5				75.86		4				75.86		1.5				57.24		26.006

		75.89		4.5				75.89		4.5				75.89		3.5				75.89		0.5				57.26		31.007

		75.92		3.5				75.92		3.5				75.92		4				75.92		1				57.28		40.343

		75.95		1.5				75.95		1.5				75.95		2.5				75.95		1.5				57.3		53.013

		75.98		4.5				75.98		4.5				75.98		2				75.98		2				57.32		48.012

		76.01		4				76.01		4				76.01		3				76.01		1				57.34		31.341

		76.04		2.5				76.04		2.5				76.04		2.5				76.04		2.5				57.36		24.339

		76.07		4.5				76.07		4.5				76.07		2				76.07		0.5				57.38		21.338

		76.1		3				76.1		3				76.1		1				76.1		0.5				57.4		19.005

		76.13		3.5				76.13		3.5				76.13		2.5				76.13		0				57.42		20.338

		76.16		5				76.16		5				76.16		1.5				76.16		1				57.44		26.673

		76.19		4.5				76.19		4.5				76.19		3				76.19		0.5				57.46		25.339

		76.22		5.5				76.22		5.5				76.22		4				76.22		0.5				57.48		28.674

		76.25		3				76.25		3				76.25		2.5				76.25		1				57.5		16.337

		76.28		2				76.28		2				76.28		4				76.28		0.5				57.52		12.003

		76.31		2.5				76.31		2.5				76.31		2				76.31		2				57.54		9.669

		76.34		2.5				76.34		2.5				76.34		3				76.34		0.5				57.56		8.0019

		76.37		2.5				76.37		2.5				76.37		3				76.37		1				57.58		6.6683

		76.4		3.5				76.4		3.5				76.4		4				76.4		2.5				57.6		6.6683

		76.43		8				76.43		8				76.43		4.5				76.43		0.5				57.62		6.6683

		76.46		2				76.46		2				76.46		3				76.46		2				57.64		7.3351

		76.49		13.5				76.49		13.5				76.49		5.5				76.49		1.5				57.66		7.3351

		76.52		8.5				76.52		8.5				76.52		13				76.52		4				57.68		7.0017

		76.55		13				76.55		13				76.55		14				76.55		4.5				57.7		7.6685

		76.58		18.5				76.58		18.5				76.58		28				76.58		2.5				57.72		8.0019

		76.61		22.5				76.61		22.5				76.61		32.5				76.61		1.5				57.74		6.3349

		76.64		15				76.64		15				76.64		35.5				76.64		5				57.76		3.3341

		76.67		14				76.67		14				76.67		28				76.67		6.5				57.78		5.0012

		76.7		9				76.7		9				76.7		22				76.7		7				57.8		6.6683

		76.73		8				76.73		8				76.73		13.5				76.73		10.5				57.82		4.6678

		76.76		8.5				76.76		8.5				76.76		12.5				76.76		1				57.84		5.668

		76.79		15.5				76.79		15.5				76.79		14				76.79		1.5				57.86		9.0022

		76.82		14.5				76.82		14.5				76.82		10.5				76.82		2.5				57.88		5.668

		76.85		8.5				76.85		8.5				76.85		11.5				76.85		2.5				57.9		7.3351

		76.88		10				76.88		10				76.88		10				76.88		3				57.92		6.3349

		76.91		4				76.91		4				76.91		6.5				76.91		6.5				57.94		5.668

		76.94		7.5				76.94		7.5				76.94		4.5				76.94		3.5				57.96		7.0017

		76.97		5				76.97		5				76.97		4.5				76.97		5				57.98		7.0017

		77		4.5				77		4.5				77		7				77		3				58		10.336

		77.03		3				77.03		3				77.03		2				77.03		3				58.02		14.67

		77.06		2				77.06		2				77.06		3.5				77.06		1				58.04		13.003

		77.09		4				77.09		4				77.09		7				77.09		1				58.06		14.67

		77.12		5.5				77.12		5.5				77.12		5				77.12		1				58.08		13.003

		77.15		4.5				77.15		4.5				77.15		3.5				77.15		1				58.1		23.006

		77.18		5				77.18		5				77.18		6.5				77.18		1				58.12		27.006

		77.21		8				77.21		8				77.21		7				77.21		2				58.14		45.678

		77.24		6				77.24		6				77.24		2.5				77.24		2				58.16		77.018

		77.27		6				77.27		6				77.27		8				77.27		2				58.18		82.353

		77.3		5.5				77.3		5.5				77.3		5.5				77.3		2.5				58.2		83.687

		77.33		5				77.33		5				77.33		9				77.33		2				58.22		57.681

		77.36		5				77.36		5				77.36		8.5				77.36		2				58.24		31.341

		77.39		8				77.39		8				77.39		7.5				77.39		5				58.26		29.34

		77.42		4.5				77.42		4.5				77.42		9				77.42		5				58.28		23.006

		77.45		3				77.45		3				77.45		7				77.45		4.5				58.3		35.342

		77.48		2				77.48		2				77.48		6.5				77.48		1				58.32		42.01

		77.51		4				77.51		4				77.51		3.5				77.51		0.5				58.34		46.344

		77.54		3.5				77.54		3.5				77.54		3				77.54		2				58.36		41.343

		77.57		4.5				77.57		4.5				77.57		2				77.57		1.5				58.38		27.34

		77.6		4				77.6		4				77.6		2.5				77.6		4				58.4		18.671

		77.63		2				77.63		2				77.63		4				77.63		2.5				58.42		13.67

		77.66		3.5				77.66		3.5				77.66		2.5				77.66		1				58.44		12.67

		77.69		2.5				77.69		2.5				77.69		2.5				77.69		1				58.46		9.669

		77.72		1				77.72		1				77.72		5				77.72		3.5				58.48		9.669

		77.75		4.5				77.75		4.5				77.75		1				77.75		2.5				58.5		10.002

		77.78		5				77.78		5				77.78		6				77.78		1.5				58.52		8.0019

		77.81		4				77.81		4				77.81		6				77.81		2.5				58.54		6.6683

		77.84		5				77.84		5				77.84		4				77.84		2.5				58.56		8.0019

		77.87		5				77.87		5				77.87		4.5				77.87		2				58.58		6.0014

		77.9		4				77.9		4				77.9		4				77.9		1.5				58.6		7.0017

		77.93		6				77.93		6				77.93		1.5				77.93		1				58.62		5.0012

		77.96		3.5				77.96		3.5				77.96		4.5				77.96		0.5				58.64		7.6685

		77.99		4.5				77.99		4.5				77.99		3.5				77.99		0.5				58.66		5.0012

		78.02		3				78.02		3				78.02		4				78.02		1				58.68		8.6687

		78.05		5				78.05		5				78.05		3				78.05		1				58.7		4.001

		78.08		4				78.08		4				78.08		2.5				78.08		2				58.72		6.0014

		78.11		4				78.11		4				78.11		7				78.11		2				58.74		4.3344

		78.14		6				78.14		6				78.14		6				78.14		2.5				58.76		7.0017

		78.17		6				78.17		6				78.17		4.5				78.17		3.5				58.78		7.3351

		78.2		2.5				78.2		2.5				78.2		5.5				78.2		2				58.8		6.3349

		78.23		3.5				78.23		3.5				78.23		5.5				78.23		1.5				58.82		6.0014

		78.26		2.5				78.26		2.5				78.26		4				78.26		0.5				58.84		5.0012

		78.29		6				78.29		6				78.29		9				78.29		1				58.86		3.3341

		78.32		6.5				78.32		6.5				78.32		8				78.32		1.5				58.88		4.3344

		78.35		8.5				78.35		8.5				78.35		5.5				78.35		2.5				58.9		6.0014

		78.38		6.5				78.38		6.5				78.38		8				78.38		1				58.92		3.6675

		78.41		7				78.41		7				78.41		6				78.41		2.5				58.94		3.3341

		78.44		5				78.44		5				78.44		5.5				78.44		0.5				58.96		5.0012

		78.47		2				78.47		2				78.47		3				78.47		1.5				58.98		4.001

		78.5		2				78.5		2				78.5		4.5				78.5		2				59		7.3351

		78.53		6				78.53		6				78.53		5				78.53		1				59.02		4.6678

		78.56		5				78.56		5				78.56		2.5				78.56		1				59.04		4.3344

		78.59		6.5				78.59		6.5				78.59		1				78.59		2				59.06		3.6675

		78.62		4				78.62		4				78.62		2.5				78.62		1				59.08		5.3346

		78.65		4				78.65		4				78.65		1.5				78.65		1				59.1		6.0014

		78.68		4.5				78.68		4.5				78.68		2				78.68		1.5				59.12		5.668

		78.71		4				78.71		4				78.71		3.5				78.71		2				59.14		7.3351

		78.74		2				78.74		2				78.74		3				78.74		1				59.16		4.6678

		78.77		2				78.77		2				78.77		1.5				78.77		1				59.18		10.002

		78.8		3.5				78.8		3.5				78.8		2.5				78.8		1				59.2		11.336

		78.83		3.5				78.83		3.5				78.83		3				78.83		0.5				59.22		8.6687

		78.86		4				78.86		4				78.86		4				78.86		2				59.24		6.6683

		78.89		3				78.89		3				78.89		6.5				78.89		1				59.26		4.001

		78.92		5.5				78.92		5.5				78.92		5.5				78.92		0.5				59.28		6.3349

		78.95		8.5				78.95		8.5				78.95		5				78.95		1				59.3		6.6683

		78.98		8.5				78.98		8.5				78.98		4.5				78.98		2				59.32		8.3353

		79.01		10				79.01		10				79.01		10				79.01		4.5				59.34		8.0019

		79.04		9.5				79.04		9.5				79.04		9				79.04		6				59.36		7.0017

		79.07		10				79.07		10				79.07		12				79.07		6.5				59.38		4.3344

		79.1		6.5				79.1		6.5				79.1		6.5				79.1		5				59.4		5.3346

		79.13		16				79.13		16				79.13		12				79.13		4.5				59.42		4.3344

		79.16		9.5				79.16		9.5				79.16		9				79.16		2				59.44		4.3344

		79.19		12				79.19		12				79.19		5.5				79.19		1.5				59.46		5.668

		79.22		14.5				79.22		14.5				79.22		11.5				79.22		0				59.48		6.0014

		79.25		8.5				79.25		8.5				79.25		9				79.25		3				59.5		5.3346

		79.28		12				79.28		12				79.28		11.5				79.28		5.5				59.52		5.3346

		79.31		16				79.31		16				79.31		13				79.31		3.5				59.54		5.3346

		79.34		16				79.34		16				79.34		17.5				79.34		3				59.56		4.001

		79.37		15.5				79.37		15.5				79.37		18				79.37		7				59.58		3.3341

		79.4		14.5				79.4		14.5				79.4		16				79.4		4.5				59.6		3.3341

		79.43		14.5				79.43		14.5				79.43		20.5				79.43		9				59.62		6.0014

		79.46		14				79.46		14				79.46		14				79.46		10.5				59.64		3.0007

		79.49		16				79.49		16				79.49		15				79.49		5.5				59.66		5.668

		79.52		13				79.52		13				79.52		15				79.52		3.5				59.68		3.6675

		79.55		11				79.55		11				79.55		12.5				79.55		4.5				59.7		6.3349

		79.58		12.5				79.58		12.5				79.58		10				79.58		4				59.72		4.6678

		79.61		15.5				79.61		15.5				79.61		11				79.61		1				59.74		5.668

		79.64		8.5				79.64		8.5				79.64		8.5				79.64		3				59.76		5.0012

		79.67		14.5				79.67		14.5				79.67		9				79.67		6				59.78		8.3353

		79.7		12.5				79.7		12.5				79.7		14				79.7		5.5				59.8		4.3344

		79.73		10.5				79.73		10.5				79.73		13				79.73		6				59.82		3.3341

		79.76		8.5				79.76		8.5				79.76		9				79.76		5				59.84		5.668

		79.79		9				79.79		9				79.79		11				79.79		5				59.86		8.0019

		79.82		8				79.82		8				79.82		7				79.82		1.5				59.88		5.3346

		79.85		9.5				79.85		9.5				79.85		6.5				79.85		3				59.9		6.0014

		79.88		5				79.88		5				79.88		8.5				79.88		4.5				59.92		7.3351

		79.91		9.5				79.91		9.5				79.91		6				79.91		1.5				59.94		7.0017

		79.94		8.5				79.94		8.5				79.94		3.5				79.94		3				59.96		11.336

		79.97		6.5				79.97		6.5				79.97		7				79.97		2				59.98		12.336

		80		2.5				80		2.5				80		5.5				80		3				60		11.336





B

		



Li2CO3 at 22.13o,24.83o and 33.92o
                    
         NiO at 43.31o

2 Q (o)

Intensity (a.u)

B2



		



NiO at 43.31o

2 Q (o)

Intensity (a.u)

B3



		



2 Q (o)

Intensity (a.u)

B4




