
Malaysian Journal of Analytical Sciences Vol 18 No 3 (2014): 485 - 490

THE CHARACTERIZATION STUDY OF FERRITES (MAGNESIUM AND MANGANESE) USING SOL GEL METHOD
(Kajian Pencirian untuk Ferit (Magnesium dan Mangan) Menggunakan Kaedah Sol Gel)

Rita Sundari*, Tang Ing Hua, Madzlan Aziz, Umar Kalmar Nizar
Department of Chemistry, Faculty of Science, 

Universiti of Technologi Malaysia, 81310 Skudai, Johor, Malaysia

*Corresponding author: ritsun2003@yahoo.com

Abstract

A sol gel method with citric acid as an anionic surfactant was used to fabricate nano magnesium ferrites (MgFe2O4) and manganese ferrites (MnFeO3) under different calcination temperatures (300°C, 600°C and 800°C) for 2h, respectively.  The Fourier Transformation Infrared (FTIR) spectra of magnesium ferrites showed the formation of tetrahedral and octahedral peaks of the metal oxides, which are getting remarkable after calcination at 300°C because of the volatile matters removal (H2O, CO2, NO2, etc.). The results of the single point Brunauer, Emmett and Teller (BET) method showed a substantial decrease of surface area for both the magnesium and manganese ferrites as the calcinated temperatures getting increased from 300°C to 800°C. The SEM micrograph of the magnesium ferrite showed flake structures at 800°C, and that of manganese ferrite showed granule structures at the same temperature.  The results of X-Ray Diffraction (XRD) analysis of magnesium ferrite obtained a range of crystalline sizes from 11 nm to 60 nm, and those of manganese ferrite from 27 nm to 38 nm as the temperatures of both ferrites (magnesium and manganese) increased from 300°C to 800°C. The results of this study are useful for further applications, such as semiconductors, heterogeneous and photo catalysts, magnetic materials and sensors.

Keywords: magnesium and manganese ferrites; calcinations; characterizations

Abstrak

Kaedah sol gel dengan  asid sitrik sebagai  anionik  surfaktan  telah  digunakan  untuk  menghasilkan  nano  ferit magnesium   (MgFe2O4)  dan ferit mangan  (MnFeO3),  di bawah  suhu pengkalsinan  yang berbeza  (300°C,  600°C  dan 800°C)  untuk  2 jam. Inframerah Transformasi Fourier (FTIR) spektrum bagi ferit magnesium menunjukkan pembentukan puncak tetrahedral dan oktahedral  oksida logam yang semakin menonjol  selepas proses pengkalsinan  pada 300°C,  disebabkan  penyingkiran  jirim mudah meruap (H2O, CO2, NO2, dll). Keputusan  kaedah titik tunggal  Brunauer,  Emmett  dan Teller (BET) menunjukkan apabila suhu pengkalsinan semakin meningkat daripada 300°C ke 800°C, luas permukaan turun dengan ketara untuk kedua- dua  ferit  magnesium  dan  mangan.  Mikrograf SEM ferit magnesium pada 800°C menunjukkan struktur serpihan, dan pada suhu yang sama ferit mangan menunjukkan struktur granul. Keputusan analisis pembelauan X-Ray (XRD) bagi ferit magnesium menunjukkan julat saiz kristal daripada 11 nm hingga 60 nm, dan ferit mangan daripada 27 nm hingga 38 nm, apabila suhu bagi kedua-dua  ferit (magnesium  dan mangan) meningkat dari 300°C ke 800°C. Keputusan kajian ini amat berguna untuk aplikasi lanjut, seperti semikonduktor, pemangkin heterogen dan foto, bahan magnet dan sensor.

Kata kunci: Magnesium dan mangan ferit, pengkalsinan, pencirian
References
1. Siemons, M., Weirich, Th., Mayer, J. & Simon, U. (2004). Preparation of nanosized  perovskite-type  oxide via polyol method. Journal of Inorganic & General Chemistry 630(12): 2083-2089.
2. Wolfram, T. & Elliatioglu,  S.  (2006). Electronic and Optical Properties of D-Band Perovskites.  United  Kingdom, University Press, Cambridge. 1-24.
3. Maensiri, S., Sangmanee, M. & Wiengmoon, A. (2008). Magnesium ferrite (MgFe2O4) nanostructure fabricated by electrospinning. Nanoscale Research Letters, 4(3): 221-228.
4. Liu, C.P., Li, M.W., Zhong, C., Huang, J.R., Tian, Y.L., Tong, L. & Mi, W.B. (2007). Comparative study of magnesium ferrite nanocrystallites prepared by sol-gel and co-precipitation methods. Journal of Material Science, 42: 6133-6138.
5. Pradeep, A. & Chandrasekaran,  G. (2005). FTIR study of Ni, Cu and Zn substituted nano-particles of MgFe2O4.  Material Letters, 60(3): 371-374.
6. Pradhan, S.K., Bidb, S., Gateshki,  M. & Petkov,  V. (2005).  Microstructure characterization  and cation distribution   of nanocrystalline magnesium ferrite prepared by ball milling. Journal  of Material Chemistry & Physics, 93(1): 224-230.
7. Mishra, S., Kundu, T.K., Barick, K.C., Bahadur, D. & Chakravorty, D. (2006). Preparation of nanocrystalline MnFe2O4 by doping with Ti4+ ions using solid state reaction route. Journal of Magnetism & Magnetic Materials, 307(2): 222-226.
8. Lick,   L.D. & Soria,   D.B.   (2009).   The   synthesis of  MnFeO3 from   the   oxidative   thermal   decomposition   of Mn[Fe(CN)5NO].2H2O. Journal of Argentine Chemical Society, 97(1): 102-108.
9. Pradeep, A., Priyadharsini, P. & Chandrasekaran, G. (2008). Sol gel route of synthesis of nanoparticles of MgFe2O4 and XRD, FTIR and VSM study. Journal of Magnetism & Magnetic Materials, 320(21): 2774-2779.
10.  Naseri, M.G.,  Saion,  E.B.,  Ahangar,  H.A.,  Hashim,  M. & Shaari,  A.H.  (2011). Synthesis  and  characterization  ofmanganese ferrite nanoparticles by thermal treatment method. Journal of  Magnetism &  Magnetic Materials, 323(13): 1745-1749.
11. Hankare, P.P., Vader, V.T., Patil, N.M., Jadhav, S.D., Sankpal, U.B., Kadama, M.R., Chouguleb, B.K. & Gajbhiye, N.S. (2009).  Synthesis, characterization  and studies on magnetic  and electrical  properties  of Mg ferrite with Cr substitution.  Journal of Material Chemistry & Physics, 113(1): 233-238.
12. Rashad, M.M. (2006). Synthesis and magnetic properties of manganese ferrite from low grade manganese ore.   Material Science & Engineering B, 127(2-3): 123-129.
