Malaysian Journal of Analytical Sciences Vol 18 No 3 (2014): 584 - 591

PREPARATION OF EPOXIDIZED PALM OLEIN AS RENEWABLE MATERIAL BY USING PEROXY ACIDS

(Penyediaan Minyak Sawit Olein Terepoksida Sebagai Bahan Keterbaharuan Menggunakan Asid Peroksi)

Darfizzi Derawi*, Jumat Salimon, Waled Abdo Ahmed

Oleochemistry Research Laboratory, School of Chemical Sciences and Food Technology, 

Faculty of  Science and Technology, 

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor Darul Ehsan, Malaysia

*Corresponding author: darfizzi@ukm.edu.my
Abstract

Epoxidized palm olein (EPOo) was prepared through generated in situ of performic acid (HCOOOH), and peracetic acid (CH3COOOH) as epoxidation agent with the presence of sulphuric acid (H2SO4) 3 % v/wt as catalyst. Formic acid (HCOOH) or acetic acid (CH3COOH) as oxygen carrier and hydrogen peroxide (H2O2) as oxygen donor in the reaction system. Highly conversion (95.5 %) of oxirane ringwas obtained by usingperformicacid as epoxidation agent at 150 minutes of reaction time. The reaction yield was 90 % by weight. EPOo has showed good physicochemical properties as renewable material for industrial applications. Carbon (13C-NMR) and proton (1H-NMR) spectra showed the present of epoxy profile at 54 ppm and 2.9 ppm. Epoxy group was detected on 844 cm-1 byfourier transformation infra-red (FTIR) spectra. 

Keywords: epoxidation, palm olein, in-situ, peroxy acid, renewable material

Abstrak

Minyak sawit olein terepoksida (EPOo) disediakan melalui proses pengepoksidaan secara in situ menggunakan asid performik (HCOOOH), asid perasetik (CH3COOOH) sebagai agen pengepoksidaan dengan kehadiran mangkin asid sulfurik (H2SO4) 3 % v/wt. Asid formik (HCOOH) atau asid asetik (CH3COOH) sebagai pembawa oksigen dan hydrogen peroksida (H2O2) sebagai penderma oksigen dalam sistem tindak balas. Peratus penukaran gelang oksirana yang tinggi (95.5 %) diperolehi dengan menggunakan asid performik pada 150 minit tindak balas. Peratus hasil tindak balas adalah sebanyak 90 % berdasarkan berat. EPOo telah menunjukan sifat fiziko kimia yang baik sebagai bahan keterbaharuan untuk aplikasi industri. Spektrum karbon (13C-NMR) dan proton (1H-NMR) menunjukan kehadiran profil epoksi pada 54 ppm dan 2.9 ppm. Kumpulan epoksi dikesan pada nombor gelombang 844 cm-1 dengan merujuk spektrum transformasi fourier inframerah (FTIR). 

Kata kunci: pengepoksidaan, minyak sawit olein, in-situ, asid peroksi, bahan keterbaharuan
References

1. Goud, V. V., Patwardhan, A. V., & Pradhan, N. C. (2006). Studies on the epoxidation of mahua oil by    hydrogen peroxide. Bioresource technology, 97 (12), 1365 – 1371.

2. Wang, X., Zhang, H., Wang, Z., & Jiang, B. (1997). In situ epoxidation of ethylene propylene diene rubber by performic acid. Polymer, 38 (21), 5407 – 5410.

3. Rangarajan, B., Havey, A., Grulke, E. A., & Culnan, P. D. (1995). Kinetic parameters of a two-phase model for in situ epoxidation of soybean oil. J. Am. Oil. Chem. Soc., 72 (10), 1161 – 1169.

4. Scala, J. L. and Wool, R. P. (2002). Effect of FA composition on epoxidation kinetic of TAG. J. Am. Oil. Chem. Soc., 79 (4), 373 – 378.

5. Gan, L. H., Goh, S. H. & Ooi, K. S. (1992). Kinetic studies of epoxidation and oxirane cleavage of palm olein methyl esters. J. Am. Oil. Chem. Soc., 69 (4), 347 – 351.

6. Goud, V. V., Pradhan, N. C., & Patwardhan, A. V. (2006). Epoxidation of karanja (Pongamiaglabra) oil by H2O2. J. Am. Oil. Chem. Soc., 83 (7), 635 – 640.

7. Gunstone, F. D. (2004). “The Chemistry of Oils and Fats: Sources, Composition, Properties and Uses” Blackwell Publishing Ltd., UK.

8. Carlson, K. D. & Chang, S. P. (1985). Epoxidation of a Natural Unsaturated Epoxy Seed Oil from Vernoniagalamensis and a Look at Epoxy Oil Markets, J. Am. Oil. Chem. Soc., 62, 934 – 939.

9. Hang, X., & Yang, H. (1999). Model for a cascade continuous epoxidation process. J. Am. Oil. Chem. Soc., 76 (1), 89 – 92.

10. Guenter, S., Rieth, R., Rowbottom, K. T. (2003). “Ullmann’s Encyclopedia of Industrial Chemistry” Wiley-VCH, 6th Edition.

11. Rios, L. A., Weckes, P., Schuster, H.. & Hoelderich, W. F. (2005). Mesoporous and amorphous Ti–silicas on the epoxidation of vegetable oils J. Catal., 232, 19 – 26.
12. Warwel, S. & Klaas, M. R. (1995). Chemo-enzymatic epoxidation of unsaturated carboxylic acids. J. Mol. Cat. B: Enzym, 1, 29 – 35.
13. Sharpless, K. B., Woodard, S. S. & Finn, M. G. (1983). On the mechanism of titanium-tartrate catalyzed asymmetric epoxidation. Pure Applied Chemistry. 55 (4), 1823 – 1836.

14. Dinda, S., Patwardhan, A. V, Goud, V. V. & Pradhan, N.C. (2008). Epoxidation of cottonseed oil by aqueous hydrogen peroxide catalysed by liquid inorganic acids. Bioresource Technology, 99, 3737 – 3744.
15. O’Brien, R. D. (1998). “Fats and Oils; Formulating and Processing for Applications”, Technomic Publishing AG, Switzerland.

16. Scrimgeour, C. (2005). “Chemistry of Fatty Acids” John Wiley & Sons Inc., Scotland, 6th Edition.

17. Campanella, A., Fontanini, C. & Baltanás, M. A. (2005). Catalysis Today, 107-108, 208-214.

18. Campanella, A., Fontanini, C. & Baltanás, M. A., (2008), High yield epoxidation of fatty acid methyl esters with performic acid generated in-situ, Chemical EngineeringJournal, 144, 466 – 475.

19. Klaas, M. R. & Warwel, S. (1999). Complete and partial epoxidation of plant oil by lipase-catalysed perhydrolysis. Ind.  Crops Prod., 9 (2), 125 – 132.

20. Derawi, D. & Salimon, J. (2010). Optimization on epoxidation of palm olein by using performic acid. E-Journal of Chemistry, 7 (4), 1440 – 1448.

21. A.O.C.S. (1998). Official Metthods and Recommended Practices of AOCS, AOCS, Illionis.

22. Paquot, C. (1979). “Standards Methods for the Analysis of Oils, Fats and Derivatives Part-1” Pergamon Press, Germany, 5th Edition

23. Pavia, D. L. (2001). “Introduction to Spectroscopy” Thomson Learning, Inc., United States 

24. Derawi, D. & Salimon, J. (2013). Palm olein based biolubricant basestocks: synthesis, characterisation, tribological and rheological analysis. Malaysian Journal of Analytical Sciences, 17 (1), 153 – 163.

25. Findley, T. W., Swern, D. & Scanlan, J. T. (1945). Epoxidation of unsaturated fatty materials with peracetic acid in glacial acetic acid solution. J. Am. Oil. Chem. Soc., 67(3), 412 – 414.

26. Greenspan, F. P. (1946). The convenient preparation of per-acids. J. Am. Oil. Chem. Soc., 68(5), 907 – 907. 

27. Socrates, G. (2001). “Infrared and Raman Characteristic Group Frequencies” John Wiley & Sons Ltd., England, 3rd Edition.
