Malaysian Journal of Analytical Sciences Vol 18 No 3 (2014): 592 - 603

REMOVAL OF METHYL RED FROM AQUEOUS SOLUTION BY ADSORPTION ON TREATED BANANA PSEUDOSTEM FIBERS USING RESPONSE SURFACE METHOD (RSM)

(Penyingkiran Metil Merah daripada Larutan Akues oleh Serapan Fiber Batang Pisang Yang Telah Dirawat Mengunakan Kaedah Permukaan Sahutan (RSM))
Zaida Rahayu Yet and Mohd Zulkhairi Abdul Rahim 

Department of Chemical Engineering Technology, 

Universiti Kuala Lumpur (Malaysian Institute of Chemical and Bioengineering Technology), Melaka, Malaysia

*Corresponding author: zaida@unikl.edu.my
Abstract

The effect of adsorbent dose, pH and contact times on the removal of Methyl Red (MR) from aqueous solution by using agriculture waste (NaOH treated banana pseudostem fibers) were studied. The influence of these parameters on the removal of Methyl Red was examined by using a response surface method (RSM). The experiment was conducted by combining three parameters: adsorbent dose (500-1500 mg/L), pH (2-8) dan contact time (5-75 minutes ). The Box-Behnken Design (BBD) in Response Surface Methodology (RSM) by Design Expert Version 8.0.4 (Stat Ease, USA) was used for designing the experiments. Results showed that the optimum conditions for removal of Methyl Red from an aqueous solution (100 mg/L) were as follows: adsorbent dose (1417.70 mg/L), pH (2.08) and contact time (42.94 minutes) with the value of a coefficient of determination, R2 is 98.98 %. Meanwhile, the second-order polynomial equation indicates that pH and contact times mostly affect the removal of Methyl Red. 

Keywords:  response surface method (RSM), adsorption, methyl red

Abstrak

Dalam penyelidikan ini, kesan dos penyerap, pH larutan dan masa untuk membuang Methyl Merah dari larutan media menggunakan sisa buangan pertanian iaitu serat batang pisang yang telah dirawat dengan larutan Sodium Hydroxide (NaOH) telah dikaji. Kesan tiga faktor dalam pengurangan Methyl Merah telah dikaji menggunakan Kaedah Permukaan Sambutan (RSM). Eksperimen dijalankan dengan menggabungkan ketiga – tiga pemboleh ubah  iaitu dos penyerap (500-1500 mg/L), pH larutan (2-8) dan masa tindakan (5-75 minit). Reka bentuk Box-Behnken (BBD) di dalam Kaedah Permukaan Sambutan (RSM) menerusi “Design Expert” versi 8.0.4 (Stat Ease, USA) telah digunakan untuk mereka bentuk eksperimen. Keadaan terbaik untuk membuang 100 mg/L Methyl Merah dari larutan media adalah seperti berikut: dos penjerapan (1417.70 mg/L), pH larutan (2.08) dan masa tindakan (42.94 minit) dengan  nilai pekali penentu, R2 sebanyak 98.98 %. Persamaan polinomial peringkat kedua diperolehi  didapati pH larutan dan masa rawatan adalah paling memberi kesan terhadap pembuangan Methyl Merah dengan menggunakan fiber batang pisang yang telah dirawat.

Keywords:  kaedah permukaan sambutan, serapan, metil merah
References

1. Azira, S., Wong, T. N., Robiah, Y. and Chuah, T. G. (2004) Adsorption of methylene blue onto palm kernel shell activated carbon. E Proceeding. Regionalm Conference For Young Chemists 2004. Universiti Sains Malaysia, Penang, Malaysia.

2. Saiful Azhar S., Ghaniey Liew , Suhardy D., Farizul Hafiz K.  , Irfan Hatim  M.D (2005). Dye Removal from Aqueous Solution by using Adsorption on Treated Sugarcane Bagasse, American Journal of Applied Sciences 2 (11): 1499-1503, 2005.
3. Grag, V.K, M. Anita, R. Kumar and R. Gupta, 2004. Removal from simulated wastewater by adsorption using Indian Rosewood sawdust: A timber industry waste. Dyes & Pigments, 63: 243-250.
4. Atef S. Alzaydien (2009). Adsorption of Methylene Blue from Aqueous Solution onto a Low-Cost Natural Jordanian Tripoli. Science Publications. American Journal of Environmental Sciences 5 (3): 197-208. 
5. Helen K.M., Iyyaswami R., Magesh G.P., and Lima R.M. (2009) Modelling, analysis and optimization of adsorpation parameter for H3PO4 activated rubber wood sawdust using response surface methodology (RSM). Journal of Colloids and Surfaces B: Biointerfaces 70: 35-45.
6. Amarasinghe B.M.W.P.K. and Williams R.A. (2007). Tea waste as a low cost adsorbent for the removal of Cu and Pb from wastewater, Chemical Engineering Journal 132: 299.
7. Hawari A.H. and Mulligan C.N. (2006) Biosorption of lead(II), cadmium(II), copper(II) and nickel(II) by anaerobic granular biomass, Bioresource Technology 97: 692.
8. Hameed B.H., El-Khaiary M.I. (2008) Batch removal of malachite green from aqueous solutions by adsorption on oil palm trunk ﬁbre: Equilibrium isotherms and kinetic studies, Journal of Hazardous Materials 154 : 237–244
9. Dhiraj S., Garima M., Kaur M.P. (2008) Agricultural waste material as potential adsorbent for sequestering heavy metal ions from aqueous solutions – A review Bioresource Technology 99: 6017–6027.
10. Goh C.S., Tan K. T., Lee  K. T., Bhatia S. (2010) Bio-ethanol from lignocellulose: Status, perspectives and challenges in Malaysia, Bioresource Technology 101: 4834–4841.
11. Mak Chai. Ho Y W., Liew K.W. and Asif J.M (2004). Biotechnology and in vitro mutagenesis for banana improvement. © 2004 Science Publications. 

12. Rahim MZA (2009), Preliminary Study on Selected Malaysian Plant Based Material as New Immobilize Matrix, 2nd National Symposium on Fermentation Technology (NSFT 2009), Malacca International Trade Centre (MiTC), Ayer Keroh, Melaka, 14-15 .
13. Abdullah A.Z., Salamatinia B. and Kamaruddin A.H. (2009). Application of response surface methodology for the optimization of NaOH treatment on oil palm frond towards improvement in the sorption of heavy metals. Desalination 244 :227–238. 
14. Montgomery, Douglas C. (2005). Design and Analysis of Experiments: Response surface method and designs. New Jersey: John Wiley and Sons, Inc.
15. Garg U.K., Kaur M.P., Sud D. and Garg V.K. (2009) Removal of hexavalent chromium from aqueous solution by adsorption on treated surgane bagase using response surface methodological approach. Desalination 249 : 475-479.
16. Annadurai G., Babu S.R., Nagarajan G. and Ragu K. (2000) Use of Box-Behnken design of experiments in the production of manganese peroxidase by Phanerochaete chrysosporium (MTCC 767) and decolorization of crystal violet. Bioprocess engineering 23: 715-719.
17. Mas Rosemal H. Mas Haris and Kathiresan Sathasivam (2009). The Removal of Methyl Red from Aqueous Solutions Using Banana Pseudostem Fibers. © 2009 Science Publications.
18. Paritosh Tripathi,  Vimal Chandra Srivastava and  Arvind Kumar (2009). Optimization of an azo dye batch adsorption parameters using Box–Behnken design. Desalination 249: 1273–1279. 
19. Santhy K. and Selvapathy P. (2006). Removal of reactive dyes from wastewater by adsorption on coir pith activated carbon. Bioresource Technology 97 : 1329–1336.
