Malaysian Journal of Analytical Sciences Vol 18 No 3 (2014): 612 - 617

PREPARATION AND CHARACTERIZATION OF TAPIOCA STARCH FILLED POLYCAPROLACTONE COMPOSITE FILMS

(Penyediaan dan Pencirian Filem Komposit Polikaprolakton Terisi Kanji Ubi Kayu)

Nurulhusna Azmi*, Aznizam Abu Bakar, Sani Amril Samsudin, Nur Azmyra Abdul Aziz

Enhance Polymer Research Group (EnPRO), Faculty of Chemical Engineering, 

Universiti Teknologi Malaysia, 81310 UTM Skudai, Johor, Malaysia

*Corresponding author: husna.azmi89@gmail.com
Abstract

This research was conducted to develop a new biodegradable polymeric packaging material to replace the current polymer packaging without changing the requirements properties. Polycaprolactone (PCL) was chosen as the matrix because of its biodegradability characteristics. Tapioca starch was used as filler from 10 to 40 wt% loading contents. The composite films were prepared using solvent casting technique and chloroform was used as solvent to dissolve the PCL pellets. The PCL matrix showed result of higher tensile strength which was 65.9 N/mm2 with elongation at break at approximately 731%.  The addition of starch in the PCL composite films increased the tensile modulus of the films. The tensile strength of the composite films decreased with increasing starch contents. Similar trends were also observed for elongation at break of the films.

Keywords: polycaprolactone (PCL), tapioca starch, casting films, biodegradable, polymer packaging

Abstrak

Kajian ini telah dijalankan bagi menghasilkan produk baru untuk menggantikan pembungkus plastik yang sedia ada dengan plastik mesra alam tanpa mengubah kriteria dan ciri-ciri yang diperlukan. Polikaprolakton (PCL) dipilih sebagai matrik kerana cirinya yang boleh terurai secara semulajadi. Kanji digunakan sebagai pengisi didalam komposit filem dari 10 hingga 40 wt%. Komposit ini telah disediakan dengan menggunakan teknik tuangan ke dalam acuan dan klorofom digunakan sebagai bahan pelarut untuk melarutkanpelet PCL. Matrik PCL menunjukkan kekuatan tegangan yang tinggi iaitu 65.9 N/mm2 dengan pemanjangan pada ketika putus lebih kurang 731%. Penambahan kanji didalam PCL meningkatkan modulus tegangan komposit filem. Didapati kekuatan tegangan komposit filem semakin menurun dengan penambahan kanji. Corak yang sama juga dapat dilihat pada pemanjangan filem pada ketika putus.

Keywords: polycaprolactone (PCL), kanji ubi kayu, filem casting, biodegradasi, pembungkusan polimer
References

1. Albertsson, A. C. and Karlsson, S. (1995). Degradable Polymer for the Future.Acta Polymer.46:114 – 123.
2. Alire, R. R. (2009). Biodegradable Plastic Packaging Materials.Free-Flow Packaging International, Inc.
3. Avella, M., Errico, M. E., Laurienzo, P., Martuscelli, E., Raimo, M. and Rimedio, R. (2000). Preparation and Characterization of CompatibisedPolycaprolactone/Starch Composites.Polymer Communication.41:3857 – 3881.
4. Matzinos, P., Tserki, V., Kontoyiannis, A. and Panayiotou, C. (2002). Processing and Characterization of Starch/PolycaprolactoneProducts.Polymer Degradation and Stability.77:17 – 24.
5. Kim, E. G., Kim, B.S. and Kim, D.S. (2006). Physical properties and Morphology of Polycaprolactone/Starch/Pine-Leaf Composites.Journal of Applied Polymer Science.103:928 – 934.
6. Khatiwala, V. K., Shekhar, N., Aggarwal, S. and Mandal, U. K. (2008). Biodegradation of Poly (ɛ-caprolactone) (PCL) Film by AlcaligenesFaecalis. Journal Polymer Environment.16:61 – 67.
7. Myllymaki, O., Myllarinen, P., Forssell, P., Suortti, T., Lahteenkorva, K., Ahvenainen, R. and Poutanen, K. (1998). Mechanical and Permeability Porperties of Biodegradable Extruded Starch/Polycaprolactone Films. Packaging Technology and Science.11:265 – 274.
8. Franco, C. R. D., Cyras, V. P., Busalmen, J. P., Ruseckaite, R. A. and Vazquez, A. (2004). Degradation of Polycaprolactone/Starch Blends and Composites with Sisal Fibre.Polymer Degradation and Stability.86:95 – 103.
9. Glenn, G. M., Klamczynski, A. P., Shey, J., Chiou, B. S., Holtman, K. M., Wood, D. F., Ludvik, C., Hoffman, G. D., Orts, W. J. and Imam, S. (2007). Controlled Release of 2-Heptanone Using Starch Gel and Polycaprolactone Matrices and Polymeric Films. Polymer Advanced Technologies. 18:636 – 642.
10. Namazi, H and Mosadegh, M. (2011). Preparation and Properties of Starch/Nanosilicate Layer/PolycaprolactoneComposites.Journal Polymer Environment.19:980 – 987.
11. Yavuz, H. and Babac, C. (2003). Preparation and Biodegradation of Strach/Polycaprolactone Films.Journal of Polymer and the Environment. 11(3): 107 – 113.
12. Choi, E. J., Kim, C. H. and Park, J. K. (1999). Synthesis and Characterization of Strach-g-Polycaprolactone Polymer.Macromolecules.32:7402 – 7408.
13. Kweon, D. K., Kawasaki, N., Nakayama, A. and Aiba, S. (2004). Preparation and Characterization of Starch/PolycaprolactoneBlend.Journal of Applied Polymer Science 92:1716 – 1723.
14. Sugih, A. K., Drijfhout, J. P., Picchioni, F., Janssen, L. P. B. M. and Heeres, H. J. (2009). Synthesis and Properties of Reactive Interfacial Agents for Polycaprolactone – Starch Blends.Journal of Applied Polymer Science.114:2315 – 2326.
15. Koenig, M. F. and Huang, S. J. (1995). Biodegradable Blends and Composites of Polycaprolactone and Starch Derivatives.Polymer. 36(9):1877 – 1882.
