Malaysian Journal of Analytical Sciences Vol 18 No 3 (2014): 718 - 723

STUDY ON THE STRUCTURE, TEXTURE AND THERMAL STABILITY OF CeZrYO2 NANOPARTICLES SYNTHESIZED VIA MICROEMULSION METHOD

(Kajian Terhadap Struktur, Tekstur dan Kestabilan Termal CeZrYO2 Nanopartikel Disintesis Melalui Kaedah Microemulsi)

Abdul Hadi1*, M. Nazri Abu Shah1, Noraakinah Hassan1, S. Azurah Suliman1, S. Hanim Md Nor1, Mahidin2, Kamariah Noor Ismail1
1Faculty of Chemical Engineering, 

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

2Department of Chemical Engineering, 

Syiah Kuala University, 23111 Banda Aceh, Indonesia

*Corresponding author: hadi9598@salam.uitm.edu.my
Abstract

The CeZrYO2 (CZY) was synthesized via microemulsion method. Phase structure, texture, and thermal stability of CZY nanoparticles were characterized by X-ray diffraction (XRD), transmission electron microscopy (TEM), N2 adsorption-desorption and thermogravimetric Analysis (TGA). XRD analysis confirmed the cubic phase and homogeneous solid solution of CZY nanoparticles formed. TEM micrograph also revealed the CZY nanoparticles well-defined crystallite, spherical shaped and nanoscale size in range of 5 – 10 nm. The surface area of CZY nanoparticles was 219.50 m2/g and isotherm profile was mesoporous type IV. It was also found that the synthesized CZY nanoparticles remain a good thermal stability, in the range of temperature more than 900oC according to thermo gravimetric analysis. 

Keywords: CeZrYO2, Yttrium, nanoparticles, microemulsion

Abstrak

CeZrYO2 (CZY) telah disintesis melalui kaedah mikroemulsi. Struktur fasa, tekstur, dan kestabilan termal nanopartikel CZY dicirikan oleh pembelauan sinar-X (XRD), mikroskop elektron transmisi (TEM), N2 penjerapan - desorpsi dan analisis termogravimetri (TGA). Analisis XRD mengesahkan fasa kubik dan homogen nanopartikel larutan pepejal terbentuk. TEM mikrograf juga mendedahkan nanopartikel CZY kristal terbentuk dengan jelas, berbentuk bulat, dan bersaiz nano dalam lingkungan 5 – 10 nm. Luas permukaan nanopartikel CZY adalah 219.50 m2/g dan isoterma profil adalah mesopori (Jenis IV). Ia juga mendapati bahawa nanopartikel CZY mempunyai kestabilan terma yang baik, dalam lingkungan suhu melebihi 900oC mengikut termogravimetri analisis. 

Kata kunci: CeZrYO2, Yttrium, nanopartikel, microemulsi
References

1. Guillen – Hurtado N., Rico-Pérez V., García-García A., Lozano-Castelló D., and Bueno-López A. (2012), Three-way catalysts: Past, present and future," DYNA (Colombia) 79: 114-121.

2. Li H., Zhu Q., Li Y., Gong M., Chen Y., and  Wang J. (2010). Effects of ceria/zirconia ratio on properties of mixed CeO2-ZrO2-Al2O3 compound. J. of Rare Earths 28: 79-83.

3. Shah M. N. A., Nor S. H. M., Ismail K. N., and Hadi A. (2014). Overview: Modification of Cerium Oxide in Three-Way Catalysts. Applied Mechanics and Materials 575: 97-102.

4. Cao H., Song W., Gong M., Wang J., Yan S. and Liu Z. (2009). MnOx/Al2O3/Ce0.45Zr0.45M0.10Oy (M = Mn, Y, La) catalysts used for ethanol catalytic combustion. J. of Natural Gas Chemistry 18: 83-87.

5. Jiaxiu G., Zhonghua S., Dongdong W., Huaqiang Y., Maochu G. and Yaoqiang C. (2013). Study of Pt–Rh/CeO2–ZrO2–MxOy (M=Y, La)/Al2O3 three-way catalysts. Applied Surface Science 273: 527-535.

6. Wang G., Dai H., Zhang L., Deang J., Liu C. and He H. (2010). CrOx/nano-Ce0.60Zr0.35Y0.05O2 catalysts that are highly selective for the oxidative dehydrogenation of isobutane to isobutene. Applied Catalysis A: General 375: 272-278.

7. Wang G., You R. and Meng M. (2013). An optimized highly active and thermo-stable oxidation catalyst Pd/Ce–Zr–Y/Al2O3 calcined at superhigh temperature and used for C3H8 total oxidation. Fuel 103: 799-804.

8. Fogler H. S. (1992) Elements of Chemical Reaction Engineering (Second Edition): Prentice Hall PTR.

9. Guo M.-N., Guo C.-X., Jin L.-Y, Wang Y.-J., Lu J.-Q. and Luo M.-F. (2010). Nano-sized CeO2 with extra-high surface area and its activity for CO oxidation.  Materials Letters 64: 1638-1640.

10. Laguna O. H., Centeno M. A., Boutonnet M. and Odriozola J. A. (2011). Fe-doped Ceria Solids Synthesized by the Microemulsion Method for CO Oxidation Reactions. Applied Catalysis B: Environmental 106: 621-629.

11. Hadi A.and Yaacob I. I. (2007). Novel synthesis of nanocrystalline CeO2 by mechanochemical and water-in-oil microemulsion methods. Materials Letters 61: 93-96.

12. Abu Shah M. N., Md Nor S. H., Ismail K. N., and Hadi A. (2014). Study on the Structure and Morphology of CexZr(1-x)O2 Mixed Oxides," Advanced Materials Research 938: 46-51.

13. Feng L G., Quiyan W., Bo Z., and Renxian Z. (2010). The promotional effect of transition metals on the catalytic behavior of model Pd/Ce0.67Zr0.33O2 three-way catalyst. Catalysis Today 158: 385-392.

14. Martinez-Arias A., Fernandez-Garcia M., Ballesteros V., Salamanca L. N., Conesa J. C. and Otero C. (1999) Characterization of High Surface Area Zr-Ce (1:1) Mixed Oxides by a Microemulsion Method. Langmuir 15: 4796-4802.

15. Masui T., Fujiwara K., Peng Y., Sakata T., Machida Ken-ichi and Mori H. (1998). Characterization and catalytic properties of CeO2–ZrO2 ultrafine particles prepared by the microemulsion method. J. of Alloys and Compounds 269: 116 -122.

16. Radlik M., Adamowska M., Lamacz A., Krzton A., Costa P. D., and Turek W., (2013). Study of the surface evolution of nitrogen species on CuO/CeZrO2 catalysts," Reaction Kinetics, Mechanisms and Catalysis 109: 43-56. 
17. He H., Dai H. X., and Au C. T. (2004). Defective structure, oxygen mobility, oxygen storage capacity, and redox properties of RE-based (RE = Ce, Pr) solid solutions. Catalysis Today 90: 245-254.

