Malaysian Journal of Analytical Sciences Vol 18 No 3 (2014): 507 - 513

SCHIFF BASES DERIVED FROM ISATIN AS MILD STEEL CORROSION INHIBITORS IN 1 M HCl
(Bes Schiff Yang Terhasil Daripada Isatin Sebagai Perencat Kakisan Keluli Lembut Dalam 1 M Asid Hidroklorik)

Aliyin Abdul Ghani1*, Hadariah Bahron1, Mohamad Kamal Harun1, Karimah Kassim2
1Faculty of Applied Sciences, 

2Institute of Science, 

Universiti Teknologi MARA (UiTM), 40450 Shah Alam, Selangor, Malaysia

*Corresponding author: aliyinabdulghani@gmail.com
Abstract

Two Schiff bases namely, 3-(phenylimino)indolin-2-one (PII) and 3,3- (1,4-phenylenebis (azan-1-yl-1-ylidene))diindolin-2-one (PDI) were successfully synthesized from the condensation reaction giving yields of 72% and 84%, respectively. The ligands were characterized via physical and spectroscopic techniques namely melting point, Elemental Analysis (C, H, N), 1H and 13C Nuclear Magnetic Resonance (NMR) and Fourier Transform Infrared (FTIR) Spectroscopy. The corrosion inhibiting property of the Schiff bases on mild steel in 1 M HCl solution were investigated by the weight loss measurements, electrochemical impedance spectroscopy (EIS) and linear polarization resistance (LPR). The concentrations of the Schiff bases were varied from 1 x 10-3 M to 1 x 10-5 M. The inhibition efficiencies obtained from all the methods employed were in good agreement where the percentage of inhibition efficiencies increased with concentration. Results showed that PDI was the better inhibitor with inhibition efficiency of 84% at 1 x 10-3 M additive concentration.  This is likely due to the effect of its bigger molecular size, higher number of heteroatoms and bigger π-electron cloud of the conjugated double bond system. 

Keywords: Schiff base, Isatin, Corrosion inhibitor, Mild steel, Hydrochloric acid

Abstrak

Dua bes Schiff, 3-(phenylimino)indolin-2-one (PII) dan 3,3- (1,4-phenylenebis (azan-1-yl-1-ylidene))diindolin-2-one (PDI) telah disintesis dengan jaya dari reaksi kondensasi memberikan hasil 72% dan 84%. Ligan-ligan telah dicirikan oleh pelbagai teknik kimia-fizikal seperti menentu takat lebur, analisis unsur, 1H and 13C spektroskopi resonans magnet nuklear, dan spektroskopi inframerah. Ciri-ciri perencat kakisan bagi Bes Schiff di atas keluli lembut dalam 1 M asid hidroklorik telah dikaji melalui kaedah penghilangan jisim, spektroskopi impedans elektrokimia dan rintangan polarisasi linear. Kepekatan Bes Schiff disediakan dari 1 x 10-3 M to 1 x 10-5 M. Kecekapan perencat dari semua kaedah telah menunjukkan keserasian di mana peratus kecekapan perencat meningkat apabila jumlah kepekatan ligan bertambah. Keputusan menunjukkan PDI adalah perencat yang lebih baik dengan kecekapan perencat sebanyak  84% pada kepekatan 1 x 10-3 M. Ini adalah kerana efek molekul yang lebih besar, jumlah heteroatom yang tinggi dan π-elektron yang lebih besar dari konjukasi system ikatan kembar.

Kata kunci: Bes Schiff, Isatin, Perencat kakisan, Keluli lembut, Asid Hidroklorik
References
1. Ahamad, I., Prasad, R., Quraishi, M.A., (2010). Adsorption and inhibitive properties of some new Mannich bases of Isatin derivatives on corrosion of mild steel in acidic media. Corrosion science, 52: 1472-1481.

2. Mallaiya, K., Subramaniam, R., Srikandan, S. S., Gowri, S., Rajasekaran, N., Selvaraj, A., (2011). Electrochemical characterization of the protective film formed by the unsymmetrical Schiff’s base on the mild steel surface in acid media. Electrochimica Acta, 56: 3857-3863

3. Emregul, K. C.,  Duzgun, E., Atakol, O., (2006). The application of some polydentate Schiff base compounds containing aminic nitrogens as corrosion inhibitors for mild steel in acidic media. Corrosion Science, 48: 3243-3260.

4. Kustu, C., Emregul, K. C., Atakol, O., (2007). Schiff bases of increasing complexity as mild steel corrosion inhibitors in 2 M HCl. Corrosion Science, 49: 2800-2814.

5. Qu, Q., Hao, Z., Li, L., Bai, W., Liu, Y. and Ding, Z., (2009). Synthesis and evaluation of Tris-hydroxymethyl-(2-hydroxybenzylidenamino)-methane as a corrosion inhibitor for cold rolled steel in hydrochloric acid. Corrosion Science, 51: 569-574.

6. Hosseini, M.G., Ehteshamzadeh, M. and Shahrabi, T., (2007). Protection of mild steel corrosion with Schiff bases in 0.5 M H2SO4 solution. Electrochimica Acta, 52: 3680-3685.

7. Lece, H., D., Emregul, K., C., Atakol, O., (2008). Difference in inhibitive effect of some Schiff base compounds containing oxygen, nitrogen and sulfur donors. Corrosion Science, 50: 1460-1468.
