Malaysian Journal of Analytical Sciences Vol 19 No 1 (2015): 88 – 96

THE IMPROVEMENT OF SCREENING THE SIGNIFICANT FACTORS OF OIL BLENDS AS BIOLUBRICANT BASE STOCK

(Penambahbaikkan Saringan Faktor Bererti Bagi Campuran Minyak Sebagai Stok Asas Biopelincir)

Noor Hajarul Ashikin Shamsuddin1, Rozaini Abdullah2*, Zainab Hamzah2,

Siti Jamilah Hanim Mohd Yusof1

1School of Bioprocess Engineering,

Universiti Malaysia Perlis, Kompleks Pengajian Jejawi Utara, 02600 Arau, Perlis, Malaysia

2Faculty of Engineering Technology,

Universiti Malaysia Perlis, Pusat Kejuruteraan, Kampus Pauh Putra, 02600 Arau, Perlis, Malaysia

*Corresponding author: rozainiabdullah@unimap.edu.my

Abstract

A new formulation biolubricant base stock was developed by blending of waste cooking oil (WCO) with Jatropha curcas oil (JCO). The objective of this research is to evaluate significant factors contributing to the production of oil blends for biolubricant application. The significant factors used in this study were oil ratio (WCO:JCO), agitation times (min) and agitation speed (rpm). The blended oil biobased lubricant was used to determine the saponification, acid, peroxide and iodine values. The experimental design used in this study was the 2 level-factorial design. In this experiment, it was found that the effect of oil ratio and interaction of oil ratio and agitation speed gave the most significant effect in oil blends as biolubricant base stock. The highest ratio of oil blend 80%:20% WCO:JCO, with low agitation speed of 300 rpm and low agitation time of 30 minutes gave the optimum results. The acid, saponification, peroxide and iodine values obtained were 0.517±0.08 mgKOH/g, 126.23±1.62 mg/g, 7.5±2.0 meq/kg and 50.42±2.85 mg/g respectively. A higher ratio of waste cooking oil blends was found to be favourable as biolubricant base stock.

Keyword: waste cooking oil, Jatropha curcas oil, oil blend, 2-Level Factorial Design

Abstrak

Formulasi baru  bagi stok asas biopelincir telah dibangunkan dengan campuran sisa minyak masak (WCO) dengan minyak Jatropha curcas (JCO). Objektif kajian ini adalah untuk menilai faktor-faktor penting yang menyumbang kepada pengeluaran minyak campuran untuk aplikasi biopelincir. Faktor-faktor penting yang digunakan dalam kajian ini ialah nisbah minyak (WCO: JCO), masa campuran (min) dan kelajuan percampuran (rpm).  Campuran minyak pelincir asas bio digunakan untuk menentukan nilai saponifikasi, asid, peroksida dan nilai iodin. Reka bentuk eksperimen yang digunakan dalam kajian ini adalah reka bentuk 2 peringkat faktorial. Dalam eksperimen ini, didapati bahawa kesan nisbah minyak dan interaksi nisbah minyak dan kelajuan percampuran memberi kesan ketara dalam campuran minyak sebagai stok asas biopelincir. Nisbah tertinggi campuran minyak 80%: 20% WCO: JCO, dengan kelajuan percampuran yang rendah 300 rpm dan masa yang rendah 30 minit memberikan hasil yang optimum. Nilai-nilai asid, saponifikasi, peroksida dan iodin yang diperolehi ialah 0.517±0.08 mgKOH/g, 126.23±1.62 mg/g, 7.5±2.0 meq/kg dan 50.42±2.85 mg/g. Nisbah yang lebih tinggi daripada campuran sisa minyak masak adalah lebih baik untuk dijadikan sebagai stok asas biopelincir.

Kata kunci: sisa minyak masak, Minyak Jatropha curcas, campuran minyak, Rekabentuk Faktorial 2 Peringkat

References

- Bartz, W.J. (2006). Ecotribology: Environmentally Acceptable Tribological Practices. Triboogy International, 39 (8): 728-733.

- Nizam, M.K. and Hayder, A.A.B. (2009). The Use Of Vegetable Oil In Lubricant As Base Oil: A Review. National Conference on Postgraduate Research (NCON-PGR).

- Talkit, K.M., Mahajan, D.T. and Masand, V.H. (2012). Physicochemical properties of soybean oil and their blends with vegetable oils for the evaluation of lubrication properties, Journal of Chemical, Biological and Physical Sciences,   3(1): 490–497.

- Berchmans, H.J. and Hirata, S. (2008). Biodiesel production from crude Jatropha curcas L. seed oil with a high content of free fatty acids. Bioresource Technology, 99(6): 1716–1721.

- Al-Hamamre, Z. And Al-Salaymeh, A. (2014). Physical properties of (jojoba oil + biodiesel), (jojoba oil + diesel) and (biodiesel + diesel) blends. Fuel, 123: 175-188.

- Mourenta, G. And Bell, J.G. (2006). Partial replacement of dietary fish oil with blends of vegetable oils (rapeseed, linseed and palm oils) in diets for European sea bass (Dicentrarchus labrax L.) over a long term growth study: Effects on muscle and liver fatty acid composition and effectiveness of a fish oil finishing diet. Comparative Biochemistry and Physiology Part B: Biochemistry and Molecular Biology, 145(3-4): 389-399.

- Mostafa, R.A., Moharram, Y.G., Attia, R.S. and El-Sharnouby, S.A. (2013). Formulation and characterization of vegetable oil blends rich in omega –3 fatty acids. Emir. J. Food Agric., 25(6): 426-433.

- Chhetri, A.B., Watts, K.C. and Rafiqul Islam M. (2008). Waste cooking oil as an alternate feedstock for biodiesel production. Energies, 1: 3-18.

- Valente, O.S., Pasa, V.M.D., Belchior, C.R.P. and Sodré, J.R. (2011). Physical–chemical properties of waste cooking oil biodiesel and castor oil biodiesel blends. Journal of Fuel, 90(4): 1700–1702.

- Kywe, T. T. and Oo, M. M. (2009). Production of biodiesel from jatropha oil (Jatropha curcas) in pilot plant. Proceedings of World Academy of Science, Engineering and Technology, 38: 2070-3740.

- Salimon, J. and Rozaini, A. (2008). Physicochemical properties of Malaysia Jatropha curcas seed oil. Sains Malaysiana, 37(4): 379-382.

- Gunam Resul, M. F. M., Mohd Ghazi, T. I., Muhammad Syam A. and Idris, A. (2008). Synthesis of Biodegradable Lubricant from Jatropha Oil with High Content of Free Fatty Acids. American Institute of Chemical Engineers, Environmental Division, 524-530.

- Shah, M. and Pathak, K. (2010). Development and Statistical Optimization of Solid Lipid Nanoparticles of Simvastatin by Using 23 Full-Factorial Design. AAPS PharmSciTech, 11 (2): 489-496.

- Chen, Y., Chen,J., Luo, Y., Shang, N., Chang, C. and Chiang, P. (2011). Property Modification of Jatropha Oil Biodiesel by Blending with Other Biodiesel or Adding Antioxidants. Energy, 36 (7): 4415-4421.

- Chang, S. H., Teng, T.T. and  Norli Ismail. (2011). Screening of factors influencing Cu(II) extraction by soybean oil-based organic solvents using fractional factorial design. Journal of Environmental Management, 92: 2580-2585.

- Myers, R.H. and Montgomery, D.C. (2002). Response Surface Methodology e Process and Product Optimization Using Designed Experiments. Seconded. John Wiley & Sons Inc., Canada.

- Rozaini, A., Farizul Hafiz, K., Siti Nur Amalieya Syaza, M. Z. and Noor Hajarul Ashikin, S. (2014). Oil Blends as Biolubricant: Screening of Effect Factors Influence To Basestock. Key Engineering Materials, 594-595: 356-361.

- Wannahari, R. and Nordin, M. F. N. (2012). Reduction of Peroxide Value in Used Palm Cooking Oil Using Bagasse Adsorbent. American International Journal of Contemporary Research, 2 (1): 185-191.

- Chen Ching, T. (2008). Experimental Study for Developing the Base Oils of the U.S. Soybean Oil Based Biolubricants, Department of Mechanical Engineering. National Taipei University of Technology.

- Jen-Jie, H., Wen-Shing, L., Wen-Fang, W. and Sih-Li, C. (2001). Effect of Lubrication on the Performance and Dynamic Loads of Scroll Compressors. Journal of Mechanics, 17: 201-210.