Malaysian Journal of Analytical Sciences Vol 19 No 1 (2015): 97 – 105

Oleic Acid based Polyesters of Trimethylolpropane and Pentaerythritol for Biolubricant Application

(Poliester Berasaskan Trimetilolpropana dan Pentaeritritol dengan Asid Oleik untuk Kegunaan Biopelincir)

Hamizah Ammarah Mahmud, Nadia Salih, Jumat Salimon*

School of Science and Food Technology,

Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 Bangi, Selangor, Malaysia

*Corresponding author: jumat@ukm.edu.my

Abstract

The production of polyesters based on oleic acid and trimethylolpropane (TMP) or pentaerythritol (PE) as potential biolubricant were carried out. The esterification processes between oleic acid with TMP or PE were carried out using sulfuric acid as a catalyst.  The esterification process produced high yield between 92%-94% w/w respectively. The formation of polyesters was confirmed using gas chromatography (GC-FID), Fourier Transform Infrared Spectroscopy (FTIR) and Nuclear Magnetic Resonance (NMR). The polyesters were analyzed for basic lubrication physicochemical properties.  The results showed that polyesters of both TMP and PE having high viscosity index between 200-309, good pour points ranging from -42°C to -59°C and high flash points of 280°C - 300 °C respectively. The polyesters also showed good thermal oxidative stability with TGA onset temperatures above 180 °C. In general both products are plausible to be used as biolubricant for industrial application.

Keywords: esterification, oleic acid, pentaerythritol, polyhydric alcohol, trimethylolpropane

Abstrak

Penghasilan poliester berasaskan asid oleik dan trimetilolpropana  (TMP) atau pentaeritritol (PE) sebagai biopelincir yang berpotensi telah dijalankan. Proses pengesteran asid oleik diantara TMP atau PE menggunakan mangkin asid sulfurik.  Sebanyak 92-94 % w/w hasil daripada pengesteran berjaya dihasilakan. Pengesahan dan pengecaman poliester adalah menggunakan Gas Kromatografi(GC-FID), Spektroskopi Inframerah Fourier Transform (FTIR) dan Resonan Magnetik Nuklear (1H NMR dan 13C NMR ). Ujian asas fisiko-kimia sifat pelinciran telah dijalankan keatas poliester. Hasil analisis menunjukkan kedua-dua poliester TMP dan PE mempunyai indeks kelikatan yang tinggi 200-309, takat tuang yang baik dari julat suhu dari -42°C  kepada -59°C; takat kilat yang tinggi 280°C - >300 °C. Kesemua poliol ester menunjukkan kestabilan oksidatif termal  yang bagus dimana suhu onset TGA melebihi 180 °C. Secara umumnya kedua hasil adalah munasabah untuk digunakan sebagai biopelincir dalam aplikasi perindustrian.

Kata kunci: pengesteran, asid oleik, pentaeritritol, polihidrik alkohol, trimetilolpropana

References

- Arnsek, A., Vizintin, L.,  (2000). Lubricating properties of rapeseed based oils. Journal Synthetic Lubricant 16, 281–295.

- Jumat, S., Nadia, S., Emad, Y., (2012). Industrial development and applications of plant oils and their biobased Oleochemicals. Arabians Journal of Chemistry. 5: 135-145

- Erhan, S. Z., Sharman, K. B and Perez, J. M. (2006). Oxidation and low temperature stability of vegetable oil-based lubricant. Industrial Crops and Product 24: 292-299.

- Lathi, P. S and Mattiasson, B. (2007). Green approach for the preparation of biodegradable lubricant base stock from epoxidized vegetable oil. Applied Catalysis 69:207-212.

- Campanella, A., Rustoy, E., Baldessari, A and Baltanás, M. A. (2010). Lubricants from chemically  modified vegetable oils. Bioresource Technology 01: 245-254.

- Korlipara, V.P., Bhamidipati, V.S.K.R., Rondla,K.R.,Potula, S.B., Arun, K.S.and Rachapudi, B.N.P. (2011). 10-Undecenoic acid-based polyol esters as potential lubricant base stocks. Industrial Crops and Products 35: 237-240

- Wilson, B., (1998). Lubricants and functional fluids from renewable sources. Ind. Lubr. Tribol. 50, 6-15

- Gryglewicz, S., Piechocki, W and Gryglewicz, G. (2003). Preparation of polyol esters based on vegetable and animal fats. Bioresource Technology 87: 35-39.

- Anita Abu Bakar, Yunus, R., Luqman Chuah and Fakhru’l-Razi, A. (2007).Study on effect of hydroxyl groups on lubrication properties of palm based trimethylolpropane esters: development of synthesis method. Journal of Applied Science 7(5): 2011-2014

- Bongardt, F.B, Bossmann, A., Westfetchetel, W.G. and Giede,W., (1996). Manufacture of synthetic esters from alcohol and high oleic low strearic fatty acid. Ger. Offen., DE 4,444, 137.

- Erhan, S.Z., and Perez, J.M. (2002). Biobased industrial Fluids and Lubricants. AOCS Pres, Champaign, IL.

- Lathi, P.S.and Mattiason, B., (2006) Green approach for the preparation of biodegradable lubricant base stock from epoxidized vegetable Oil. Applied Catalyst Lipid. 77: 155-171.

- Hwang, H.S. and  Erhan, S.Z., (2001). Modification of epoxidized soybean oil for lubricant formulations with improved oxidative stability and low pour point. Journal America Chemist Oils Society 78: 1179-1184

- Hwang, H.S., Adhvaryu, A. and Erhan, S.Z., (2003). Preparations and Properties of lubricants base stock from epoxidized soybean oil and 2-ethylhexanol. Journal America Chemist Oils Society. 80: 811-815

- Adhvaryu, A., Liu, Z.S. and Erhan, S.Z., (2005). Synthesis of novel alkoxylated triacylglycerols  and their lubricant base oil properties. Ind. Prod. 21:113-119

- Sharma,B.K., Liu, Z., Adhvaryu, A. and  Erhan, S.Z., (2008). One pot synthesis of chemically modified vegetable oils. Journal Agriculture Food Chemistry. 56: 3049-3056

- Asadauskas,S.,Perez,J.M. and Duda, J.L. (1996). Oxidative Stability and antiwear properties of high Oleic Acid vegetable oils. Lubr. Eng. 52: 877-882.

- Erhan, S. Z and Asadauskas, S. (2000). Lubricant basestocks from vegetable oils. Industrial Crops and Products 11: 277-282.

- Yunus, R., Fakhru’l-Razi, A., Ooi, T. L., Iyuke, S. E and Idris, A. (2003).Development of optimum synthesis methods for transesterification of palm oil methyl esters and trimethylolpropane to environmentally acceptable palm oil-based lubricant. Journal of Oil Palm Research 15 (2): 35-41.

- Yunus, R., Fakhru’l-Razi, A., Ooi, T. L., Iyuke, S. E and Idris, A. (2003).Preparation and characterization of trimethylolpropane esters from palm kernel oil methyl esters. Journal of Oil Palm Research 15(2): 42-49.

- Yunus, R., Fakhru’l-Razi, A., Ooi, T. L., Iyuke, S. E and Idris, A. (2004). Lubrication properties of trimethylolpropane esters based on  palm oil and palm kernel oils. European Journal Lipid Science Technology. 106: 52-60

- Pavia, D.L., Lampman, G.M. and Kriz, G.S. 2009. Introduction to Spectroscopy. 4th ed., United States: Thomson Learning, Inc.

- Robiah, Y., Ooi, T.L., Fakhru’l-Razi, A. and Shahnor, B. (2002.) A Simple Capillary Column GC Method for Analysis.  Journal of the American Oil Chemist’s Society 79: 1075-1080.

- Cermak, S.C. and Isbell, T.A. (2003). Synthesis and  physical properties of estolide-based functional fluids. Industrial Crops and Products 18:183-196.