Malaysian Journal of Analytical Sciences Vol 19 No 1 (2015): 118 – 128

SYNTHESIS AND PHYSICOCHEMICAL STUDIES OF SUBERATES AS BIOLUBRICANT BASETOCK

(Sintesis dan Kajian Fiziko-Kimia bagi Suberat sebagai Minyak Asas Biopelincir)

Maratun Najiha Abu Tahari, Salma Samidin, Mohd Ambar Yarmo, Nadia Salih,  Jumat Salimon*

School of Chemical Sciences &Food Technology,

Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 Bangi, Selangor, Malaysia

*Corresponding author: jumat@ukm.edu.my

Abstract

Synthesis of biolubricant through chemically modified suberic acid (SA) with 3 different types of alcohols which are 1-octanol (Oc), 1-decanol (De) and 1-dodecanol (Do) was conducted with presence of 4% p-toluenesulfonic acid (PTSA) as a catalyst. Preparation, characterization and physico-chemical properties of three types diester (suberate) is discussed in this paper. The diester products were confirmed by NMR and FTIR spectroscopic analysis. Addition of alcohols at the side chains of diacid increases the molecular weight and chain length resulted in the increment of viscosity index (VI), oxidative stability (OT) and flash point (FP) of the diesters. The result showed that 1,8-dioctanyl suberate (DOS) exhibited the most favorable low temperature performance (PP -8.5°C) while 1,8-didodecanyl suberate (DDoS) exhibited higher OT (190°C) and higher FP (224°C) than the other diester oils. On the other hand, the highest VI around 197°C was obtained for 1,8-didecanyl suberate (DDS). These diester oils have a good potential in formulation of industrial biolubricants.

Keywords: biolubricant, diester suberic acid, chemically modified

Abstrak

Sintesis biopelincir melalui modifikasi kimia terhadap asid suberik (SA) dengan 3 jenis alkohol iaitu 1-oktanol (Oc), 1-dekanol (De) dan 1-dodekanol (Do) dilakukan dengan kehadiran 4% asid p-toluenasulfonik (PTSA) sebagai katalis. Penyediaan, pencirian dan sifat fisiko-kimia bagi tiga jenis diester (suberat) dibincangkan dalam manuskrip ini. Produk diester yang terhasil ditentusahkan melalui analisis spektroskopi NMR dan FTIR. Penambahan alkohol pada rantai sisi diasid meningkatkan berat molekul dan panjang rantai mengakibatkan peningkatan indeks kelikatan, kestabilan oksidatif dan takat kilat diester. Hasil kajian  menunjukkan bahawa 1,8-dioktanil suberat (DOS) mempamerkan prestasi bekerja pada suhu rendah yang baik (PP -8.5°C) dan 1,8-didodekanil suberat (DDoS) memperlihatkan OT yang lebih tinggi (190°C) dan FP yang lebih tinggi (224°C) berbanding minyak diester yang lain. Selain itu, 1,8-didekanil suberat (DDS) memiliki VI yang tertinggi iaitu 197°C. Semua minyak diester ini memiliki potensi yang baik dalam formulasi biopelincir industri.

Kata kunci: biopelincir, diester suberik asid, modifikasi kimia

References

- Sharma, B.K., Adhvaryu, A., Liu, Z. and Erhan, S.Z. (2006). Chemical modification of vegetable oils for lubricant applications. Journal of American Oil Chemical Society 83(2): 129-136.

- Rhee, I.S. (1996). Evaluation of environmentally acceptable hydraulic fluids. NLGI Spokesman 60: 5.

- Rudnick, L.R. (2003). Lubricant Additives, Chemistry and Applications. New York: CRC Press Taylor & Francis Group.

- Hwang, H.S. and Erhan, S.Z. (2006). Synthetic lubricant basestock from epoxidized soybean oil and Guerbet alcohols. Industrial Crops and Products 23: 1257-1260.

- Adhvaryu, A. and Erhan. S.Z. (2002). Epoxidiezed soybean oil as a potential source of high temperature lubricants. An International Journal of Industrial of Crops and Products 15: 247-254

- Basiron, Y., Loh, S.K. and Choo, Y.M. (2000). Additive for petroleum fuels and lubricant, biofuels and biolubricant. Oil Palm Bulletin 40: 1-5

- Salunkhe, D.K., Chavan, J.K., Adsulke, R.N. and Kadam, S.S. (1992). Worl Oil Seeds: Chemistry Technology and Utilization. Van Nostrand Reinhold, New York, 1-8.

- Bokish, M. (1998). Fats and Oils Handbook. AOCS Prss, Champaign, IL. pp 838.

- Battersby, N.S. (2000). The biodegradability and microbial toxicity testing of lubricants-Some recommendations. Chemosphere 41(7): 1011-1027.

- Havet, L., Blouet, J., Valloire, F., Brasseur, E., Slomka, D. (2001). Tribology characteristics of some environmentally friendly lubricant. Wear 248: 140-146.

- Walsh, W. (2002). Determination of Triglyceride Composition of Vegetable Oils Using HPLC aand Light Scattering Detection. Annual Meeting and Food Expo, Session 30G, Anaheim, CA.

- Krzan, B. and Vizintin, J. (2003). Tribological properties of environmentally adopted universal tractor transmission oil based on vegetable oil. Tribology Industry 36: 827-833.

- Jumat, S., Nadia, S. and Emad, Y. (2012). Improvement of pour point and oxidative stability of synthetic ester basestocks for biolubricant applications. Arabian Journal of Chemistry 5: 193-200.

- Gryglewicz, S., Oko, F.A., Stankiewicz, M. and Surawska, I. (2006). Esters of dicarboxylic acids as additives for lubricating oils. Tribology International 39: 560–564.

- Gunstone, F.D. (2004). The Chemistry of Oils and Fats: Sources, Compositions, Properties and Uses. U.K: Blackwell Publishing Ltd.

- Pavia, D.L., Lampman, G.M., Kriz, G.S. and Vyvyan, J.R. (2010). Introduction of Spectroscopy. (fourth Ed.). Canada: Nelson Education, Ltd.

- Robiah, Y., Razi, A.F., Ooi, T.L., Iyukie, S.E. and Idris, A. (2003). Development of optimum synthesis method for transesterification of palm oil methyl ester and trimethylpropane to environmentally acceptable palm oil-based lubricant. Journal of Palm Research 15(2): 35-41

- ASTM Standard D5949, Standard test method for pour point of petroleum (automatic pressure pulsing method), ASTM, West Conshohocken, PA, USA.

- Jumat, S., Nadia, S. and Emad, Y. (2012). Synthetic biolubricant basestocks based on environmentally friendly raw materials. Journal of King Saud University – Science 24(3): 221-226.

- ASTM Standard D 56-79, Standard test method for flash point of liquids with a viscosity less than, 45 Saybolt Universal Seconds (SUS) at 37.8 °C (that don’t contain suspended solids and don’t tend to form a surface film under test), ASTM, West Conshohocken, PA, USA.

- ASTM Standard D 2270-93, Standard test method for calculating viscosity index from kinematic viscosity at 40 and 100 °C, ASTM, West Conshohocken, PA, USA.

- Jumat, S. and Nadia, S. and Emad, Y. (2012). Biolubricant basestocks from chemically modified ricinoleic acid. Journal of King Saud University – Science 24(1): 11-17.

- Williamson, K.L. (1994). Synthesis of Isobutyl Propionate via Esterification: Macroscale and Microscale Organic   Experiments. (second Ed.). Houghton Mifflin, Boston.

- George, S.A., Swift, E.J., Thompson, J.Y. and Heymann, H.O. (2003). Irradiance effects on the mechanical properties of universal hybrid and flowable resin composites. Dental Materials 19(15): 406-413.

- Jumat, S., Nadia, S. and Emad, Y. (2010c). Biolubricants: Raw materials, chemical modifications and environmental benefits. European Journal Lipid Science Technology 112: 519-530.

- Erhan, S. Z., Sharma, B. K., Adhvaryu, A. and Liu, Z. (2006). Chemical modification of vegetable oils for lubricant applications. Journal of American Oil Chemist Society 83: 129-136.