Malaysian Journal of Analytical Sciences Vol 19 No 1 (2015): 155 – 162

EFFECT OF CHITOSAN BINDER ON WATER ABSORPTION OF EMPTY FRUIT BUNCHES FILTER MEDIA

(Kesan Kitosan Sebagai Pengikat Keatas Penjerapan Air Media Penapis Tandan Kosong Kelapa Sawit)

Aziatul Niza Sadikin1, 3*, Mohd Ghazali Mohd Nawawi1, 3, Norasikin Othman1, 3, Umi Aisah Asli1, 4,

Roshafima Rasit Ali1, 5, Hasrinah Hasbullah2, 6, Norazana Ibrahim2, 7

1Faculty of Chemical Engineering,

2Faculty of Petroleum & Renewable Engineering,

3Center of Lipid and Applied Research,

4Institute Hydrogen Economy,

5Composite Centre,

6Advanced Membrane Technology Research Centre,

7Gas Technology Centre,

Universiti Teknologi Malaysia, 81310 Johor Bahru, Johor, Malaysia

*Corresponding author: aziatulniza@cheme.utm.my

Abstract

The potential of chitosan as filter media binder was investigated in this study. Chitosan solution with different concentrations were applied to the empty fruit bunches using two different deposition techniques, namely, spray method and addition method. In this study, a water absorption test was used to study the sorption behaviour of empty fruit bunches filter media. The water absorption study showed that the water uptake for empty fruit bunches filter media without the chitosan binder increases with time, until the water sorption reaches the equilibrium state. It was observed that the water uptake decreased from 23% to 14% for the chitosan-filled filter media as compared to binder-less filter media, over the duration of 24 hours. For 1% chitosan concentration, the water uptake is higher compared to 3% chitosan-filled filter media. The water absorption is relatively lower for filter media with a higher concentration of chitosan due to the high compatibility achieved at this interfacial region between empty fruit bunches fibres and chitosan. Alkali-treated filter media showed the lowest water uptake compared to diethyl ether, ethanol and hot water pretreatment methods.

Keywords: empty fruit bunch, filter media, chitosan, water absorption

Abstrak

Potensi kitosan sebagai pengikat media penapis telah dikaji dalam kajian ini. Pelarut kitosan dengan kepekatan yang berbeza telah digunakan untuk tandan kosong buah kelapa sawit dengan menggunakan dua teknik penyaduran yang berbeza, iaitu, kaedah semburan dan kaedah tambahan. Dalam kajian ini, ujian penyerapan air digunakan untuk mengkaji kelakuan serapan media penapis dari tandan kosong buah kelapa sawit. Kajian penyerapan air menunjukkan bahawa pengambilan air untuk tandan buah kosong penapis media tanpa pengikat kitosan meningkat dengan masa, sehingga penyerapan air mencapai keseimbangan. Diperhatikan bahawa pengambilan air sepanjang 24 jam, menurun daripada 23% kepada 14% untuk media penapis berisi kitosan berbanding media penapis tanpa pengikat. Untuk kepekatan 1% kitosan, serabut media mempunyai jurang lebar yang lebih tinggi berbanding dengan penapis kitosan yang berkepekatan 4%. Penyerapan air untuk penapis media dengan kepekatan yang lebih tinggi adalah rendah kerana keserasian yang tinggi dicapai pada rantau di antara permukaan serat tandan kosong kelapa sawit dan kitosan.

Kata kunci: tandan kosong kelapa sawit, media penapis, kitosan, penjerapan air

References

- Rowell, R.M., Chemical modification of lignocellulosics, in 223rd National Meeting on American Chemical Society: Orlando, FL.

- Aliabadi, M., K. Morshedzadeh, and H. Soheyli. (2006). Removal of hexavalent chromium from aqueous solution by lignocellulosic solid wastes. International Journal Environment Science Technology, 3(3): 321-325.

- Shin, E.W., K.G. Karthikeyan, and M.A. Tshabalala. (2007). Adsorption mechanism of cadmium on juniper bark and wood. Bioresource Technology, 98(3): 588-594.

- Shukla, S.R. and R.S. Pai. (2005). Adsorption of Cu(II), Ni(II) and Zn(II) on modified jute fibres. Bioresource Technology, 96(13): 1430-1438.

- Karageorgiou, K., M. Paschalis, and G.N. Anastassakis. (2007). Removal of phosphate species from solution by adsorption onto calcite used as natural adsorbent. Journal of Hazardous Materials, 139(3): 447-452.

- Kim, R.H., et al. (2007). Reuse of greywater and rainwater using fiber filter media and metal membrane. Desalination, 202(1-3): 326-332.

- Riahi, K., A. Ben Mammou, and B. Ben Thayer. (2009). Date-palm fibers media filters as a potential technology for tertiary domestic wastewater treatment. Journal of Hazardous Materials, 161(2-3): 608-613.

- Sreekala, M.S., M.G. Kumaran, and S. Thomas. (1997). Oil palm fibers: Morphology, chemical composition, surface modification, and mechanical properties. Journal of Applied Polymer Science, 66(5): 821-835.

- Sreekala, M.S., George, J., Kumaran, M. G., & Thomas, S. (2001). Water-sorption kinetics in oil palm fibers. Journal of Polymer Science Part B-Polymer Physics, 39(11): 1215-1223.

- Sreekala, M.S., Kumaran, M. G., Joseph, R., & Thomas, S. (2001). Stress-relaxation behaviour in composites based on short oil-palm fibres and phenol formaldehyde resin. Composites Science and Technology, 61(9): 1175-1188.

- Yahya, M.Z.A. and A.K. Arof. (2003). Effect of oleic acid plasticizer on chitosan-lithium acetate solid polymer electrolytes. European Polymer Journal, 39(5): 897-902.

- Umemura, K., K. Kaiho, and S. Kawai. (2009). Characterization of Bagasse-Rind Particleboard Bonded with Chitosan. Journal of Applied Polymer Science, 113(4): 2103-2108.

- Abdul Khalil, H.P.S., Issam, A. M., Ahmad Shakri, M. T., Suriani, R., & Awang, A. Y. (2007). Conventional agro-composites from chemically modified fibres. Industrial Crops and Products, 26(3): 315-323.

- Moshiul Alam, A.K.M. Beg, M. D. H., Reddy Prasad, D. M., Khan, M. R., and Mina, M. F. (2012). Structures and performances of simultaneous ultrasound and alkali treated oil palm empty fruit bunch fiber reinforced poly(lactic acid) composites. Composites Part A: Applied Science and Manufacturing, 43(11): 1921-1929.

- Hassan, E.A., M.L. Hassan, and K. Oksman (2011). Improving bagasse pulp paper sheet properties with microfibrillated cellulose isolated from xylanase-treated bagasse. Wood and Fiber Science, 43(1): 76-82.