Malaysian Journal of Analytical Sciences Vol 19 No 1 (2015): 213 – 221

PHOTOSTABILIZING EFFICIENCY OF PVC BASED ON EPOXIDIZED OLEIC ACID

(Kecekapan Kestabilanfoto Filem PVC berasaskan Asid Oleik Terepoksida)

Emad Yousif1 , Rahimi M. Yusop2,3*, Ahmed Ahmed1, Jumat Salimon2, Nadia Salih2

1Department of Chemistry, College of Science,

Al-Nahrain University, Baghdad, Iraq

2School of Chemical Sciences and Food Technology, Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 Bangi, Selangor, Malaysia

3Regenerative Advanced Medical & Dental Institute,

Universiti Sains Malaysia, 13200 Bertam Kepala Batas, Pulau Pinang, Malaysia

*Corresponding author: rahimi@ukm.edu.my

Abstract

The photostabilization of poly (vinyl chloride) (PVC) films by epoxidized oleic acid compounds was investigated. The PVC films containing concentration of complexes 0.5% by weight were produced by the casting method from tetrahydrofuran (THF) solvent. The photostabilization activities of these compounds were determined by monitoring the carbonyl, polyene and hydroxyl indices with irradiation time. The changes in viscosity average molecular weight of PVC with irradiation time were also tracked (using THF as a solvent). The quantum yield of the chain scission (Φcs) of these complexes in PVC films was evaluated and found to range between 4.98´10-8 and 8.72´10-8. According to the experimental results obtained, mechanisms were suggested depending on the structure of the additive (oleic acid).

Keywords: photostabilizer, PVC, oleic acid

Abstrak

Proses kestabilanfoto filem poli(vinil klorida) (PVC) dengan asid oleik terepoksida telah dikaji. Filem PVC yang mengandungi kompleks berkepekatan 0.5% berat telah dihasilkan dengan kaedah acuan yang sama daripada pelarut tetrahidrofuran (THF). Aktiviti kestabilanfoto sebatian-sebatian ini ditentukan dengan pengawasan indeks karbonil, poliena dan hidroksi dengan masa penyinaran. Perubahan dalam kelikatan berat molekul purata bagi PVC dengan masa penyinaran turut dikesan (menggunakan THF sebagai pelarut). Hasil kuantum rantai guntingan (Φcs) kompleks-kompleks ini di dalam filem-filem PVC telah dikira dan di dapati berada dalam julat 4.98´10-8 and 8.72´10-8. Berdasarkan keputusan eksperimen yang diperolehi, beberapa mekanisme telah dicadangkan bergantung kepada struktur bahan tambah yang digunakan (asid oleic).

Kata kunci:  kestabilanfoto, PVC, asid oleik

References

- Yousif, E. and Haddad, R. (2013). Photodegradation and photostabilization of polymers, especially polystyrene: review, Springer plus 2: 1-32.

- Moulay, S., (2010). Chemical modification of poly(vinyl chloride)-Still on the run.  Progress in Polymer Science. 35: 303-331.

- Braun, D.  (2004). Poly(vinyl chloride) on the way from the 19th century to the 21st century. J. Polym. Sci. A Polym. Chem. 42: 578–586.

- Yousif, E.,  Salimon, J. and Salih, N. (2012). Improvement of the photostabilization of PMMA films in the presence 2N-salicylidene-5-(substituted)-1,3,4-thiadiazole, J. King Saud University (Science). 24: 11-17.

- Gardette, J. Gaumet, S. and Philippart, J. (1993). Influence of the experimental conditions on the photooxidation of poly(vinyl chloride). Journal of Applied Polymer Science. 48(11): 1885-1895.

- Harper, D., McKellar, N. and Turner, P. (1974). Photostabilizing effect of Ni(II) chelates in polymers II. Effect of diamagnetic chelates on polypropylene phosphorescence. Journal of Applied Polymer Science. 311 (1974) 2802-2805.

- Salimon, J., Salih, N. and Yousif, E. (2011). Chemically modified biolubricant basestocks from epoxidized oleic acid: Improved low temperature properties and oxidative stability. Journal of Saudi Chemical Society 15: 195-201.

- Yousif, E. (2013). Triorganotin(IV) complexes photo-stabilizers for rigid PVC against photodegradationJournal of Taibah University for Science, 7: 79-87.

- Yousif, E., Salimon, J.,  Salih, N. 2014. Mechanism of photostabilization of poly(methy methacrylate) films by 2-thioacetic acid benzothiazol complexes, Arabian Journal of Chemistry, 7: 306-311.

- Mark, J. 2007. Physical properties of polymers handbook. Springer, New York.

- Yousif, E., Salih, N., Salimon, J. (2011). Improvement of the " Improvement of the Photostabilization of PVC Films in the Presence of 2N-Salicylidene-5-(Substituted)-1,3,4-Thiadiazole. Journal of Applied Polymer Science. 120: 2207–2214.

- Andrady, A., Hamid, S., Hu, X. and Torikai, A. (1998). Effects of increased solar ultraviolet radiation on materials. Journal of Photochemistry and photobiology B-Biology. 46: 96-103.

- Rabek, J. & Ranby, B. (1975). Photodegradation, photooxidation and photostabilization of Polymers, John Wiley, New York.

- Shyichuk, A., White, J. (2000). Analysis of chain-scission and crosslinking rates in the photo-oxidation of polystyrene. Journal of Applied Polymer Science,  77(13): 3015-3023.

- Yousif, E., Hameed, A., Rasheed, R., Mansoor, H., Farina, Y., Graisa, A., Salih, N., Salimon, J. (2010). Synthesis and Photostability Study of Some Modified Poly(vinyl chloride) Containing Pendant Benzothiazole and Benzimidozole Ring. International Journal of Chemistry, 2(1): 65-80.

- Yousif, E., Aliwi, S., Ameer, A. (2009). Improved photostability of PVC films in the presence of 2-thioacetic acid -5-phenyl-1,3,4-oxadiazole complexes. Turkish J.Chem. 33: 399-410.

- Harun, N. S., Talip, N. N. M., Hong, L. K., Jamil, M. S. M., & Yusop, R. M. (2013). Phase Behaviour of Fatty Alcohol Sulphate and Fatty Alcohol Ether Sulphate from Palm Based. Malaysian Journal of Analytical Sciences, 17(1), 139-145..

- Hong, L. K., Harun, N. S., Jamil, M. S. M., & Yusop, R. M. (2013). Phase Behavior and Rheology of Fatty Alcohol Sulphate, Fatty Alcohol Ether Sulphate from Palm based and Mixtures with other Surfactants. Malaysian Journal of Analytical Sciences, 17(1), 101-108.