Malaysian Journal of Analytical Sciences Vol 19 No 2 (2015): 388 – 397

EFFECTS OF MODIFIED CHITOSAN TO THE PROPERTIES OF

POLY (N-ISOPROPYLACRYLAMIDE/O-NITROCHITOSAN) NETWORK

(Kesan Kitosan Terubahsuai Terhadap Sifat Rangkaian Poli (N-Isopropilakrilamida/O-Nitrokitosan))

Noriah Abdul Rahman1 and Sharina Abu Hanifah1, 2*

1School of Chemical Sciences and Food Technology,

2Polymer Research Center,

Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: sharina@ukm.edu.my

Received: 4 December 2014; Accepted: 24 February 2015

Abstract

New chitosan derivative was successfully prepared that changed swelling property of NIPAAm based polymer network. An interpenetrating polymer network (IPN), N-isopropylacrylamide/O-nitrochitosan (NONK) was synthesized in the presence of ammonium persulfate using solution polymerization technique. Two compositions of IPN were used; 90% of NIPAAm and 10% of ONK (w/w) poly (NONK91) and 80% of NIPAAm and 20% of ONK (w/w) poly (NONK82). A new vibration of the C–N bond formed between NH from ONK and CH2 from NIPAAm were detected at 1154 and 1171 cm-1 using Attenuated Total Reflection Fourier-transform Infrared (ATR-FTIR) spectroscopy. The primary amine became a secondary amine, and the peaks of amide I (C=O peak) and amide II (N–H) were broadened. The structure of ONK was confirmed using Nuclear Magnetic Resonance (NMR). At 10 °C, it was found that IPN poly (NONK82) had the highest swelling percentage, 1171%, compared to poly (NIPAAm) at 467%. Micrograph from scanning electron microscopy (SEM) indicated large pores were formed on the IPN NONK surface when ONK ratio was further increased. ONK and NIPAAm, have good miscibility in polymer networks. This ONK contributes significant effect towards swelling behavior of NIPAAm.

Keywords: N-isopropylacrylamide (NIPAAm), O-nitrochitosan (ONK), Interpenetrating Polymer Network

Abstrak

Satu terbitan baru kitosan telah berjaya disediakan yang mengubah sifat pembengkakan polimer rangkaian berasaskan NIPAAm. Polimer rangkaian saling tembus (IPN) N-Isopropilakrilamida/O-nitrokitosan (NONK) disintesis dengan kehadiran ammonium persulat menggunakan teknik pempolimeran larutan. Dua komposisi IPN digunakan; 90% NIPAAm dan 10% of ONK (w/w) poli (NONK91) dan 80% NIPAAm dan 20% NIPPAm dan 20% ONK (w/w) poli(NONK82). Satu terbitan baru kitosan berjaya dilakukan, O-nitrokitosan (ONK) yang disintesis dari kitosan sebelum ia ditindak balas dengan N-Isopropilakrilamida (NIPAAm). Getaran baru bagi ikatan C-N terbentuk di antara NH dari ONK dan CH2 dari NIPAAM dikesan pada 1154 dan 1171 cm-1 menggunakan spektroskopi (ATR-FTIR). Amina primer menjadi amina sekunder dan puncak pada amida I (C=O) dan amida II (N-H) menjadi lebih lebar. Stuktur ONK dipastikan menggunakan NMR. Pada 10oC , didapati IPN poli (NONK82) mempunyai peratusan pembengkakan paling tinggi, 1171 % berbanding poli (NIPAAM) pada 467 %. Mikrograf dari mikroskopi imbasan elektron mendapati liang besar terbentuk pada permukaan IPN NONK apabila nisbah ONK ditingkatkan. ONK dan NIPAAm mempunyai daya kecampuran yang baik apabila digabungkan dalam jaringan polimer.  ONK menyumbang kepada kesan signifikan terhadap sifat pembengkakan NIPAAm.

Kata Kunci: N-isopropilakrilamida (NIPAAm), O-nitrokitosan (ONK), Polimer Rangkaian Saling Menembus

References

- Kumar M.N.V.R. (2000). A review of chitin and chitosan applications. Reactive Functional Polymer. 46 (1): 1-27.

- Prabaharan, M. & Jayakumar R. (2009). Chitosan-graft-β-cyclodextrin scaffolds with controlled drug release capability for tissue engineering applications. International Journal of Biological Macromolecules 44(4): 320-325.

- Baldrick P. (2010). The safety of chitosan as a pharmaceutical excipient. Regulatory Toxicology and Pharmacology 56 (3): 290-299.

- Dutta, P.K.,Tripathi, S., Mehrotra, G.K. &  Dutta, J. (2009). Perspectives for chitosan based antimicrobial films in food applications. Food Chemistry. 114 (4):1173-1182.

- Don, T.M, & Chen, H.R. (2005). Synthesis and characterization of AB-crosslinked graft copolymers based on maleilated chitosan and N-isopropylacrylamide. Carbohydrate Polymers 61 (3): 334- 347.

- Verestiuc, L. Ivanov, C. Barbu, E. & Tsibouklis, J. (2004). Dual-stimuli responsive hydrogels based on poly(N-isopropylacrylamide)/chitosan semi-interpenetrating networks. International Journal of Pharmaceutics 269(1): 185-194.

- Guo, B.L. & Gao, Q.Y. (2007). Preparation and properties of a pH/temperature-responsive carboxymethylchitosan/poly (N-isopropylacrylamide) semi-IPN hydrogel for oral delivery of drugs. Carbohydrate Research 342(16):2416-2422.

- Rinaudo, M. (2006). Chitin and chitosan: Properties and applications.Progress in Polymer Science 31(7): 603-632.

- Alli, A. & Hazer, B. (2008). Poly (N-isopropylacrylamide) thermoresponsive cross-linked conjugates containing polymeric soybean oil and/or polypropylene glycol. European Polymer Journal 44 (6):1701-1713.

- Zhang, H-F. Zhong, H. Zhang, L. Chen, S. Zhao, Y. & Zhu, Y-l. (2009). Synthesis and characterization of thermosensitive graft copolymer of N-isopropylacrylamide with biodegradable carboxymethylchitosan. Carbohydrate Polymers 77(4):785-790.

- Chen, J. Sun, J. Yang, L. Zhang, Q. Zhu, H. Wu, H. Hoffman, A.S. & Kaetsu I. (2007). Preparation and characterization of a novel IPN hydrogel memberane of poly (N -isopropylacrylamide)/carboxymethyl chitosan (PNIPAAM/CMCS). Radiation Physics and Chemistry 76 (8-9): 1425-1429.

- Zeng, M. Zhang, L. & Kennedy, J.F. (2005). Intermolecular interaction and properties of cross-linked materials from poly (ester-urethane) and nitrochitosan. Carbohydrate Polymers 60(3): 399-409.

- Han J. Wang K. Yang D. & Nie J. (2009). Photopolymerization of methacrylated chitosan/PNIPAAm hybrid dual-sensitive hydrogels as carrier for drug delivery. International Journal of Biological Macromolecules 44(3): 229-235.

- Guinesi, L.S. & Cavalheiro, E.T.G. (2004). The use of DSC curves to determine the acetylation degree of chitin/chitosan samples. Thermochimica Acta 444(2): 128-133.

- Lang, G. In: Zakaria, M, Muda W. M. W. & Abdullah, M. P. (1995). Chitin and Chitosan: The Versatile Environmentally Friendly Modern Materials, (ed) Universiti Kebangsaan Malaysia, Bangi,. p. 113.

- Caykara, T. Kiper, S. & Demirel, G. (2006). Thermosensitivepoly(N-isopropylacrylamide-co-acrylamide) hydrogels: Synthesis, swelling and interaction with ionic surfactants. European Polymer Journal 42 (2): 348-355.

- Van de Velde, K & Kiekens, P. (2004). Structure analysis and degree of substitution of chitin, chitosan and dibutyrylchitin by FT-IR spectroscopy and solid state 13C NMR Carbohydrate Polymers 58: 409–416.

- Cardenas, G. Cabrera, G. Taboada, E. & Rinaudo, M. (2006). Synthesis and Characterization of Chitosan Alkyl Phosphate. Journal of the Chilean Chemical Society 51(1): 1-8.

- Bhattarai, N. Gunn, J. & Zhang, M. (2010). Chitosan-based hydrogels for controlled, localized drug delivery. Advanced Drug Delivery Reviews 62: 83–99.

- Nagahama, H. Maeda, H. Kashiki, T. Jayakumar, R. Furuike, T. & Tamura, H. (2009). Preparation and characterization of novel chitosan/gelatine membranes using chitosan hydrogel. Carbohydrate Polymers 76 (2): 255-267.