# Malaysian Journal of Analytical Sciences Vol 19 No 2 (2015): 388 – 396

# SINTESIS AMORFUS MANGAN DIOKSIDA (MnO2) NANO-POROS MENGGUNAKAN PROSES SONOKIMIA DAN BUKAN SONOKIMIA

# (Synthesis of Nanoporous Amorphous Manganese Dioxide (MnO2) via Sonochemical and Non-Sonochemical Processes)

# Siti Zubaidah Hasan, Muhammad Rahimi Yusop, Mohamed Rozali Othman*

# School of Chemical Science and Food Technology,

# Faculty of Science and Technology,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: rozali@ukm.edu.my

Received: 17 February 2015; Accepted: 17 March 2015

Abstrak

# Amorfus-MnO2 nano-poros telah disintesis menggunakan proses sonokimia (sonikasi) dan bukan sonokimia (hidroterma) terhadap larutan 0.1 M KMnO4 menggunakan mangkin silika dan silika-alumina yang permukaannya terubahsuai masing-masingnya pada suhu bilik dan 100⁰C. Amorfus-MnO2 nano-poros yang diperolehi seterusnya dicirikan dengan menggunakan spektrometer FTIR, dan spektrum yang diperolehi menunjukkan kewujudan serapan ikatan MnO2. Produk juga dicirikan menggunakan pembelauan sinar-X (XRD), dan morfologi diimbas dengan menggunakan mikroskopi pengimbas elektron-pembolehubah tekanan (VP-SEM) dan juga mikroskopi elektron transmisi (TEM). Kelakuan elektrokimia MnO2 dikaji menggunakan kaedah voltametri berkitar dan ia menunjukkan MnO2/Mn2+ yang berbalik.

# Kata kunci: proses sonokimia, proses bukan sonokimia, amorfus MnO2 nano-poros, voltametri berkitar

Abstract

# Nano-porous amorphous MnO2 was synthesized using sonochemical (sonication) and non-sonochemical (hydrothermal) processes to a 0.1 M KMnO4 solution with modified surface of silica and silica-alumina catalyst at room temperatures and 100⁰C respectively. Nano-porous amorphous MnO2 obtained was then characterized using infrared spectrometer (FT-IR), and the spectrum shows the absorption of MnO2 bonding. Structure of the product was later characterized by X-ray diffraction (XRD), and morphology scanned using a scanning electron microscope-variable pressure (VP-SEM) and transmission electron microscopy (TEM). The electrochemical behavior of MnO2 was studied and it shows reversible of MnO2 / Mn2+.

# Keywords: sonochemical process, non-sonochemical process, nanoporous amorphous-MnO2, cyclic voltammetry

References

- Mohammad, A.W., Lau, C. H., Zaharim, A. & Omar, M. Z. (2012). Elements of Nanotechnology Education in Engineering Curriculum Worldwide. Procedia - Social and Behavioral Sciences, 60(0): 405-412.

- Raam Dheep, G. & Sreekumar, A. (2014). Influence of Nanomaterials on Properties of Latent Heat Solar Thermal Energy Storage Materials – A Review. Energy Conversion and Management, 83(0): 133-148.

- Setyawati, M. I., Tay, C. Y. & Leong, D. T. (2013). Effect of Zinc Oxide Nanomaterials-Induced Oxidative Stress on the P53 Pathway. Biomaterials, 34(38): 10133-10142.

- Tang, W. W., Zheng, G. M., Gong, G. L., Liang, J., Xu, P., Zhang, C. & Huang, B. B. (2014). Impact of Humic/Fulvic Acid on the Removal of Heavy Metals from Aqueous Solutions Using Nanomaterials: A Review. Science of the Total Environment, 468–469(0): 1014-1027.

- Henglein, A. (1989). Small-Particle Research: Physicochemical Properties of Extremely Small Colloidal Metal and Semiconductor Particles. Chemical Reviews, 89(8): 1861-1873.

- Suslick, K. S., Choe, S. B., Cichowlas, A. A. & Grinstaff, M. W. (1991). Sonochemical Synthesis of Amorphous Iron. Nature, 353(6343): 414-416.

- Dupont, M., Hollenkamp, A. F. & Donne, S. W. (2013). Electrochemically Active Surface Area Effects on the Performance of Manganese Dioxide for Electrochemical Capacitor Applications. Electrochimica Acta, 104(0): 140-147.

- Ge, J. & Qu, J. (2003). Degradation of Azo Dye Acid Red B on Manganese Dioxide in the Absence and Presence of Ultrasonic Irradiation. Journal of Hazardous Materials, 100(1–3): 197-207.

- Ilyas, M. & Saeed, M. (2011). Synthesis and Characterization of Manganese Oxide and Investigation of Its Catalytic Activities for Oxidation of Benzyl Alcohol in Liquid Phase. International Journal of Chemical Reactor Engineering, 9:  A75.

- Ren, Y., Chen, Z., Cai, Y. & Lin, J. (2011). Electrosynthesis of Glyceraldehyde by Cyclic Nano-MnO2/Mn2+ in Bipolar Membrane-Equipped Electrolytic Cell. Electrochemistry Communications, 13(12): 1317-1319.

- Ching, S., Hughes, S. M., Gray, T. P. & Welch, E. J. (2004). Manganese Oxide Thin Films Prepared by Nonaqueous Sol–Gel Processing: Preferential Formation of Birnessite. Microporous and Mesoporous Materials, 76(1): 41-49.

- Kumar, H., Manisha, & Sangwan, P. (2013). Synthesis and Characterization of MnO2 Nanoparticles Using Co-precipitation Technique. International Journal of Chemistry and Chemical Engineering, 3(3): 155-160.

- Li, Q., Luo, G., Li, J. & Xia, X. (2003). Preparation of Ultrafine MnO2 Powders by the Solid State Method Reaction of KMnO4 with Mn(II) Salts at Room Temperature. Journal of Materials Processing Technology, 137(1–3): 25-29.

- Pang, S. C., Chin, S. F. & Ling, C. Y. (2012). Controlled Synthesis of Manganese Dioxide Nanostructures via a Facile Hydrothermal Route. Journal of Nanomaterials, 2012: 7.

- Yu, Z. M., Luo, G., Li, J. & Xia, X. (2011). The Preparation, Texture and Electrodeposition Mechanism of Reticular MnO2 Catalytic Materials with High Porosity. Advanced Materials Research, 311: 1784-1788.

- Zhang, X., Yue, L. Jin, D. & Zheng, Y. (2010). A Facile Template-Free Preparation of Porous Manganese Oxides by Thermal Decomposition Method. Inorganic Materials, 46(1): 51-54.

- Zhu, S., Zhou, Z., Zhang, D. & Wang, H. (2006). Synthesis of Mesoporous Amorphous MnO2 from SBA-15 via Surface Modification and Ultrasonic Waves. Microporous and Mesoporous Materials, 95(1): 257-264.

- Kumar, B. M., Karikkat, S., Krishna, R. H., Udayashankara, T. H., Shivaprasad, K. H. & Nagabhushana, B. M. (2014). Synthesis, Characterization of Nano MnO2 and Its Adsorption Characteristics Over an Azo Dye. Research & Reviews: Journal of Material Sciences, 2(1): 27-31.

- Adelkhani, H., Ghaemi, M. & Jafari, S. (2008). Novel Nanostructured MnO2 Prepared by Pulse Electrodeposition: Characterization and Electrokinetics. Journal of Materials Science & Technology, 24(6): 857-862.

- Ryu, S. H., Hwang, S. G., Yun, S. R., Cho, K. K., Kim, K. W. & Ryu, K. S. (2011). Synthesis and Electrochemical Characterization of Silica-Manganese Oxide with a Core-Shell Structure and Various Oxidation States. Bulletin of the Korean Chemical Society, 32(8): 2683.

- Henglein, A. (1987). Sonochemistry: Historical Developments and Modern Aspects. Ultrasonics, 25(1): 6-16.