Malaysian Journal of Analytical Sciences Vol 19 No 3 (2015): 481 – 492

NEW FUNCTIONALISED SOL-GEL HYBRID SORBENT COATING FOR STIR BAR SORPTIVE EXTRACTION OF SELECTED NON-STEROIDAL ANTI INFLAMMATORY DRUGS IN HUMAN URINE SAMPLES

(Bahan Salutan Baharu Hibrid Sol-Gel Terfungsi Untuk Pengekstrakan Erapan Bar Berputar Ubat  Anti-Radang Bukan Steroid Terpilih Dalam  Sampel Urin Manusia)

Mashkurah Abd Rahim1 , Wan Aini Wan Ibrahim*1, 2, Zainab Ramli1, 2,  Mohd Marsin Sanagi1, 2

1Separation Science and Technology Group (SepSTec),

Department of Chemistry, Faculty of Science,

2Ibnu Sina Institute for Scientific & Industrial Research (ISI-SIR),

Universiti Teknologi Malaysia, 81310 UTM, Johor Bahru, Johor, Malaysia

*Corresponding author: wanaini@kimia.fs.utm.my, waini@utm.my

Received: 30 January 2015; Accepted: 1 April 2015

Abstract

A new sol-gel hybrid material, methyltrimethoxysilane-cyanopropyltriethoxysilane (MTMOS-CNPrTEOS) was successfully synthesized and used as a coating material in stir bar sorptive extraction (SBSE) of selected non-steroidal anti-inflammatory drugs (NSAIDs) in urine samples. The MTMOS-CNPrTEOS hybrid was synthesized by hydrolysis and condensation of MTMOS and CNPrTEOS in the presence of trifluoroacetic acid as catalyst via sol–gel method. Several factors influencing the synthesized sol-gel hybrid MTMOS-CNPrTEOS process such as mole ratio of MTMOS-CNPrTEOS, NaOH concentrations as etching solution, etching time, coating time and water content were investigated and optimized in this study. The optimum synthesis conditions obtained were 1:1 mol ratio of MTMOS-CNPrTEOS, 1 M NaOH as etching solution, 60 min etching time, 2 h coating time and 6 mmol water. The sol-gel hybrid MTMOS-CNPrTEOS synthesized under the optimum conditions was used to determine selected NSAIDs in human urine samples using normal stacking mode capillary electrophoresis with ultraviolet detection. MTMOS-CNPrTEOS SBSE method demonstrated good linearity (60 to 20,000 µg L-1) with excellent coefficient of determination (r2 > 0.9990). The sol-gel hybrid MTMOS-CNPrTEOS SBSE method showed low limit of detection (35 – 41 µg L-1) with good precision (RSD < 6 %, n = 3) and excellent extraction recoveries (83.5 – 98.9%) for the selected NSAIDs. The sol-gel hybrid MTMOS-CNPrTEOS SBSE method demonstrated good potential as an alternative sorbent in SBSE method for NSAIDs.

Keywords: Sol-gel hybrid, stir bar sorptive extraction, non-steroidal anti-inflammatory drugs, normal stacking mode, capillary electrophoresis-UV detection

Abstrak

# Sol-gel hibrid baharu, metiltrimetoksisilana-sianopropiltrietoksisilana (MTMOS-CNPrTEOS) telah berjaya disintesis dan digunakan sebagai bahan baharu penyalutan untuk pengekstrakan erapan bar berputar (SBSE) dalam penentuan ubat anti-radang bukan steroid (NSAIDs) terpilih di dalam sampel urin manusia. Hibrid MTMOS-CNPrTEOS disintesis melalui hidrolisis dan kondensasi MTMOS dan CNPrTEOS dengan kehadiran asid trifluoroasetik sebagai mangkin melalui kaedah sol-gel. Beberapa faktor yang mempengaruhi proses penghasilan hibrid sol-gel MTMOS-CNPrTEOS seperti nisbah mol MTMOS-CNPrTEOS, kepekatan NaOH sebagai larutan punaran, masa punaran, masa salutan dan kandungan air dalam proses sol-gel telah dikaji dan dioptimumkan. Keadaan sintesis yang optimum ialah 1:1 nisbah mol MTMOS-CNPrTEOS, 1 M NaOH sebagai larutan punaran, 60 min masa punaran, 2 jam masa salutan dan 6 mmol air. Hibrid sol-gel MTMOS-CNPrTEOS yang disintesis di bawah keadaan optimum telah digunakan untuk menentukan NSAID terpilih dalam sampel urin manusia menggunakan mod normal tersusun elektroforesis rerambut dengan pengesan ultralembayung. Kaedah hibrid sol-gel MTMOS-CNPrTEOS SBSE menunjukkan kelinearan yang baik (60 - 20,000 μg L-1) dengan pekali penentuan, r2 > 0.9990 yang cemerlang. Kaedah hibrid sol-gel MTMOS-CNPrTEOS SBSE ini menunjukkan had pengesanan yang rendah (35 - 41 μg L-1) dengan ketepatan yang baik (RSD < 6%, n = 3) dan pengembalian pengekstrakan yang cemerlang (83.5 – 98.9%) untuk NSAID terpilih. Kaedah hibrid sol-gel MTMOS-CNPrTEOS menunjukkan potensi tinggi sebagai pengerap alternatif untuk kaedah SBSE.

# Kata kunci: 	Hibrid sol-gel, pengekstrakan bar berputar, ubat anti radang bukan steroid, mod tersusun normal, elektroforesis rerambut-pengesan ultralembayung

References

- Lisa, C. K. and Eliezer, M. R. (1994). Sol-gel optic: processing and application. Berlin: Springer International Series.

- Wan Ibrahim, W. A., Veloo, K. V., and Sanagi, M. M. (2012).  Novel sol-gel hybrid methyltrimethoxysilane-tetraethoxysilane as solid phase extraction sorbent for organophosphorus pesticides. J. Chromatogr. A, 1229:55-62.

- Rao, A. V. and Haranath, D. (1999). Effect of Methyltrimethoxysilane as a Synthesis Component on the Hydrophobicity and some physical properties of silica aerogels. Microporous Mesoporous Mater., 30: 267–273.

- Brambilla, R., Poisson, J., Miranda, M. S. L., Cardoso, M. B. and Butler, I. S. (2011). Sol-gel preparation of aminopropyl-silica-magnesia hybrid materials. J. Sol-Gel Sci. Tech., 2: 1–10.

- Wan Ibrahim, W. A., Abdul Keyon, A. S., Prastomo, N. and Atsunori, M. (2011). Synthesis and characterization of polydimethylsiloxane-cyanopropyltriethoxysilane-derived hybrid coating for stir bar sorptive extraction. J. Sol-Gel Sci. Technol., 59: 28–134.

- Wan Ibrahim, W. A., Wan Ismail, W. A. and Sanagi, M. M. (2013). Selective and Simultaneous Solid Phase Extraction of Polar and Non- Polar Organophosphorus Pesticides Using Sol-Gel Hybrid Silica-Based Sorbent. J. Tec., 62(3): 83–87.

- Colon, L. A., Guo, Y. and Fermier, A. (1997). Capillary Electrochromatography. Anal.Chem. 69: 461A–467A.

- Lopes, A. L. and Augusto, F. (2004). Preparation and characterization of polydimethylsiloxane/poly(vinylalcohol) coated solid phase microextraction fibers using sol–gel technology. J. Chromatogr. A. 1056: 13–19.

- Ebell, M. H. (2004). NSAIDs vs opiates for pain in acute renal colic. Am. Fam. Physician. 70(9): 1682–1690.

- Gajraj, N. M. (2003). The effect of cyclooxygenase-2 inhibitors on bone healing. Reg. Anesth. Pain. med. 28(5): 456–465.

- Chiang, J. and Huang, S. (2008). Simultaneous derivatization and extraction of amphetamine and methylenedioxyamphetamine in urine with headspace liquid-phase microextraction followed by gas chromatography-mass spectrometry. J. Chromatogr. B. 1185: 19–22.

- Pountos, I., Georgouli, T., Bird, H. and Giannoudis, P. V. (2011). Nonsteroidal anti-inflammatory drugs: prostaglandins, indications, and side effects. Int. J. Interferon. Cytokine Mediator. Res. 3: 19–27.

- Albero, B., Sanchez-Brunete, C. and L. Tadeo, J. (2003). Determination of Organophosphorus Pesticides in Fruit Juices by Matrix Solid-Phase Dispersion and Gas Chromatography. J. Agric. Food Chem. 51: 6915–6921.

- Lin, W. C., Chen, H. C. and Ding, W. H. (2005). Determination of pharmaceutical residues in waters by solid-phase extraction and large-volume on-line derivatization with gas chromatography-mass spectrometry. J. Chromatogr. A. 1065(2): 279–285.

- Basheer, C., Alnedhary, A. A., Rao, B. S. M., Valliyaveettil, S. and Lee, H. K. (2006). Development and application of porous membrane-protected carbon nanotube micro-solid-phase extraction combined with gas chromatography/mass spectrometry. Anal. Chem. 78(8):  2853–2858.

- He, Y. and Kang, Y. J. (2006). Single drop liquid-liquid-liquid microextraction of methamphetamine and amphetamine in urine. J. Chromatogr. A. 1133: 35–40.

- Allen, D. L. and Oliver, J. S. (2000). The use of supercritical fluid extraction for the determination of amphetamines in hair. Forensic Sci. Int.107(1-3), 191–199.

- Fan, Y., Feng, Y. Q., Zhang, J. T., Da, S. L. and Zhang, M. (2005). Poly(methacrylic acid-ethylene glycol dimethacrylate) monolith in-tube solid phase microextraction coupled to high performance liquid chromatography and analysis of amphetamines in urine samples. J. Chromatogr. A. 1074: 9–16.

- Chou, C. C. and Lee, M. R. (2005). Solid phase microextraction with liquid chromatography–electrospray ionization–tandem mass spectrometry for analysis of amphetamine and methamphetamine in serum. Anal. Chim. Acta. 538: 49–56.

- Zhou, J. and Zeng, Z. (2006). Novel fiber coated with β-cyclodextrin derivatives used for headspace solid-phase microextraction of ephedrine and methamphetamine in human urine. Anal. Chim. Acta. 556(2): 400–406.

- Segro, S. S., Cabezas, Y. and Malik, A. (2009). Ultra-high-stability, pH-resistant sol-gel titania poly(tetrahydrofuran) coating for capillary microextraction on-line coupled to high-performance liquid chromatography. J. Chromatogr. A. 1216(20): 4329–4338.

- Moner-Girona, M., Roig, A. and Molins, E. (2003). Sol-Gel Route to Direct Formation of Silica Aerogel Microparticles. J. Sol-gel Sci. Techol. 26: 645–649.

- Guido, K., Caseri, W., Bourgeat-Lami, E., Zhu, J. and A. Wilkie, C. (2007). Hybrid material: Synthesis, characterization and application. Guido, K., Ed., 2nd edition,  Wiley-Vch Verlag GmbH.

- Pandey, S. and Mishra, B. S. (2011). Sol-gel derived organic-inorganic hybrid materials : synthesis , characterizations and applications. J. Sol-gel Sci Technol. 57: 126-138.

- Khan, B. A., Farid, A., Asi, M. R., Shah, H. and Badshah, A. K. (2009). Determination of residues of trichlorfon and dimethoate on guava using HPLC. Food Chem. 114(1): 286–288.

- Kaplan, S. L. and Rose, P. W. (1991). Plasma surface treatment of plastics to enhance adhesion. Int. J. Adhes. Adhes. 11(2): 109–113.

- Momose, Y., Noguchi, M. and Okazaki, S. (1989). Ar, O and CF4 plasma treatment of poly-(vinylidene fluoride), polyimide and polyamidoimide and its relationship to wettability. Nucl. Inst. Methods Phy. Res. 39: 805–808.

- Gerenser, L. J. (1993). XPS studies of in situ plasma-modified polymer surfaces. J. Adhes. Tech. 7(10): 1019–1040.

- Varinder, K., Ashok, K. M. and Neelam, V. (2006). Applications of solid - phase microextraction for the determination of metall ic and organometallic species. Wiley Inter Science publication.

- Nicolaon, G.A. and Teichner, S,J. (1968). New preparation process for silica xerogels and aerogels and their textural properties. Bull. Soc. Chim. France 5: 1900–1906.