Malaysian Journal of Analytical Sciences Vol 19 No 3 (2015): 503 – 512

SAGO STARCH BASED HYDROGEL PREPARED USING ELECTRON BEAM IRRADIATION TECHNIQUE FOR CONTROLLED RELEASE APPLICATION

(Hidrogel berasaskan kanji sagu disedia menggunakan teknik radiasi alur elektron untuk aplikasi pelepasan terkawal)

Zakiah Jamingan1, Mansor B. Ahmad1*, Kamaruddin Hashim2, Norhazlin Zainuddin1

1Department of Chemistry,

Universiti Putra Malaysia, 43400 Serdang, Selangor, Malaysia

2Malaysian Nuclear Agency (Nuclear Malaysia),

43000 Kajang, Selangor, Malaysia

*Corresponding author: mansorahmad@upm.edu.my

Received: 1 April 2015; Accepted: 23 April 2015

Abstract

Carboxymethyl Sago starch (CMSS) is one of the natural polymers with high value as a polymeric device for medical application due to its potential as biocompatible materials. The monomer blending with modified natural polymers by irradiation technique has received wide attention due to the simple method of preparation, more promising material and free chemical residue in the product. CMSS/methacrylic acid (MAA) hydrogels were synthesized by Electron Beam irradiation at 2meV, 10mA. The objective of this study was to evaluate the ability of hydrogels from modified carboxymethyl sago starch CMSS for oral drug delivery. The hydrogels were characterized by FT-IR, TGA and DTG. The effects of the preparation conditions such as the, monomer composition and irradiation dose on the gel fraction of the synthesized hydrogel were investigated. The swelling properties of the hydrogel were carried out in acidic media, neutral and alkaline media at different temperatures (27˚C – 60 ˚C). The pH sensitive properties of CMSS/MAA hydrogel showed that it can be used as drug delivery devices due to suitability of pH response to the environment in gastrointestine tract.

Keywords: carboxymethyl sago starch, hydrogels, controlled release

Abstrak

Karboksimetil kanji sagu (CMSS) adalah salah satu polimer semula jadi yang mempunyai nilai tinggi sebagai peranti polimer untuk aplikasi perubatan kerana berpotensi sebagai bahan bioserasi. Adunan monomer dengan polimer semulajadi yang dimodifikasi dengan teknik penyinaran telah menerima perhatian yang meluas kerana kaedah penyediaan yang mudah, bahan yang lebih berkualiti terhasil dan tiada sisa kimia dalam produk tersebut. Hidrogel CMSS/asid metakrilik (MAA) disintesis menggunakan penyinaran alur elektron pada kondisi 2meV, 10mA. Objektif kajian ini adalah untuk menilai kemampuan hidrogel daripada karboksimetil yang telah diubahsuai daripada kanji sagu, untuk penghantaran ubat secara oral. Hidrogel telah dicirikan menggunakan FT-IR, TGA dan DTG. Kesan daripada keadaan persediaan seperti komposisi monomer dan dos sinaran ke atas hidrogel yang disintesis telah diselidik. Sifat pembengkakan hidrogel dalam media berasid, neutral dan alkali pada suhu yang berbeza (27 ºC - 60 ºC) juga diuji. Sifat sensitif yang ditunjukkan oleh hidrogel terhadap pH telah menjadikannya sesuai untuk digunakan sebagai alat pembawa ubat kerana kesesuaian respon pH kepada persekitaran dalam saluran gastrousus.

Kata kunci: karboksimetil-kanji sagu, hidrogel, pelepasan terkawal

References

- Peppas, N. A., and Mikos, A. G. (1986). Preparation methods and structure of hydrogels. Hydrogels in Medicine and Pharmacy 1:1-27.

- Peppas, N. A., Bures, P., Leobandung, W., and Ichikawa, H. (2000). Hydrogels in pharmaceutical formulations. European Journal of Pharmaceutics and Biopharmaceutics, 50(1): 27-46.

- Mahkam, M. (2010). Starch‐based polymeric carriers for oral‐insulin delivery. Journal of Biomedical Materials Research Part A 92(4): 1392-1397

- Pushpamalar, V., Langford, S. J., Ahmad, M., and Lim, Y. Y. (2006). Optimization of reaction conditions for preparing carboxymethyl cellulose from sago waste. Carbohydrate Polymers, 64(2): 312-318.

- Saboktakin, M. R., Tabatabaie, R. M., Maharramov, A., and Ramazanov, M. A. (2010). Synthesis and characterization of chitosan-carboxymethyl starch hydrogels as nano carriers for colonspecific drug delivery. J. Pharm. Educ. Res 1: 37-47.

- Saboktakin, M. R., Maharramov, A., and Ramazanov, M. A. (2009). pH-sensitive starch hydrogels via free radical graft copolymerization, synthesis and properties. Carbohydrate Polymers, 77(3): 634-638.

- Zhao, S. P., Cao, M. J., Li, L. Y., and Xu, W.L. (2010). Synthesis and properties of biodegradable thermo- and pH-sensitive poly[(N-isopropylacrylamide)-co-(methacrylic acid)] hydrogels. Polymer Degradation and Stability, 95(5): 719-724.

- Zhao, S.P., Cao, M.J., Li, L.Y., and Xu, W. L. (2011). Synthesis and properties of photopolymerized pH-sensitive hydrogels of methacrylic acid and biodegradable PEG-b-PCL macromer. Iranian Polymer Journal, 20(4): 329-340.

- Luo, Y., Zhang, K., Wei, Q., Liu, Z., and Chen, Y. (2009). Poly (MAA-co-AN) hydrogels with improved mechanical properties for theophylline controlled delivery. Acta Biomaterialia, 5(1): 316-327.

- Chen, L.G., Liu, Z.L., and Zhuo, R.X. (2005). Synthesis and properties of degradable hydrogels of konjac glucomannan grafted acrylic acid for colon-specific drug delivery. Polymer 46(16); 6274-6281.

- Hennink, W., and Van Nostrum, C. (2012). Novel crosslinking methods to design hydrogels. Advanced Drug Delivery Reviews, 64: 223-236.

- Panda, A., Manohar, S., Sabharwal, S., Bhardwaj, Y. and Majali, A. (2000). Synthesis and swelling characteristics of poly (N-isopropylacrylamide) temperature sensitive hydrogels crosslinked by electron beam irradiation. Radiation Physics and Chemistry, 58(1): 101-110.

- Said, H. M., Abd Alla, S. G., and El-Naggar, A. W. M. (2004). Synthesis and characterization of novel gels based on carboxymethyl cellulose/acrylic acid prepared by electron beam irradiation. Reactive and Functional Polymers, 61(3): 397-404.

- Mohd Amin, M. C. I., Ahmad, N., Halib, N., and Ahmad, I. (2012). Synthesis and characterization of thermo- and pH-responsive bacterial cellulose/acrylic acid hydrogels for drug delivery. Carbohydrate Polymers, 88(2): 465-473.

- Yaacob, B., Amin, M. C. I. M., Hashim, K. and Bakar, B. A. (2011). Optimization of reaction conditions for carboxymethylated sago starch. Iranian Polymer Journal, 20(3): 195-204.

- Nagasawa, N., Yagi, T., Kume, T. and Yoshii, F. (2004). Radiation crosslinking of carboxymethyl starch. Carbohydrate Polymers, 58(2): 109-113.

- El-Hag Ali, A., and AlArifi, A. (2009). Characterization and in vitro evaluation of starch based hydrogels as carriers for colon specific drug delivery systems. Carbohydrate Polymers, 78(4): 725-730.

- El-Naggar, A. W. M., Alla, S. G. A. and Said, H. M. (2006). Temperature and pH responsive behaviours of CMC/AAc hydrogels prepared by electron beam irradiation. Materials chemistry and physics, 95(1):158-163.

- McNeill, I.C., Ahmed, S., and Memetea, L. (1995). Thermal degradation of vinyl acetatemethacrylic acid copolymer and the homopolymers. II. Thermal analysis studies. Polymer Degradation and Stability 48: 89-97.

- da Silva, R. and Ganzarolli de Oliveira, M. (2007). Effect of the cross-linking degree on the morphology of poly(NIPAAm-co-AAc) hydrogels. Polymer, 48(14), 4114-4122.

- Chuah, C. T., Sarko, A., Deslandes, Y., and Marchessault, R. H. (1983). Packing analysis of carbohydrates and polysaccharides. Part 14. Triple-helical crystalline structure of curdlan and paramylon hydrates. Macromolecules, 16(8): 1375-1382.

- Akala, E. O., Kopečková, P. and Kopeček, J. (1998). Novel pH-sensitive hydrogels with adjustable swelling kinetics. Biomaterials, 19(11): 1037-1047.

- Halib, N., Amin, M. C. I. M., and Ahmad, I. (2010). Unique stimuli responsive characteristics of electron beam synthesized bacterial cellulose/acrylic acid composite. Journal of Applied Polymer Science, 116(5): 2920-2929.

- Chauhan, G. S. and Chauhan, S. (2008). Synthesis, characterization, and swelling studies of pH‐and thermosensitive hydrogels for specialty applications. Journal of Applied Polymer Science, 109(1): 47-55.

- Nizam El-Din, H. M., Abd Alla, S. G. and El-Naggar, A. W. M. (2010). Swelling and drug release properties of acrylamide/carboxymethyl cellulose networks formed by gamma irradiation. Radiation Physics and Chemistry, 79(6): 725-730.

- Tomić, S. L., Mićić, M., Filipović, J. and Suljovrujić, E. (2007). Swelling and drug release behavior of poly (2-hydroxyethyl methacrylate/itaconic acid) copolymeric hydrogels obtained by gamma irradiation. Radiation Physics and Chemistry, 76(5): 801-810.