Malaysian Journal of Analytical Sciences Vol 19 No 3 (2013): 531 – 540

OPTIMIZATION OF ELECTROCHEMICAL PARAMETERS FOR LANDFILL LEACHATE TREATMENT USING CHARCOAL BASE METALLIC COMPOSITE ELECTRODE

# (Pengoptimuman Parameter Elektrokimia untuk Rawatan Air Larut Lesap Menggunakan Elektrod komposit Logam Berasaskan Arang)

# Majd Ahmed Jumaah and Mohamed Rozali Othman*

# School of Chemical Sciences and Food Technology

# Faculty of Sciences and Technology

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

# *Corresponding author: rozali@ukm.edu.my

Received: 12 March 2015; Accepted: 18 May 2015

Abstract

# Landfill leachate normally contains organic and inorganic pollutants in high concentrations. Electrochemical oxidation technique is an effective method to treat landfill leachate, have high efficiency in organic pollutants degradation and ammonia removal. In this study, a cost effective charcoal base metallic composite electrode to treat landfill leachate by electrochemical oxidation was fabricated. The effects of operational parameters such as supporting electrolyte, applied voltage and electrolysis time on the removal percentage of Color, COD, NH3-N and total-P (PO4-3) were carried out. The results obtained show that the removal percentage of Color, COD, NH3-N and total- P (PO4-3) are 70, 89, 73 and 80 % respectively. Under the optimum operating condition, sodium chloride concentration of 1.5 % (w/v), applied voltage of 10 V, operating time 180 min and C60CG15Co10-PVC15 electrode as an anode were used.

# Keywords: landfill leachate, charcoal, electrode, electrochemical

Abstrak

# Air larut lesap dilaporkan mengandungi jumlah bahan pencemaran organik dan bukan organik dalan kuantiti yang tinggi. Kaedah pengoksidaan elektrokimia adalah merupakan satu kaedah yang berkesan dalam merawat air larut lesap kerana kecekapannya yang tinggi dalam pemecahan bahan pencemaran organik dan ammonia. Dalam kajian ini, elektrod logam komposit yang berasaskan arang yang tidak saja murah tetapi berkesan dalam merawat air larut lesap secara elektrokimia telah berjaya difabrikasikan. Kesan parameter pengoperasian seperti kepekatan elektrolit penyokong, keupayaan yang dikenakan dan masa elektrolisis dalam mengurangkan warna, COD, NH3-N dan jumlah- P(PO4-3) telah dijalankan. Hasil kajian mendapati pada keadaan optimum, peratus penyingkiran warna, COD, NH3-N dan jumlah-P(PO4-3) masingnya-masingnya ialah 70, 89, 73 dan 80 % telah dicapai. Keadaan optimum yang diguna ialah kepekatan NaCl 1.5 % (w/v) sebagai elektrolit penyokong, keupayaan yang dikenakan 10 V, masa operasi 180 min dan elektrod C60CG15Co10-PVC15 digunakan sebagai elektrod kerja (anod)

# Kata kunci: air larut lesap, arang, elektrod, elektrokimia

References

- Ihara, I., Kanamura, N.K., Shimada, E. and Watanabe, T. (2004). High Gradient Magnetic Separation Combined with Electrocoagulation and Electrochemical Oxidation for the Treatment of Landfill Leachate. IEEE Transactions on Applied Superconductivity, 14(2): 1558-1560.

- Masoumeh Moayeri Kashani, Salman Masoudi Soltani and Sobri, S. (2012). Treatment of Malaysian Leachate Sample Using Electrocoagulation. International Journal of Chemical Engineering and Applications, 3(1): 63-66.

- Renou, S., Givaudan, J., Poulain, S., Dirassouyan, F. and Moulin, P. (2008). Landfill Leachate Treatment: Review and Opportunity. Journal of Hazardous Materials, 150(3): 468-493.

- Ni'am, M.F., Othman, F., Sohaili, J. and Fauzia, Z. (2007). Electrocoagulation Technique in Enhancing COD and Suspended Solids Removal to Improve Wastewater Quality. Water Science & Technology, 56(7): 47-53.

- Amuda, O.S. (2006). Removal of COD and Color from Sanitary Landfill Leachate by using Coagulation–Fenton’s Process. Journal of Applied Sciences and Environmental Management, 10(2): 49-53.

- Zhao, X., Qu. J., Liu, H., Wang, C., Xiao, S., Liu, R., Liu, P., Lan, H. and Hu, C. (2010). Photoelectrochemical Treatment of Landfill Leachate in a Continuous Flow Reactor. Bioresource Technology, 101(3): 865-869.

- Kurniawan, T.A., Lo, W.H. and Chan, G.Y.S. (2006). Degradation of Recalcitrant Compounds from Stabilized Landfill Leachate using a Combination of Ozone-GAC Adsorption Treatment. Journal of Hazardous Materials, 137(1): 443-455.

- Bashir, M.J.K., Isa, M.H., Kutty, S.R.M., Awang, Z.B., Aziz, H.A., Mohajeria S. and Farooqi, I.H. (2009). Landfill Leachate Treatment by Electrochemical Oxidation. Waste Management, 29(9): 2534-2541.

- Fátima, E.M. and Dinis, S.J. (2004). Electrochemical Degradation of Reactive Blue 19 Dye in Textile Wastewater. 4th. AUTEX World Textile Conference, June 22-24, 2004 Roubaix, 1-6 pp.

- Chen, X., Shen, Z., Zhu, X., Fan, Y. and Wang, W. (2005). Advanced Treatment of Textile Wastewater for Reuse using Electrochemical Oxidation and Membrane Filtration. Water SA, 31(1): 127-132.

- Ihoş, M., Bocea, G. and Iovi, A. (2005). Use of Dimensionally Stable Anodes for the Electrochemical Treatment of Textile Wastewaters. Chemical Bulletin, 50(64): 1-2.

- Norazzizi Nordin, Siti Fathrita Mohd Amir, Riyanto and Mohamed Rozali Othman. (2013). Textile Industries Wastewater Treatment by Electrochemical Oxidation Technique Using Metal Plate. International Journal of Electrochemical Science, 8: 11403-11415.

- APHA., AWWA. and WPCF. (1981). Standard Methods for the Examination of Water and Wastewater, 15th. ed. Washington, DC: American Public Health Association

- Riyanto, Salimon, J. and Othman, M. R. (2007). Perbandingan Hasil Pengoksidaan Elektrokimia Etanol dalam Larutan Alkali yang Menggunakan Elektrod Platinum Polivinilklorida (Pt-PVC) dan Kepingan Logam Pt. Sains Malaysiana, 36(2): 175-181.

- Mussa, Z. H. Othman, M. R. and Abdullah, M. P. (2015). Electrochemical Oxidation of Landfill Leachate: Investigation of Operational Parameters and Kinetics Using Graphite-PVC Composite Electrode as Anode. Journal of Brazil Chemical Society, 26(5): 939-948.

- Deng, Y. and Englehardt, J.D. (2007). Electrochemical Oxidation for Landfill Leachate Treatment. Waste Management, 27(3): 380-388.

- Riyanto, Mohamed Rozali Othman, Jumat Salimon. (2007). Analysis of Ethanol using Copper and Nickel Sheet Electrodes by Cyclic Voltammetry. Malaysian Journal of Analytical Sciences, 11(2): 379-387.

- Sun Zhao-nan, Huang Yong-gang, Dong Chang-e and Hu Xiao-min. (2012). The Study of Removing the Organic from Wastewater by Periodically Reversing Electrocoagulation. World Automation Congress (WAC), 1-4 pp.

- Raju, G.B., Karuppiah, M.T., Lathaa, S.S., Parvathy, S. and Prabhakar, S. (2008). Treatment of Wastewater from Synthetic Textile Industry by Electrocoagulation–Electrooxidation. Chemical Engineering Journal, 144(1): 51-58

- Wang, C.T., Chou, W.L., Kuo, Y.M. and Chang, F.L. (2009). Paired Removal of Color and COD from Textile Dyeing Wastewater by Simultaneous Anodic and Indirect Cathodic Oxidation. Journal of Hazardous Materials, 169(1-3): 16-22.

- Awad, H. and Galwa, N.A. (2005). Electrochemical Degradation of Acid Blue and Basic Brown Dyes on Pb/PbO2 Electrode in the Presence of Different Conductive Electrolyte and Effect of Various Operating Factors. Chemosphere, 61: 1327-1335.

- Li-Choung Chiang, Juu-En Chang, Ten-Chin Wen. (1995). Indirect Oxidation Effect in Electrochemical Oxidation Treatment of Landfill Leachate. Water Research, 29(2): 671-678.

- Rajkumar, D. and Jong Guk Kim. (2006). Oxidation of Various Reactive Dyes with in-situ Electrogenerated Active Chlorine for Textile Dyeing Industry Wastewater Treatment. Journal of Hazardous Materials, 136(2): 203-212.

- Yong Kong, Jia Yuan, Zhiliang Wang, Shiping Yao and Zhidong Chen. (2009). Application of Expanded Graphite/Attapulgite Composite Materials as Electrode for Treatment of Textile Wastewater. Applied Clay Science, 46(4): 358-362

- Comninellis, C. and Pulgarin, C. (1993). Electrochemical Oxidation of Phenol for Wastewater Treatment using Tin Dioxide Anodes. Journal of Applied Electrochemistry, 23: 108-112.

- Chen, J., Liu, M., Zhang, J., Xian, Y. and Jin, L. (2003). Electrochemical Degradation of Bromopyrogallol Red in Presence of Cobalt Ions. Chemosphere 53(9): 1131-1136.