Correction for Figure 3 in the manuscript

Figure 3: X-ray diffractogram (XRD) patterns of prepared TiO2 by MAS treatment at 150 oC for (i) 6 hours, (ii) 4 hours, (iii) 2 hours and subsequently calcined at 450 oC for 1 hour, respectively. XRD pattern for (iv) commercial TiO2 (SIGMA) was included for comparison. (A: Anatase (TiO2); C: Na2Ti6O13)